[image: image1.jpg]



Fig. 1: Sputtering target. Purity >99.99%.

[image: image2.emf]
Fig. 2: Reciprocating-filing machine that is enclosed in a glove box for operation.
[image: image3.png])

Ay

v/
’
SR





Fig. 3: Stainless steel vial with two different sizes of balls.

[image: image4.png]



Fig. 4: High energy SPEX 8000M ball milling.
[image: image5.png]Count

1200°C60min A L N
1100°C60min___\_ }‘ I
A AL
N
800°CE0min /Ln N
200:C60min A
CE0m AN ey
asmilled _em, Pt
50 60 70 80 90 10

26

0




Fig. 5: XRD patterns for as-milled OF-Fe14Cr4Hf and annealed for 60 min at temperatures from 500 to 1200°C.
[image: image7.png]70

Grain size (nm)
N w B [4.] D
o o e o o

-
o

Annealing temperature (°C)

A Fel4CraHf
B OF-Fe14CraHf -
A
A -
B n
A
"
- | |
L} a = "
1 1 1 1 1 1
200 400 600 800 1000 1200





Fig.6: Grain size vs. annealing temperature curves for OF-Fe14Cr4Hf, Fe14Cr4Hf and thermodynamic model predictions. 
[image: image8.png]



Fig. 7: TEM images and diffraction pattern for OF-Fe14Cr4Hf annealed at 900[image: image10.emf]


℃		










 for 60 min. 
