Created by Adnan Abu-Yousif 
Modified from Guidelines for Use provided by BD Biosciences

 Protocol for Plating Encapsulated Cells in BD PuraMatrix
Technical Notes:
· Gelation is initiated by the addition of salts. Therefore, it is CRITICAL that no salts come in contact with PuraMatrix until gelation is desired; exposure to salts of very low ionic strength (e.g., < 0.05 M) will cause irreversible gelation.

· Leftover stock solutions that are prepared can be used at a later date provided they have not come in contact with salts. You do not need to worry about repeat sonication.
· Air bubbles can be removed aliquoting PuraMatrix into sterile tubes followed by centrifugation.
· Be very careful during media changes as aspiration can easily disrupt the PuraMatrix bed.
Materials: 

BD PuraMatrix RAD16 Peptide Hydrogel-1% (Cat # 354250): The total peptide concentration of the undiluted mixture is 10 mg/ml. 
Water Bath Sonicator or Vortex
96-well cell culture dish
Cell Culture Media

Sterile Filtered H20
Sterile Filtered 20% Sucrose

Cells (all at 5,000 cells/well): OVCAR-5

All steps must be performed under aseptic conditions.

Procedure: 

1) Sonicate the 1% PuraMatrix (RAD16) in a water bath sonicator for 30 minutes to reduce the viscosity prior to use.

2) The 1% PuraMatrix solution can now be aliquoted into sterile tubes to simplify future experiments. 

a. Avoid the formation of air bubbles; if they form simply spin down the sterile tubes containing PuraMatrix at 1000 rpm (300 x g) for 5 minutes.

b. The total peptide concentration of the undiluted mixture is 10 mg/ml.
3) Two sets of 4 wells will be plated at 2.5 mg/ml and 1.25 mg/ml total peptide concentration, respectively.
4) Dilute the PuraMatrix in each well set with 0.2 μm sterile filtered 20% sucrose and 13.3% sucrose to total peptide concentrations of 5 mg/ml and 2.5 mg/ml, respectively to achieve a 2x concentration of BD PuraMatrix in 10% sucrose.
a. To Make 20% sucrose, dilute 10 g of sucrose, then volume to 50 ml water.

b. 13% and 10% sucrose can be prepared by diluting the 20% stock solution.

i. 13% Sucrose (for every 10 ml):  6.5 ml 20% sucrose + 3.5 ml sterile H20.
ii. 10% Sucrose (for every 10 ml): 5.0 ml 20% sucrose + 5.0 ml sterile H20.
5) Prepare a master mix of PuraMatrix peptide based on the number of wells you intend to plate. (See example below.) Then aliquot into individual tubes containing 25 l of the master mix.
a. The master mix should be prepared at twice the desired final concentration of total peptide as it will be diluted with an equal volume of cells during plating.  



6) Prepare cell suspensions by trypsinizing cell monolayer cell cultures. 

a. 2 ml of 0.05% Trypsin EDTA can be used for each T-75 Flask.
7) Neutralize the trypsin by addition of cell culture media containing 10% heat inactivated fetal bovine serum (use at least 2 ml of media per ml of trypsin used in the previous step.)

8) Centrifuge the cells at 1000 rpm (~ 300 x g) for 5 minutes to create a cell pellet.

a. Resuspend the cells in 10% sterile filtered sucrose.
b. Count the cells and spin down again at 1000 rpm (~ 300 x g) for 5 minutes to remove trace amounts of salt found in the media.

9) Resuspend the OVCAR-5 cells in 10% sucrose at 2.0 x 105 cells/ml so that the final cell count per well will be 5,000 cells in each well.
The following steps should be performed rapidly.
10) Add 25 l of the 2.0 x 105 cells/ml suspension to the first individual tube containing 25 l of the master mix of PuraMatrix™ as shown in the above schematic.
a. Quickly mix by pipetting (~5 times up and down) in the tube without introducing air bubbles.
b. Then pipette the 50 l cell suspension/PuraMatrix™ mixture into the appropriate well of a 96 well dish.

c. Initiate gelation of the BD PuraMatrix by gently pipetting 100 l cell culture media (RPMI + 10% FBS)  to the side of the well 







 


11) Repeat the steps outlined in 8 until all wells have been plated.
12) After 30 minutes Very Gently remove ~2/3 of the media using a 200 l pipette to equilibrate the pH of the hydrogel.  
a. DO NOT USE A VACUUM ASPIRATOR AS THIS WILL DISRUPT THE MATRIX
b. Place the pipette tip in the well so that it does not touch the PuraMatrix™ bed and gently remove media from the well.
c. Care should be taken to not disrupt the matrix during the culture of cells in PuraMatrix™.
13) Very Gently add 150 l of fresh cell culture media to the side of the well containing cells encapsulated in PuraMatrix.

14) Change the cell culture media in each well every 48 hours with fresh culture media by carefully repeating steps 10 and 11.
C





B





A


   B


      C


          D


             E


                F


                   G


                      H








1       2      3      4      5       6      7      8      9     10    11    12





Individual Tubes 


Containing 5mg/ml PuraMatrix


(25 l each)








Master Mix


Containing 5mg/ml PuraMatrix


(120 l Total)








Master Mix


Containing 2.5mg/ml PuraMatrix


(120 l Total)








Individual Tubes 


Containing 2.5mg/ml PuraMatrix


(25 l each)








Individual Tubes


Containing 5mg/ml PuraMatrix


(25 l each)








1





Individual Tubes 


Containing 2.5mg/ml PuraMatrix


(25 l each)








Cell Suspension


In 10% Sucrose


(2 x 105 cells/ml)





D





Set 1:


Desired Final concentration = 2.5 mg/ml total peptide





Set 2:


Desired Final concentration = 1.25 mg/ml total peptide











