Real-time monitoring of ligand-receptor interactions with Fluorescence Resonance Energy Transfer

Navneet Dogra, Julia C. Reyes, Nishi Garg, and Punit Kohli

Department of Chemistry and Biochemistry

Southern Illinois University

Carbondale, IL 62901

Correspondence to: Punit Kohli at pkohli@chem.siu.edu

Keywords:

Fluorescence Resonance Energy Transfer (FRET), Polydiacetylene (PDA), Biosensor, Liposome, Sensing

Short Abstract

We demonstrate FRET between conjugated polymer PDA and fluorophores attached to the surface of liposomes for the sensing of biomolecules.  PDA liposomes also contained receptor molecules on their surface for biomolecules to be used as probes. Ligand-receptor interactions lead to changes in the FRET efficiency between the fluorophore and PDA which is the basis of the sensing mechanism.

Long Abstract:

FRET is a process whereby energy is non-radiatively transferred from an excited donor molecule to a ground-state acceptor molecule through long-range dipole-dipole interactions1.  In the present sensing assay, we utilize an interesting property of PDA:  blue-shift in the UV-Vis electronic absorption spectrum of PDA after an analyte in the solution interacts with receptors attached to PDA2,3,4,7. This shift in the PDA absorption spectrum provides changes in the spectral overlap (J) between PDA (acceptor) and rhodamine (donor) that leads to changes in the FRET efficiency.  Thus, the interactions between analyte (ligand) and receptors are detected by FRET changes between donor fluorophores and PDA.  In particular, we show the sensing of a model protein molecule streptavidin.  We also demonstrate the covalent-binding of bovine serum albumin (BSA) to the liposome surface with FRET mechanism.  These interactions between the bilayer liposomes and protein molecules can be sensed in real-time. The proposed method is a general method for sensing small chemical and biochemical molecules and large particles as well.  Since fluorescence is intrinsically more sensitive than colorimetry, the detection limit of the assay can be in sub-nanomolar range or lower8.  Further, PDA can act as a universal acceptor which means that multiple sensors can be developed with PDA (acceptor) functionalized with donors and different receptors attached on the surface of PDA liposomes.

Figure 1.  Absorption spectra of blue and red PDA solutions.  (Inset) optical micrographs taken with a digital camera.

A. Synthesis and characterization of PDA liposomes4,5,6

Note: Protect the solution from light using aluminum foil wrapping on every container throughout all the experimental steps.

- Synthesis of N-hydroxysuccinimide diacteylene (NHS-PCDA).  10,12-pentacosadiynoic acid (PCDA) (0.267 g, 0.713 mmol) in dry CH2Cl2 (10 mL), N-hydroxysuccinimide (0.0914 g, 0.786 mmol) and 1-(3-(dimethylamino)propyl)-3-ethylcarbodiimide hydrochloride (0.144 g, 0.713 mmol) were stirred at room temperature for 2 hrs.  The solvent was then rotary evaporated. The residue was extracted with diethyl ether and washed with water three times. The organic layer was dried with MgSO4 for half an hour, and then it was filtered off. The solvent was removed by rotary evaporation to give a white solid powder. 0.24g (>90%) of white solid. 1H NMR (300 MHz, DMSO), δ (ppm): 0.893 (t, 3H), 1.268 (m, 26H), 1.512 (m, 4H), 1.754 (m, 2H), 2.252 (t, 4H), 2.365 (m, 1H), 2.610 (m, 1H), 2.842 (s, 2H).

- Liposome Preparation5,6,7. A desired weight of PCDA: PCDA-NHS: 1,2-dimyristoyl-sn-glycero-3-phosphocholine (DMPC) :: 8:1:1 were dissolved in 20 mL dichloromethane. The solvent was then evaporated completely to yield a thin film of monomers. The film was hydrated with deionized water to make a liposome solution of desired concentration (usually 1 mM). The resultant suspension was sonicated at 76 °C for ∼15 min. The solution was then passed through a paper filter to remove the lipid aggregates and then cooled at 4 °C overnight to promote self assembly of the monomers. The final solution was optically clear. The diacetylene monomers were polymerized by irradiation with 254 nm of UV radiation for ∼2 min using a Pen Ray UV source (4.5 mW/cm2) in air.

B.  Preparation of Rhodamine-tagged Bovine Serum Albumin (BSA-Rh) modified PDA liposomes

- A desired amount of BSA-Rh was dissolved in PBS buffer (ionic concentration was 0.01M, pH 7.2) to make the final concentration of 1.2 µM BSA-Rhodamine solution.

- Binding of BSA-Rh to liposome surface. 2 mL (1.2 µM) of BSA-Rhodamine was added to 10 mL of liposomes prepared in step A2 (see above) at room temperature. The classical reaction for the binding of amine groups from the lysine residue of proteins to carboxylic acid activated by NHS group was used in our experiments. NHS-PCDA was designed for covalently binding protein molecules with liposomes using NHS-amine reactions.  NHS is an excellent leaving agent that drives the amine-carboxylic acid reaction in the forward direction. The yield of this reaction under appropriate condition should be quantitative.

- Removal of free BSA-Rh. A Spectra/Por® Biotech Cellulose Ester (CE) membrane (MWCO:  100,000) was soaked in deionized water for 15 min. This is followed by dialysis of unreacted BSA-Rhodamine (Molecular weight ~66000 Da) in deionized water.  The water was changed at 2 h, 8 h, 14 h, 24, and 36 hrs during dialysis.

C. Monitoring of protein attachment to liposomes using FRET1

- Monitoring of FRET between Rhodamine and PDA liposomes. Excitation and emission spectra of BSA-Rh and absorption spectrum of PDA are taken (Figure 2A).

Figure 2A.  Change in FRET efficiency due to change in the UV-Vis absorption spectrum of the PDA. Rhodamine is a donor (red) and polymerized PDA liposomes as an acceptor (blue).

- We can clearly see that the emission spectrum of BSA-Rh overlaps with the absorption spectrum of PDA. This satisfies the resonance requirement for the FRET mechanism.  BSA-Rhodamine tagged liposomes before and after polymerization were analyzed with UV-Vis and fluorescence spectroscopy. For the isolated donor and acceptor, the FRET efficiency is highly dependent on donor-acceptor distance (r) and J1. . The quenching in the emission was observed (Figure 2B) because of FRET between rhodamine and PDA due to appearance of electronic absorption spectrum of blue PDA after photopolymerization.  In our case FRET efficiency is zero for unpolymerized liposomes and Rhodamine because J=0 for unpolymerized liposomes in the visible region.

- Similar experiments were performed with only PDA liposomes that did not contain NHS on their surface.  Thus, BSA-Rh was not tagged to the surface of the liposomes; that is FRET between PDA and rhodamine was ~zero.  In this case, the average distance between rhodamine and PDA (raverage) was much larger than Forster radius (R0).  Thus, we didn’t observe a large decrease in the fluorescence intensity (Figure 2B). This also suggests that the fluorescence quenching occurs only when r < 2.8 nm.

Figure 2B. Fluorescence spectra of BSA-Rh tagged liposomes before (blue) and after PCDA polymerization (red).  A large decrease in the rhodamine emission was observed due to FRET between rhodamine and PDA.

D.  Biotin tagged liposomes and real time sensing of Biotin-Streptavidin binding.

Instead of using DMPC in step A.3, biotin-tagged- (1,2-dioleoyl-sn-glycero-3-phosphoethanolamine-N-(biotinyl) (biotin-DOPE) was used.  The liposomes now contained biotin on their surface. Subsequent steps were similar to A (see above) with one exception:  streptavidin was added to the solution to investigate if we could observe biotin-streptavidin interactions through changes in the FRET efficiency.

E.  Monitoring of FRET in biotin-tagged liposome after addition of streptavidin to the solution.

Figure 3A. Spectral overlap (J) change for PDA (blue or red) absorption spectrum and rhodamine emission spectrum.  It is clearly seen that J increases with blue-shift of the PDA absorption spectrum

- Unpolymerized and polymerized biotin tagged liposomes were analyzed with UV-Vis and fluorescence spectroscopies.

- The emission of rhodamine (SR-101) decreased by about 45% after polymerization (Figure 3B).

Figure 3B. Fluorescence spectra before (blue) and after (red) liposome polymerization.

- 40 µL aliquots (1µM) of streptavidin solution were added to 2 mL of liposome solution.

With the addition of streptavidin to the solution, changes in the J value was observed (Figure 3C). As biotin binds with streptavidin, the blue peak intensity of PDA liposome (centered at ~645nm) was observed a decrease while an increase in the absorption at 540 nm was observed. Figure 3D shows changes in the FRET efficiency. The FRET efficiency decreased with the increase in streptavidin concentration which is consistent with our prediction.

- After every 40 µL aliquot addition of streptavidin, the SR-101 emission was recorded. We observed a steady increase in the rhodamine emission after the addition of streptavidin (Figure 4). This increase in rhodamine emission is due to a decrease in the J value for the sulphorhodamine emission spectrum and PDA absorbance spectrum following biotin-streptavidin interactions.  At the molecular level, the biotin-streptavidin interactions lead to subtle changes in the effective conjugation length of the PDA that results in a more thermodynamically stable red-PDA form2 and also is the basis of changes in J values.  Interestingly, the subtle differences in the molecular interactions for covalently or non-covalently bonded biotin to PDA liposome can be probed using our sensing assay4.

- Forster radius (R0) for rhodamine and PDA pair is calculated to be ~2.80 nm.  This means that for isolated PDA-rhodamine pairs, 50% of the excited state rhodamine molecules will have their energy transferred to PDA when r is 2.80 nm.

- We observed that when biotin was covalently attached to the PDA backbone, the emission increase was 2-3 times larger than that of non-covalently bonded biotin to liposomes.4 These results strongly suggest that our proposed system is sensitive to distinguish subtle differences in the interactions at the transducer (linker between biotin and liposome bilayer) due to covalently and non-covalently bonded receptors attached to liposomes.

- Real time monitoring (in millisecond to second time scale) of protein interactions (in the UV-Vis spectroscopy) depends upon the scanning and data acquisition capabilities of the spectrophotometer.

Figure 3C. Condition for FRET: J change between donor (sulphorhodamine) and acceptor (PDA) with the streptavidin addition to the liposome solution.

Figure 3D. FRET efficiency change between the donor (sulphorhodamine) and acceptor (PDA) with the streptavidin addition to the liposome solution.

Figure 4.  Rhodamine emission spectrum after the addition of streptavidin aliquots to the PDA liposome solution.

Discussion

- Selective binding of lysine residue of protein was done using NHS-lysine amine reaction

- Real-time monitoring of biotin-streptavidin binding and protein (BSA) binding with liposomes was observed using FRET.

- Similar procedure can be applied to study the binding dynamics of various protein interactions with their receptors.

- There is flexibility in choosing fluorophores that will provide changes in the J values depending upon the spectral characteristics of the fluorophores.  PDA is a universal acceptor. Thus, the use of PDA (acceptor) along with multiple fluorophores and receptors raises the possibility of providing us with multiple sensors.  The sensitivity of our sensors is sub-nanomolar and with optimization, it can be further enhanced.  The specificity of the sensors is controlled through the use of molecular interactions between receptors and ligands.  These sensors can also be used for larger particles such as viruses and bacteria.

Acknowledgements

Financial support for this work was provided through the National Science Foundation, National Institute of Health (NIH), Materials Technology Center (MTC) and ORDA at SIUC.  We thank NSF for a grant (CHE-0959568) for the purchase of an FE-SEM.  We would like to thank Prof. Matthew McCarroll for helpful discussions.

References

- Lakowicz, J. R. (1999). Principles of Fluorescence Spectroscopy. Kluwer Academic/Plenum Publishers

- Charych, D. H.; Nagy, J. O.; Spevak, W.; Bednarski, M. D. Science 1993, 261, 585–588.

- Bora Yoon, Sumi Lee and Jong-Man Kim Chem. Soc. Rev., 2009, 38, 1958-1968.

- Xuelian Li and Punit Kohli, J. Phys. Chem. C 2010, 114, 6255–6264

- Xuelian Li, Shelton Matthews and Punit Kohli, J. Phys. Chem. B 2008, 112, 13263–13272

- Xuelian Li, Matthew McCarroll, and Punit Kohli, Langmuir, October 10, 2006 Volume 22, Number 21

- New, R. R. C. In Liposomes: A Practical Approach; New, R. R. C., Ed.; Oxford University Press: Oxford, 1990; pp 33-104.

- Xiaoqiang Chen, Jung Lee, Min Jung Jou, Jong-Man Kim and Juyoung Yoon  Chem. Commun., 2009, 3434-3436

- Oktay Yarimaga, Maesoon Im, and Yang-Kyu Choi, Tae Won Kim, Yun Kyung Jung, and Hyun Gyu Park, Sumi Lee and Jong-Man Kim, Macromolecular Research, Vol. 18, No. 4, pp 404-407 (2010)