Figure 5. Typical particle number concentration changing trend during abrasion test. (a) neutralizer off (b) neutralizer on
[image: image1.jpg]particle number concentration, #/cc

4000

3000

2000

1000

60 120 180

time, min

[ Abrasion time (100 grit, 0.98 kN / 72 rpm, 1000 rotations)
—— Condensation Particle Counter
— Optical Particle Counter

240




(a)
[image: image2.jpg]particle number concentration, #/cc

4000

3000

2000

1000

60 120 180

time, min

[ Abrasion time (100 grit, 0.98 kN / 72 rpm, 1000 rotations)
—— Condensation Particle Counter
— Optical Particle Counter

240




(b)
