Table 2. Abrasion test conditions. lpm. liter per min; rpm, revolutions per min

| Chamber | Ventilation | 50 lpm |
| --- | --- | --- |
| Abrasor | Test specimen | ⌀140 mm, 3 mm thickness |
|  | Abrasion wheels | Sand Paper (100 grit) (brand new) |
|  | Rotation | 72 rpm, 1000 rotations |
|  | Additional air flow rate (for particle suspension) | 25 lpm |
| Neutralizer (soft X-ray ionizer) | Location | 45 degrees, 28 cm (from center of test specimen) |