TITLE:

Testing of nanoparticle release from a composite containing nanomaterial using a chamber system

AUTHORS:

Gun Ho Lee, Kang-Ho Ahn*, Il Je Yu*

AUTHORS: INSTITUTION(S)/AFFILIATION(S) FOR EACH AUTHOR:

Gun Ho Lee

Department of Mechanical Engineering,

Hanyang University,

Ansan, R. of Korea

rebirthii@icloud.com

Kang-Ho Ahn

Department of Mechanical Engineering,

Hanyang University,

Ansan, R. of Korea

khahn@hanyang.ac.kr

Il Je Yu

Institute of Nanoproduct Safety Research,

Hose University

Asan, R. of Korea

u1670916@chollian.net

CORRESPONDING AUTHORS:

Il Je Yu

Institute of Nanoproduct Safety Research,

Hose University

Asan, R. of Korea

u1670916@chollian.net

Kang-Ho Ahn

Department of Mechanical Engineering,

Hanyang University,

Ansan, R. of Korea

khahn@hanyang.ac.kr

KEYWORDS:

Nanoparticles, Nanomaterials, Release, Nanocomposites, Simulation, Chamber

SHORT ABSTRACT:

Nanoparticle release is tested using a chamber system that includes a condensation particle counter, an optical particle counter, and sampling ports that collect filter samples for electron microscopy analysis. The proposed chamber system can be effectively used for nanomaterial-release testing of products containing nanomaterials, with a repeatable and consistent data range.

LONG ABSTRACT:

With the rapid development of nanotechnology as one of the most important technologies in the 21st century, interest in the safety of consumer products containing nanomaterials is also increasing. Evaluating the nanomaterial release from products containing nanomaterials is a crucial step in assessing the safety of these products and has resulted in several international efforts to develop consistent and reliable technologies for standardizing the evaluation of nanomaterial release. In this study, the release of nanomaterials from products containing nanomaterials is evaluated using a chamber system that includes a condensation particle counter, an optical particle counter, and sampling ports that collect filter samples for electron microscopy analysis. The proposed chamber system is tested using abrasor and disc-type nanocomposite material specimens to determine whether the measured nanomaterial release is repeatable and consistent within an acceptable range. The test results indicate that the total number of particles in each test is within 20% of the average after several trials. The release trends are similar and show very good repeatability. Therefore, the proposed chamber system can be effectively used for nanomaterial-release testing of products containing nanomaterials.

INTRODUCTION:

Nanomaterial exposure has mostly been studied in relation to workers in workplaces that manufacture, handle, fabricate, and package nanomaterials; consumer exposure has not been studied extensively. A recent analysis of the environmental and health literature database created by the International Council of Nanotechnology (ICON) also indicated that most nanomaterial safety research has focused on hazards (83%) and potential exposure (16%), with the release from nanocomposites—indicating consumer exposure—only representing 0.8%1. Thus, very little is known about consumer exposure to nanomaterials.

Nanoparticle release has been used to estimate consumer exposure in simulation studies, including abrasion and weathering of nanocomposites, textile washing, and dustiness testing methods (e.g., the rotating drum method, vortex shaking method, and other shaker methods)2-3. Additionally, several international attempts, such as the International Life Science Institute (ILSI) NanoRelease and EU NanoReg, have been made to develop technology to help understand the release of nanomaterials used in consumer products. The ILSI NanoRelease consumer product, launched in 2011, represents a life-cycle approach to nanomaterial release from consumer products. Phase 1 involves nanomaterial selection, phase 2 covers evaluation methods, and phase 3 implements interlaboratory studies. Several monographs and publications on the safety of nanomaterials in consumer products have also been published4-6.

Meanwhile, NanoReg represents a common European approach to the regulatory testing of manufactured nanomaterials and provides a program of methods for use in simulation approaches to nanorelease from consumer products2. ISO TC 229 is also trying to develop standards relevant to consumer safety and to submit a new working item proposal for consumer safety. The OECD WPMN (working party on nanomaterials), especially SG8 (a steering group on exposure assessment and exposure mitigation), recently conducted a survey on the direction of future work, especially a consumer and environmental exposure assessment. Therefore, in light of these international activities, the Korean Ministries of Trade, Industry, and Energy launched a tiered project in 2013 focused on the "Development of technologies for the safety, evaluation, and standardization of nanomaterials and nanoproducts." Also, several consumer safety-relevant studies to standardize nanomaterial release from consumer products have been published7-8.

An abrasion test is one of the simulation approaches included in the ILSI NanoRelease and the NanoReg2-3 for determining the potential emission level of nanoparticles from different commercial composite products. The mass weight loss is deduced based on the difference in the specimen weight before and after abrasion using a Taber device. The nanocomposite sample is abraded at a constant speed, a sampler sucks up the aerosol, and the particles are then analyzed using particle counting devices, such as a condensation particle counter (CPC) or an optical particle counter (OPC); finally, the particles are collected on a transmission electron microscopy (TEM) grid or membrane for further visual analysis. However, conducting an abrasion test for nanocomposite materials requires consistent nanoparticle release, which is difficult due to particle charging caused by abrasion and by the conditions when the particle sampling is conducted near the emission point2-3, 9-11.

Accordingly, this paper presents a chamber system as a new method for evaluating nanomaterial release in the case of abrasion of nanocomposite materials. When compared with other abrasion and simulation tests, the proposed chamber system provides consistent nanoparticle release data in the case of abrasion. Moreover, this new test method has been used widely in the field of indoor air quality and in the semi-conduct industry as a total particle number counting method12, 13. Therefore, it is anticipated that the proposed method can be developed into a standardized method for testing nanoparticle release from consumer products containing nanomaterials.

PROTOCOL:

1. Preparation of instruments and specimens

1.1) Abrasor

1.1.1) This apparatus is based on a Taber abrasion tester. Use an abrasor with one specimen rotation stage (140 mm diameter), two abrasion wheel holders, and a rotation speed of 30-80 rpm.

1.1.2) Use a weight to secure the abrasion wheel to the abrasion wheel holder, which also applies load to the test specimen.

1.1.3) Install an additional air inlet to provide better suspension for the abrased particles, as shown in Figure 3. Use a 1/8”-diameter tube located 15 mm above and 40 mm away from the center of the test specimen

1.2) Abrasion wheel

1.2.1) Wrap the abrasion wheel (55 mm diameter, 13 mm thick) with sand paper (100 grit and brand new).

1.3) Specimen

1.3.1) Prepare the specimen with a diameter of 140 mm and install it on the abrasor.

NOTE: Specimen is a composite containing a nanomaterial for the abrasion test.

1.4) Chamber

1.4.1) Use stainless steel for the chamber walls to avoid particle deposition due to electrostatic force. Place the abrasor inside the chamber (volume 1 m3) (Table 1) and position the air inlet and outlet in the upper and lower parts of the chamber, respectively. Use a mixer consisting of three perforated plates at the air outlet to achieve a uniformly-mixed particle flow.

1.5) Neutralizer

1.5.1) As electrostatically charged particles enhance particle deposition on the chamber walls, use a neutralizer (soft X-ray ionizer) to minimize the charged state of the particles.

1.6) Online measuring instruments12, 13

1.6.1) Use a CPC and an OPC to measure the particle number concentration and particle size distribution as per the manufacturer’s instructions.

1.6.2) Install the CPC and OPC at the outlet of the chamber to measure the particle number concentration and particle size distribution.

1.7) Particle sampling instruments

1.7.1) Sample the released particles using a particle sampler containing filter media or a TEM grid to analyze the particle morphology and components.

1.7.2) Install the particle sampler, containing filter media or a TEM grid, at the outlet of the chamber to analyze the morphology of the released particles.

2. Abrasion test for nanoparticle release using the chamber system

NOTE: The abrasion test conditions are described in Table 2.

2.1) Place the abrasor in the center of the chamber.

2.2) Install the test specimen on the specimen rotation stage of the abrasor.

2.3) Secure the abrasion wheels in the abrasion wheel holders with a 1,000 g weight to apply load to the test specimen.

2.4) Position the neutralizer (soft X-ray ionizer) 28 cm away from the center of the test specimen at a 45o angle, as seen in Figure 2, to reduce the electrostatic particle deposition on the chamber walls.

Note: The neutralizer removes the electrostatic force by beam exposure. However, since the air inlet and abrasion wheels are located above the specimen rotation stage, this restricts the access of the neutralizer beam to the surface of the test specimen. Therefore, the neutralizer is located diagonally to allow the beam to reach as much of the specimen surface as possible.

2.5) Operate the blower installed at the outlet of the chamber at a 50 L/min flow rate.

2.6) Supply 25 L/min of additional particle-free suspension air using an air compressor through the additional air inlet.

Note: The particles, which are generated by abrasion, are deposited on surface of the specimen and abrasion wheels. Therefore, it is hard to measure the abrased particles. The additional air inlet can help to solve this problem of particle suspension.

2.7) Using the CPC, check the background particle number concentration inside the chamber to reach an average particle number concentration of less than 1 #/cc for 1 hr, as described in Figure 4.

2.8) Operate the specimen rotation stage of the abrasor using a step motor that rotates the specimen rotation stage at 72 rpm with 1,000 rotations.

2.9) Measure and record the released particle number concentration and particle size distribution using the CPC and OPC.

Note: The particles released from the nanocomposites are suspended and carried by the air that is being pumped. These suspended particles are eventually transported to the outlet by following the airstream. The released particles are then detected by the CPC and OPC at the outlet of the chamber. A CPC and an OPC are most frequently used for measuring the particle number concentration, while an OPC can also measure the particle size distribution.

2.10) Sample the released particles using a particle sampler that contains filter media or a TEM grid.

Note: The released particles collected on filter media or a TEM grid can then be analyzed using TEM or scanning electron microscopy (SEM).

2.11) Stop the measurement and sampling when the particle number concentration reaches below 0.1% of the peak particle number concentration.

2.12) Save the all data (CPC, OPC) and remove all the samples (test specimens).

2.13) Use a new specimen and new abrasion wheels for each test. Wash the chamber and abrasor with lab wipes and iso-propyl alcohol (IPA) after each abrasion test to confirm repeatability.

REPRESENTATIVE RESULTS:

Abrasion test repeatability using the chamber system

The total particle numbers were consistent for 8 abrasion tests, as shown in Table 3. The CPC measured an average of 3.67 x109 particles, while the OPC counted an average of 1.98 x 109 particles (> 0.3 μm). The deviations were within 20%, which represented a consistent release of particles during abrasion.

Nanorelease from the nanocomposite

As shown in Figures 5, nanocomposites containing carbon nanotubes (CNTs) 0% and 2% showed a circle 40 mm away from the center after abrasion. After abrasion, the original test specimens lost approximately 0.6 g (1.56%) (Table 4). The nanocomposite containing CNTs released 12.6% more particles than the control composite, as shown in Table 5. Several micrometer particles were sampled on the filter, while a TEM grid was used to sample the nanoscale particles. Most of the particles were torn due to abrasion. Field emission scanning electron microscopy (FE-SEM) revealed no free CNT structures from the nanocomposite containing 2% CNTs in the filter samples (Figure 6) or mini particle sampler samples (Figure 7) after abrasion.

TABLES AND FIGURES:

Figure 1. Nanorelease test chamber configuration. Figure 1 shows the configuration of the abrasion test chamber system, and the chamber specifications are presented in Table 1. To provide particle-free air to the chamber, a charcoal filter was inserted in the air inlet to inflow sheath air; a mixer, consisting of three perforated plates, was installed in the outlet to achieve a uniformly-mixed particle flow. For air circulation in the chamber, an orifice flow meter and blower were installed at the end of the outlet. A condensation particle counter (CPC) and an optical particle counter (OPC) were installed downstream of the mixer to measure the particle number concentration and particle size distribution.

Figure 2. Placement of neutralizer and abrasor. Particles generated by the friction of two different materials are highly charged. Thus, to reduce the charged particles, a neutralizer (soft X-ray ionizer) was installed. The specifications of the neutralizer are presented in Supplement 1. The neutralizer (soft X-ray ionizer) was located 28 cm away from the center of the test specimen at an angle of 45o.

Figure 3. Configuration of the additional air inlet: (a) front view (b) top view.  For the abrasion test, the abrasor was located in the center of the chamber. To provide better suspension for the abrased particles released from the test specimen, an additional air flow was supplied using a 1/8” tube located 15 mm above and 40 mm away from the center of the test specimen.

Figure 4. Abrasion test procedure. Before the main experiment, the instruments and test specimens were prepared. The chamber background values, such as the VOC, ozone, and dust, were checked, and then the abrasor with the test specimen and neutralizer were placed in the chamber. For the main test, a zero check was performed in the standby phase by starting and stopping the abrasion. Sampling was performed throughout the abrasion test. After removing the test specimen, the chamber was prepared for the next specimen test.

Figure 5. Typical change in particle number concentration during the abrasion test. (a) neutralizer off (b) neutralizer on. Figure 5 shows the typical change in the particle number concentration during the abrasion test. During abrasion, the particle number concentration increased, whereas after abrasion, the particle number concentration decreased. (a) is the neutralizer off condition, and (b) is the neutralizer on condition. During the neutralizer on condition, the particle number concentration was higher than during the off condition. This is because the neutralizer can decrease the particle wall loss by minimizing the charged state of the particles.

Figure 6. Nanocomposites containing 0% CNTs and 2% CNTs. (a) and (b) are before abrasion and do not contain CNTs, while (c) and (d) are after abrasion and contain CNTs.

Figure 7. Particles sampled on the filter media. The particles released from the composite by abrasion were sampled on the filter and analyzed by FE-SEM. Most of the particles were torn particles due to abrasion, and no free CNT structures were observed.

Figure 8. Particles sampled on the TEM grid. The particles released from the nanocomposite by abrasion were sampled on the TEM grid and analyzed by FE-SEM. Most of the particles were torn due to abrasion, and no free CNT structures were observed.

Table 1. Chamber specifications for abrasion test. HEPA, high efficiency particulate air.

Table 2. Abrasion test conditions. lpm, liter per min; rpm, revolutions per min.

Table 3. Total particle number measured using CPC and OPC in 8 abrasion tests. The data are presented as the mean and standard deviation of 8 tests.

Table 4. Weight changes for nanocomposite specimens containing CNTs before and after abrasion.

Table 5. Total particle number released from the nanocomposites after the abrasion test.

DISCUSSION:

The most critical components of the nanorelease test of nanocomposite materials using abrasion were: 1) using a chamber system made of stainless steel with a neutralizer to remove the electrostatic charge generated by abrasion and to reduce the deposition of particles on the chamber walls; 2) supplying additional air to provide better particle suspension; and 3) sampling the released particles and monitoring them online using a CPC and OPC from the outlet that contained a mixer consisting of three perforated plates.

The abrasion tester was originally designed to evaluate abrasion resistance based on ISO 7784-1 or ISO 5470-114-15. Taber abrasion testers are now widely used to simulate sanding processes and to study the abrasion resistances of materials and coatings; such abrasion methods have been modified to examine the nanoparticle release from nanocomposite materials9-11. An abrasion test is also one of the simulation approaches included in the EU NanoReg2. However, conducting an abrasion test for nanocomposite materials requires consistent nanoparticle release, which is difficult due to particle charging caused by abrasion and by the conditions when the particle sampling is conducted near the emission point. Therefore, the proposed chamber setting for an abrasion test solves these problems by neutralizing the particles and sampling down-stream of the chamber outlet that contains a mixer. Thus, consistent particle release from nanocomposite specimens is achieved.

Several attempts have already been made to identify free CNTs released from nanocomposite materials. For example, epoxy-based nanocomposites containing CNTs have been tested for the release of carbon nanotubes using an abrasion process. As a result, transmission electron microscopy (TEM) observation indicated the emission of free-standing individual CNTs and agglomerates during abrasion16. In contrast, no free or bundled CNTs were observed in electron microscopic examinations of two different hybrid CNT composites (CNT-carbon composite and CNT-alumina composite) during machining processes, such as dry and wet band-sawing and rotary cutting17. Meanwhile, another CNT-epoxy nanocomposite study showed that the particles generated during sanding were mostly micron-sized particles with protruding CNTs and no free CNTs18. The current study of nanocomposite abrasion also found no generation of free CNTs when evaluated with extensive electron microscopy. Notwithstanding, the emitted CNT structures will differ depending on many factors, such as the mechanical process, the method of manufacturing the nanocomposite, the variety of CNT, the CNT content in the composite, and the resin used.

A chamber system has already been used to evaluate nanorelease from other products containing nanomaterials. For example, to evaluate the risk of silver nanoparticle exposure from antibacterial sprays containing silver nanoparticles, a chamber was successfully used to simulate exposure to silver nanoparticles7. Additionally, to overcome the difficulties involved with conducting exposure assessment studies in the workplace, simulation studies have been conducted in a chamber to evaluate the extent of silver nanoparticle exposure when working with printed electronic devices that use nanosilver ink. In this case, a chamber system containing a printed electronic device and all the sampling instruments described in this paper was shown to be effective for simulation silver nanoparticle exposure evaluation studies8. Thus, the proposed chamber method protocol is not limited to abrasion tests but can also be applied to other simulation studies in order to identify nanoparticle release from consumer products containing nanomaterials or nanocomposites.

Therefore, when taken together, the proposed protocol using a chamber system can be used to evaluate the safety of consumer products by simulating the handling and manufacturing processes of many products containing nanomaterials. In particular, the consistent results from the proposed chamber system in terms of particle release from products will contribute to the evaluation of the risk of exposure to nanomaterials released from products. The future goal is to standardize this protocol, with extended application to other nanocomposites or consumer products containing nanomaterials, in order to characterize human and environmental exposure through the nanomaterial life-cycle and to provide a tool for risk assessment.

ACKNOWLEDGMENTS:

This research was supported by the “Development of technologies for safety, evaluation, and standardization of nanomaterials and nanoproducts” grant (10059135) through the Korea Evaluation Institute of Industrial Technology and by the Korean Ministry of Trade, Industry, and Energy.

DISCLOSURES:

The authors have nothing to disclose.

REFERENCES:

1. Froggett, S. J., Clancy, S. F., Boverhof, D. R. & Canady, R. A. A review and perspectives of existing research on the release of nanomaterials from solid nanocomposites. Part Fibre Toxicol 11, 17, doi: 10.1186/1743-8977-11-17 (2014).

2. NanoReg, 2015. http://nanoreg.eu/images/2015_09_21_NANoREG_Factsheet_D3.3.pdf. (2015). accessed at 11/28/2015

3. ILSI (International Life Science Institute) Nanorelease consumer products, http://www.ilsi.org/ResearchFoundation/RSIA/Pages/NanoRelease1.aspx (2014), accessed at 12/3/20154.

4. Kingston, C., Zepp, R., Andrady, A., Boverhof, D., Fehir, R., Hawkins, D., et al. Release characteristics of selected carbon nanotube polymer composites. Carbon 68, 33-57, doi:10.1016/j.carbon.2013.11.042 (2014)

5. Kaiser, D., Stefaniak, A., Scott, K., Nguyen, T. & Schutz, J. Methods for the Measurement of Release of MWCNTs from MWCNT-Polymer Composites, NIST. Accessed at 12/3/2015 (2014)

6. Nowack, B., David, RM., Fissan, H., Morris, H., Shatkin, J. A., Stintz, M. et al. Potential release scenarios for carbon nanotubes used in composites. Environ. Int. 59, 1-11, doi: 10.1016/j.envint.2013.04.003 (2013)

7. Kim, E., Lee, J. H., Kim, J. K., Lee, G. H., Ahn, K., Park, J.D., et al. Case Study on Risk Evaluation of Silver Nanoparticle Exposure from Antibacterial Sprays Containing Silver Nanoparticles. J of Nanomaterial Article ID 346586, http://dx.doi.org/10.1155/2015/346586 (2015)

8. Kim, E., Lee, J. H., Kim, J. K., Lee, G. H., Ahn, K., Park, J.D., et al. Case study on risk evaluation of printed electronics using nanosilver ink. Nano Convergence, in press, DOI 10.1186/s40580-016-0065-y (2016)

9. Vorbau, M., Hillemann, L., & Stintz, M. Method for the characterization of the abrasion induced nanoparticle release into air from surface coatings. J. Aerosol Sci. 40, 209−217, doi:10.1016/j.jaerosci.2008.10.006, (2009)

10. Golanski, L., Gaborieau, A., Guiot, A., Uzu, G., Chatenet, J., Tardif, F. Characterization of abrasion-induced nanoparticle release from paints into liquids and air. J. Phys. Conf. Ser.304, 012062. doi: 10.1088/1742-6596/304/1/012062. (2011)

11. Wohlleben, W., Brill, S., Meier, M. W., Mertler, M., Cox, G., Hirth, S. et al. On the lifecycle of nanocomposites: Comparing released fragments and their in-vivo hazards from three release mechanisms and four nanocomposites. Small 7, 2384−2395. doi: 10.1002/smll.201002054, (2011)

12. ECMA-328, Determination of Chemical Emission Rates from Electronic Equipment, ECMA International, Geneva, Switzerland, (2013), available at http://www.ecma-international.org/publications/files/ECMA-ST/Ecma-328.pdf, accessed at 2/11/2016

13. SEMI (Semiconductor Equipment and Materials International) 4771A, New Standard: Test Method for Equipment Fan Filter Unit (EFFU) Particle Removal, SEMI. San Jose, CA. (2013). available at Source: http://downloads.semi.org/web/wstdsbal.nsf/de4d7939711aeedf8825753e0078317f/70256fe63dab49de8825788e0001d374/$FILE/4771A.pdf, accessed at 2/11/2016

14. ISO 7784-1, Paints and varnishes -- Determination of resistance to abrasion -- Part 1: Rotating abrasive-paper-covered wheel method, International Organization for Standardization, Geneva, Switzerland (1997).

15. ISO 5470-1, Rubber- or plastics-coated fabrics -- Determination of abrasion resistance -- Part 1: Taber abrader, International Organization for Standardization, Geneva, Switzerland, (1999).

16. Schlagenhauf L., Chu B. T. T., Buha J., Nüsch F, Wang J. Release of carbon nanotubes from an epoxy-based nanocomposites during an abrasion process. Enviorn. Sci. Tech. 46: 7366-7372, doi: 10.1021/es300320y (2012)

17. Bello, D., Wardle, B. L., Yamamoto, N., deVilloria, R. G., Garcia, E. J., Hart, A. J., et al. Exposure to nanoscale particles and fibers during machining of hybrid advanced composites containing carbon nanotubes. J. Nanopart. Res. 11, 231−249. doi: 10.1007/s11501-008-9499-4, (2009)

18. Cena, L. G., Peters, T. M. Characterization and control of airborne particles emitted during production of epoxy/carbon nanotube nanocomposites. J. Occup. Environ. Hyg. 8, 86−92. doi: 10.1080/15459624.2011.545943, (2011)