Table 4. Weight changes for nanocomposite specimens containing CNTs before and after abrasion.

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
|  | Before (g) | After (g) | Weight loss (g)=  Before-After | Weight loss, % |
| CNT (0%) | 38.6074 | 38.0032 | 0.6042 | 1.56 |
| CNT (2%) | 39.5159 | 38.9001 | 0.6158 | 1.56 |