July 29, 2026

Dr. Robert Lindsay

Corrosion and Protection Centre

School of Materials

The University of Manchester

Sackville Street

Manchester

M13 9PL, UK

Tel: +44 161 306 4824

Email: robert.lindsay@manchester.ac.uk

JoVE

Re: Manuscript Resubmission

Dear Editor,

On behalf of all the authors, I would like to thank the reviewers for their careful consideration of our manuscript, entitled “Determining the Chemical Composition of Corrosion Inhibitor/Metal Interfaces with XPS: Minimizing Post Immersion Oxidation”.  We have addressed their comments, along with the editorial comments (see below for our detailed responses). Alterations to the text are highlighted by red, bold text in the revised version of the manuscript (with track changes also on).

Sincerely,

Rob Lindsay

Editorial Comments/Responses:

- Formatting: Please remove references to the video.

The reference to the video has been removed (line 103).

2.	Grammar: -Please use American English throughout the manuscript, including figures. For instance, “normalised" should be “normalized”.

We ensured ‘Language’ was set to American English in Word to check for suitable spelling.  Also, have changed ‘Normalised’ to Normalized in figure labels.

3.	Line 91 – “a highly surface sensitive spectroscopy” – delete “a” and “highly”; if you mean “highly sensitive, “surface” needs to be moved.

The intention is to indicate a spectroscopy where the vast majority of the detected signal comes from the surface region (top few nanometers).  On this basis, have changed text to ‘a surface sensitive technique’.  This is a commonly accepted description of XPS, and so we believe it is appropriate to use it here.

4.	1.2.1 – “fume cupboard” – should be “fume hood”.

We have replaced ‘fume cupboard’ with ‘fume hood’.

5.	3.2.13, 3.2.14 – How is this performed? Manually or via software?

These operations are carried out manually.  Have modified 3.2.13 and 3.2.14 to reflect this approach.

6.	4.1, 4.6, 4.7 – How is this done? Manually or via software?

For 4.1 and 4.6, a keypad is used to drive the sample manipulator motors.  The text has been edited to reflect this procedure.

For 4.7, the XPS data acquisition software is used to acquire the XPS spectra.  Have modified text to reflect this action more clearly.

7.	Branding: 4.2 – Vision Manager

We have removed reference to Vision Manager from 4.2.

8.	Discussion: Please discuss any future applications of the protocol.

A final paragraph has been added to the Discussion to address this issue, i.e.

Finally, given the effectiveness of the approach outlined here, we expect it to be applied to other topics in corrosion (i.e. in addition to corrosion inhibition), where acquisition of XPS data from air-sensitive interfaces would add to understanding.  Moreover, such an approach should be considered in other fields where XPS measurements are undertaken from air-sensitive interfaces formed in a fluid environment.  Clearly, this procedure is not restricted to XPS, but could also be applied to any other UHV-based measurement from a surface that has previously been immersed in a liquid, e.g. scanning probe microscopy.

9.	For figures and tables that have been published before, please include phrases such as “Re-print with permission from (reference#)” or “Modified from..” etc. And please send a copy of the re-print permission for JoVE’s record keeping purposes.

Figure 2 is a significantly modified version of Figure 5 in Ref. 9.  Have added text to figure caption to acknowledge this point.

10.	JoVE reference format requires that the DOIs are included, when available, for all references listed in the article. This is helpful for readers to locate the included references and obtain more information. Please note that often DOIs are not listed with PubMed abstracts and as such, may not be properly included when citing directly from PubMed. In these cases, please manually include DOIs in reference information.

DOIs are included for all references where a DOI is available.  Could not find DOIs for Refs. 1, 2 and 6.

Reviewers' Comments/Responses:

Reviewer #1:

- Page 3 line 118-119, authors wrote: »Employ inhibited cooling fluid during the cutting procedure to mitigate any corrosion«. This is not due to corrosion, but not to induce additional mechanical damage.

We agree with the author that this is the purpose of the cooling fluid, and have modified the text accordingly.

- -Page 3, line 128: why in acetone. Is that really necessary? Any reference for that?

We have no specific reference for this procedure.  It is our usual procedure to ensure, as far as possible, that the substrate surface is contaminant free.  We have not systematically explored other solvent combinations, but are satisfied that our procedure is fit for purpose.  We note that, from empirical experience, the acetone is not strictly necessary.

- -What is the composition of carbon steel?

The following sentence has been added to the Representative Results section (lines 270-271) to state the composition of the carbon-steel:

The carbon-steel possessed a nominal weight% composition of C (0.08-0.13), Mn (0.30-0.50), P (0.04), S(0.05), and Fe (balance).

Reviewer #2:

- I am quite impressed with the success of the method in avoiding oxide build up during sample transfer. This results, I think, from maintaining a reacting surface right up to the point that a vacuum is drawn. This probably differs from earlier attempts to maintain a representative reactive surface where too much time is spent washing the sample in other solvents. I wonder if the authors agree. Perhaps there could be some discussion of this in the ms? To see that if this hypothesis is so, then it would be a good idea to minimize the sample area since acid vapors would be drawn into the pump and would eventually degrade the oil.

Our initial reason for avoiding post-immersion washing of the substrate was to preserve the inhibitor coverage and structure as far as possible. We were concerned that solvent washing was more likely to remove adsorbed corrosion inhibitor.  However, we do agree with the reviewer that oxidation may also occur during washing, especially if the solvent(s) used have not been de-aerated. We have not tested this hypothesis, and so have no experimental evidence.  To ensure that readers are aware of our thinking behind our specific procedure we have added a Note to 3.2.5:

Note:  Rinsing with solvents at this stage is not undertaken to minimize the potential of damaging the inhibited interface, e.g. inhibitor removal or interface oxidation.

We also agree with the reviewer that acid vapors may reduce the life of the load lock pumps.  As the reviewer suggests, a smaller sample may be reduce such damage.  However, if it is too small sample handling becomes increasingly challenging, especially as the glove-box gloves are being used.

- I know that the research results are secondary in this ms. However, it would be nice to see detailed S 2p and Cl 2p spectra to determine the nature of the bonding of these species to the metal.

As the reviewer implies, the purpose of the current paper is to detail the experimental procedure, so that others may employ it, and to show some representative results to demonstrate it utility. In our opinion, this goal has been achieved without presenting the S 2p/Cl 2p spectra.  These spectra for MBI have been presented previously (see Ref. 9, including Supplementary Data).  As regards OMID, we are preparing a manuscript to discuss this system, and prefer to not present/comment further on these data.