## Slide 1
15 um, 2 um, 2um
5kV-13nA
Carbon e-dep
(10 minutes)
15 um, 2 um, 2um
30kV- .3nA, 52° tilt
Tungsten i-dep
(6 minutes)*
Area Selected
Boundary observed at void-like structures
22 um, 25/27 um, 15um
30kV- 30nA, 52 ° tilt
Trench Mill: Si
(72 minutes)
20 um, 4um, 60 um
60kV-3nA, 52 ± 1.5° tilt
Cleaning cross-section: Si new
(15 minutes)**
U-cut (30kV-3nA)
Tungsten weld (30kV- .3nA):
C and W protective layer almost milled away
(18 minutes)***
*Spreading of W due to beam alignment at 20kx compared to 100kx
**Trench mill 2.5 um from protective layer: 4.2 um thick after trench mill, 2.2 um thick after cleaning
*** (width = 2um z-depth =thickness*3)
2um
4um
1
2
3
4a
5
4b

## Slide 2
6a
90°
90°
Rotation of needle 180° to rotate sample to suitable orientation, preventing preferential milling
As-Is
180 ° Rotation
10 um
12 um
12 um
10 um
6b
6c

## Slide 3
Deposit Tungsten i-beam front and back (8a, 8b) of the STO sample due to angled bottom u-cut (7)
30kV-.5nA
3 um z-depth
(17 minutes)
7
8a
8b
Deposit protective layers:
Carbon e-dep (9)
16um, 3um, 4 um
5kV- 13nA
(41 minutes)
Tungsten i-dep (10a/10b)
13.6 um, 2.61 um, 8 um
30kV- .3nA, 52° tilt
(40 minutes)
9
10a
10b