## Slide 1
Cu current collector
DC sputtered, 100 nm
Amorphous silicon anode
RF sputtered, 80 nm
LiPON electrolyte
RF sputtered, 1 μm
LiCoO2 cathode
RF sputtered, 2 μm
Pt current collector
DC sputtered, 150 nm
Al2O3 substrate