PROTOCOL FOR FILMING:

1. Preparation of sample and system:

- Mount a complete thin film battery on a 25 mm diameter aluminum SEM stub, and use a minimal amount of colloidal silver paste to electrically connect the cathode current collector to the SEM stub to minimize charging effects.

- Prior to pumping down the chamber, confirm a low-noise electrical pathway exists to the copper grid, which the nanobattery will be mounted to and will serve as the conductive pathway to the cathode (Figure 1).

    - If present, connect to the stage through a shielded electrical feedthrough, as is present in systems equipped for electron beam induced current (EBIC) measurements. Connect the positive lead of the potentiostat to this feedthrough using a shielded cable with the appropriate connection type. Internally, connect the feedthrough to the stage with a shielded wire with an exposed tip; method of securing the exposed wire tip will depend on the sample stage type, and, here, is held in place by an unused stage set screw.

- Similarly, create a conductive pathway from the micromanipulator tip to the outside of the probe by connecting the anode lead of the potentiostat to the micromanipulator ground using a BNC cable or an alligator clip as shown in Figure 1.

1.4.1. 	Perform the low-current noise test using the potentiostat in constant current mode. Using the connections described in step 1.4, a minimum stable current achieved was 10 pA ± 1 pA was achieved, due to unshielded grounds connected to the micromanipulator.

2. Lift-Out of Nanobattery

  - Load the sample into the SEM/FIB chamber and pump down to system specified high vacuum ( 10-5 mbar) before turning on electron beam and ion beam imaging.

  - With the focused beam and sample at eucentric height, tilt the sample such that the ion beam is normal to the battery surface (here 52°), and deposit a 1.5 to 2 µm thick layer of FIB-deposited organometallic platinum on the top current collector of the thin-film battery using an ion beam current of around 0.3 nA and dwell time of 200 ns over an area of 25 x 2 µm (Figure 2).

  - Set ion beam voltage to 30 kV and ion beam dwell time to 100 ns for the remainder of the experimental protocol.

  - Use a step-pattern cross-sectional FIB milling option, as provided in the FIB software, to expose the nanobattery stack around the Pt-deposit, as in TEM lamella preparation.1 Select a milling current  2.8 nA. Input a mill depth extending at least 1 µm beneath the active thin film battery (Z = 5 µm in this case) , a cross-sectional width (X) of 25 µm and a cross sectional height (Y) of 1.5 x Z (here, Y = 7.5 µm). Afterwards, the battery cross-section is exposed, to be viewed in SEM (here, the electron beam is 52° from surface normal).

  - Use a cross-section cleaning procedure, provided in the FIB software, where the ion beam incrementally rasters closer to the surface being cleaned, with an ion beam current  0.3 nA to clean off re-deposited material and clearly expose the layered structure (Figure 3).

  - Perform a series of rectangle under-cuts (also called J-cuts or U-cuts) at a stage tilt of 0°, beam current  2.8 nA to isolate the majority of the nanobattery (Figure 4a).2 Make under-cuts consisting of i) a lower rectangular 0.5 x 25 µm below the Au current collector onto the Al2O3 substrate, ii) a vertical rectangle 0.5 µm wide (X) and through the entirety of the nanobattery thickness (Y), and iii) a vertical rectangle 0.5 µm wide (X) and height less than the nanobattery thickness (Y - 2.5 µm) around the Pt-coated nanobattery. These three under-cuts should be performed in parallel mode (simultaneously milled), to prevent re-deposition of material within the under-cut regions.

  - Rotate the sample 180° and perform the same horizontal undercut as in step 2.5. This isolates the bottom and sides of the nanobattery except for the remaining connected region.

  - Rotate the sample 180°. Insert the micromanipulator to the park position specified in the control software, then slowly bring it in contact with the nanobattery using the x-y-z movement of the software.

  - Fix the micromanipulator to the Pt region on top of the nanobattery by ion-beam depositing 0.5 µm thick Pt using a 30 keV ion beam with a current of 10 pA over an area of 2 µm x 1 µm

  - Ion mill the remaining connected portion of the nanobattery with a beam current around 1 nA, and raise the nanobattery vertically with the micromanipulator (Figure 4b).

  - Mount the nanobattery on a Cu FIB lift-out grid with 2 µm thick ion-beam deposited Pt using a 30 keV ion beam with a current of 0.28 nA over an area of 10 µm x 5 µm.

  - Ion mill away the connection between the micromanipulator and nanobattery using a 30 keV ion beam with a current of 0.28 nA over an area of 1 µm x 1 µm to a depth of 2 µm, leaving a freestanding section attached to the Cu grid (Figure 5).1

3. Cleaning and Cycling Nanobattery

- Tilt the sample such that the ion beam is normal to the battery surface and use a cross-sectional cleaning procedure (see step 2.4) to remove re-deposited material over a 5 μm wide section of the nanobattery near the Cu grid, leading to a clear view of individual layers of the nanobattery (Figure 6a).

- Deposit 500 nm thick FIB-Pt using a 30 keV beam with a current of 0.1 nA over an area of 1 µm x 2 µm to create an electrical contact between the cathode current collector and the metallic grid, which is electrically connected to the stage (Figure 6b).

- Tilt the sample to 0° and using an ion beam current of 1 nA make a rectangle cut 3 µm wide and deep enough (Z ~ 2 µm)  to completely remove the anode current collector and electrolyte, isolating the anode from the Cu grid (Figure 6c).

- Use the cross-section cleaning procedure (see step 2.4) with an ion beam current around 0.1 nA to remove the re-deposited material around all the sides of the nanobattery cross-section until all the individual layers are distinctly visible as shown in Figure 6d.

- Insert the micromanipulator to the park position and using the control software bring the micromanipulator in contact with the Pt above the anode current collector, and ion beam deposit 0.2 µm thick Pt using 30 keV ion beam with a current of 10 pA over an area of 2 µm x 1 µm to “weld” connect the micromanipulator and current collector (Figure 6d).1

- Run the potentiostat in galvanostatic cycling mode. Current parameters used depend on the ultimate cross-sectional area of the fabricated nanobattery and desired C-rate, but will generally be on the order of a few nA.  We select charge and discharge currents such that the current density is on the order of tens of µA/cm2. For LiCoO2-based thin film batteries, the voltage range is 2.0 and 4.2 V.