# Submission ID #: 57696

# Scriptwriter Name: Bridget Colvin

Project Page Link: http://www.jove.com/files_upload.php?src=17597328

Title: A Novel Tenorrhaphy Suture Technique with Tissue Engineered Collagen Graft to Repair Large Tendon Defects

Authors and Affiliations: Prasad Sawadkar1, Jason Wong2, and Vivek Mudera1

1Division of Surgery and Interventional Science, University College London

2Blond McIndoe Laboratories, Division of Cell Matrix and Regenerative Medicine, MAHSC, University of Manchester

# Corresponding Author:

Prasad Sawadkar

Prasad.sawadkar@ucl.ac.uk

Tel:- (+44) 020 89542300 (ext 5839)

# Co-authors:

# Jason.K.Wong@manchester.ac.uk

# v.mudera@ucl.ac.uk

## Author Questionnaire

1. Microscopy: Does your protocol involve video microscopy, such as filming a complex dissection or microinjection technique?  N

2. Software: Does the part of your protocol being filmed demonstrate software usage? N

3. Filming location: Will the filming need to take place in multiple locations (greater than walking distance)?   N

# Introduction

- Introductory Interview Statements

REQUIRED:

  - Enter author name.: This method can help answer key questions in the tendon tissue engineering field about using collagen grafts for tendon reconstruction [1].

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera

REQUIRED:

  - Enter author name: The main advantage of this technique is that it uses a surgically optimized graft insertion technique to accommodate a tissue engineered tendon graft in vivo [1].

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera

OPTIONAL:

  - Enter author name: The implications of this technique extend toward the therapy of the tendon gap, because it is off the shelf and readily available to surgeons [1].

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera

OPTIONAL:

  - Enter author name: Though this method can provide insight into the surgical repair of tendons, it can also be applied to other repair procedures, such as nerve repair [1].

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera

OPTIONAL:

  - Enter author name: Visual demonstration of this method is critical, as the in vivo application of the suture can be difficult master without the use of a large number of live animals [1].

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera

# Introduction of Demonstrator on Camera

  - Enter name of author who will introduce demonstrator: Demonstrating the procedure will be Prasad Sawadkar, a post doc from our laboratory [1][2].

    - INTERVIEW: Author saying the above

    - Named demonstrator(s) looks up from workbench or desk or microscope and acknowledges camera

Ethics Title Card

  - Procedures involving animal subjects have been approved by the Institutional Review Board at University College London.

# Protocol

- Tissue Engineered (ET) Graft Preparation

  - Begin by adding 4 milliliters of rat tail collagen type 1 monomeric collagen solution to 500 microliters of 10x Minimal Essential Medium [1] and titrate against 5 and 1 molar sodium hydroxide to neutralize the solution [2].

    - WIDE: Talent adding collagen solution to medium, with collagen and medium containers visible in frame

    - Talent adding NaOH to solution, with 1- and 5-M NaOH containers visible in frame

  - Next add 500 microliters of Dulbecco’s Modified Eagle Medium to the solution [1] and transfer 5 milliliters of the mixture into a custom-built rectangular metal mold [2].

    - Medium being added to solution, with medium container label visible in frame

    - Talent adding mixture to mold Videographer: Important step

  - Then place the mold at 37 degrees Celsius and 5% CO2 for 15 minutes to facilitate matrix assembly [1].

    - Talent placing mold into incubator Videographer: Important step

  - After polymerization, transfer the collagen hydrogel from the mold into a standard plastic compression assembly in between two 50-micrometer nylon mesh sheets [2].

    - Hydrogel being placed into assembly between sheets, with empty mold visible in frame Videographer: Important step

  - Apply a static load of 120 grams to the assembly for 5 minutes to remove the interstitial fluid from the hydrogel [1], using four layers of filter paper to absorb the discharged fluid [2].

    - Talent placing load into assembly Videographer: Important step

    - Shot of filter absorbing fluid Videographer: Important step

  - After preparing three more hydrogels in the same manner [1], roll all four compressed gels together [2] and cut the roll into 15-millimeter segments [3].

    - Shot of 4 individual, compressed hydrogels

    - Shot of 4 layers of hydrogel, then gels being rolled up

    - Talent cutting roll

- Novel Tenorrhaphy

  - Before beginning the procedure, trim the hair on both hind limbs of a 16-25-week-old, male rabbit [1-TXT] and use a number 20 surgical blade to make a 9-centimeter incision in one limb around the inferior tibiofibular area to expose the tibialis posterior tendon [2].

    - WIDE: Talent trimming limb Videographer: More Talent than mouse in shot TEXT: Euthanasia: Anesthesia overdose

    - Incision being made/tendon being exposed

  - Then expose a 70-millimeter section of tendon [1] and wet the tissue with PBS to keep the tissue hydrated [2].

    - Tendon being exposed

    - PBS being added to tissue

  - Next, remove a 15-millimeter segment from the tendon at the midpoint [1] and replace the excised tissue with the engineered tissue collagen graft [2].

    - Tendon being cut Videographer: Important/difficult step

    - ET being placed Videographer: Important/difficult step

  - Using 3-0 core sutures, interlock the graft proximally from the native tendon ends, passing the sutures over the entire length of the graft to interlock the graft distally from the cut end [1].

    - Graft being sutured Videographer: Important/difficult step; Split action into separate shots as necessary

  - Secure both ends of the engineered tissue to the native tendon with 6-0 continuous running sutures around the periphery of the graft [1].

    - End(s) being secured

  - Then manually confirm that the tension on the sutures is appropriate and that there is no flaccidity in any of the sutures [1].

    - Tension being confirmed

## Protocol Script Questions

- Which steps from the protocol are the most important for viewers to see?

2.2.-2.5., 3.3., 3.4.

- What is the single most difficult aspect of this procedure and what do you do to ensure success?

3.3., 3.4.

# Results

- Results: Representative ET Mechanical Strength Testing

  - As demonstrated, the excised tendon gap is filled with a 15-millimeter-long engineered tissue tendon graft [1] and secured with 3-0 interlocked sutures at 70 millimeters to act as load barriers [2] and with 6-0 sutures to the native tissue [3].

    - LAB MEDIA: Figure 3 Video Editor: please emphasize light blue piece of “tissue” in center of graph

    - LAB MEDIA: Figure 3 Video Editor: please add arrow and “Epitendon Running Sutures” text

    - LAB MEDIA: Figure 3 Video Editor: please add arrow and “Modified Interlocked Sutures” text

  - The mean break strength of the repair was about 51 Newtons [1], significantly higher than that of the control Kessler repair of approximately 12 Newtons [2], demonstrating the influence of the core suture length and the distal interlocking in preventing repair failure at higher magnitude forces [3].

    - LAB MEDIA: Figure 4 left graph Video Editor: please emphasize Modified repair data bar

    - LAB MEDIA: Figure 4 left graph Video Editor: please add bracket and asterisk as in original Figure 4A

    - LAB MEDIA: Figure 4 left graph

  - In situ resistance experiments demonstrated a mean break strength of approximately 25 Newtons [1], significantly higher than the control mean break strength of about 14 Newtons [2].

    - LAB MEDIA: Figure 4 right graph Video Editor: please emphasize Modified repair data bar

    - LAB MEDIA: Figure 4 right graph Video Editor: please add bracket and asterisk as in original Figure 4B

# Conclusion

- Conclusion Interview Statements

  - Enter author name: Remember to formulate the neutralized collagen solution at an ideal pH and to manually ensure that the suture tension is appropriate and that there is no flaccidity within the suture [1].

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera

  - Enter author name: After its development, this technique paved the way for researchers in the fields of tissue engineering and tendon regeneration to explore tendon gap repair in human patients [1].

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera