# Submission ID #: 59553

# Scriptwriter Name: Melissa Ceo

# Project Page Link: https://www.jove.com/account/file-uploader?src=18163713

Title: Electrochemical Roughening of Thin-Film Platinum Macro and Microelectrodes

Authors and Affiliations: Anna N. Ivanovskaya1*, Anna M. Belle1*, Allison Yorita1, Fang Qian2, Supin Chen1, Angela Tooker1, Rose García Lozada1, Dylan Dahlquist1, Vanessa Tolosa1

1Engineering Directorate, Lawrence Livermore National Laboratory

2Physical and Life Science Directorate, Lawrence Livermore National Laboratory

*These authors share equal contribution

# Corresponding Author:

# Anna M. Belle

# belle1@llnl.gov

# Email addresses for Co-authors:

# ivanovskaya1@llnl.gov

# yorita1@llnl.gov

# qian3@llnl.gov

# supin@neuralink.com

# tooker1@llnl.gov

# garcialozada1@llnl.gov

# dahlquist2@llnl.gov

# vanessa@neuralink.com

# PLEASE READ THE INSTRUCTIONS IN THE GRAY BOXES CAREFULLY AND USE TRACK CHANGES WHILE MAKING ANY EDITS TO THE DOCUMENT.

# This document has several sections on separate pages, so take care to view each page.

Author Questionnaire:

Authors, please fill out the unanswered questions below.

1. Microscopy: Does your protocol involve video microscopy? Y, involves looking at device under microscope but no ‘microscopy action shots’

Can you record movies/images using your own microscope camera? Y, images

2. Does your protocol include software usage? Y

If yes, we will need you to record using screen recording software to capture the steps. If you use a Mac, QuickTime X also has the ability to record the steps.

3. Which steps from the protocol section below are the most important for viewers to see? Please list 4-6 individual steps using the step numbers listed in this document. This information is important to prepare your Videographer for your shoot. (You do not need to include steps that will be screen captured. Please do not list entire sections.)

    - (Now 2.1.1) Talent submerges the electrode tip of the device in a perchloric acid solution containing a platinum wire counter electrode and mercury reference sulfate electrode.

    - (Now 2.2.1) Talent connects the electrode of a multielectrode device.

    - (Now 2.2.2) Talent connects the working, counter and reference electrodes to the potentiostat.

    - (Now 4.1.1) Talent submerges the electrode tip of the device in a beaker of perchloric acid containing a platinum wire counter electrode and mercury reference sulfate electrode.

    - (Now 4.1.2) Talent connects an individual electrode and applies the pulsing paradigm.

    - (Now 4.5.1) Talent determines the increase in effective surface area of the macroelectrodes.

4. What is the single most difficult aspect of this procedure and what do you do to ensure success? Please list 1-2 individual steps using the step numbers listed in this document. (Please do not list entire sections.)

4.1.	Submerge the electrode tip of the device in a beaker of deoxygenated 500 millimolar perchloric acid that also contains a platinum wire counter electrode and mercury sulfate reference electrode [1].

5. Will the filming need to take place in multiple locations? N

# Section - Introduction

Videographer: Interviewee Headshots are required. Take a headshot for each interviewee.

Authors, these headshots will be used for the JoVE Dedicated Author Webpage. Here is one example if you wish to take a look.

- REQUIRED Interview Statements: (Said by you on camera)  - All interview statements may be edited for length and clarity.

- The total introduction length (i.e., Required and Optional Interview Statements) cannot exceed 150 words.

- Restrict the length of each statement to no more than 30 words.

- Please answer the questions below in full sentences to highlight the significance of your protocol. You will be expected to memorize and deliver these sentences as spoken interview statements during filming.

- Indicate the full name of each author who will give each statement. If only one author is giving the REQUIRED statements, the same author may speak both statements.

# Why is your protocol significant? OR What key questions can this method help answer?

  - Anna Ivanovskaya: Our protocol further develops an existing approach used over the last four decades and extends the applicability of electrochemical roughening to thin films and opens doors for miniaturization.

# What is the main advantage of this technique?

  - Anna Belle: By increasing the surface area of platinum electrodes without an additional coating, the devices are more robus and can last longer for electrical stimulation than a plated device.

OPTIONAL Interview Statements: (Said by you on camera)  - All interview statements may be edited for length and clarity.

- The following OPTIONAL questions may be answered to provide additional introductory information about your protocol.

- These OPTIONAL statements must be spoken by different authors than those who gave the Required Interview Statements.

- The length of each OPTIONAL statement is restricted to no more than 30 words and contributes to the total introduction length, which cannot exceed 150 words.

- Indicate the full name of each author who will give each OPTIONAL statement.

# How would you expect an individual who has never performed this technique to struggle?

# Do you have any advice to offer to somebody who is trying this technique for the first time?

  - Allison Yorita: We work with many different electrode geometries and found that parameters like electrode size, shape and layout influence roughening. We encourage researchers to vary pulsing parameters for their specific electrodes.

# Introduction of Demonstrator: (Said by you on camera)

- Please use this statement ONLY if any of the individuals who will be demonstrating the procedure on camera have not given a required or optional Introduction interview statement already.

- Include the full name(s) of the person(s) demonstrating the experiment followed by their title (e.g., technician, post doc, grad student, clinician, etc.)

- Also indicate the full name of the author who will introduce the demonstrator(s).

# Section - Protocol

- Read through the entire protocol carefully to understand what you will need on the filming day and prepare accordingly.

- The two-digit numbers (e.g. 2.1., 2.2.) represent the “steps” of you protocol and will be read by a professional voiceover talent.

- The three-digit numbers (e.g. 2.1.1., 2.2.2.) represent the “shots” that our videographer will capture at your lab.

- To ensure that your protocol can be filmed in a single work day, the protocol is restricted to 30 steps and/or 60 shots.

- It is critical for a smooth and organized shoot that all materials and work spaces are prepared and labeled (if applicable) in advance.

- Any specimens/samples that require long or overnight incubation steps should be prepared in advance. (i.e. day 0 sample preparation will be filmed on the day of the shoot; day 1 samples should be prepared the day before the shoot so their processing can be filmed on the day of the shoot/after their overnight culture/treatment/etc.)

- Cleaning the Pt Electrode(s) Before Initial Characterization and Surface Roughening

  - Next, submerge the electrode tip of the device in a 500 millimolar perchloric acid solution that also contains a platinum wire counter electrode and mercury sulfate reference [1].

    - Talent submerges the electrode tip of the device in a perchloric acid solution containing a platinum wire counter electrode and mercury reference sulfate electrode.

  - Connect one electrode or several short electrodes of a multielectrode device together as the working electrode [1]. Then, connect the working, counter, and reference electrodes to the potentiostat [2]. Authors, will one electrode or several electrodes be used in the video?

    - Talent connects the electrode of a multielectrode device.

    - Talent connects the working, counter and reference electrodes to the potentiostat.

  - To electrochemically clean the surface of electrodes by repetitive potential cycling, first open the EC-Lab software of a potentiostat [1]. To apply cyclic voltammograms, or CVs to the electrodes, press the plus sign to add electrochemical technique under the Experiment tab. In the pop-up window, Insert techniques will appear [2]. Click on Electrochemical techniques. When it expands, click on Voltamperometric techniques. When that expands, double click on Cyclic Voltammetry – CV [1]. In the Experiment window, fill in the appropriate parameters [1-TXT]. In the Experiment window of the EC-Lab software, press Advanced settings on the left. Under Advanced settings, select Electrode configuration = CE to ground [1]. Connect the working, counter and reference electrode to the instrument leads as shown on the Electrode connection diagram [2]. Press the Run button to begin the experiment. Perform repetitive potential cycles until the voltammograms visually appear to overlap from one cycle to the next, which typically occurs after 50 to 200 CVs [1].

    - Talent approaches the potentiostat and opens the software on the computer.

  - Click on Electrochemical techniques. When it expands, click on Voltamperometric techniques. When that expands, double click on Cyclic Voltammetry – CV [1].

    - SCREEN: To be provided by the authors. Authors, please upload this screen capture to your project page. TEXT: See text for parameters.

- Electrochemical Characterization of the Electrode Surface Before Roughening

  - To perform the electrochemical characterization, submerge the electrode tip of the device in a beaker of deoxygenated 500 millimolar perchloric acid that also contains a platinum wire counter electrode and mercury sulfate reference electrode [1].

    - Talent submerges the electrode tip of the device in a beaker of perchloric acid containing a platinum wire counter electrode and mercury reference sulfate electrode.

    - Talent connects the working, counter and reference electrodes to the instrument leads.

  - Under the Experiment tab in the EC-Lab software, press the plus sign to add electrochemical technique. In the pop-up window, Insert techniques will appear [1]. Click on Electrochemical techniques. When it expands, click on Voltamperometric techniques. When that expands, double click on Cyclic Voltammetry – CV [1]. In the Experiment window, fill in the appropriate parameters [1-TXT]. Under Advanced settings, select Electrode configuration = CE to ground [1]. Connect the working, counter and reference electrodes to the instrument leads as shown on the Electrode connection diagram [2]. Press the Run button to begin the experiment.

# Click on Electrochemical techniques. When it expands, click on Voltamperometric techniques. When that expands, double click on Cyclic Voltammetry – CV [1].

    - SCREEN: To be provided by the authors. Authors, please upload this screen capture to your project page. TEXT: See text for parameters.

  - Perform repetitive potential cycles until the voltammograms visually appear to overlap from one cycle to the next [1].Under Advanced settings, select Electrode configuration = CE to ground [1]. Connect the working, counter and reference electrodes to the instrument leads as shown on the Electrode connection diagram [2].

    - SCREEN: To be provided by the authors. Authors, please upload this screen capture to your project page.

    - Talent connects the working, counter and reference electrodes to the instrument leads.

  - If the two cathodic peaks of a platinum CV are poorly resolved, estimate the electrode surface area from the double layer capacitance at the electrode-solution interface [1]. Authors, can you provide a figure showing the poorly resolved peaks to be shown during this step?

    - Figure showing two cathodic peaks that are poorly resolved.

# Poorly resolved Peaks

# Better resolved peaks for the same electrode geometry, slower scan rate used to get better resolved peaks (this is Fig. 5B).

  - To measure the impedance spectra of a single electrode under open circuit conditions, first submerge the electrode tip of the device in PBS that also contains a platinum wire counter electrode and mercury sulfate reference [1]. Connect one electrode at a time as the working electrode [2].

    - Talent submerges the electrode tip of the device in a beaker of PBS containing a platinum wire counter electrode and mercury reference sulfate electrode.

    - Talent connects one electrode at a time to the instrument leads.

  - Under the Experiment tab in the EC-Lab software, press the plus sign to add electrochemical technique. In the pop-up window, Insert techniques will appear [1]. Click on Electrochemical techniques. When it expands, click on Impedance Spectroscopy. When that expands, double click on Potentio Electrochemical Impedance Spectroscopy. The 1-PEIS line will appear in the Experiment window [1]. In the Experiment window, fill in the appropriate parameters [1-TXT]. In the Experiment window in the EC-Lab software, press Advanced settings on the left [1]. Under Advanced settings, select Electrode configuration = CE to ground [1]. Connect the working, counter and reference electrodes to the instrument leads as shown on the Electrode connection diagram [2]. Then, press the Run button to begin the experiment [1].

  - Click on Electrochemical techniques. When it expands, click on Impedance Spectroscopy. When that expands, double click on Potentio Electrochemical Impedance Spectroscopy. The 1-PEIS line will appear in the Experiment window [1].

    - SCREEN: To be provided by the authors. Authors, please upload this screen capture to your project page. TEXT: See text for parameters.

- Electrochemical Roughening of a Macroelectrode and Characterization of Electrode Surface After Roughening

  - Submerge the electrode tip of the device in a beaker of deoxygenated 500 millimolar perchloric acid that also contains a platinum wire counter electrode and mercury sulfate reference electrode [1]. Then, connect an individual electrode as the working electrode and apply the pulsing paradigm to roughen the electrode [2].

    - Talent submerges the electrode tip of the device in a beaker of perchloric acid containing a platinum wire counter electrode and mercury reference sulfate electrode.

    - Talent connects an individual electrode and applies the pulsing paradigm.

  - Begin the roughening protocol with a series of oxidation/reduction pulses between minus 0.15 volts and 1.9 to 2.1 volts at 250 Hertz with a duty cycle of 1 to 1 for 10 to 300 seconds [1].

    - Open VersaStudio program for the PAR potentiostat. Expand the Experiment menu and select New.

  - In the Select Action pop-up window that appears, choose Fast potential pulses and enter the desired file name when prompted. The Fast potential pulses line will then appear under Actions to be performed tab [1]. Under the Properties of Fast Potential Pulses/Pulse properties, enter Number of pulses as 2, Potential 1 as minus 0.59 volts versus Ref for 0.002 seconds, and Potential 2 as 1.59 volts versus Ref for 0.002 seconds [1]. Authors, does ‘Ref’ stand for reference? Under Scan properties, enter Time per point as 1 second, number of cycles as 50,000 for a 200 second duration. Under Instrument properties, enter Current range = Auto [1]. Program the potentiostat with a prolonged application of a constant reduction potential by first pressing the plus button to insert a new step [1]. Next, double click on Chronoamperometry. Enter Potential as minus 0.59 volts, Time per point as 1 second and Duration as 180 seconds [1]. Press the Run button in the menu to start the roughening [1].

    - SCREEN: To be provided by the authors. Authors, please upload this screen capture to your project page.

  - Submerge the electrode tip of the device in a beaker of deoxygenated 500 millimolar perchloric acid that also contains a platinum wire counter electrode and mercury sulfate reference electrode [1]. Then, connect an individual electrode as the working electrode and apply the pulsing paradigm to roughen the electrode [2].

    - Talent submerges the electrode tip of the device in a beaker of perchloric acid containing a platinum wire counter electrode and mercury reference sulfate electrode.

    - Talent connects an individual electrode and applies the pulsing paradigm.

    - Talent at computer presses the Run button in the software.

  - Program will stop automatically when roughening procedure is complete.

    - SCREEN: To be provided by the authors. Authors, please upload this screen capture to your project page.

  - After the roughening is finished, determine the increase in effective surface area of the macroelectrodes as previously described [1]. Authors, which of the previous step do you want to show to demonstrate how to determine the increase in effective surface area?

    - Talent confirms roughening occurred (visually at microscope).

    - Talent performs cyclic voltammetry measurement (step 3) to determine the surface area of the roughened macroelectrodes.

    - SCREEN: To be provided by the authors. Authors, please upload this screen capture to your project page.

# Section – Results

# The Results section is restricted to 200 words of narrative. Please read through the results as presented to make sure that it accurately represents your findings. If you would like to highlight other data, please revise this section accordingly, keeping in mind the word count restriction. Please note that we cannot include narrative without an accompanying visual.

- Results: Characterization of Roughened of Thin-Film Platinum Electrodes

# Authors, please feel free to change the results title if you had something more fitting in mind.

  - A schematic showing the voltage application for roughening both macroelectrodes and microelectrodes is shown here [1].

    - LAB MEDIA: Figure 2

  - Optical microscopy can be used to visualize the difference in the appearance of a roughened macroelectrode or microelectrode [1].

    - LAB MEDIA: Figures 3 and 4 – Video Editor: Highlight figure 3 at mention of “roughened macroelectrode” and figure 4 at mention of “microelectrode”.

  - In addition, electrochemical characterization of the platinum surface using impedance spectroscopy and cyclic voltammetry can readily show the increased active surface area of a roughened macroelectrode and microelectrode [1].

    - LAB MEDIA: Figures 1 and 5 – Video Editor: Highlight figure 1 at mention of “a roughened macroelectrode” and figure 5 at mention of “microelectrode”.

  - The relationship between surface roughness and the number of roughening pulses applied for macroelectrodes is shown here [1].

    - LAB MEDIA: Figure 4

  - An example of different roughening parameters to maximally increase electrode active surface area for different electrode geometries is shown here [1].

    - LAB MEDIA: Table 1

# Section - Conclusion

- Conclusion Interview Statements: (Said by you on camera) - All interview statements may be edited for length and clarity.

- Below are questions for statements that can be used to further emphasize the significance of your protocol. At least one statement is required.

- Each statement is limited to 30 words.

- Answer the questions in full sentences, as you will be expected to memorize and deliver the sentences as spoken interview statements during filming.

- Indicate the full name of the author who will give each Conclusion Interview statement.

# What is most important thing to remember when attempting this procedure? Please indicate the steps (e.g., 2.4., 2.5.) in the Protocol section this advice correlates to.

  - Anna Ivanovskaya: Use high purity electrolytes for roughening (steps 3., 4.). Dilute high purity perchloric acid with deionized water, glass pipettes, plastic may dissolve in concentrated acid and use only dedicated glassware.

# Following this procedure, what other methods can be performed? What questions would these additional methods answer?

  - Anna Ivanovskaya: This procedure will improve techniques that benefit from high surface area. For example, enhancing optical spectroscopy signals of surface adsorbed species, increasing electrochemical reactor efficiency, and improving biosensor characteristics.

# After its development, did this technique pave the way for researchers to explore new questions within a specific scientific field? If so, how?

  - Anna Belle: This approach to electrode roughening will allow researchers to roughen the surfaces of thin-film electrodes for many different applications without compromising the integrity or lifetime of the electrode.

# Are any of the reagents or instruments hazardous? If so, please use this interview statement to remind viewers of what precautions they should take.

# Allison Yorita:  Perchloric acid is hazardous. When working with perchloric, use all appropriate personal protective equipment and only handle undiluted acid in a fume hood.

  - Thank you for following the instructions and addressing our questions. We will incorporate your answers/suggestions and send you the finalized script before your shoot. You will also receive detailed shoot preparation instructions in the email accompanying the finalized script.