Supplementary Information

Developing photosensitizer-Cobaloxime hybrid for solar-driven H2 production in aqueous aerobic conditions

Ab Qayoom Mir1, Dependu Dolui1, Shikha Khandelwal1, Harshil Bhatt2, Beena Kumari1, Sanmitra Barman3, Sriram Kanvah1, Arnab Dutta1*

[1] Chemistry Discipline, Indian Institute of Technology Gandhinagar, Gujarat 382355, India

[2] Chemistry Department, Uka Tarsadia University, Bardoli, Gujarat 394350, India

[3]Applied Sciences Department, BML Munjal University, Haryana 122413, India

Bulk Electrolysis or chronocoulometric experiment

The chronocoulometric experiment for complex C1 was executed in a four-neck glass vessel (Volume 150 mL including the head space) where a coiled 23 cm Pt wire (counter electrode), Ag/AgCl (in 1.0 M AgNO3 as reference electrode), and reticulated vitreous carbon (working electrode) was inserted in three of those necks. The last of the necks was closed with a 14/20 rubber septum, which was used for N2 purging before the experiment and for headspace gas collection (via gas tight leur-lock syringe). During the experiment, 75 mL of 0.20 mM C1 was included in the vessel along with all the electrodes and a magnetic bead in a gas-tight manner. After that, the solution was purged with N2 for one hour. Then, the purging was stopped, and the chrono-coulometric experiment was started at -1.3 V vs. ferrocene couple in 30:70 water/DMF. The solution was continuously stirred at 500 rpm with a magnetic stirrer during the experiment. The headspace gas was collected by a gas-tight leur-lock syringe after 30 minutes to analyze via a gas chromatography (GC) instrument. The GC was calibrated with a control gas mixture (49.5% H2 in N2).

Figure S1. (A) The charge passed during the chronocoulometric experiment performed with 0. 20 mM C1 in 30:70 water: acetonitrile media after 1 hour of electrolysis at -1.3 V vs. ferrocene couple. (B) The gas chromatography trace of the headspace gas following the bulk electrolysis experiment demonstrated the formation of H2 during the experiment.

Calculation of Faradic efficiency during chronocoulometric experiment

Overall charge passed for catalytic HER=3.62 C

Amount of H2 expected= 3.62 C96485 ×2 C mol=18.75 μmol=0.224 mLμmol × 18.75 mmol=4.2 mL

Amount of H2 detected in headspace by GC=2.9 mL (calibrated by control)

% of current effciency  of C1 bulk electrolysis= 2.94.2%=69%

Figure S2. The comparative optical spectra recorded for C1 before (black trace) and after the illumination (red trace) exhibiting the stability of the complex during the experiment.

Table 1. Crystallographic important parameters for C1.

| Crystal Data |  |
| --- | --- |
| CCDC Number | 1883987 |
| Moiety formula | C1.(CHCl3) |
| Empirical formula | C23H30ClCoN6O4. (CHCl3) |
| Formula weight | 668.28 |
| Crystal Size (mm3) | 0.348 x 0.179 x 0.051 |
| Crystal Habit | Red Cubic |
| Temperature (K) | 297.31 |
| Radiation | MoKα (λ=0.71073) |
| Crystal system | Triclinic |
| Space group | P-1 |
| Unit cell dimensions a/b/c Ao | 11.345 (3) 12.534 (3) 13.244 (3) |
| Unit cell angles α/β/ γ (θ) | 64.215 (6) 68.735 (4) 89.672 (5) |
| Unit cell volume (Ao3) | 1554.2 (6) |
| Z | 2 |
| Calculated density (g/cm3) | 1.428 |
| Absorption coefficient (mm-1) | 0.935 |
| F (000) | 688.0 |
| Θ range for all data collection (θ) | 5.834 to 55.862 |
| Index ranges | -14 < h < 14 -16 < k < 16 -17 < l < 17 |
| Reflections collected | 38751 |
| Independent reflections | 7396 [Rint= 0.0816, Rsigma= 0.0625] |
| Data/restraints/parameters | 7396/0/366 |
| Completeness to θmax | 0.993 |
| Refinement statistics |  |
| Final R indices [>2σ(I)] | R1= 0.0754, wR2= 0.2109 |
| R indices (all data) | R1= 0.1143, wR2= 0.2392 |
| Goodness-of-fit on F2 | 1.451 |

Table 2. Bond Lengths for C1(CHCl3).

| Atom | Atom | Length/Å | Atom | Atom | Length/Å |
| --- | --- | --- | --- | --- | --- |
| Co(1) | Cl(1) | 2.2342(11) | C(3) | C(4) | 1.497(7) |
| Co(1) | N(1) | 1.884(3) | C(5) | C(6) | 1.491(6) |
| Co(1) | N(2) | 1.898(3) | C(6) | C(7) | 1.457(6) |
| Co(1) | N(3) | 1.896(3) | C(7) | C(8) | 1.492(6) |
| Co(1) | N(4) | 1.885(3) | C(9) | C(10) | 1.366(5) |
| Co(1) | N(5) | 1.965(3) | C(10) | C(11) | 1.388(5) |
| O(1) | N(1) | 1.334(4) | C(11) | C(12) | 1.397(6) |
| O(2) | N(2) | 1.348(5) | C(11) | C(14) | 1.453(5) |
| O(3) | N(3) | 1.353(5) | C(12) | C(13) | 1.350(6) |
| O(4) | N(4) | 1.335(4) | C(14) | C(15) | 1.313(5) |
| N(1) | C(6) | 1.293(5) | C(15) | C(16) | 1.442(5) |
| N(2) | C(2) | 1.282(6) | C(16) | C(17) | 1.390(6) |
| N(3) | C(3) | 1.277(5) | C(16) | C(21) | 1.398(5) |
| N(4) | C(7) | 1.278(5) | C(17) | C(18) | 1.374(6) |
| N(5) | C(9) | 1.343(5) | C(18) | C(19) | 1.397(6) |
| N(5) | C(13) | 1.332(5) | C(19) | C(20) | 1.403(7) |
| N(6) | C(19) | 1.368(6) | C(20) | C(21) | 1.368(6) |
| N(6) | C(22) | 1.489(9) | Cl(1S) | C(1S) | 1.690(9) |
| N(6) | C(23) | 1.379(8) | Cl(2S) | C(1S) | 1.666(8) |
| C(1) | C(2) | 1.503(6) | Cl(3S) | C(1S) | 1.657(8) |
| C(2) | C(3) | 1.465(7) |  |  |  |