60899_screenshot_1.mp4

  - Focus the microscope on a network of interest and take a standard or tiled image.

  - Adjust the exposure time and neutral density filters to image the LNTs and minimize saturated exposure of the GUVs. Acquire images both in red and green channels.

NOTE: In these experiments, the red channel permits visualization of the Texas Red lipids, while the green channel permits visualization of the Oregon Green lipids and HiLyte488 microtubules.

60899_screenshot_2.mp4

  - Create composite image by overlaying red and green channels (Figure 1).

60899_screenshot_3.mp4

  - Characterize the LNT networks by measuring the lengths of the LNTs.

    - Open the acquired images using an image analysis software such as ImageJ.

    - Calibrate the scale for the microscope by using the set scale feature, filling in the pixels to m conversion factor, and click “ok.”

NOTE: The conversion factor is dependent on the microscope, objective lens, and camera, and may be obtained using a microscope calibration slide and generally expressed in pixels/m.

    - Use the multipoint line tool to measure the length of the nanotubes starting from the parent GUV. Hold “Ctrl +M” to measure the length.

    - Continue measuring lengths of individual tubes following the above procedure. The image processing tool will save each new measurement in the results window.

    - Hold “Ctrl + D” after drawing each line to keep track of which tubes have been measured.

60899_screenshot_4.mp4

  - Measure LNT thickness (Figure 2).

    - Open image in ImageJ and select the threshold feature under the Image tab.

    - Click “Apply” to apply the threshold.

    - Draw a rectangle of known length over the desired tube. Black pixels have a value of 0 and red pixels have a value of 255.

    - Measure the integrated density of the area.

    - Divide the density by the length (in pixels) of the LNT and 255 to obtain the thickness (in pixels)

NOTE: The thickness measurements may only be compared across images when the imaging settings and threshold are set identically.

60899_screenshot_5.mp4

  - Determine the lipid partitioning in nodes of LNTs (Figure 3).

    - Open the image in ImageJ

    - Use the line tool to draw a line over the desired node.

    - Measure the node intensity in both the Oregon Green and Texas Red channels.

    - Move the line to the LNT and measure the LNT intensity in both the Oregon Green and Texas Red channels.