# Supporting Information

Directed Assembly of Elastin-like Proteins into defined Supramolecular Structures and Cargo Encapsulation in vitro

Andreas Schreiber1,2†, Lara G. Stühn1,2†, Matthias C. Huber1,2, Süreyya E. Geissinger1,2, Stefan M. Schiller1,2,3,4, 5

1Center for Biological Systems Analysis University of Freiburg, Habsburgerstrasse 49, 79104 Freiburg, Germany.

2Faculty of Biology, University of Freiburg, Schänzlestrasse 1, 79104 Freiburg, Germany

4BIOSS Centre for Biological Signaling Studies, University of Freiburg, Schänzlestrasse 18, 79104 Freiburg, Germany

5IMTEK Department of Microsystems Engineering, University of Freiburg,

Georges-Köhler-Allee 103, 79110 Freiburg, Germany

6Cluster of Excellence livMatS @ FIT – Freiburg Center for Interactive Materials and Bioinspired Technologies, University of Freiburg, Georges-Köhler-Allee 105, 79110 Freiburg, Germany

†These authors contributed equally to this work

*Corresponding authors: Andreas Schreiber, E-mail: andreas.schreiber@zbsa.uni-freiburg.de, Stefan Schiller, E-mail: stefan.schiller@zbsa.uni-freiburg.de, Fax: +49761 203 8456

Table S2: Plasmids used for the expression of all amphiphilic ELP library proteins used in this study and the corresponding amphiphilic protein domains and sequences.

| plasmid | expressed amino acid sequence |
| --- | --- |
| pET28-NMBL-F20R20-mEGFP-His | MSSSGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGMVSKGEELFTGVVPILVELDGDVNGHKFSVSGEGEGDATYGKLTLKFICTTGKLPVPWPTLVTTLTYGVQCFSRYPDHMKQHDFFKSAMPEGYVQERTIFFKDDGNYKTRAEVKFEGDTLVNRIELKGIDFKEDGNILGHKLEYNYNSHNVYIMADKQKNGIKVNFKIRHNIEDGSVQLADHYQQNTPIGDGPVLLPDNHYLSTQSKLSKDPNEKRDHMVLLEFVTAAGITLGMDELYKGGREASSHHHHHH |
| pET28-NMBL-F20R20-mCherry-His | MSSSGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGMVSKGEEDNMAIIKEFMRFKVHMEGSVNGHEFEIEGEGEGRPYEGTQTAKLKVTKGGPLPFAWDILSPQFMYGSKAYVKHPADIPDYLKLSFPEGFKWERVMNFEDGGVVTVTQDSSLQDGEFIYKVKLRGTNFPSDGPVMQKKTMGWEASSERMYPEDGALKGEIKQRLKLKDGGHYDAEVKTTYKAKKPVQLPGAYNVNIKLDITSHNEDYTIVEQYERAEGRHSTGGMDELYKGGREASSHHHHHH |
| pET28-NMBL-mEGFP-E20F20-his | MDPMSSSGMVSKGEELFTGVVPILVELDGDVNGHKFSVSGEGEGDATYGKLTLKFICTTGKLPVPWPTLVTTLTYGVQCFSRYPDHMKQHDFFKSAMPEGYVQERTIFFKDDGNYKTRAEVKFEGDTLVNRIELKGIDFKEDGNILGHKLEYNYNSHNVYIMADKQKNGIKVNFKIRHNIEDGSVQLADHYQQNTPIGDGPVLLPDNHYLSTQSKLSKDPNEKRDHMVLLEFVTAAGITLGMDELYKGVPGEGVPGEGVPGEGVPGEGVPGEGVPGEGVPGEGVPGEGVPGEGVPGEGVPGEGVPGEGVPGEGVPGEGVPGEGVPGEGVPGEGVPGEGVPGEGVPGEGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGGREASSHHHHHH |
| pET28-(TAG)NMBL-R20F20-his | MA*SSSGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGGREASSHHHHHH |
| pET28-(TAG)NMBL-R40F20-his | MA*SSSGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGGREASSHHHHHH |
| pET28-(TAG)NMBXL-HTV-R40I20-his | MA*SSSGHHHHHHGENLYFQGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGIGVPGIGVPGIGVPGIGVPGIGVPGIGVPGIGVPGIGVPGIGVPGIGVPGIGVPGIGVPGIGVPGIGVPGIGVPGIGVPGIGVPGIGVPGIGVPGIG |
| pET28-(TAG)NMBXL-HTV-R40I30-his | MA*SSSGHHHHHHGENLYFQGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGRGVPGIGVPGIGVPGIGVPGIGVPGIGVPGIGVPGIGVPGIGVPGIGVPGIGVPGIGVPGIGVPGIGVPGIGVPGIGVPGIGVPGIGVPGIGVPGIGVPGIGVPGIGVPGIGVPGIGVPGIGVPGIGVPGIGVPGIGVPGIGVPGIGVPGIG |
| pET28-(TAG)NMBL-E20F20-his | MA*SSSGVPGEGVPGEGVPGEGVPGEGVPGEGVPGEGVPGEGVPGEGVPGEGVPGEGVPGEGVPGEGVPGEGVPGEGVPGEGVPGEGVPGEGVPGEGVPGEGVPGEGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGVPGFGGREASSHHHHHH |
|  | * depicts for unnatural amino acid e.g. para-Azidophenylalanin (pAzF) |