# -Submission ID #: 61184

# Scriptwriter Name: Bridget Colvin

Project Page Link: https://www.jove.com/account/file-uploader?src=18661168

Title: Standard Test Method ASTM D 7998-15 for the Cohesive Strength Development of Wood Adhesives

Authors and Affiliations: Charles R. Frihart and Linda F. Lorenz

USDA, Forest Service, Forest Products Laboratory

☒   All author names are spelled correctly, and the affiliations are correct (city/state/country information not included in video title page).

# Corresponding Author:

Charles R. Frihart

# Charles.r.frihart@usda.gov

# Co-authors:

Linda.f.lorenz@usda.gov

## Author Questionnaire

1. Microscopy: Does your protocol involve video microscopy, such as filming a complex dissection or microinjection technique?  No

2. Software: Does the part of your protocol being filmed demonstrate software usage?  Yes

3. Filming location: Will the filming need to take place in multiple locations (greater than walking distance)?   No

If Yes, how far apart are the locations? Click to enter distance between locations.

# Introduction

- Introductory Interview Statements

Your answers to these questions will become author interview statements, which will be incorporated into the script. Authors will memorize the statements and then deliver them on camera.

- Enter the full name of the author who will deliver the statement on camera.

- Each author should deliver no more than two statements.

- Please answer in full sentences, in a style suitable for being spoken aloud.

- Limit the length of each statement to 30 words or fewer.

- Answers will be edited for length, clarity, and consistency with journal style guidelines.

REQUIRED: Why is your protocol significant? OR What key questions can this method help answer?

  - Chuck Frihart: The Automated Bonding Evaluation System is the only test of wood adhesive bond shear strength that can provide information on the kinetics of cure of the adhesive.[1].

    - INTERVIEW: Chuck says the statement above in an interview-style shot, looking slightly off-camera

REQUIRED: What is the main advantage of this technique?

  - Chuck Frihart: This testing method has been very helpful in understanding the strength development of wood adhesives because it is much faster than other test methods and easy to use.[1].

    - INTERVIEW: Chuck says the statement above in an interview-style shot, looking slightly off-camera

OPTIONAL: Do the implications of this technique extend toward the therapy (or diagnosis) of a particular disease, disability, or challenge? How so?

  - Chuck Frihart: No.[1].

    - INTERVIEW: Chuck says the statement above in an interview-style shot, looking slightly off-camera

OPTIONAL: Are there any specific areas of research that this method could provide insight into? OR Can this method be applied to any other systems?

  - Chuck Frihart: This testing method can be applied to other adhesive systems, if it would be helpful to determine the strength of the adhesive, perhaps with different substrates. [1].

    - INTERVIEW: Chuck says the statement above in an interview-style shot, looking slightly off-camera

OPTIONAL: How would you expect an individual who has never performed this technique to struggle? Do you have any advice to offer to somebody who is trying this technique for the first time?

  - Linda Lorenz: I would not expect an individual who has never performed this technique to struggle. It is very easy to learn.[1].

    - INTERVIEW: Linda says the statement above in an interview-style shot, looking slightly off-camera

OPTIONAL: Why is visual demonstration of this method critical?

  - Linda Lorenz: It is always easier to learn to do something by watching someone do it rather than reading about how to do it.[1].

    - INTERVIEW: Linda says the statement above in an interview-style shot, looking slightly off-camera

# Introduction of Demonstrator on Camera

Complete this statement ONLY if any of the individuals who will be demonstrating the procedure on camera will not be delivering an Introductory Interview Statement.

  - Linda Lorenz:  I will be demonstrating the procedure [1][2].

    - INTERVIEW: Author saying the above

    - The named demonstrator(s) looks up from workbench or desk or microscope and acknowledges the camera

# Protocol

Please review this section to make sure that it accurately describes your protocol. Use Track Changes when making edits or revisions.

- The one-digit numbers represent sections of the video. The text will appear onscreen.

- The two-digit numbers (e.g. 2.1., 2.2.) represent steps of your protocol. The text will be recorded by a professional voiceover talent.

- The three-digit numbers (e.g. 2.1.1., 2.2.2.) represent the shots that our videographer will capture at your lab.

- To ensure that your protocol can be filmed in one day, the protocol is restricted to 30 steps and/or 60 shots. Current script of protocol: 24 steps, 54 shots.

Please use this draft script to help you prepare for filming day.

- Filming should take no more than 10 minutes per step. If a step will take more than 10 minutes, prepare the product from that step in advance.

- Substrate Preparation

  - To prepare the substrate, select a substrate surface that is suitable for the application [1]. For wood, use a sliced veneer of about 0.6-0.8-millimeters thick [2-TXT].

    - WIDE: Talent selecting surface

    - Side shot of 0.6-0.8-mm-thick wood TEXT: See text for full suggested wood veneer details

  - Avoid veneers that are excessively wavy [1], have an uneven surface [2], and/or contain defects, including discoloration [3].

    - Shot of veneers to be avoided Video Editor: please emphasize excessively wavy veneer

    - Use 2.2.1. Video Editor: please emphasize uneven veneer

    - Use 2.2.1. Video Editor: please emphasize veneer with defects

  - At least one day before its use, condition the wood, unstacked, at 21 degrees Celsius and a 50% relative humidity [1].

    - Linda placing wood at 21 °C and 50% RH

- Specimen Preparation

  - To prepare the specimen from the selected substrate, after conditioning, check the veneer for any cracks, discoloration, or grain irregularities to be avoided when cutting [1] and confirm the functionality of the pneumatically driven specimen cutting device [2].

    - WIDE: Linda checking specimen

    - Linda checking device

  - Next, use a special die cutter that can trim the specimen to a 20- x 117- x 0.6-0.8-millimeter dimension [1] and place an at least 150- x 300-millimeter piece of veneer under the cutting blades with the veneer grain parallel to the long direction [2].

    - Linda using cutter

    - Linda placing veneer under blades parallel to grain

  - Depress the air pressure button to cut 20- x 117-millimeter pieces of wood [1], moving the piece of veneer under the cutting blades to an uncut area [2] and depressing the button again to cut each new piece of wood until the entire substrate has been cut into pieces [3].

    - Linda pressing button and removing the sample to show a smooth cut compared to a ragged edge

    - Linda moving veneer/cutting wood

    - Linda pressing button/cutting wood

- Equipment Operability

  - Before initiating the bonding process, make sure that the Automated Bonding Evaluation System equipment is operating properly according a standard operating procedure [1] and set the LP (low pressure gauge) to 0.2 megapascals, the HP (high pressure gauge) to 0.2 megapascals, the Pull gauge to 0.65 megapascals, and the Cool Air gauge to 0.2 megapascals [2].

    - WIDE: Linda checking equipment functionality

    - Linda setting device settings

  - Clean the platens of any adhesive that resulted from squeeze out from the prior sample [1] and adjust the platen temperature to the desired temperature [2].

    - Linda cleaning platen

    - Linda adjusting temperature

  - Then equilibrate the platens [1].

    - Linda being equilibrated

- Specimen Bonding

  - For adhesive bonding of the specimen, first tare each specimen on a balance [1] before spreading 5 milligrams of the experimental adhesive over the terminal 0.5 centimeter of each specimen [2], providing sufficient cover of the bonding area without excessive squeeze out upon application of the second specimen [3].

    - WIDE: Linda placing specimen onto balance

    - Linda spreading adhesive

    - Shot of sufficient adhesive on end of specimen

  - Then re-weigh the specimen after the adhesive application [1] and place a second specimen onto the adhesive [2], taking care that the two specimens are aligned [3].

    - Linda placing specimen onto balance

    - Linda placing a second specimen onto adhesive

    - Pieces being aligned

- Final Strength Data

  - To bond the specimens, close the grips on the ABES tester [1], making sure that the sample is aligned with the tester [2] and press Start [3] … to have the 120-degree Celsius platens apply pressure to the overlapped section for 2 minutes [4].

    - WIDE: Linda closing grips

    - Sample being aligned with tester

    - Linda pressing Start, emphasizing safety by hands not being near the platens

    - Platens applying pressure (close up)

  - At the end of the heat pressing time , retract the platens and retract the grips [1] and place the specimens at 21 degrees Celsius and 50% relative humidity overnight [2].

    - Linda retracting platens and retracting grips

    - Linda placing specimen(s) at 21 °C

  - The next morning, insert a conditioned sample into the ABES tester [1] and press Start [2] to have the instrument pull one end of the specimen through the servodrive [3] while the other end of the sample pulls on a load cell [4] attached to the grips until the bond breaks [5].

    - Linda inserting sample into tester

    - Linda pressing Start

    - Instrument pulled end through servodrive (.3, .4, and .5)

    - Sample pulling load cell

    - Bond break/shot of broken bond

  - The computer will record the maximum force the sample can withstand as the bond strength [1].

    - SCREEN: To be provided by Authors: Readout of bond strength/maximum strength

- Kinetic Strength Development

  - To determine the rate of strength development of an adhesive to estimate the press time required for large scale products [1], begin the strength testing at a 100-degree Celsius platen temperature for 10 seconds [2].

    - WIDE: Linda closing grips on specimen

    - Linda pressing Start/platens pressing specimen

  - At the end of bonding time, retract the platens [1] and use the air cooling feature of the ABES to cool the sample to near room temperature [2].

    - Platens being retracted (close up)

    - Sample being cooled (close up)

  - When the sample has cooled, test the sample again at the same temperature but for an increased period of pressure [1-TXT], until increasing the time results in little or no increasing strength [2].

    - Sample being pressed TEXT: i.e., 10, 30, 60, 90, 120, 150, 180, and 210 s

    - Strength being tested

  - When all of the bond times have been tested, raise the temperature by 10 degrees Celsius [1] and repeat the heated pressure applications for increasing periods of time [2] until there is no longer any linear section of strength versus time at the bonding times [3].

    - Linda checking temperature

    - Linda pressing Start/platens pressing sample

    - LAB MEDIA: Figure 3A

- Heat Resistance and Failed Bonding Surface Image Analysis

  - If the product needs to meet a certain temperature resistance, [1] heat the platens to the temperature above which the adhesive starts to degrade and insert the bonded sample into the ABES unit.[2].

    - WIDE: Linda setting temperature

    - Linda inserting sample into unit

  - Close the platens onto the pre-bonded sample for 2 minutes [1] and measure the bond strength demonstrated to determine any thermal softening of the adhesive compared to the bonding temperature of 120 degrees Celsius [2].

    - Linda closing platens

    - Specimen being pulled

  - Then repeat the test after a 30-minute heat pressure application [1] and test for strength to determine strength if the adhesive is thermally degraded [2].

    - Linda closing platens

    - Specimen being pulled

  - Because the main objective is to determine the adhesive strength or rate of cohesive strength development, be sure to test if the failure is within the adhesive or with the adhesion to the substrate or substrate failure [1].

    - Authors: How is this tested? Please provide more details. After the bond is broken, the entire sample and bonded area is observed to determine where failure has occurred. View samples of different types of break with Linda describing them.

  - If substrate failure occurs, then the adhesive has sufficient strength [1], while cohesive failure in the bulk adhesive indicates adhesive weakness [2].

    - LAB MEDIA: Figure 4 Video Editor: please emphasize left wood image

    - LAB MEDIA: Figure 4 Video Editor: please emphasize right wood image

## Protocol Script Questions

# Authors: Please use the step numbers from the script above (not step numbers from the manuscript) when answering the questions below. Please do not include steps that will be screen-captured and do not list entire sections.

  - A. Which steps from the protocol are the most important for viewers to see? Please list 4 to 6 individual steps.

2.1.	To prepare the substrate, select a substrate surface that is suitable for the application [1]. For wood, use a sliced veneer of about 0.6-0.8-millimeters thick [2-TXT]

3.2 Next, use a special die cutter that can trim the specimen to a 20- x 117- x 0.6-0.8-millimeter dimension [1] and place an at least 150- x 300-millimeter piece of veneer under the cutting blades with the veneer grain parallel to the long direction.

  - 3.3 Depress the air pressure button to cut 20- x 117-millimeter pieces of wood [1], moving the piece of veneer under the cutting blades to an uncut area [2] and depressing the button again to cut each new piece of wood until the entire substrate has been cut into pieces [3].

  - 5.1 For adhesive bonding of the specimen, first tare each specimen on a balance [1] before spreading 5 milligrams of the experimental adhesive over the terminal 0.5 centimeter of each specimen [2], providing sufficient cover of the bonding area without excessive squeeze out upon application of the second specimen [3].

  - 6.1 To bond the specimens, close the grips on the ABES tester [1], making sure that the sample is aligned with the tester [2] and press Start [3] … to have the 120-degree Celsius platens apply pressure to the overlapped section for 2 minutes [4].

  - 6.3 The next morning, insert a conditioned sample into the ABES tester [1] and press Start [2] to have the instrument pull one end of the specimen through the servodrive [3] while the other end of the sample pulls on a load cell [4] attached to the grips until the bond breaks [5].

B. What is the single most difficult aspect of this procedure and what do you do to ensure success? Please list 1 or 2 individual steps from the script above.

5.1 For adhesive bonding of the specimen, first tare each specimen on a balance [1] before spreading 5 milligrams of the experimental adhesive over the terminal 0.5 centimeter of each specimen [2], providing sufficient cover of the bonding area without excessive squeeze out upon application of the second specimen [3].

To ensure success in applying the experimental adhesive to the specimen, it is useful to weigh the amount of adhesive applied to the specimen.

6.1 To bond the specimens, close the grips on the ABES tester [1], making sure that the sample is aligned with the tester [2] and press Start [3] … to have the 120-degree Celsius platens apply pressure to the overlapped section for 2 minutes [4].

To ensure success in aligning the sample with the tester, set it in the sample supports and observe that the sample is straight and overlapped 0.5 centimeter in the bonding area.

If answered, your answers to C and D will become interview-style shots, which may be incorporated into the script after the relevant step in the protocol. Authors will memorize the statements and then deliver them on camera.

# C. OPTIONAL: If there is no single most critical step in the filmed portion of the protocol, do not answer this question. What is the best way to perform the required technique for the most critical step in the protocol?

# Chuck Frihart: (6.1) Make sure that the bonded area is overlapped 0.5 centimeters, because that area is critical in determining the strength of the bond.

# D. OPTIONAL: If there are no hazardous reagents or instruments in the filmed portion of the protocol, do not answer this question. Which of the reagents or instruments are uniquely hazardous? What precautions should viewers take?

# Linda Lorenz: (6.1) The platens are hot and can cause burns if the operator touches them. Be aware of the hot platens and do not touch them. Make sure hands are not near the closing platens.

# Results

Please review this section to make sure that it accurately reflects your findings.

- Use Track Changes when making edits or revisions.

- If you would like the video to include different results, please revise this section.

- When revising, please keep the length of the voiceover below 200 words. Current word count: XXX. (Voiceover is the text that follows the two-digit numbers.)

- Please note that the video cannot include voiceover without an accompanying visual.

- Results: Representative Protein Adhesion Analyses

  - As this set of isothermal strength development plots demonstrate, the temperature and time of bonding effect of the strength development of adhesive bonds and therefore, the sensitivity of wood processing conditions. As the bonding temperature increases, higher bonding strengths can be developed in shorter bond pressing times. Authors: please provide text (1-2 sentences) describing what information can be gained from this figure [1].

    - LAB MEDIA: Figure 3A

  - In this derived plot of regressed bonding rate against temperature, an increased strength development rate is achieved at higher temperatures. A stronger bond can be developed in less time at higher temperatures. Authors: please provide text (1-2 sentences) describing what information can be gained from this figure [1].

    - LAB MEDIA: Figure 3B

  - As observed in this image of failed samples, an adhesion failure due to the adhesive being stronger than the wood, resulting in the bond breaking in the wood and wood failure, Authors: please provide additional text to describe what is illustrated with the sample on the left can be visualized [1], while in this sample a cohesive failure due to the adhesive being weaker than the wood, with the bond breaking within the adhesive, Authors: please provide additional text to describe what is illustrated with the sample on the right can be seen [2].

    - LAB MEDIA: Figure 4 Video Editor: please emphasize boards on left of image

    - LAB MEDIA: Figure 4 Video Editor: please emphasize boards on right of image

# Conclusion

- Conclusion Interview Statements

Below are prompts for interview statements that can be used to further emphasize the significance of your protocol.

- At least one statement is required.

- Each statement is limited to 30 words.

- Answer the questions in full sentences; you will need to memorize and deliver the sentences as spoken interview statements during filming.

- Indicate the full name of the author who will give each statement.

# What is the most important thing to remember when attempting this procedure? Please indicate the steps (e.g., 2.4., 2.5.) in the Protocol section of the script that this advice applies to.

  - Chuck Frihart: Make sure that the bonded area is overlapped 0.5 centimeters, because the bonded area is critical in determining the strength of the bond.[1].

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera (6.1)

# Following this procedure, what other methods can be performed? What questions would these additional methods answer?

  - Chuck Frihart: The heat sensitivity of bonds can be measured to answer the question of what is the temperature at which the adhesive will degrade or fail. [1].

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera

# After its development, did this technique pave the way for researchers to explore new questions within a specific scientific field? If so, how?

  - Chuck Frihart: Because the strength of wood adhesive bonds at different times and temperatures can be measured, kinetic data can be determined, which was not possible before this technique was developed. [1].

Thank you for addressing our questions. We will incorporate your answers and suggestions and send you the final script before your filming day. You will also receive detailed preparation instructions in the email accompanying the final script.