# Submission ID #: 61184

# Scriptwriter Name: Bridget Colvin

Project Page Link: https://www.jove.com/account/file-uploader?src=18661168

Title: Standard Test Method ASTM D 7998-15 for the Cohesive Strength Development of Wood Adhesives

Authors and Affiliations: Charles R. Frihart and Linda F. Lorenz

USDA, Forest Service, Forest Products Laboratory

☐   All author names are spelled correctly, and the affiliations are correct (city/state/country information not included in video title page).

# Corresponding Author:

Charles R. Frihart

# Charles.r.frihart@usda.gov

# Co-authors:

Linda.f.lorenz@usda.gov

## Author Questionnaire

1. Microscopy: Does your protocol involve video microscopy, such as filming a complex dissection or microinjection technique?  N

2. Software: Does the part of your protocol being filmed demonstrate software usage?  N

3. Filming location: Will the filming need to take place in multiple locations (greater than walking distance)?   Enter Yes or No.

If Yes, how far apart are the locations? Click to enter distance between locations.

# Introduction

- Introductory Interview Statements

Your answers to these questions will become author interview statements, which will be incorporated into the script. Authors will memorize the statements and then deliver them on camera.

- Enter the full name of the author who will deliver the statement on camera.

- Each author should deliver no more than two statements.

- Please answer in full sentences, in a style suitable for being spoken aloud.

- Limit the length of each statement to 30 words or fewer.

- Answers will be edited for length, clarity, and consistency with journal style guidelines.

REQUIRED: Why is your protocol significant? OR What key questions can this method help answer?

  - Enter author name.: Click here to answer question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.[1].

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera

REQUIRED: What is the main advantage of this technique?

  - Enter author name: Click here to answer question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.[1].

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera

OPTIONAL: Do the implications of this technique extend toward the therapy (or diagnosis) of a particular disease, disability, or challenge? How so?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.[1].

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera

OPTIONAL: Are there any specific areas of research that this method could provide insight into? OR Can this method be applied to any other systems?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.[1].

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera

OPTIONAL: How would you expect an individual who has never performed this technique to struggle? Do you have any advice to offer to somebody who is trying this technique for the first time?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.[1].

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera

OPTIONAL: Why is visual demonstration of this method critical?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.[1].

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera

# Introduction of Demonstrator on Camera

Complete this statement ONLY if any of the individuals who will be demonstrating the procedure on camera will not be delivering an Introductory Interview Statement.

  - Enter name of author who will introduce demonstrator: Demonstrating the procedure will be Click here to enter name of demonstrator(s)., a Click here to enter demonstrator job title. from my laboratory. Include additional demonstrators as needed.[1][2].

    - INTERVIEW: Author saying the above

    - The named demonstrator(s) looks up from workbench or desk or microscope and acknowledges the camera

# Protocol

Please review this section to make sure that it accurately describes your protocol. Use Track Changes when making edits or revisions.

- The one-digit numbers represent sections of the video. The text will appear onscreen.

- The two-digit numbers (e.g. 2.1., 2.2.) represent steps of your protocol. The text will be recorded by a professional voiceover talent.

- The three-digit numbers (e.g. 2.1.1., 2.2.2.) represent the shots that our videographer will capture at your lab.

- To ensure that your protocol can be filmed in one day, the protocol is restricted to 30 steps and/or 60 shots. Current script of protocol: 24 steps, 54 shots.

Please use this draft script to help you prepare for filming day.

- Filming should take no more than 10 minutes per step. If a step will take more than 10 minutes, prepare the product from that step in advance.

- Substrate Preparation

  - To prepare the substrate, select a substrate surface that is suitable for the application [1]. For wood, use a sliced veneer of about 0.6-0.8-millimeters thick [2-TXT].

    - WIDE: Talent selecting surface

    - Side shot of 0.6-0.8-mm-thick wood TEXT: See text for full suggested wood veneer details

  - Avoid veneers that are excessively wavy [1], have an uneven surface [2], and/or contain defects, including discoloration [3].

    - Shot of veneers to be avoided Video Editor: please emphasize excessively wavy veneer

    - Use 2.2.1. Video Editor: please emphasize uneven veneer

    - Use 2.2.1. Video Editor: please emphasize veneer with defects

  - At least one day before its use, condition the wood, unstacked, at 22 degrees Celsius and a 50% relative humidity [1].

    - Talent placing wood at 22 °C and 50% RH

- Specimen Preparation

  - To prepare the specimen from the selected substrate, after conditioning, check the veneer for any cracks, discoloration, or grain irregularities to be avoided when cutting [1] and confirm the functionality of the pneumatically driven specimen cutting device [2].

    - WIDE: Talent checking specimen

    - Talent checking device

  - Next, attach a special die cutter that can trim the specimen to a 20- x 117- x 0.6-0.8-millimeter dimension [1] and place an at least 150- x 300-millimeter piece of veneer under the cutting blades with the veneer grain parallel to the long direction [2].

    - Talent attach cutter to device

    - Talent placing veneer under blades

  - Depress the air pressure button to cut 20- x 117-millimeter pieces of wood [1], moving the piece of veneer under the cutting blades to an uncut area [2] and depress the button again to cut each new piece of wood until the entire substrate has been cut into pieces [3].

    - Talent pressing button

    - Talent moving veneer/cutting wood

    - Talent pressing button/cutting wood

- Equipment Operability

  - Before initiating the bonding process, make sure that the Automated Bonding Evaluation System equipment is operating properly according a standard operating procedure [1] and set the LP Press to 0.2 megapascals, the HP Press to 0.2 megapascals, the Pull to 0.65 megapascals, and the Cool Air to 0.2 megapascals [2].

    - WIDE: Talent checking equipment functionality

    - Talent setting device settings

  - Clean the platens of any adhesive that resulted from squeeze out from the prior sample [1] and adjust the platen temperature to the desired temperature [2].

    - Talent cleaning platen

    - Talent adjusting temperature

  - Then equilibrate the platens [1].

    - Platens being equilibrated

- Specimen Bonding

  - For adhesive bonding of the specimen, first tare each specimen on a balance [1] before spreading 5 milligrams of the experimental adhesive over the terminal 0.5 centimeters of each specimen [2], providing sufficient cover of the bonding area without excessive squeeze out upon applicant of the second specimen [3].

    - WIDE: Talent placing specimen onto balance

    - Talent spreading adhesive

    - Shot of sufficient adhesive on end of specimen

  - Then re-weigh the specimen after the adhesive application [1] and place a second specimen onto the adhesive [2], taking care that the two specimens are aligned [3].

    - Talent placing specimen onto balance

    - Talent placing specimen onto adhesive

    - Pieces being aligned

- Final Strength Data

  - To bond the specimens, close the grips on the ABES tester [1], making sure that the sample is aligned with the tester [2] and press Start [3] … to have the 120-degree Celsius platens apply pressure to the overlapped sections for 2 minutes [4].

    - WIDE: Talent closing grip(s)

    - Sample being aligned with tester

    - Talent pressing Start

    - Platens applying pressure

  - At the end of the heat press, retract the platens and loosen the grips [1] and place the specimens at 22 degrees Celsius and 50% relative humidity overnight [2].

    - Talent retracting platens and/or loosening grip(s)

    - Talent placing specimen(s) at 22 °C

  - The next morning, lock a conditioned sample onto the ABES tester [1] and press Start [2] to have the instrument pull one end of the specimen through the servodrive [3] while the other end of the sample pulls on a load cell [4] attached to the grips until the bond breaks [5].

    - Talent locking sample onto tester

    - Talent pressing Start

    - Instrument pulled end through servodrive

    - Instrument pulling load cell

    - Bond break/shot of broken bond

  - The computer will record the maximum force the sample can withstand as the bond strength [1].

    - SCREEN: To be provided by Authors: Readout of bond strength/maximum strength

- Kinetic Strength Development

  - To determine the rate of strength development of an adhesive to estimate the press time required for large scale products [1], begin the strength testing at a 100-degree Celsius platen temperature for 10 seconds [2].

    - WIDE: Talent tightening grip around specimen

    - Talent pressing Start/platens pressing specimen

  - At the end of bonding session, retract the platens [1] and use the air cooling feature of the ABES to cool the sample to near room temperature [2].

    - Platen being retracted

    - Sample being cooled

  - When the sample has cooled, test the sample again at the same temperature but for an instead period of pressure [1-TXT], until increasing the time results in little or no increasing strength [2].

    - Sample being pressed TEXT: i.e., 10, 30, 60, 90, 120, 150, 180, and 210 s

    - Strength being tested

  - When all of the bond times have been tested, raise the temperature by 10 degrees Celsius [1] and repeat the pressure applications for increasing periods of time [2] until there is no longer any linear section of strength versus time at the low bonding times [3].

    - Talent checking temperature

    - Talent pressing Start/platens pressing specimen

    - LAB MEDIA: Figure 3A

- Heat Resistance and Failed Bonding Surface Image Analysis

  - If the product needs to meet a certain temperature resistance, clamp the bonded sample into the ABES unit [1] and heat the platens the temperature above which the specimen starts to degrade [2].

    - WIDE: Talent clamping sample onto unit

    - Talent setting temperature

  - Close the platens onto the pre-bonded sample for 2 minutes [1] and measure the bond strength demonstrated to determine any thermal softening of the adhesive compared to the bonding temperature of 120 degrees Celsius [2].

    - Talent closing platen(s)

    - Specimen being pulled

  - Then repeat the test after a 30-minute heat pressure application [1] and test for strength to determine strength if the adhesive is thermally degraded [2].

    - Talent closing platen(s)

    - Specimen being pulled

  - Because the main objective is to determine the adhesive strength or rate of cohesive strength development, be sure to test that the failure is within the adhesive and not with the adhesion to the substrate or to substrate failure [1].

    - Authors: How is this tested? Please provide more details

  - If substrate failure occurs, then the adhesive has sufficient strength [1], while, cohesive failure in the bulk adhesive indicates adhesive weakness [2].

    - LAB MEDIA: Figure 4 Video Editor: please emphasize left wood image

    - LAB MEDIA: Figure 4 Video Editor: please emphasize right wood image

## Protocol Script Questions

# Authors: Please use the step numbers from the script above (not step numbers from the manuscript) when answering the questions below. Please do not include steps that will be screen-captured and do not list entire sections.

A. Which steps from the protocol are the most important for viewers to see? Please list 4 to 6 individual steps.

Click here to list 4 to 6 individual steps, using the step numbers from the protocol section of the video script.

B. What is the single most difficult aspect of this procedure and what do you do to ensure success? Please list 1 or 2 individual steps from the script above.

Click here to list 1 or 2 individual steps, using the step numbers from the protocol section of the video script.

If answered, your answers to C and D will become interview-style shots, which may be incorporated into the script after the relevant step in the protocol. Authors will memorize the statements and then deliver them on camera.

# C. OPTIONAL: If there is no single most critical step in the filmed portion of the protocol, do not answer this question. What is the best way to perform the required technique for the most critical step in the protocol?

# Enter author name.: (Enter step numbers from script.) Click here to answer. Please use language that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

# D. OPTIONAL: If there are no hazardous reagents or instruments in the filmed portion of the protocol, do not answer this question. Which of the reagents or instruments are uniquely hazardous? What precautions should viewers take?

# Enter author name.: (Enter step numbers from script.) Click here to answer. Please use language that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

# Results

Please review this section to make sure that it accurately reflects your findings.

- Use Track Changes when making edits or revisions.

- If you would like the video to include different results, please revise this section.

- When revising, please keep the length of the voiceover below 200 words. Current word count: XXX. (Voiceover is the text that follows the two-digit numbers.)

- Please note that the video cannot include voiceover without an accompanying visual.

- Results: Representative Protein Adhesion Analyses

  - As this set of isothermal strength development plots demonstrate Authors: please provide text (1-2 sentences) describing what information can be gained from this figure [1].

    - LAB MEDIA: Figure 3A

  - In this derived plot of regressed bonding rate against temperature, the Authors: please provide text (1-2 sentences) describing what information can be gained from this figure [1].

    - LAB MEDIA: Figure 3B

  - As observed in this image of failed samples, an adhesion failure due to  Authors: please provide additional text to describe what is illustrated with the sample on the left can be visualized [1], while in this sample a cohesive failure due to Authors: please provide additional text to describe what is illustrated with the sample on the right can be seen [2].

    - LAB MEDIA: Figure 4 Video Editor: please emphasize boards on left of image

    - LAB MEDIA: Figure 4 Video Editor: please emphasize boards on right of image

# Conclusion

- Conclusion Interview Statements

Below are prompts for interview statements that can be used to further emphasize the significance of your protocol.

- At least one statement is required.

- Each statement is limited to 30 words.

- Answer the questions in full sentences; you will need to memorize and deliver the sentences as spoken interview statements during filming.

- Indicate the full name of the author who will give each statement.

# What is the most important thing to remember when attempting this procedure? Please indicate the steps (e.g., 2.4., 2.5.) in the Protocol section of the script that this advice applies to.

  - Enter author name: Click here to answer. Please use language that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.[1].

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera (Enter step numbers referred to.)

# Following this procedure, what other methods can be performed? What questions would these additional methods answer?

  - Enter author name: Click here to answer. Please use language that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words. [1].

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera

# After its development, did this technique pave the way for researchers to explore new questions within a specific scientific field? If so, how?

  - Enter author name: Click here to answer. Please use language that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words. [1].

Thank you for addressing our questions. We will incorporate your answers and suggestions and send you the final script before your filming day. You will also receive detailed preparation instructions in the email accompanying the final script.