# Submission ID #: 61334

# Scriptwriter Name: Bridget Colvin

Project Page Link: http://www.jove.com/files_upload.php?src=18706918

Title: Demonstration of Spin-Multiplexed and Direction-Multiplexed All-Dielectric Visible Metaholograms

Authors and Affiliations: Inki Kim1, Dasol Lee1, and Junsuk Rho1,2

1Department of Mechanical Engineering, Pohang University of Science and Technology (POSTECH)

2Department of Chemical Engineering, Pohang University of Science and Technology (POSTECH)

# Corresponding Author:

# Junsuk Rho

# jsrho@postech.ac.kr

# Co-authors:

inki93@postech.ac.kr

# dasol2@postech.ac.kr

## Author Questionnaire

1. Microscopy: Does your protocol involve video microscopy, such as filming a complex dissection or microinjection technique?  Y

If Yes, can you record movies/images using your own microscope camera?

Y

2. Software: Does the part of your protocol being filmed demonstrate software usage?  Y

3. Filming location: Will the filming need to take place in multiple locations (greater than walking distance)?   N

# Introduction

- Introductory Interview Statements

REQUIRED:

  - Junsuk Rho: Multifunctional metasurfaces holograms that can produce multiple holographic images are key, flat optical devices for real-life, ultra-compact holographic display application [1].

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera

REQUIRED:

  - Inki Kim: To generate a multiplexed metahologram, we use a straightforward approach in which two different holographic images can be rendered depending on the spin of light and the propagation direction [1].

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera

OPTIONAL:

  - Inki Kim: To understand the multiplexed metahologram setup, visual demonstration of both the fabrication process and the optical characterization and measurement steps are equally important [1].

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera

# Introduction of Demonstrator on Camera

  - Junsuk Rho: Demonstrating the procedure with Inki Kim will be Dasol Lee, a PhD student from my laboratory [1][2].

    - INTERVIEW: Author saying the above

    - Named demonstrator(s) looks up from workbench or desk or microscope and acknowledges camera

# Protocol

- Scanning Electron Microscope (SEM) Characterization

  - To characterize the pattern deposition by scanning electron microscopy, drop a conductive polymer onto the substrate [1-TXT] and spin-coat at 2000 revolutions per minute for 1 minute [2].

    - WIDE: Talent dropping polymer onto substrate TEXT: See text for substrate fabrication details

    - Substrate being spin coated

  - Fix the substrate onto the sample holder with carbon tape [1] and press the AIR button to vent the load lock chamber [2].

    - Talent fixing substrate with tape

    - Talent pressing AIR

  - Place the holder onto the holding rod of the load-lock chamber [1] and press EVAC to evacuate the load lock chamber [2].

    - Talent placing holder onto holding rod

    - Talent pressing EVAC

  - To set the stage height and tilting angle, set the Z sensor to 8 millimeters and the T sensor to zero degrees [1].

    - Talent setting Z and/or T sensor

  - Press the OPEN button to open the load lock chamber door [1] and press the holding rod to transfer the holder to the main scanning electron microscope chamber [2].

    - Talent pressing OPEN button

    - Talent pressing holding rod/transferring holder to chamber

  - Pull out the rod [1] and press the CLOSE button [2].

    - Talent pulling out rod

    - Talent pressing CLOSE

  - Check the vacuum state [1] and press Execute to remove carbon or dust in the electron gun with an instant high voltage [2].

    - Talent checking vacuum state

    - SCREEN: 3.7.2

  - Click ON in the microscope software to turn on the electron gun with an accelerating voltage of 5 kilovolts [1] and click Beam Alignment to adjust the beam alignment to precisely locate the electron beam in the center position [2].

    - Talent clicking ON, with monitor visible in frame

    - SCREEN: 3.8.2. Video Editor: can speed up

  - Use a stage controller to locate the beam in the center [1] and click Aperture Alignment to adjust the aperture and stigma alignments to make a circular electron beam [2].

    - Talent using controller to adjust beam

    - SCREEN: 3.9.2. Video Editor: please speed up

  - Use a stigma controller to make a stable beam to scan on the same spot [1] and capture scanning electron images with an appropriate focus and stigmator adjustment [2].

    - Talent making stable beam on scan spot

    - SCREEN: 3.10.2.: 00:00-00:35 Video Editor: can speed up

  - When all of the images have been acquired, click OFF to turn off the electron beam and click Home to return the stage to its original position [1].

    - SCREEN: 3.11.1. Video Editor: can speed up

  - When the stage is in position, open the door of the main chamber [1] and push the rod to pick up the sample holder [2].

    - Talent opening door

    - Talent pushing rod

  - Press the AIR button to vent the load lock chamber [1] and unload the holder [2].

    - Talent pressing AIR button

    - Talent unloading holder

  - Then rinse the sample with deionized water to remove the conductive polymer layer [1].

    - Sample being rinsed

- Optical Spin-Multiplexed Metahologram Characterization

  - For optical characterization using a spin-multiplexed metahologram, attach a diode laser module to an adapter that can be plugged into a 1-inch optical mount [1] and use a post and a post holder to adjust the height of the diode laser [2].

    - WIDE: Talent attaching module to adapter

    - Talent adjusting laser height

  - Use a clamp to fix the position [1] and use a 1-inch rotational mount to assemble the half-wave plate [2].

    - Talent placing clamp

    - Talent using mount to assemble plate

  - Place the plate in front of the laser module to rotate the linearly-polarized light [1] and mount two mirrors onto individual 1-inch kinematic mounts [2].

    - Talent placing plate in front of module

    - Talent mounting mirror(s)

  - To align the direction of initial beam, place an alignment disk in front of the laser [1] and set the laser height [2].

    - Talent placing disk in front of laser

    - Talent setting disk height to be fit to laser height

  - Adjust the two mirrors so that the beam bends twice at 90 degrees in alternating directions [1] and position the alignment disk near the second mirror [2].

    - Talent adjusting mirror(s)

    - Talent placing disk near second mirror

  - Rotate the knobs to align the light in the center to adjust the angle of the first mirror [1] and move the alignment disk far from the second mirror [2].

    - Talent rotating knob(s)

    - Talent moving disk

  - Then rotate the knobs to align the light in the center to adjust the angle of the second mirror [1].

    - Talent rotating knob(s)

  - Repeat the alignment until the light passes through the center of the alignment disk in both places [1] and place a neutral density filter behind the mirror to control the intensity of light [2].

    - Disk being moved into position so that light passes through center of disk in both places

    - Talent placing filter behind mirror

  - Place an iris behind the neutral density filter to control the diameter of incident light [1], mount a linear polarizer and a quarter wave plate on its own rotational mount [3.10.1], and place a linear polarizer and a quarter wave plate behind the iris to make a circularly polarized light [3].

    - Iris being placed NOTE: Move 3.10.1 between 3.9.1 and 3.9.2.

    - Linear polarizer and quarter wave plate being placed

  - Attach the fabricated metasurface to a plate with a hole [2].

    - Talent mounting component Videographer: Important step NOTE: This shot moved above.

    - Talent attaching metasurface to plate Videographer: Important step

  - Mount the plate on the XY translation mount for rectangular optics [1] and adjust the XY translation mount so that light is directed to the pattern in the sample [2].

    - Talent placing plate onto mount

    - Talent adjusting mount

  - Place a lens after the metasurface [1] and adjust the position of lens to be placed at the focal length [2].

    - Talent placing lens

    - Talent adjusting lens position

  - Then place a charge-coupled device camera after the lens to capture a hologram image [1].

    - Talent placing camera

- Optical Direction-Multiplexed Metahologram Characterization

  - For optical characterization using a direction-multiplexed metahologram, place a beam splitter between the quarter-wave plate and the XY translation mount to split the beam into two directions [1] and place another beam splitter between the XY translation mount and the lens [2].

    - WIDE: Talent placing beam splitter between quarter-wave plate and XY translation mount Videographer: Important/difficult step

    - Talent placing beam splitter between XY translation mount and lens Videographer: Important/difficult step

  - Place two mirrors so that the beam bends twice at 90 degrees in alternating directions [1] and adjust the beam to be directed into the second beam splitter [2].

    - Talent placing mirror(s) Videographer: Important/difficult step

    - Talent adjusting beam to be directed into second beam splitter Videographer: Important/difficult step

  - Finely align the light so that the beam irradiates the sample correctly in the opposite direction [1] and place another lens at 90 degrees to the right of the first beam splitter [2].

    - Talent aligning light Videographer: Important/difficult step

    - Talent placing lens at 90° to right of first beam splitter Videographer: Important/difficult step

  - Then place a charge-coupled device camera to capture a hologram image from the opposite direction [1].

    - Talent placing camera Videographer: Important/difficult step

  - Inki Kim: The best way to produce clear spin- and direction-multiplexed holographic images is to precisely align the multiple optical components [1].

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera

## Protocol Script Questions

A. Which steps from the protocol are the most important for viewers to see?

3.10., 4.1.-4.4.

B. What is the single most difficult aspect of this procedure and what do you do to ensure success?

4.1.-4.4.

# Results

- Results: Representative Spin- and Directed-Multiplexed Metahologram Imaging

  - In this scanning electron microscopy image, fabricated hydrogenated amorphous silicon metasurfaces can be observed [1].

    - LAB MEDIA: Figure 2 LAB MEDIA: Figure 3A Video Editor: please outline/emphasize at least one metasurface

  - A spin-multiplexed metahologram [1] can switch the projected holographic images by simply flipping the handedness of the incident circularly polarized light [2].

    - LAB MEDIA: Figure 3A Video Editor: please emphasize blue Metahologram

    - LAB MEDIA: Figure 3A Video Editor: please emphasize yellow arrows

  - Different metasurfaces can produce different responses depending on whether the light is circularly polarized to the left or to the right [1].

    - LAB MEDIA: Figure 3B Video Editor: please emphasize SEM image

  - As a result, depending on the input beam polarization states, the Information Technology University and Rho laboratory holographic images can be switched in real-time with high fidelity [1].

    - LAB MEDIA: Figures 3C-3E Video Editor: please sequentially add/emphasize Figures from 3C to 3E

  - A direction-multiplexed metahologram can switch the projected holographic images by changing the incident light direction [1].

    - LAB MEDIA: Figure 4 Video Editor: please sequentially emphasize top to bottom rounded yellow arrows in Figure 4A

  - For instance, if the light comes in the forward direction from the substrate side [1], the holographic Rho lab images can be observed [2].

    - LAB MEDIA: Figure 4 Video Editor: please emphasize top rounded yellow arrow

    - LAB MEDIA: Figure 4 Video Editor: please emphasize Figures 4B and 4D

  - If the light comes in the backward direction from the metasurface side [1], the holographic Information Technology University images can be visualized [2].

    - LAB MEDIA: Figure 4 Video Editor: please emphasize bottom rounded yellow arrow

    - LAB MEDIA: Figure 4 Video Editor: please emphasize Figures 4C and 4E

# Conclusion

- Conclusion Interview Statements

  - Inki Kim: Because the clearness of the projected images is very sensitive to the polarization and direction of the incident light, the component alignment is particularly important for producing clear holographic images [1].

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera (4.1-4.4.)

  - Inki Kim: We plan to develop an active metahologram that combines this multiplexed metahologram with an active materials platform to easily change the projected hologram images by external stimuli [1].

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera