# Submission ID #:  61458

# Scriptwriter Name: Anastasia Gomez

# Project Page Link: https://www.jove.com/account/file-uploader?src=18744738

# Title:   Graphene Enclosure of Chemically Fixed Mammalian Cells for Liquid-Phase Electron Microscopy

# Authors and Affiliations:

# Patricia Blach1,2, Sercan Keskin1, Niels de Jonge1,2

# 1INM-Leibniz Institute for New Materials, Campus D2 2, Saarbrücken, 66123, Germany.

# 2Department of Physics, Saarland University, 66123 Saarbrücken, Germany

# Corresponding Authors:

# Niels de Jonge 	(Niels.deJonge@leibniz-inm.de)

# Email Addresses for All Authors:

Patricia.Blach@leibniz-inm.de

# Sercan.Keskin@leibniz-inm.de

# Niels.deJonge@leibniz-inm.de

## Author Questionnaire

1. Microscopy: Does your protocol involve video microscopy, such as filming a complex dissection or microinjection technique?  No

2. Software: Does the part of your protocol being filmed include step-by-step descriptions of software usage?  No

3. Filming location: Will the filming need to take place in multiple locations?   No, but two different rooms in the same building.

Current Protocol Length

Number of Steps:  20

Number of Shots:  37

# Introduction

- Introductory Interview Statements

REQUIRED:

  - Patricia Blach: This method keeps biological samples in a native environment and reduces electron beam induced artifacts.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

  - Patricia Blach: The main advantage is that the technique is applicable to whole cells, so cells don’t need to be dehydrated, stained or sectioned before electron microscopy.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

OPTIONAL:

  - Patricia Blach: The ability to image receptors on cancer cells in the context of the whole, intact plasma membrane is a major aspect that can lead to new therapy approaches and the development of new anti-cancer drugs.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

# Introduction of Demonstrator on Camera

    - INTERVIEW: Author saying the above.

    - The named demonstrator(s) looks up from workbench or desk or microscope and acknowledges the camera.

# Protocol

- Cell Seeding and HER2 Labeling

  - To begin, add 100 microliters of cell suspension to two wells of a 96-well plate containing PLL and FLP-coated microchips with the silicon nitride membrane facing up and 50 microliters of serum-free medium [1-TXT]. Incubate the plate at 37 degrees Celsius and 5% carbon dioxide for 5 minutes to allow cells to attach to the microchip [2]. Videographer: This step is difficult!

    - Talent adding cells to a few wells. TEXT: 25,000 cells/well

    - Talent putting the plate in the incubator and closing the door.

  - Check the density of the cells on the microchip with an inverted microscope and make sure that the cells cover the window with sufficient space to flatten out and adhere [1].

    - Talent using the microscope.

  - To label HER2 in the cells, place the microchips into the wells of the first row of labeling plate 1 [1]. Then, wash the microchips with PBS-BSA [2].

    - Talent transferring the microchips to the labeling plate.

    - Talent washing the microchips.

  - To prevent unspecific binding of the antibody mimetic, incubate the microchips with PBS-BSA-GS for 5 minutes [1], then with 200-nanomolar antibody mimetic for 10 minutes at 37 degrees Celsius and 5% carbon dioxide [1].

    - Talent putting the cells in PSA-BSA-GS. TEXT: Perform this at 37 C and 5% CO2

    - Talent putting the cells in the incubator and closing the door.

- Cleaning and Transferring Graphene onto Salt Crystals

  - To remove the PMMA-graphene from the polymer, pipette a few droplets of water on the polymer around the PMMA-graphene [1], then immerse it in water with an angle of 30 to 45 degrees to release the PMMA-graphene [2].

    - Talent pipetting water on the polymer.

    - Talent immersing the polymer in water.

  - To etch copper-based contaminants, prepare a 50-milliliter solution of 0.42-molar sodium persulfate in water [1]. Use a standard glass slide to transfer PMMA-graphene into the sodium persulfate solution with the graphene side down [2]. The PMMA-graphene will float to the top of the solution, leave it there overnight [3]. Videographer: This step is important!

    - Talent preparing the sodium persulfate solution.

    - Talent transferring the PMMA-graphene into the sodium persulfate solution.

    - PMMA-graphene floating to the top.

  - On the next day, transfer the PMMA-graphene from the sodium persulfate solution into clean water. Let it float on the water for half an hour [1]. Repeat the wash a total of three times to remove all sodium persulfate residues from the PMMA-graphene [2].

    - Talent transferring the PMMA-graphene into clean water.

    - Talent moving the PMMA-graphene from one container of water to another.

  - Then, transfer the PMMA-graphene onto a sodium chloride crystal. Prepare a saturated solution of sodium chloride in water in a Petri dish [1] and transfer the PMMA-graphene on top of the solution with the graphene side down [2].

    - Talent preparing NaCl in the Petri dish.

    - Talent transferring the PMMA-graphene to the NaCl.

  - Hold the sodium chloride crystal with tweezers and pick up the floating PMMA-graphene [1], then hold it vertically for 2 minutes to let excess water flow out [2]. Let it dry at room temperature for 30 minutes and bake it in an oven at 100 degrees Celsius for 20 minutes to completely remove the water [3]. Videographer: This step is important!

    - Talent picking up the PMMA-graphene.

    - Talent holding the PMMA-graphene vertically.

    - Talent placing the PMMA-graphene in an oven.

  - Preheat acetone in a glass Petri dish to approximately 50 degrees Celsius on a hotplate in the fume hood, watching the temperature carefully to avoid fire [1]. Immerse the PMMA-graphene-on-salt into the Petri dish filled with acetone and leave it to dissolve the PMMA for 30 minutes [2-TXT].

    - Acetone preheating.

    - Talent immersing the PMMA-graphene-on-salt in the acetone. TEXT: Repeat for a total of 3 X

  - Let the graphene-on-salt air-dry thoroughly before using it for sample preparation [1].

    - Graphene on salt air drying.

- Graphene Coating

  - Wash one prepared and labeled microchip in pure water to remove any residues of salt from the buffer and place it on a filter paper [1]. The cells should be visible as dark spots [2].

    - Talent washing the microchip with water.

    - Cells visible as dark spots.

  - Use a razor blade to cut the multilayer graphene on the sodium chloride crystal into a piece that fits the silicon nitride window of a microchip [1]. Remove the graphene from the sodium chloride crystal by dipping it in a beaker of water, tilting the crystal at a 45-degree angle with respect to the surface [2].

    - Talent cutting the graphene.

    - Talent dipping the graphene into the water and the graphene floating on top.

  - Catch the graphene with a metal loop from the surface of the water [1]. Then, touch the upper surface of the microchip with the lower loop surface, causing the microchip to stick to the metal loop [2]. The graphene can be seen on top of the microchip [3]. Videographer: This step is important!

    - SCOPE: Talent catching the graphene with the loop. NOTE: Filmed with scope cam MC120169.mph

    - ECU: Talent touching the microchip on the loop.

    - SCOPE: Graphene on top of the microchip. NOTE: Filmed with scope cam MC120170.mph

  - Under a stereomicroscope, use filter paper to remove the remaining water from the microchip so that the graphene covers all cells on the silicon nitride window [1]. Place the microchip onto a filter paper with tweezers. The graphene is visible as a purple shimmer on the microchip [2]. Videographer: This step is difficult and important!

    - SCOPE: Talent draining the microchip with filter paper. NOTE: Filmed with scope cam MC120171.mph. Also, shot was added so 4.4.2 might be slated as 4.4.1.

    - Talent placing the microchip on filter paper.

  - Transfer the microchip from the paper to a compartment Petri dish [1]. Pipette a droplet of water into one of the free compartments and close the lid to provide a water-saturated atmosphere [2], then seal the compartment dish with paraffin film and store in the fridge at 4 degrees Celsius [3].

    - Talent transferring the microchip to the Petri dish.

    - Talent pipetting water into the dish.

    - Talent sealing the dish.

- STEM

  - Set the STEM to 200 kilovolt beam energy using an alignment sample for a probe size of at least 0.2 nanometers by adjusting the condenser lenses, set a probe current of 180 picoampere, and a beam convergence semi-angle of 13.2 milliradians by inserting an aperture [1].

    - Talent adjusting the beam energy, probe current, and beam convergence.

  - Set the ADF STEM detector opening semi-angle range to 68 to 280 milliradians by adjusting the projector lens settings, then set the STEM image size to 2048 by 2048 pixels and the pixel dwell time to 6 microseconds [1].

    - Talent adjusting the projector lens settings and setting the image size and pixel dwell time.

  - Load the microchip with graphene-coated cells in a standard specimen holder for TEM in such a way that the cells are facing up [1] and load the holder into the electron microscope [2].

    - Talent loading the microchip in the specimen holder.

    - Talent loading the holder into the microscope.

  - Acquire an overview picture at 800 X magnification, then identify a region of interest and image the quantum dot nanoparticles at 80,000 X with a pixel size of 1.3 nanometers [1].

    - Talent acquiring images and setting ROIs.

# Results

- Results: STEM of Graphene Coated SKBR3 cells on silicon nitride Window

  - Optimally seeded cells are shown here. The window is covered, but there is sufficient space to allow them to flatten out and adhere [1]. When too many cells were seeded on a microchip, there was insufficient space for all cells to adhere [2]. After 24 hours, more than half of the cells didn’t flatten [3].

    - LAB MEDIA: Figure 1 A and B.

    - LAB MEDIA: Figure 1 C and D. Video Editor: Emphasize C.

    - LAB MEDIA: Figure 1 C and D. Video Editor: Emphasize D.

  - If too few cells are seeded [1], the silicon nitride window will end up with a large empty space after 24 hours [2]. DIC and fluorescence images of optimally seeded cells are shown here, demonstrating successful labeling of HER2 (pronounce ‘her-2’) [3].

    - LAB MEDIA: Figure 1 E and F. Video Editor: Emphasize E.

    - LAB MEDIA: Figure 1 E and F. Video Editor: Emphasize F.

    - LAB MEDIA: Figure 1 G and H.

  - STEM was performed on graphene-coated [1] and non-coated SKBR3 cells [2]. The insets in the 800 X magnification images [3] were imaged at 80,000 X [4]. The quantum dot nanoparticles are visible as bright spots at 50,000 X magnification [5].

    - LAB MEDIA: Figure 4. Video Editor: Emphasize the left column.

    - LAB MEDIA: Figure 4. Video Editor: Emphasize the right column.

    - LAB MEDIA: Figure 4 A and B. Video Editor: Emphasize the rectangle insets.

    - LAB MEDIA: Figure 4 C and D.

    - LAB MEDIA: Figure 4 E and F.

  - To investigate the effect of electron beam illumination on the sample, STEM images were acquired in an image series with an accumulating electron dose [1]. Representative results for non-coated [2] and graphene-coated samples are shown here [3].

    - LAB MEDIA; Figure 5 A – G.

    - LAB MEDIA: Figure 5 A – G. Video Editor: Emphasize A – D.

    - LAB MEDIA: Figure 5 A – G. Video Editor: Emphasize E – G.

  - The exposure of non-coated samples led to bright structures appearing on the cell surfaces, which did not occur with any of the graphene coated samples [1]. The average relative distance change of particle pairs stayed below 1.3% for non-coated samples and below 0.8% for the coated samples [2].

    - LAB MEDIA: Figure 5 A – D. Video Editor: Emphasize where the yellow arrows are pointing.

    - LAB MEDIA: Figure 5 H.

# Conclusion

- Conclusion Interview Statements

  - Patricia Blach: Following this procedure, different kinds of membrane proteins can be imaged on whole cells using other microscopy methods.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

  - Patricia Blach: This technique makes it possible to image proteins in the intact plasma membrane to gain more information about the organization of the plasma membrane and the interactions between proteins.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.