# Submission ID #:  61663

# Scriptwriter Name: Anastasia Gomez

# Project Page Link: https://www.jove.com/account/file-uploader?src=18807263

# Title:   Detergent-Free Decellularization of the Human Pancreas for Soluble Extracellular Matrix (ECM) Production

# Authors and Affiliations:

# Riccardo Tamburrini1,2,3, Deborah Chaimov1,3, Amish Asthana1,3, Kevin Enck3, Sean M. Muir4,  Justine Mariam Aziz5, Sandrine Lablanche6, Emily Tubbs6, Alice A. Tomei7,8, Mark Van Dyke9,  Shay Soker3, Emmanuel C Opara3, Giuseppe Orlando1,3

# 1Department of Surgery, Wake Forest Baptist Medical Center, Medical Center Boulevard, Winston Salem, NC, USA

# 2Department of General Surgery, PhD Program in Experimental Medicine, University of Pavia, Pavia, Italy

# 3Wake Forest Institute for Regenerative Medicine, Wake Forest School of Medicine, Medical Center Boulevard, Winston-Salem, NC, USA

# 4Wake Forest University College of Arts and Science, Winston Salem, NC, USA

# 5Wake Forest University School of Medicine, Winston-Salem, NC, USA

# 6Grenoble Alps University, Laboratory of Fundamental and Applied Bioenergetics (LBFA), and Environmental and System Biology (BEeSy), Inserm, Grenoble, France

# 7Department of Biomedical Engineering, University of Miami, Coral Gables, FL, USA

# 8Diabetes Research Institute, University of Miami Miller School of Medicine, Miami, FL, USA

# 9Department of Biomedical Engineering and Mechanics, Virginia Polytechnic Institute and State University, School of Biomedical Engineering and Sciences, Blacksburg, VA, USA

# Corresponding Authors:

# Giuseppe Orlando

Riccardo Tamburini

gorlando@wakehealth.edu

riccardo.tamburrini@gmail.com

# Email Addresses for All Authors:

rtamburr@wakehealth.edu

dchaimov@wakehealth.edu

kenck@wakehealth.edu

smuir@wakehealth.edu

aasthana@wakehealth.edu

jaziz@wakehealth.edu

slablanche@chu-grenoble.fr

Emily.tubbs@univ-grenoble-alpes.fr

atomei@med.miami.edu

mvandyk5@vt.edu

ssoker@wakehealth.edu

eopara@wakehealth.edu

gorlando@wakehealth.edu

riccardo.tamburrini@gmail.com

## Author Questionnaire

1. Microscopy: Does your protocol require the use of a dissecting or stereomicroscope for performing a complex dissection, microinjection technique, or something similar?  No

2. Software: Does the part of your protocol being filmed include step-by-step descriptions of software usage?  No

3. Interview statements: Considering the COVID-19-imposed mask-wearing and social distancing recommendations, which interview statement filming option is the most appropriate for your group? Please select one.

☒ 	Interviewees wear masks until videographer steps away (≥6 ft/2 m) and begins filming, then the interviewee removes the mask for line delivery only. When take is captured, the interviewee puts the mask back on. Statements can be filmed outside if weather permits.

4. Filming location: Will the filming need to take place in multiple locations?   No

Current Protocol Length

Number of Steps:  13

Number of Shots:  20

# Introduction

- Introductory Interview Statements

REQUIRED:

  - Riccardo Tamburrini: The purpose of the development of this method was to explore ways to produce extracellular matrix from human pancreata with minimal use of ionic and non-ionic chemical detergents.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

OPTIONAL:

  - Riccardo Tamburrini: This protocol could be potentially used for the production of extracellular matrix from human and non-human organs if appropriate DNA clearance is achieved.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

  - Riccardo Tamburrini: Human pancreata from donors with a BMI less than 30 were deemed suitable for decellularization while some human-to-human organ variability before and after decellularization was observed. Generally, donors with BMI greater than 30 and excessive peri- and intra-pancreatic adiposity were not optimal for this protocol.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

Ethics Title Card

  - Procedures involving human subjects have been approved by the Institutional Review Board (IRB) at Wake Forest Baptist Medical Center.

# Protocol

- Surgical Preparation of the Human Pancreas

  - Thaw the frozen pancreases overnight at 4 degrees Celsius [1]. Before initiating surgical dissection, prepare 1 liter of washing solution that consists of 950 milliliters of deionized water, 50 milliliters of iodine-based reagent, and 1% Pen-Strep solution [2].

    - WIDE: Establishing shot of talent taking the pancreas out of the refrigerator.

    - Talent preparing the washing solution.

  - Wear sterile gloves and a lab coat and perform all surgeries under a cell-culture-grade hood to avoid contamination [1]. Transfer the pancreas from the sterile transport bag into the sterile placenta basin, making sure to orient it with the head of the organ to the left and the tail to the right [2].

    - Talent at the hood wearing appropriate PPE.

    - Talent transferring the pancreas into the basin and orienting it properly.

  - Carefully dissect the duodenum from the head of the pancreas using sterile scissors and non-toothed forceps, taking care to not make a hole in the duodenum [1]. Videographer: This step is difficult and important!

    - Talent dissecting the duodenum.

  - Once the dissection of the head of the pancreas is completed, dispose of the duodenum into an appropriate biohazard bag [1].

    - Talent disposing of the duodenum.

  - Dissect and discard all extra-pancreatic tissue remaining around the head of the pancreas, including major blood vessels and the common bile duct, which are usually marked at the time of organ procurement with non-absorbable sutures [1].

    - Talent dissecting extra-pancreatic tissue around the head of the pancreas.

  - Then, dissect and discard all extra-pancreatic and peripancreatic adipose tissue surrounding the tail of the pancreas, exposing the splenic blood vessels [1].

    - Talent dissecting extra-pancreatic and adipose tissue around the tail of the pancreas.

  - Once the vascular pedicle of the spleen is exposed, remove the spleen [1], and dissect the splenic blood vessels in their entirety, including those attached to the posterior surface of the pancreas [2]. Dispose of the spleen and removed tissue [3]. Videographer: This step is important!

    - Talent removing the spleen.

    - Talent dissecting the blood vessels.

    - Talent disposing of the spleen and removed tissue.

  - Remove any extra-pancreatic fat that is clearly visible, especially peripancreatic fat [1]. Videographer: This step is important!

    - Talent removing extra-pancreatic fat.

  - At the level of the tail of the pancreas, the retroperitoneum may be visible. This should be lifted with non-toothed forceps, removed with surgical forceps, and disposed of properly [1]. The pancreas should now be free of any extra-pancreatic tissue [2].

    - Talent removing the retroperitoneum.

    - Pancreas after dissection.

  - Cut the pancreas to obtain 1-centimeter cubes of pancreatic tissue using surgical scissors, sterilized histological blades, or surgical scalpels [1]. The pancreatic tissue cubes will then undergo the decellularization process [2]. Videographer: This step is difficult and important!

    - Talent cutting the pancreas into cubes.

    - Pancreatic tissue cubes.

- Production of Pancreatic ECM Powder – Lyophilization and Cryo-milling

  - After a minimum of 24 to 40 hours of storage of the decellularized material at -80 degrees Celsius, transfer the pancreatic ECM into a freeze dryer [1]. After lyophilization, transfer the materials into a cell-culture-grade hood [2].

    - Talent transferring tissue into the freeze dryer.

    - Talent transferring the tissue to the hood.

  - Cut each piece of the dried ECM into half of its size using sterile scissors [1].

    - Talent cutting dried ECM.

  - To produce ECM powder, use a cryo-milled automatic processor to avoid a rise in temperature and subsequent denaturation of the biological properties of the ECM. Make sure to adjust the setting of the cryo-milling machine to obtain a fine powder after the milling process [1].

    - Talent using the cryo-milled automatic processor.

# Results

- Results: Effect of ECM on Viability and Function of Encapsulated Isolated Human Pancreatic Islets

  - Native [1] and acellular pancreatic samples [2] were processed for histological staining with H and E, MT, and AB [3]. The H and E staining confirmed successful decellularization [3], while staining with MT and AB showed the framework of the ECM, highlighting qualitatively collagenous and stromal components [5].

    - LAB MEDIA: Figure 1. Video Editor: Emphasize A, C, and E.

    - LAB MEDIA: Figure 1. Video Editor: Emphasize B, D, and F.

    - LAB MEDIA: Figure 1.

    - LAB MEDIA: Figure 1. Video Editor: Emphasize A and B.

    - LAB MEDIA: Figure 1. Video Editor: Emphasize C-F.

  - Native, acellular, and solubilized pancreatic ECM were biochemically characterized in order to assess basic biological composition. The pancreatic ECM was determined to be acellular and DNA-free [1]. Clearance of DNA was demonstrated in both acellular and solubilized pancreatic ECM [2].

    - LAB MEDIA: Figure 2 A.

    - LAB MEDIA: Figure 2 A. Video Editor: Emphasize the decelled pancreas and soluble ECM bars.

  - Total collagen was quantified in the native pancreas, in the acellular and in the solubilized pancreatic ECM [1].

    - LAB MEDIA: Figure 2 C.

  - Quantification of glycosaminoglycans showed a statistically significant decrease of GAG content in the acellular tissue and solubilized pancreatic ECM [1].

    - LAB MEDIA: Figure 2 B. Video Editor: Emphasize the decelled pancreas and soluble ECM bars.

  - Encapsulated islets cultured in non-tissue culture treated plates were viable 8 days post-encapsulation [1]. They maintained their spherical shape with a well-rounded border, a stable diameter, and almost no single cells in culture [2].

    - LAB MEDIA: Figure 3 A. Video Editor: Emphasize the Live/Dead images.

    - LAB MEDIA: Figure 3 A. Video Editor: Emphasize the alginate and alginate-ECM capsule images.

  - Free islets showed a tendency to aggregate, to develop irregularities at the borders and shapes, and to exhibit a darker core, suggestive of a necrotic event [1].

    - LAB MEDIA: Figure 3 A. Video Editor: Emphasize the free islet images.

  - Islets encapsulated in ECM-alginate showed a significant increase in insulin secretion following high glucose stimulation and potassium chloride depolarization compared to both free and alginate-only encapsulated islets [1].

    - LAB MEDIA: Figure 3 B. Video Editor: Emphasize the black bars.

# Conclusion

- Conclusion Interview Statements

  - Riccardo Tamburrini: Sterility is a priority to achieve a clean product, avoid contamination and accumulation of endotoxins. It is of fundamental importance to remove all extra-pancreatic tissue from the organ before undergoing decellularization.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B-roll: 2.2, 2.8.

  - Riccardo Tamburrini: This is an effective, detergent-free decellularization method for the human pancreas which allows the production of a soluble extracellular matrix scaffold for tissue culture.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.