Supporting Information

TITLE:

Microscopic Visualization of Porous Nanographenes Synthesized Through Combination of Solution and On-surface Chemistry

AUTHORS AND AFFILIATIONS:

Rafal Zuzak,1 Iago Pozo,2 Mads Engelund,3 Manuel Vilas-Varela,2 José M. Alonso,2 Enrique Guitián,2 Dolores Pérez,2 Diego Peña,2 Szymon Godlewski1

1 Centre for Nanometer-Scale Science and Advanced Materials, NANOSAM, Faculty of Physics, Astronomy and Applied Computer Science, Jagiellonian University, Łojasiewicza 11, PL 30-348 Kraków, Poland

2 Centro de Investigación en Química Biolóxica e Materiais Moleculares (CiQUS), Departamento de Química Orgánica, Universidade de Santiago de Compostela, 15782-Santiago de Compostela, Spain

3 Espeem S.A.R.L., L-4365 Esch-sur-Alzette, Luxembourg

Corresponding Author:

Szymon Godlewski

szymon.godlewski@uj.edu.pl

Tel: (48)-12-664-46-05

Email Addresses of Co-authors:

Rafał Zuzak	(rafal.zuzak@uj.edu.pl)

Iago Pozo	(iago.p.m@hotmail.com)

Mads Engelund	(mads.engelund@espeem.com)

Manuel Vilas-Varela	(manuelvilasvarela@gmail.com)

José M. Alonso	(xosemag@yahoo.es)

Enrique Guitián	(enrique.guitian@usc.es)

Dolores Pérez	(dolores.perez@usc.es)

Diego Peña	(diego.pena@usc.es)

KEYWORDS:

on-surface synthesis, scanning tunneling microscopy, atomic force microscopy, nanographenes

Figure S1 shows spectroscopic characterization of docecaphenyl[7]starphene.

Figure S1. Spectrowscopic characterixzation of docecaphenyl[7]starphene.

Figures S2 and S3 show the reference measurements of the Schockley surface state on Au(111) and the appearance of CO molecules measured with metallic/functionalized tips, respectively.

Figure S2. Au(111) surface, (a) filled state high resolution STM image with clearly discernible herringbone pattern, the inset shows magnified image with mark fcc and hcp areas, -1.0 V, 100 pA, (b) typical single point STS data acquired with well-shaped metallic tip presenting the onset of the Au surface state at approximately -0.5 V.

Figure S3. nc-AFM tip functionalization with a CO molecule, (a) schematic drawing of the process, (b) typical STM image of Au(111) with CO molecules imaged with a CO functionalized tip, the CO molecule is visualized as a dark depression surrounded with a bright halo and a characteristic bright lobe in the center, (c) typical STM image of Au(111) with CO molecules imaged with a metallic tip, the CO molecule is visualized as a dark depression surrounded with a bright halo without the characteristic bright lobe in the center, exemplary CO molecules are highlighted by white dashed circles in (b,c), +0.5 V, 15 pA.