| Collagen stock concentration (Cs) : |  |  |  | 8 | mg/mL |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Desired Volume (Vf): |  |  |  | 1 | mL |  |  |  |
| Normalizing NaOH Adjustment*: |  |  |  | 1 | X |  |  |  |
| *Each lot of collagen needs to be tested to determine the amount of NaOH needed to set pH 7.4 |  |  |  |  |  |  |  |  |
|  |  | Desired Collagen Concentration (mg/mL) |  |  |  |  |  |  |
|  |  | 2 | 3 |  |  | 4 |  | 5 |
| 10X PBS (Vpbs) |  | 0.1 | 0.1 |  |  | 0.1 |  | 0.1 |
| Collagen stock (Vs) |  | 0.25 | 0.375 |  |  | 0.5 |  | 0.625 |
| 1N NaOH (VNaOH) |  | 0.00575 | 0.008625 |  |  | 0.0115 |  | 0.014375 |
| Media (Vmedia) |  | 0.64425 | 0.516375 |  |  | 0.3885 |  | 0.260625 |