## Slide 1
Figure #1
1. Urine sample
Measure urine pH and volume.
2. Centrifuge
Spin at 1200 x g for 10 minutes at room temperature (RT) and discard supernatant.
3. Clean Pellet
Wash pellet with 5 mL of 100% EtOH and
Spin at 1200 x g or 10 minutes at RT (2x).
4. Prepare Pellet
Resuspend pellet with 1ml of 100% EtOH.
5. Stain Nanocrystals
Dilute samples in water (20x) and stain with
5 μM Fluo-4 AM for 30 mins at RT.
6. Visualize Nanocrystals using Nanoparticle Tracking Analysis (NTA)
Load and analyze samples using fluorescent filter settings.
7. Data Acquisition and Analysis
Collect and analyze data from the software.

## Slide 2
Figure #2
Instrument
Computer
Injector
A
B
Optical Surface
Inlet and Outlet
Tubing
Injector
Objective
Lens
Camera

## Slide 3
Chart: CaP
| 25 | 35 | 45 | 55 | 65 | 75 | 85 | 95 | 105 | 115 | 125 | 135 | 145 | 155 | 165 | 175 | 185 | 195 | 205 | 215 | 225 | 235 | 245 | 255 | 265 | 275 | 285 | 295 | 305 | 315 | 325 | 335 | 345 | 355
Concentration average | 10044.9 | 10794507.8 | 13505736.8 | 13650234.7 | 19740190.7 | 35226366.8 | 75272619.6 | 121876256.9 | 145792709.6 | 173021491 | 216934745 | 255060434.9 | 261240174.9 | 241302435.7 | 214399023.9 | 175777625.5 | 114771017.6 | 58957340.8 | 28076862.3 | 14325829.2 | 8132081.2 | 5161131.7 | 3659130.7 | 2892580.4 | 2744729.1 | 2912353.6 | 2683855.2 | 2117135.4 | 1507104.8 | 882075.4 | 354602.1 | 81175 | 9369.8 | 577.5
Chart: CaOx
| 25 | 35 | 45 | 55 | 65 | 75 | 85 | 95 | 105 | 115 | 125 | 135 | 145 | 155 | 165 | 175 | 185 | 195 | 205 | 215 | 225 | 235 | 245 | 255 | 265 | 275 | 285 | 295 | 305 | 315 | 325 | 335 | 345 | 355 | 365 | 375 | 385 | 395 | 405
Concentration average | 1178.3 | 434748.9 | 2861953.4 | 4178873.3 | 5853648.8 | 9883139.7 | 18192012.6 | 34687893.7 | 59792798 | 83112964 | 98218028.1 | 108891362.4 | 118584666.8 | 124417885.7 | 121319336.9 | 109905143.5 | 94885030.7 | 79391334.6 | 63723253.6 | 47108001.9 | 30534593.5 | 17227920.5 | 8956039.5 | 4741666 | 2866268.4 | 2069213.8 | 1589220.4 | 1091046 | 599621.4 | 254940.4 | 85776.5 | 24359.1 | 6501.2 | 2006.9 | 1025.8 | 937.2 | 1076.5 | 1225.3 | 1263.6
Figure #3
A
B

## Slide 4
Chart: Size (nm)
Figure #4

## Slide 5
Figure #5
Chart: Post-Oxalate
| 5 | 15 | 25 | 35 | 45 | 55 | 65 | 75 | 85 | 95 | 105 | 115 | 125 | 135 | 145 | 155 | 165 | 175 | 185 | 195 | 205 | 215 | 225 | 235 | 245 | 255 | 265 | 275 | 285 | 295 | 305 | 315 | 325 | 335 | 345 | 355 | 365 | 375 | 385 | 395 | 405 | 415
Post-Ox-I | 0 | 0 | 0 | 110 | 28982.6 | 163446.9 | 275860.1 | 189478.3 | 95421 | 54765.8 | 108621.9 | 438743.2 | 1734046.2 | 6153848.6 | 17596466.1 | 34928571.6 | 49504023.9 | 54706500.7 | 59999394.1 | 61867652.4 | 55602081.3 | 47059036.1 | 37923911.8 | 27054141.1 | 16364830.8 | 8783255.4 | 4189660.7 | 2120620 | 1419433.2 | 820749.2 | 291758.7 | 55586.8 | 5409.5 | 273.7
Post-Ox-II | 0 | 0 | 1271.3 | 29723.7 | 7498.5 | 4574.5 | 11983.9 | 36636 | 93532.8 | 243547.1 | 670023 | 1818265.1 | 4205571.9 | 8417951.2 | 16464781.6 | 29807812.2 | 44296939.7 | 56101037.1 | 64536569.8 | 69366344.4 | 70537598.7 | 67913536.6 | 61825942.8 | 53591176 | 44646568.5 | 35782767.8 | 27311562.2 | 19525737.4 | 12846169.6 | 7632476.6 | 3997060.1 | 1800222 | 698675.6 | 247130.2 | 87060.1 | 32304.2 | 12529.6 | 4788.9 | 1663.3 | 498.5 | 135.9 | 40.7
Post-Ox-III | 0 | 0 | 0 | 0 | 40.9 | 7924.6 | 19011.7 | 5951.8 | 1549.9 | 10047.2 | 171842.6 | 923033.1 | 2667511.8 | 6640763.1 | 14255192.6 | 22228071.1 | 28291216.1 | 35876481.5 | 48701700.9 | 66516750.7 | 80686118.3 | 81678542.2 | 70699409.9 | 55816085.2 | 43029282 | 33590797 | 25440377.7 | 17141505.5 | 10310314.4 | 6143689.9 | 3780199 | 2281132.5 | 1241618.9 | 564111.4 | 203434.3 | 56451.5 | 11982 | 2030.9 | 297 | 39.1
Pre-Ox-mean | 0 | 0 | 423.7667 | 9944.5667 | 12174 | 58648.6667 | 102285.2333 | 77355.3667 | 63501.2333 | 102786.7 | 316829.1667 | 1060013.8 | 2869043.3 | 7070854.3 | 16105480.1 | 28988151.6333 | 40697393.2333 | 48894673.1 | 57745888.2667 | 65916915.8333 | 68941932.7667 | 65550371.6333 | 56816421.5 | 45487134.1 | 34680227.1 | 26052273.4 | 18980533.5333 | 12929287.6333 | 8191972.4 | 4865638.5667 | 2689672.6 | 1378980.4333 | 648568 | 270505.1 | 145247.2 | 44377.85 | 12255.8 | 3409.9 | 980.15 | 268.8 | 135.9 | 40.7
B
A
Chart: Pre-Oxalate
| 5 | 15 | 25 | 35 | 45 | 55 | 65 | 75 | 85 | 95 | 105 | 115 | 125 | 135 | 145 | 155 | 165 | 175 | 185 | 195 | 205 | 215 | 225 | 235 | 245 | 255 | 265 | 275 | 285 | 295 | 305 | 315 | 325 | 335 | 345 | 355 | 365 | 375 | 385 | 395 | 405 | 415 | 425 | 435 | 445 | 455 | 465 | 475 | 485 | 495 | 505 | 515 | 525 | 535 | 545 | 555 | 565 | 575 | 585 | 595
Pre-Ox-I | 0 | 0 | 0 | 0 | 0 | 0 | 41 | 14874.9 | 262691.8 | 635502.6 | 1382171.7 | 2908729.8 | 5397369.8 | 12107936.5 | 22334183.7 | 24125353.6 | 17318913.5 | 11422319.4 | 9454577.5 | 11046136.1 | 15361344.2 | 19108143.7 | 18002756 | 13156307.8 | 8547197.1 | 5563704.2 | 3676494.3 | 2255348.8 | 1138164.6 | 433203.1 | 120404.7 | 24571.9 | 3734.9 | 423.7 | 35.4 | 2.1 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 1.1 | 32.9 | 602.2 | 6446.3 | 39626.9 | 139635 | 284174.3 | 338249.6 | 239108.3 | 102059.3 | 26754.9 | 4381.6 | 455.8 | 30.6
Pre-Ox-II | 0 | 0 | 0 | 0 | 0 | 0 | 3 | 418.9 | 51561.3 | 670579.3 | 662980.3 | 400024.5 | 697158.7 | 2312548.2 | 5761907.9 | 7820920.8 | 7043141 | 5919088.1 | 5832103.4 | 7050862.4 | 9606579.3 | 12934367.8 | 15353312.9 | 14964457.9 | 11673207.9 | 7441373.5 | 4154709.2 | 2258169.4 | 1329718.6 | 903686.2 | 704251 | 589045.1 | 482554.2 | 356560.6 | 225265.8 | 119332.1 | 53557.2 | 21034.1 | 7565.2 | 2619.7 | 915.3 | 335 | 131.6 | 56.1 | 25.8 | 12.7 | 6.5 | 3.4 | 1.8
Pre-Ox-III | 0 | 0 | 0 | 9.3 | 138.5 | 862.1 | 3094.6 | 8664.2 | 25625.8 | 93946.6 | 288521 | 728462.4 | 1951221.5 | 5088784.3 | 7646256.1 | 8690320.5 | 6610242.8 | 7685682.4 | 11012379 | 13069001.6 | 14410447.4 | 16413352.8 | 16774209 | 14098199.8 | 9885749.5 | 7400177.9 | 5607252.8 | 3972606.1 | 2751042.2 | 2008899.1 | 1557864.2 | 1254149.7 | 1036344.8 | 891880.8 | 843050.4 | 829466.7 | 626436.8 | 422260.8 | 322107.5 | 238259 | 166217.1 | 110715.7 | 71536.2 | 45305.7 | 28182.1 | 17158.4 | 10182.3 | 5881.5 | 3316.9 | 1840.9 | 1018.7 | 573 | 338.2 | 221.8 | 177.8 | 191.1 | 274.2 | 475.7 | 900.1 | 1735
Pre-Ox-mean | 0 | 0 | 0 | 3.1 | 46.1667 | 287.3667 | 1046.2 | 7986 | 113292.9667 | 466676.1667 | 777891 | 1345738.9 | 2681916.6667 | 6503089.6667 | 11914115.9 | 13545531.6333 | 10324099.1 | 8342363.3 | 8766353.3 | 10388666.7 | 13126123.6333 | 16151954.7667 | 16710092.6333 | 14072988.5 | 10035384.8333 | 6801751.8667 | 4479485.4333 | 2828708.1 | 1739641.8 | 1115262.8 | 794173.3 | 622588.9 | 507544.6333 | 416288.3667 | 356117.2 | 316266.9667 | 226664.6667 | 147764.9667 | 109890.9 | 80292.9 | 55710.8 | 37016.9 | 23889.2667 | 15120.6 | 9402.6333 | 5723.7 | 3396.6333 | 1972.6 | 1306.9667 | 4143.6 | 20322.8 | 70104 | 142256.25 | 169235.7 | 119643.05 | 51125.2 | 13514.55 | 2428.65 | 677.95 | 882.8