# Submission ID #: 62691

# Scriptwriter Name: Swati Madhu

# Project Page Link:  https://www.jove.com/account/file-uploader?src=19120803

# Title: 3D Bioprinting of Murine Cortical Astrocytes for Engineering Neural-Like Tissue

# Authors and Affiliations:

Bruna A. G. de Melo, Elisa M. Cruz, Taís N. Ribeiro, Mayara V. Mundim, Marimelia A. Porcionatto

Department of Biochemistry, Escola Paulista de Medicina, Universidade Federal de São Paulo

# Corresponding Authors:

# Bruna A. G. de Melo		g.melo.bruna@gmail.com; bagmelo@unifesp.br

# Email Addresses for All Authors:

g.melo.bruna@gmail.com; bagmelo@unifesp.br

elisa.marozzi@unifesp.br

tais.novaki@unifesp.br

mayara.terra@unifesp.br ; mayaratvv@gmail.com

marimelia.porcionatto@unifesp.br

## Author Questionnaire

1. Microscopy: Does your protocol require the use of a dissecting or stereomicroscope for performing a complex dissection, microinjection technique, or something similar?  No

2. Software: Does the part of your protocol being filmed include step-by-step descriptions of software usage?  Yes

3. Filming location: Will the filming need to take place in multiple locations?   No

Current Protocol Length

Number of Steps:  20

Number of Shots:  53

# Introduction

- Introductory Interview Statements

REQUIRED:

  - Bruna Melo: 3D bioprinting of astrocytes represents an advance in neural tissue engineering, allowing the biofabrication of in vitro models that are useful to understand mechanisms involved in neurological diseases.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

  - Elisa Cruz: The main advantage of 3D bioprinting is to biofabricate cell-laden structures that mimic the tissue’s biochemical and mechanical features, providing a better understanding of cell dynamics in health and damaged tissues.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B-roll: LAB MEDIA: Figure 3B (ii)

OPTIONAL:

  - Bruna Melo: This protocol can be applied to the biofabrication of other soft tissues, as it is based on the 3D bioprinting of a bioink composed of natural polymers and extracellular matrix components.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B-roll: 3.4.1

Ethics Title Card

  - Procedures involving animal subjects have been approved by the Committee for Ethics in Research of Universidade Federal de São Paulo.

# Protocol

- Astrocyte Isolation and Culture

  - To begin with [1], cut the cortical tissue isolated from the euthanized mouse into small pieces with a curved micro scissor [2]. Wash the tissue pieces three times with 1 milliliter of HBSS (H-B-S-S) by pipetting up and down [3].

    - WIDE: Establishing shot of talent in front of the laminar flow hood.

    - Talent cutting the cortical tissue in small pieces.

    - Talent washing the tissue with HBSS.

  - After removing HBSS added for the third time, add 1 milliliter of 0.05% trypsin [1] and incubate the tissue for 5 minutes at 37 degrees Celsius [2].

    - Talent adding trypsin to the tissue.

    - Talent put the tube inside the incubator

  - For mechanical tissue dissociation, gently pipette the tissue-trypsin mixture up and down 15 times [1]. Next, transfer the dissociated mixture to a 15-milliliter conical tube [2] and add an equal volume of FBS (F-B-S) to neutralize trypsin activity [3].

    - Talent pipetting the tissue-trypsin mixture up and down.

    - Talent transferring the dissociated mixture to a 15-milliliter conical tube.

    - Talent adding FBS in the tube containing dissociated mixture.

  - Filter the suspension through a 0.4-micrometer cell strainer filter to remove non-dissociated fragments [1]. Wash the filter with 1 milliliter of astrocytes medium [2]. Pellet down the filtered cell suspension by centrifugation [3-TXT].

    - Talent adding suspension to the filter.

    - Talent adding astrocyte medium to the filter.

    - Talent placing the tube in the centrifuge. TEXT: Centrifugation: 200 x g, 25 °C, 5 min

  - After discarding the supernatant, suspend the cell pellet in 1 milliliter of astrocytes culture medium [1]. Transfer the cell suspension to a T25 (T-twenty five) culture flask [2], make up the total medium volume of 3.5 milliliters [3], and incubate the cells at 37 degrees Celsius and 5% carbon dioxide [4].

    - Talent resuspending the cell pellet.

    - Talent transferring the cell suspension to a T25 culture flask.

    - Talent adding medium in the flask.

    - Talent placing the flask in the incubator.

- Astrocytes-laden Gelatin/GelMA/Fibrinogen Bioink Preparation

  - For obtaining the fibrinogen at the final concentration of 3 milligrams per milliliter, transfer 0.9 milliliters of 10 milligrams per milliliter fibrinogen solution to the gelatin-gelatin-methacryloyl solution [1].

    - WIDE: Talent adding fibrinogen solution to the gelatin/GelMA solution.

  - For obtaining the photoinitiator at the final concentration of 0.5% weight by volume, add 0.015 grams of photoinitiator to the prepared gelatin- gelatin-methacryloyl-fibrinogen solution [1]. After vortexing, keep the solution at 40 degrees Celsius protected from light to avoid PI degradation [2].

    - Talent adding photoinitiator to the gelatin/GelMA/fibrinogen solution.

    - Talent mixing content of the tube.

  - Next, filter the solution through a 0.2-micrometer filter into a sterile 15-milliliter conical tube [1]. Transfer 980 microliters of the biomaterial solution to a 15-milliliter conical tube [2].

    - Talent adding the solution to the filter.

    - Talent adding biomaterial solution to a conical tube.

  - For obtaining the laminin at the final concentration of 2 micrograms per milliliter, add 20 microliters of diluted laminin to the tube containing bioink [1]. Mix gently by pipetting up and down, avoiding bubbles, and keep the bioink solution at 37 degrees Celsius until ready to get mixed with the cells [2-TXT].

    - Talent adding diluted laminin to the tube containing bioink.

    - Talent mixing the solution by pipetting. TEXT: Remove bubbles by centrifugation.

  - Trypsinize the primary astrocytes with 0.05% trypsin for 5 minutes [1-TXT] and neutralize the trypsin activity with FBS at a ratio of 1 to 1 [2]. Then, transfer the cells to a 15-milliliter conical tube [3] and centrifuge at 200 times g for 5 minutes [4].

    - Talent adding trypsin solution to the cells. TEXT: Use astrocytes from passages 1 to 3

    - Talent adding FBS to the trypsinized cells.

    - Talent transferring the cells to a 15-milliliter conical tube.

    - Talent placing the tube in the centrifuge.

  - After counting the cells, transfer 1 x 106 cells to a different conical tube and centrifuge as demonstrated [1]. Leave only 200 microliters of the supernatant in the tube and suspend the cell pellet by gently tapping the bottom of the conical tube [2].

    - Talent transferring the cell suspension in a new tube.

    - Talent tapping bottom of the conical tube.

  - To obtain a final concentration of 1 x 106 cells per milliliter, transfer 1 milliliter of gelatin- gelatin-methacryloyl-fibrinogen solution to the tube containing the cells [1] and homogenize by gently pipetting up and down [2]. Videographer: This step is important!

    - Talent adding 1 mL of gelatin/GelMA/fibrinogen solution to the tube containing the cells.

    - Talent mixing by pipetting.

- Bioprinting Syringe Preparation and Bioprinting

  - Use a 1000-microliter pipette to slowly transfer the astrocytes-laden gelatin-gelatin-methacryloyl-fibrinogen bioink solution to a 5-milliliter plastic syringe avoiding bubble formation [1]. Connect a sterile 22-Gauge blunt needle to the syringe [2]. Videographer: This step is important!

    - Talent transferring the astrocytes-laden gelatin/GelMA/fibrinogen bioink to a 5 mL plastic syringe.

    - Talent connecting the needle to the syringe.

  - Expose the bioprinter to UV light for 15 minutes [1] and then wipe the bioprinter with 70% ethanol [2]. Then, connect the syringe to the bioprinter printhead [3] and manually flush the bioink to remove the remaining bubbles [4]. Videographer: This step is important!

    - Bioprinter under UV light.

    - Talent wiping the bioprinter with 70% ethanol.

    - Talent connecting the syringe to the bioprinter printhead.

    - LAB MEDIA: Screen 62691.mp4: 00:03 to 00:10

  - To conduct bioprinting, place a 35-millimeter culture dish on the bioprinter table [1], position the needle 0.1 millimeters away from the culture dish surface to allow movement of the needle, and press the Print button [2]. Videographer: This step is important!

    - Talent placing a 35 mm culture dish on the bioprinter table.

    - LAB MEDIA: Screen 62691.mp4: 00:14 to 00:20

  - Once the bioprinting over [1], ensure that the syringe moves away from the dish [2] and close the culture dish [3].

    - The material is getting printed.

    - The syringe is moving away from the dish.

    - Talent placing the lid on the culture dish.

- Bioprinted Construct and Culture Crosslinking

  - Place the culture dish under UV light for gelatin-methacryloyl crosslinking [1-TXT]. Use a sterile spatula to transfer the bioprinted construct to a 24-well plate [2]. Add 500 microliters of thrombin-calcium chloride solution and leave for 30 minutes to allow fibrin crosslinking [3]. Videographer: This step is important!

    - Talent placing the plate under UV light. TEXT: Incubation under UV light: at 2 mW/cm2, 60 s up; 60 s down.

    - Talent transferring the bioprinted construct to a 24-well plate.

    - Talent adding thrombin/CaCl2 solution in the wells.

  - After removing the crosslinking solution, wash the construct with 2 milliliters of PBS [1]. Then, replace the PBS with 1 milliliter of astrocytes culture medium [2], incubate at 37 degrees Celsius and 5% carbon dioxide, and change the medium every 3 days [3]. Videographer: This step is important!

    - Talent washing the construct with 2 mL of PBS.

    - Talent adding astrocytes culture medium to the wells.

    - Talent placing the plate in the incubator.

- Astrocytes Viability Assessment

  - Use a spatula to transfer the bioprinted construct to a 35-millimeter culture dish [1]. Wash the construct with 1 milliliter of PBS [2]. Deposit 100 microliters of the Live-Dead reagent over the construct [3] and keep it at 37 degrees Celsius for 30 minutes, keeping it protected from light [4].

    - Talent transferring the bioprinted construct to a 35 mm culture dish.

    - Talent washing the construct with PBS.

    - Talent adding the Live-Dead reagent over the construct.

    - Talent placing the plate in the incubator.

  - After removing the Live-Dead reagent, wash the construct with PBS as demonstrated [1]. Transfer the sample to a confocal dish and observe the cells within the construct under a confocal microscope using 488 and 570 nanometers excitation for image acquirement [2].

    - Talent washing the construct with PBS.

    - Talent transferring the sample to a confocal dish.

# Results

- Results: 3D Bioprinted Astrocyte Cell Viability and Morphology Assessment

  - After 3D bioprinting, the integrity of the bioprinted scaffold was estimated [1], and the formation of a well-defined structure was observed with cells entrapped within the biomaterial [2].

    - LAB MEDIA: Figure 3C, D, and E

    - LAB MEDIA: Figure 3C

  - After bioprinting and crosslinking processes, most cells presented round morphology when the construct was incubated with an astrocyte medium [1].

    - LAB MEDIA: Figure 3D

  - The bioprinted scaffolds maintained integrity after 7 days of incubation, and although some round cells were observed, many astrocytes spread throughout the construct, presenting astrocytic morphology and interconnection [1].

    - LAB MEDIA: Figure 3E

  - The cell viability was evaluated right after bioprinting [1], and results showed that at the lower speed, viable cells represented up to 74% of total cells [2], being significantly higher than cells bioprinted at the higher speed [3].

    - LAB MEDIA: Figure 4A

    - LAB MEDIA: Figure 4A Video editor: Please emphasize the first bar at 400 mm/min.

    - LAB MEDIA: Figure 4A Video editor: Please emphasize the second and third bar at 400 and 800 mm/min.

  - The viability of bioprinted astrocytes was normalized to 2D cultured astrocytes [1], and the results indicated that on the 7th day, the bioprinted astrocytes had significantly increased viability [2].

    - LAB MEDIA: Figure 4B

    - LAB MEDIA: Figure 4B Video editor: Please emphasize the bar at Day 7.

  - Immediately after the bioprinting [1], the astrocytes showed round morphology in live dead assay [2]. After 1 week, the astrocytes spread throughout the construct and presented a distinct morphology of cells [3] identical to 2D culture [4].

    - LAB MEDIA: Figure 4C

    - LAB MEDIA: Figure 4C i

    - LAB MEDIA: Figure 4C ii

    - LAB MEDIA: Figure 4C iii

  - The 3D bioprinted astrocytes were characterized by Immunofluorescence [1]. After 7 days of incubation, in the bioprinted construct, highly dense astrocytes with a star-like morphology were observed [2].

    - LAB MEDIA: Figure 5

    - LAB MEDIA: Figure 5A

  - The bioprinted astrocytes cells expressed the specific astrocytes marker glial fibrillary acidic protein indicates retainment of astrocytic phenotype after 7 days of bioprinting, and these results indicate that the bioink composition provided a biocompatible microenvironment to promote astrocytes’ adhesion, spread, and growth [1].

    - LAB MEDIA: Figure 5B

# Conclusion

- Conclusion Interview Statements

  - Elisa Cruz: The evaluation of specific genes and cell markers expression by the bioprinted astrocytes would provide evidence of the neural tissue-like function, such as the astrocitary reactivity following specific stimuli.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B-roll: LAB MEDIA: Figure 5A

  - Bruna Melo: This protocol paves the way for the biofabrication of more complex neural-like structures composed of different types of cells and biomolecules, allowing the mimicking of specific neurogenic niches.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B-roll: 4.4.1