Supplemental File #1

Production of Liposome Sample:

- Sample was produced by Dr. Sagar Rayamajhi working in Dr. Santosh Aryal’s Lab.

- Liposomes were produced using 900 µg of DSPE-PEG-Succinyl:100 µg of Cholesterol at 1.0 mg/mL in milliQ water.

- The average hydrodynamic size of the liposomes was 180 nm, and the PDI was 0.2 immediately after extrusion using dynamic light scattering on the Malvern ZetaSizer.

- This initial concentration was diluted 1:200 in milliQ water for the final liposome product used in this experiment.