# Submission ID #: 67246

# Scriptwriter Name: Sulakshana Karkala

# Project Page Link: https://review.jove.com/account/file-uploader?src=20510078

# Title: Modeling the Endothelial Glycocalyx Post-Pneumonectomy in a 3D Fluidic Chip – An Approach to Fabricating a Vascular-Based Organ-on-Chip System

# Authors and Affiliations:

# Jacob Elliott, Camden Holm, Mia Long, Zoe Vittum, Eric Johnson, Solomon A. Mensah

# Worcester Polytechnic Institute

# Corresponding Authors:

Solomon A. Mensah 		smensah@wpi.edu

# Email Addresses for All Authors:

Jacob Elliot			jtelliott4@outlook.com

Camden Holm 			cholm@wpi.edu

Mia Long 			mlong2@wpi.edu

Zoe Vittum 			zlvittum@wpi.edu

Eric Johnson 			ejohnson@wpi.edu

Solomon A. Mensah 		smensah@wpi.edu

## Author Questionnaire

1. We have marked your project as author-provided footage, meaning you film the video yourself and provide JoVE with the footage to edit. JoVE will not send the videographer. Please confirm that this is correct.

√ Correct

2. Microscopy: Does your protocol require the use of a dissecting or stereomicroscope for performing a complex dissection, microinjection technique, or something similar?  No

3. Software: Does the part of your protocol being filmed include step-by-step descriptions of software usage?  No

4. Proposed filming date: To help JoVE process and publish your video in a timely manner, please indicate the proposed date that your group will film here: 09/07/2025

When you are ready to submit your video files, please contact our Content Manager, Utkarsh Khare.

Current Protocol Length

Number of Steps:  18

Number of Shots:  28

# Introduction

  - Solomon Mensah: The Mensah Lab is focused on vascular research and is developing new techniques for researching the endothelial glycocalyx and its role in vascular diseases [1].

    - INTERVIEW: Named Talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B. roll: 3.1

What are the most recent developments in your field of research?

  - Camden Holm: Recent developments involve creating more advanced in vitro models for glycocalyx research and researching therapeutic strategies to target endothelial glycocalyx health and repair in diseases [1].

    - INTERVIEW: Named Talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B. roll: 2.8

What are the current experimental challenges?

  - Camden Holm: Experimental challenges include incomplete in vitro models which fail to accurately replicate healthy glycocalyx, as well as difficult quantification and measurement techniques [1].

    - INTERVIEW: Named Talent says the statement above in an interview-style shot, looking slightly off-camera.

What significant findings have you established in your field?

  - Solomon Mensah: Our contributions to the field have expanded the current understanding of the endothelial glycocalyx, particularly its roles in cancer metastasis, regeneration of damaged glycocalyx, and interactions with vascular surface receptors [1].

    - INTERVIEW: Named Talent says the statement above in an interview-style shot, looking slightly off-camera.

What advantage does your protocol offer compared to other techniques?

  - Camden Holm: Our method presents an inexpensive and effective method for creating organ-on-chip vascular systems that express more well-developed and biomimetic endothelial glycocalyx compared to conventional techniques [1].

    - INTERVIEW: Named Talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B. roll: 2.17

Ethics Title Card

This research has been approved by the Institutional Review Board (IRB) at the Worcester Polytechnic Institute

# Protocol

- Fabrication and Cell Seeding of a PDMS-Based Microvascular Flow System

Demonstrator: Camden Holm

  - To begin, weigh 10 parts silicone elastomer base in a 50-milliliter centrifuge tube [1].

    - LAB MEDIA: 20240702_182836000_iOS.MOV 	00:00 – 00:22
AND 20240702_183008000_iOS.MOV		00:00 – 00:01

  - Pour 1 part curing agent into the tube containing the silicone elastomer base, to a final volume of 30 milliliters [1]. Mix thoroughly to obtain a uniform solution [2].

    - LAB MEDIA: 20240702_183023000_iOS.MOV 	00:00 – 00:20

    - LAB MEDIA : 20240702_183256000_iOS.MOV	00:00 – 00:09

  - Now, pour the well mixed solution into the molds [1].

    - LAB MEDIA: 20240702_183615000_iOS.MOV	00:02 – 00:14

  - Then place the molds into a vacuum chamber to degas the PDMS (P-D-M-S) for 30 to 60 minutes or until no bubbles remain [1-TXT].

    - LAB MEDIA: 20240702_183834000_iOS.MOV 	00:03 – 00:23
AND 20240702_183917000_iOS.MOV		00:03 – 00:08 TXT: PDMS: polydimethylsiloxane

  - Remove the degassed PDMS from the vacuum chamber and allow it to cure at room temperature for 48 hours [1].

    - LAB MEDIA: 20240702_191741000_iOS.MOV	00:14 – 00:34
AND 20240702_191824000_iOS.MOV		00:00 – 00:02

  - Extract the cured PDMS from the PLA (P-L-A) mold [1-TXT]. Then place two pieces of double-sided tape in each cell culture plate [2].

    - LAB MEDIA: 20240705_150730000_iOS.MOV 	00:35 – 00:45 TXT: PLA: polylactic acid

    - LAB MEDIA: 20240705_150502000_iOS.MOV 	00:04 – 00:19

  - Next, position each PDMS vasculature half on top of the tape in its own cell culture dish [1].

    - LAB MEDIA: 20240705_151237000_iOS.MOV 	00:11 – 00:21, 00:30-00:35

  - Place several 30 microliter drops of fibronectin along the PDMS vasculature using a micropipette. Tilt the PDMS as needed and use a pipette tip to evenly coat the surface [1-TXT].

    - LAB MEDIA: 20240705_151417000_iOS.MOV 	01:32 – 02:06
TXT: Fibronectin: 20 µg/mL

  - After a 30-minute incubation, aspirate the fibronectin solution from the PDMS then let the pieces air dry inside the cabinet [1]. Place 3D-printed plugs at each end of the PDMS vasculature halves to prevent cell suspension leakage, using two plugs per piece [2].

    - LAB MEDIA: 20240705_151739000_iOS.MOV 00:03 – 00:18, 00:27-00:36

    - LAB MEDIA: 20240705_151417000_iOS.MOV 00:10 – 00:22, 00:50-00:53

  - With a micropipette, seed 300 microliters of HLMVEC (H-L-M-V-E-C) cell suspension into each PDMS piece and incubate [1-TXT].

    - LAB MEDIA: 20240705_151953000_iOS.MOV 	00:20 – 00:35
TXT: HLMVEC: Human Lung Microvascular Endothelial Cells;
Incubation: 37 °C, 5% CO2

  - Then return the halves to the cabinet and remove the four plugs [1]. Add HLMVEC culture medium to submerge the PDMS vasculature halves and incubate again for 6 to 10 hours [2].

    - LAB MEDIA: 20240705_152211000_iOS.MOV 0	0:08-00:14

    - LAB MEDIA: 20240705_152211000_iOS.MOV 	00:47 – 01:02

  - Now, aspirate the HLMVEC media from the Petri dish containing the vasculature halves [1]. Place each PDMS half into the polycarbonate blocks, ensuring proper alignment [2].

    - LAB MEDIA: 20240705_153208000_iOS.MOV 	00:13 – 00:23

    - LAB MEDIA: 20240705_153417000_iOS.MOV 	00:15 – 00:32

  - Apply silicone sealant to the ends of the PDMS vasculature [1]. Insert inch-long tubing into both ends of the bottom PDMS piece [2]. Then flip the top acrylic block containing the top PDMS half onto the bottom acrylic block [3].

    - LAB MEDIA: 20240705_153313000_iOS.MOV	 00:02 – 00:11

    - LAB MEDIA: 20240705_153417000_iOS.MOV 	01:25 – 01:36

    - LAB MEDIA: 20240705_153417000_iOS.MOV 	01:40 – 01:48

  - Bolt the acrylic blocks together, ensuring the threaded block is on the bottom [1]. Plug the free ends of the tubing using 3D-printed plugs [2].

    - LAB MEDIA: 20240705_153417000_iOS.MOV 	01:50 – 02:00; 03:00 – 03:10

    - LAB MEDIA: 20240705_154009000_iOS.MOV 	00:00 – 00:17

  - Remove one plug and gently inject 500 microliters of HLMVEC culture medium into the vasculature using a micropipette. Tilt to remove air bubbles and then replace the plug [1].

    - LAB MEDIA: 20240705_154107000_iOS.MOV 	00:00 – 00:30

  - Bring the assembled chip and sterile components into the biosafety cabinet [1]. Connect all tubing and assemble the flow system, ensuring the inlet tubing connects to the bottom of the syringe reservoir to facilitate gravity flow [2].

    - LAB MEDIA: 20240705_165113000_iOS.MOV 	00:00 – 00:12

    - LAB MEDIA: 20240705_165350000_iOS.MOV 	00:10 – 00:37

  - Now, gently prime the flow system with HLMVEC medium [1]. Use a 50-milliliter serological pipette, inject 30 milliliters of medium into the top of the syringe reservoir and operate the peristaltic pump at low speed to fill tubing [2-TXT].

    - LAB MEDIA: 20240705_165451000_iOS.MOV 	00:00 – 00:18

    - LAB MEDIA: 20240705_165451000_iOS.MOV 	00:18 – 00:50
TXT: Continue adding medium until system is fully primed and free of air bubbles

  - Wash each PDMS vasculature half in PBS for 5 minutes, adding enough solution to fully submerge the vascular section [1].

    - LAB MEDIA: 20240705_171334000_iOS.MOV 	00:01 – 00:21

# Results

- Results

  - The fluid simulation showed significantly elevated shear stress at vessel bifurcations in the pneumonectomy model compared to the control model [1].

    - LAB MEDIA: Figure 11. Video editor: Please emphasize B first and then A

  - Brightfield microscopy confirmed uniform HLMVEC cell attachment in both static [1] and flow conditions at 93.1 milliliters per minute after 24 hours [2].

    - LAB MEDIA: Figure 12. Video editor: Highlight the image labeled "A"

    - LAB MEDIA: Figure 12. Video editor: Highlight the image labeled "B"

  - Fluorescence imaging of the inlet bifurcation showed intact and well-distributed cell layers in both control and pneumonectomy models [1].

    - LAB MEDIA: Figure 13. Video editor: Emphasize A and the red box in the inset image then highlight B and the red square in the Inset image

  - Imaging immediately after the second bifurcation revealed substantial cell loss in both the control and pneumonectomy models [1].

    - LAB MEDIA: Figure 14. Video editor: Emphasize A and the blue box in the inset image then highlight B and the blue square in the Inset image

  - Cells remained adherent and showed consistent staining in the region downstream of the second bifurcation in both models [1].

    - LAB MEDIA: Figure 15. Video editor: Emphasize A and the green box in the inset image then highlight B and the green square in the Inset image

  - Uniform DAPI (da-pee)-stained nuclei in the vascular models indicated that confluence was maintained despite flow exposure [1].

    - LAB MEDIA: Figure 13-15. Video editor: Show only image B

  - An early control model trial resulted in uneven cell distribution due to air bubbles introduced during system priming [1].

    - LAB MEDIA: Figure 16.

Pronunciation Guide:

# Elastomer
Pronunciation link:
https://www.merriam-webster.com/dictionary/elastomer
IPA: /ɪˈlæstoʊmɚ/
Phonetic Spelling: ih-las-toh-mer

# Centrifuge
Pronunciation link:
https://www.merriam-webster.com/dictionary/centrifuge
IPA: /ˈsɛntrəˌfjuːdʒ/
Phonetic Spelling: sen-truh-fyooj

# Vasculature
Pronunciation link:
https://www.merriam-webster.com/dictionary/vasculature
IPA: /ˈvæskjələˌtʃʊr/
Phonetic Spelling: vas-kyuh-luh-choor

# Fibronectin
Pronunciation link:
https://www.merriam-webster.com/dictionary/fibronectin
IPA: /ˌfaɪbroʊˈnɛktɪn/
Phonetic Spelling: fai-broh-nek-tin

# Micropipette
Pronunciation link:
https://www.merriam-webster.com/dictionary/micropipette
IPA: /ˌmaɪkroʊpaɪˈpɛt/
Phonetic Spelling: my-kroh-pai-pet

# Endothelial
Pronunciation link:
https://www.merriam-webster.com/dictionary/endothelial
IPA: /ˌɛndoʊˈθiliəl/
Phonetic Spelling: en-doh-thee-lee-uhl

# Polycarbonate
Pronunciation link:
https://www.merriam-webster.com/dictionary/polycarbonate
IPA: /ˌpɑliˈkɑrbəˌneɪt/
Phonetic Spelling: pah-lee-kar-buh-nayt

# Acrylic
Pronunciation link:
https://www.merriam-webster.com/dictionary/acrylic
IPA: /əˈkrɪlɪk/
Phonetic Spelling: uh-kri-lik

# Serological
Pronunciation link:
https://www.merriam-webster.com/dictionary/serological
IPA: /ˌsɪrəˈlɑdʒɪkəl/
Phonetic Spelling: sih-ruh-lah-ji-kuhl

# Peristaltic (as in peristaltic pump)
Pronunciation link:
https://www.merriam-webster.com/dictionary/peristaltic
IPA: /ˌpɛrəˈstɔltɪk/
Phonetic Spelling: peh-ruh-stawl-tik

# Pneumonectomy
Pronunciation link:
https://www.merriam-webster.com/dictionary/pneumonectomy
IPA: /ˌnuːməˈnɛktəmi/
Phonetic Spelling: noo-muh-nek-tuh-mee

# Fluorescence
Pronunciation link:
https://www.merriam-webster.com/dictionary/fluorescence
IPA: /flʊˈrɛsəns/ or /flɔˈrɛsəns/
Phonetic Spelling: floo-res-ens or flor-es-ens

# Bifurcation
Pronunciation link:
https://www.merriam-webster.com/dictionary/bifurcation
IPA: /ˌbaɪfɚˈkeɪʃən/
Phonetic Spelling: bai-fer-kay-shun

# Confluence
Pronunciation link:
https://www.merriam-webster.com/dictionary/confluence
IPA: /ˈkɑnfluəns/
Phonetic Spelling: kon-floo-uhns