# Submission ID #: 67778

# Scriptwriter Name: Sulakshana Karkala

# Project Page Link: https://review.jove.com/account/file-uploader?src=20672338

# Title: Effects of Mechanical Methods Used in Peri-Implantitis Treatment on Implant Surface Decontamination and Roughness

# Authors and Affiliations:

# Ipek Ozgu, Kemal Ustun

# Faculty of Dentistry, Department of Periodontology, Akdeniz University

# Corresponding Authors:

# Ipek Ozgu                      ipekozgu@akdeniz.edu.tr

# Email Addresses for All Authors:

Ipek Ozgu		ipekozgu@akdeniz.edu.tr

Kemal Ustun		kemalustun@akdeniz.edu.tr

## Author Questionnaire

1. We have marked your project as author-provided footage, meaning you film the video yourself and provide JoVE with the footage to edit. JoVE will not send the videographer. Please confirm that this is correct.

√ Correct

2. Microscopy: Does your protocol require the use of a dissecting or stereomicroscope for performing a complex dissection, microinjection technique, or something similar?   NO

3. Software: Does the part of your protocol being filmed include step-by-step descriptions of software usage?   YES, all done

4. Proposed filming date: To help JoVE process and publish your video in a timely manner, please indicate the proposed date that your group will film here: 7/01/2025

When you are ready to submit your video files, please contact our Content Manager, Utkarsh Khare.

Current Protocol Length

Number of Steps:  15

Number of Shots:  32

# Introduction

  - Ipek Ozgu: This study evaluates the effectiveness of air abrasive systems, PEEK ultrasonic tips and titanium curettes for implant surface decontamination and their impact on surface roughness using SEM analysis [1].

    - INTERVIEW: Named Talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B.roll:2.10

What research gap are you addressing with your protocol?

  - Ipek Ozgu: The prevalence of periimplantitis in increasing worldwide and there is no definitive protocol for effective treatment of this disease [1].

    - INTERVIEW: Named Talent says the statement above in an interview-style shot, looking slightly off-camera.

What new scientific questions have your results paved the way for?

  - Kemal Ustun: The results showed that air abrasion can be safely and efficiently used for the decontamination of implant surfaces for regenerative purposes [1].

    - INTERVIEW: Named Talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B.roll:2.9

What research questions will your laboratory focus on in the future?

  - Kemal Ustun: Although SEM can provide details of the implant surface, there is a need for an objective index for differentiating the changes after surface treatment [1].

    - INTERVIEW: Named Talent says the statement above in an interview-style shot, looking slightly off-camera.

Ethics Title Card
This research has been approved by the Ethical Committee at Akdeniz University

# Protocol

SCREEN timestamps for protocol were added at the postshoot stage. Please contact the postshoot note integrator (Balamurugan) for queries regarding SCREEN timestamps

- Fabrication and Decontamination of Experimental Implant Models

Demonstrator: Ipek Ozgu

  - To begin, remove the first molar from an educational mandibular phantom model [1]. Using a screwdriver, loosen and remove the screw securing the first molar tooth [2]. Extract the thread from the socket [3]. Mold soft silicone material into the socket to create a flat alveolar ridge [4].

    - WIDE: Talent removing the first molar from the phantom model.

    - Shot of the screw being loosened.

    - Shot of the thread being removed from the socket.

    - Talent filling the socket with soft silicone material.

  - Print the digital models using a model resin [1].

    - Shot of the 3D printer in operation, printing the experimental models.

  - Now, rinse the printed experimental models in 96% ethanol for 5 to 10 minutes [1]. After cleaning, place the models in a light-emitting curing device [2]. Cure the models with light for 5 minutes [3].

    - Talent immersing the printed models in ethanol.

    - Shot of the models being placed in the curing device.

    - Shot of the curing device illuminating the models.

  - To stain the implants, submerge them completely, in viscous water-resistant red ink for 15 seconds [1]. Air-dry the stained implants with a dental unit air syringe to achieve even dispersion of the ink [2-TXT].

    - Talent fully immersing the implants in red ink.

    - Talent using an air syringe to dry the implants. TXT: Let the implant air-dry at RT for 24 h

  - Next, adjust the settings of a dental physio dispenser to 800 revolutions per minute, 40 Newton torque, with no saline irrigation [1]. Using surgical implant drills, create implant sockets in the experimental models for implants measuring 11 millimeters in length and 4.2 millimeters in width [2].

    - Shot of the dental physio dispenser settings being set to 800 rpm, 40 N torque.

    - Talent using a surgical implant drill to create the socket in the model.

  - Now insert the implants into the sockets using a carrier handpiece [1]. Ensure 5 millimeters of the implant remains exposed on the buccal surface [2]. Align the implant to be submerged at the same level as the lingual bone crest of the model [3].

    - Talent inserting the implant using the carrier handpiece.

    - Shot of the 5-millimeter exposed implant area.

    - Shot of the implant aligned with the lingual bone crest.

  - For an air abrasive system, set the device to full power with water irrigation and apply 14-micrometer erythritol powder [1]. Hold the device tip 2 to 3 millimeters from the implant surface and apply the powder evenly [2-TXT].

    - Talent sets the device to full power with water irrigation.

    - Talent holding the device at 2–3 millimeters from the implant surface while applying erythritol powder.TXT: Limit application to 2 min (Class 1A) and 3 min (Class 1B)

  - For a polyetheretherketone or PEEK (peek) ultrasonic tip, set the device to power level 8 with maximum water irrigation [1]. Perform decontamination with linear and parallel movements, ensuring application between the implant threads where possible [2-TXT].

    - Shot of the PEEK ultrasonic tip settings at power level 8.

    - Talent using linear and parallel movements for decontamination. TXT: Limit application to 2 min (Class 1A) and 3 min (Class 1B)

  - For titanium curettes, apply consecutive contacts with constant pressure at a 60 to 90-degree angle to the implant surface [1-TXT].

    - Talent using a titanium curette at a 60°-90° angle. TXT: Force: 0.75 N; Limit application to 2 min (Class 1A) and 3 min (Class 1B)

- Photographic Documentation, Image Analysis, and SEM Evaluation of Implant Surfaces

  - Remove the implants from the model with a compatible implant driver piece [1]. Air-dry the implants for 20 seconds to eliminate any loosened particles or remnants on the surface [2].

    - Talent using an implant driver to remove an implant from the model.

    - Talent air-drying the implant with compressed air for 20 seconds.

  - Place the implants on custom-designed acrylic photographic models to evaluate the apical and coronal regions of the implant threads [1]. Then, mount the camera on a tripod and standardize the camera settings [2-TXT]. Ensure that the room is adequately lit [3].

    - Talent positioning the implants on acrylic models for photography.

    - Talent adjusting the camera on a tripod and configuring the settings. TXT: Camera settings: Distance: 15 cm; ISO: 160; Aperture: f/16; Exposure time: 1/250 s

    - Shot of the room lighting setup ensuring proper illumination.

  - Take digital photographs in RAW (raw) format with a flash [1-TXT].

    - Talent taking digital RAW images of the implants. TXT: Capture 90 buccal photos for Class 1A defects and 270 photos for Class 1B defects

  - For image analysis, click on Image, followed by Type, and press 8-bit (eight-bit) to convert the images to 8-bit format [1]. Adjust the thresholds by sequentially clicking on Image, Adjust, and Threshold for area calculations [2].

    - SCREEN: 67778-3.4.1.MOV 00:18-00:27

    - SCREEN: 67778-3.4.2-3.5.1.MOV 00:07-00:12; 00:17-00:22

  - Next, press Analyze, followed by Measure, then click on Area to calculate the total implant surface area and the red residue area [1].

    - SCREEN: 67778-3.4.2-3.5.1.MOV 00:31-00:37; 00:56-01:04; 1:09-01:10

  - For SEM (sem) analysis, first spray the implant with nitrogen gas using a gas gun for 20 seconds to remove any micro-powder from the implant surface [1]. Mount each implant on SEM stubs using conductive carbon adhesive discs [2-TXT]. Arrange the implants in order by number to prevent misidentification before SEM imaging [3].

    - Talent using a nitrogen gas gun to clean the implant surface.

    - Talent placing implants on SEM stubs with conductive adhesive. TXT: Position the implants to allow for analysis without hand decontamination

    - Shot of implants arranged numerically.

# Results

- Representative Results

  - The most effective decontamination was observed in the AA-1A (A-A-one-A) group [1]. The least decontamination was detected in the TIT-1A (Tit-one-A) and TIT-1B (Tit-One-B) groups [2].

    - LAB MEDIA: Figure 3 Video Editor: Please highlight the plot of AA-1A

    - LAB MEDIA: Figure 3 Video Editor: Please highlight the plots of TIT-1A and TIT-1B

  - In the mesial and distal areas of the 1B defect group, more ink residues were found under the threads compared to the buccal area, in the AA treatment group [1]. Additionally, a powder particle was observed in the buccal micro-thread site of the 1B defect group [2].

    - LAB MEDIA: Figure 5A and B Video Editor: Please highlight 1B-AA images of A and B panels.

    - LAB MEDIA: Figure 6

  - A blurred and perforated appearance was observed in the PEEK group [1]. However, the PEEK treatment yielded similar results to AA in the mesial and distal areas of the 1B defect group at 1000X and 5000X magnifications [2].

    - LAB MEDIA: Figure 4B, Figure 5B Video Editor: Please highlight 1A-PEEK of 4B and 1B-PEEK images of 5B

    - LAB MEDIA: Figure 5B-D	Video Editor: Please sequentially highlight 1B-PEEK images of 5B, C and D

  - Titanium curettes caused extensive surface alterations, with the rough structure in the micro-threaded buccal area of the 1A defect group becoming indistinguishable [1]. Other sites exhibited flattening and longitudinal and horizontal scratches [2].

    - LAB MEDIA: Figure 4. Video Editor: Please highlight the 1A-curette images of A and B panels

    - LAB MEDIA: Figure 5 A and B Video Editor: Please highlight the 1B-curette images of A and B panels.

  - In the mesial and distal sites of the 1B defect group, the rough structure disappeared, and the number of scratches increased [1].

    - LAB MEDIA: Figure 5 C-D. Video Editor: Please highlight the 1B-curette images of C and D panels.

  - Elemental analysis of the sterile reference implant revealed 99.2% titanium content [1]. Analysis of black hole-like structures in other groups and the completely ink-covered untreated implant surface showed a carbon-dominant composition [2].

    - LAB MEDIA: Figure 7. Video editor: Please emphasize the red peak in the “Full Area 1” graph and the row corresponding to TK in the “eZAF Smart Quant Results” table

    - LAB MEDIA: Figure 8A-C. Video editor: Please sequentially show A with the corresponding graph, B with the corresponding graph, and C with the corresponding graph

Pronunciation Guide:

  alveolar
Pronunciation link: https://www.merriam-webster.com/dictionary/alveolar dictionary.cambridge.org+1synonyms.com+1en.wikipedia.org+12merriam-webster.com+12merriam-webster.com+12
IPA: /ælˈviː.ə.lɚ/
Phonetic spelling: al-VEE-uh-ler

  bronchoalveolar
Pronunciation link: https://www.merriam-webster.com/medical/bronchoalveolar howtopronounce.com+15merriam-webster.com+15dictionary.cambridge.org+15
IPA: /ˌbrɑŋ.koʊ-ælˈviː.ə.lɚ/
Phonetic spelling: BRONG-koh-al-VEE-uh-ler

  polyetheretherketone
Pronunciation link: https://www.howtopronounce.com/polyetheretherketone merriam-webster.comen.wiktionary.org+8howtopronounce.com+8howtopronounce.com+8
IPA: /ˌpɑːliːˌiːθərˌiːθərˈkiːtoʊn/
Phonetic spelling: pah-lee-ee-THUR-ee-thur-KEE-tohn

  erythritol
Pronunciation link: https://www.merriam-webster.com/medical/erythritol howtopronounce.com
IPA: /ɪˈrɪθ.rə.tɑl/
Phonetic spelling: ih-RITH-ruh-tal

  mandibular
Pronunciation link: https://www.merriam-webster.com/dictionary/mandibular merriam-webster.com+6en.wikipedia.org+6howtopronounce.com+6merriam-webster.com+2howtopronounce.com+2howtopronounce.com+2merriam-webster.com
IPA: /mænˈdɪb.jə.lɚ/
Phonetic spelling: man-DIB-yuh-ler

  silicone
Pronunciation link: https://www.merriam-webster.com/dictionary/silicone merriam-webster.com+3dictionary.cambridge.org+3merriam-webster.com+3
IPA: /ˈsɪl.ɪˌkoʊn/
Phonetic spelling: SIL-ih-kohn

  torque
Pronunciation link: https://www.merriam-webster.com/dictionary/torque 
IPA: /tɔːrk/
Phonetic spelling: tork

  buccal
Pronunciation link: https://www.merriam-webster.com/dictionary/buccal 
IPA: /ˈbʌk.əl/
Phonetic spelling: BUCK-uhl

  lingual
Pronunciation link: https://www.merriam-webster.com/dictionary/lingual 
IPA: /ˈlɪŋ.ɡwəl/
Phonetic spelling: LING-gwuhl

  micrometer
Pronunciation link: https://www.merriam-webster.com/dictionary/micrometer 
IPA: /ˌmaɪ·krəˈmi·t̬ɚ/
Phonetic spelling: my-kroh-MEE-ter

  decontamination
Pronunciation link: https://www.merriam-webster.com/dictionary/decontamination 
IPA: /ˌdiːˌkɑːn·təˈmeɪ·ʃən/
Phonetic spelling: dee-kon-tuh-MAY-shun

  curette
Pronunciation link: https://www.merriam-webster.com/dictionary/curette 
IPA: /kjʊˈrɛt/
Phonetic spelling: kyoo-RET

  apical
Pronunciation link: https://www.merriam-webster.com/dictionary/apical 
IPA: /ˈeɪ.pɪ.kəl/
Phonetic spelling: AY-pih-kuhl

  coronal
Pronunciation link: https://www.merriam-webster.com/dictionary/coronal 
IPA: /ˈkɔːr.ə.nəl/
Phonetic spelling: KOR-uh-nuhl