# Submission ID #: 68126

# Scriptwriter Name: Pallavi Sharma

# Project Page Link: https://review.jove.com/account/file-uploader?src=20778478

Title: Laser Micromachining for Polymer Surface Topography Design

# Authors and Affiliations:

Izidor Straus1#, Gaia Kravanja2#, Luka Hribar2, Raphael Kriegl3, Mikhail Shamonin3, Irena Drevenšek-Olenik1,4, Matija Jezeršek2, Gašper Kokot1,4*

1University of Ljubljana, Faculty of Mathematics and Physics

2University of Ljubljana, Faculty of Mechanical Engineering

3Ostbayerische Technische Hochschule Regensburg

4Jožef Stefan Institute, Department of Complex Matter

#These authors contributed equally to this work

# Corresponding Authors:

Gašper Kokot			(gasper.kokot@ijs.si)

# Email Addresses for All Authors:

Izidor Straus			(izidor.straus@fmf.uni-lj.si)

Gaia Kravanja			(gaia.kravanja@fs.uni-lj.si)

Luka Hribar			(luka.hribar@fs.uni-lj.si)

Raphael Kriegl			(raphael.kriegl@oth-regensburg.de)

Mikhail Shamonin		(mikhail.chamonine@oth-regensburg.de)

Irena Drevenšek-Olenik	(irena.drevensek@ijs.si)

Matija Jezeršek		(matija.jezersek@fs.uni-lj.si)

Gašper Kokot			(gasper.kokot@ijs.si)

## Author Questionnaire

1. Microscopy: Does your protocol require the use of a dissecting or stereomicroscope for performing a complex dissection, microinjection technique, or something similar?  No

2. Software: Does the part of your protocol being filmed include step-by-step descriptions of software usage?  Yes

Authors: Please create screen capture videos of the shots labeled as SCREEN, create a screenshot summary, and upload the files to your project page as soon as possible:https://review.jove.com/account/file-uploader?src=20778478

3. Filming location: Will the filming need to take place in multiple locations?   Yes

1.1 km

Current Protocol Length

Number of Steps:  08

Number of Shots:  28

# Introduction

Videographer: Obtain headshots for all authors available at the filming location.

REQUIRED: What is the scope of your research? What questions are you trying to answer?

  - Gašper Kokot: We are researching new applications and capabilities of laser micromachining. We are working on determining the conditions and parameter space for processing different types of materials.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

What are the current experimental challenges?

  - Gašper Kokot: Currently, our main focus is surfaces of polymers, in particular magnetoactive elastomers, that can be difficult to process using other techniques, due to their stickiness.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera Suggested B-roll: Figure 3

What advantage does your protocol offer compared to other techniques?

  - Gašper Kokot: Our protocol describes a maskless structuring of surfaces, which enables rapid prototyping. It also allows for the creation of slanted structures that are not possible with other techniques.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera

Videographer: Obtain headshots for all authors available at the filming location.

# Protocol

- Laser Micromachining

Demonstrators: Gaia Kravanja and Izidor Straus

  - To begin, place the cured magnetoactive elastomer sample on the working area of the scanning head [1], ensuring it is positioned in the focal plane and tilted to the preselected angle [2]. Using the laser control software, design the scanning trajectory by tracing the area where material should be removed [3].

    - WIDE: Talent positioning the cured magnetoactive elastomer sample on the scanning head.

    - Talent adjusting for focus and tilt.

    - SCREEN: Show the design window where the scanning trajectory is traced over the sample area to form the negative pattern.

Authors: Please create screen capture videos of the shots labeled as SCREEN, create a screenshot summary, and upload the files to your project page as soon as possible: https://review.jove.com/account/file-uploader?src=20778478

  - For optical microscopy, clean the sample using pressurized nitrogen gas to gently blow away any dust or debris particles [1]. Place the cleaned sample on the microscope table and switch on the reflective microscopy light source [2]. Select the 10X  (Time) objective lens to measure lateral dimensions such as the pitch between lamellae [3]. Then, switch to the 40X objective lens to capture data on the height of the structures [4].

    - Talent using a nitrogen gas gun to clean the sample surface.

    - Talent placing the sample on the microscope stage and turning on the reflective light source.

    - SCREEN:: Shot of the sample under 10X objective.

    - Talent rotating the objective turret to switch to the 40X lens and focusing on the sample.

  - Then, open the field aperture on the microscope to reduce the depth of the field [1]. Adjust the height of the micrometer stage [2] to focus on the top surface of the structures [3] and record the reading on the micrometer screw [4].

    - Talent adjusting the field aperture to shallow the depth of field.

    - Talent adjusting the height of the micrometer stage

    - SCREEN:: Shot of the structure top.

    - Talent noting the micrometer screw reading.

  - Afterward, gradually raise the stage by turning the micrometer screw [1] until the substrate surface comes into focus [2], then record this new value [3-TXT].

    - Talent slowly turning the micrometer screw to raise the stage.

    - Shot of the focused substrate.

    - Talent noting the reading. TXT: Calculate height by subtracting the two micrometer readings

- Scanning Electron Microscopy of MAE Sheets

Demonstrator: Izidor Straus

  - Wear gloves and, using a scalpel, cut the samples to match the size of the scanning electron microscopy sample holder pins [1]. With the help of plastic tweezers, attach the trimmed samples to the pins, taking care not to damage them [3]. Then, clean the mounted samples with pressurized nitrogen gas to remove any dust or debris [4]. Place the pins with the attached samples into the stage and record their positions [5].

    - Talent cutting a sample to size using a scalpel.

    - Talent using plastic tweezers to carefully place the trimmed sample onto an SEM pin.

    - Talent cleaning the mounted sample with pressurized nitrogen gas.

    - Talent inserting the pins into the SEM stage and noting down the sample positions.

  - Next, to perform backscattered electron measurements, first evacuate air from the vacuum chamber to reach a high vacuum state [1]. Capture an optical navigation image of the samples and use it to guide the stage, positioning the sample of interest at the correct distance from the detector edge [2]. Activate the electron beam and display the image from the concentric backscatter detector [3]. To set the beam parameters, select a 30-kilovolt accelerating voltage, a spot size of 4.0, and a dwell time of 5 microseconds [4].

    - Talent initiating vacuum pumping on the SEM to achieve high vacuum.

    - SCREEN: Show optical navigation image being captured and the stage moving the sample into position near the detector edge.

    - SCREEN: Show the electron beam activation and display from the concentric backscatter detector.

    - SCREEN: Navigate the SEM software to set beam parameters: 30 kilovolt accelerating voltage, 4.0 spot size, and 5 microsecond dwell time.

  - For secondary electron measurements, adjust the chamber to a low vacuum of 0.70 millibar [1]. Move the samples to a working distance of approximately 3.5 millimeters [2]. Then, switch on the electron beam and view the image captured by the low-vacuum secondary electron detector [3].

    - SCREEN: Show SEM vacuum settings being adjusted to 0.70 millibar.

    - SCREEN: Talent adjusting the sample stage to a 3.5 millimeter working distance.

    - SCREEN: Display the image output from the low-vacuum secondary electron detector after activating the beam.

  - Next, attach a piece of double-sided adhesive tape to the center of the sample holder between the poles of the electromagnet [1]. Place the sample on the adhesive tape, ensuring it is centered between the poles [2]. While capturing images, apply a 3.2 ampere direct current to the electromagnet to generate a homogeneous magnetic field of approximately 340 millitesla in the 20-millimeter pole gap [3].

    - Talent attaching a strip of double-sided adhesive tape to the sample holder between the electromagnet poles.

    - Talent carefully placing the sample atop the adhesive tape in the central position.

    - SCREEN: Show the current control panel applying 3.2 ampere direct current to the electromagnet, with field readout showing 340 millitesla.

# Results

- Results

  - Optical microscopy confirmed the defect-free pattern of the magnetoactive elastomer surface, with clear lateral structuring and focus adjustments validating vertical profile visibility [1]. Scanning electron microscopy revealed that the structured pillars have a coarse surface texture with distinct micro-particles embedded throughout the side profile [2].

    - LAB MEDIA: Figure 3A. Video editor: Highlight the wide view showing evenly spaced vertical ridges with no visible defects.

    - LAB MEDIA: Figure 3B. Video editor: Emphasize the side profile image where the vertical structure is covered in scattered bright micro-particles.

  - Secondary electron imaging revealed a rugged and irregular polymer surface structure at high resolution [1].

    - LAB MEDIA: Figure 3B. Video editor: Highlight the lower image showing wavy, irregular surface patterns in grayscale.

  - Magnetic manipulation resulted in visible tilting of the microstructures over time, as observed in the side views under different field exposures [1].

    - LAB MEDIA: Figure 4. Video editor: Show the side view images with all protrusions.