# Submission ID #: 68185

# Scriptwriter Name: Poornima G

# Project Page Link: https://review.jove.com/account/f  u ile-uploader?src=20796473

# Title: Development of a Microfluidics-Based Approach for Investigating Microtubule Polymer Mechanics

# Authors and Affiliations:

# Matthew Rogers1, Laura Richardson1, Marija Zanic1,2,3

# 1Department of Chemical and Biomolecular Engineering, Vanderbilt University 
2Department of Cell and Developmental Biology, Vanderbilt University 
3Department of Biochemistry, Vanderbilt University

# Corresponding Authors:

# Marija Zanic			marija.zanic@vanderbilt.edu

# Email Addresses for All Authors:

Matthew Rogers		matthew.rogers2@outlook.com

# Laura Richardson		laura.b.richardson@vanderbilt.edu

# Marija Zanic			marija.zanic@vanderbilt.edu

## Author Questionnaire

1. Microscopy: Does your protocol require the use of a dissecting or stereomicroscope for performing a complex dissection, microinjection technique, or something similar?  No

2. Software: Does the part of your protocol being filmed include step-by-step descriptions of software usage?  No

3. Filming location: Will the filming need to take place in multiple locations?   No

Current Protocol Length

Number of Steps:  17

Number of Shots:  31

# Introduction

Videographer: Obtain headshots for all authors available at the filming location.

  - Laura Richardson: Microtubules are cytoskeletal polymers that play essential roles in cell division and intracellular cargo transport. This work adopts microfluidics to investigate the mechanical properties of microtubules in vitro.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B-roll: 2.3.1

What are the current experimental challenges?

  - Laura Richardson: This work addresses two specific limitations in studying microtubules in microfluidic devices: the potential for air bubble formation within the device, which can denature proteins; and the underutilization of high-throughput assays.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B-roll: 4.1.1

What advantage does your protocol offer compared to other techniques?

  - Laura Richardson: Our microfluidic device and protocol allow for a range of experimental setups with more robust, high-throughput testing capabilities than previous flow-cell assays.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B-roll: 5.1.1

Videographer: Obtain headshots for all authors available at the filming location.

# Protocol

- Photolithography to Prime the Silicon Wafer

Demonstrator: Laura Richardson

  - To begin, plasma clean a 3-inch silicon wafer under vacuum for 5 minutes using either oxygen or clean dry air plasma [1]. Ensure that the vacuum pressure is below 5 × 10⁻⁵ torr [2].

    - WIDE: Talent placing the silicon wafer inside the plasma cleaner.

    - Talent setting plasma cleaning parameters.

  - Center the cleaned silicon wafer onto the spin coater for photoresist deposition [1] and deposit 1 to 2 milliliters of SPR 220 7.0 (S-P-R-two twenty- seven-point-Oh) photoresist onto the center of the silicon wafer [2].

    - Talent placing the wafer in the center of the spin coater chuck.

    - Talent using a pipette to drop the photoresist onto the center of the wafer.

  - Spin-coat the photoresist to achieve a 13-micrometer thick layer at 1,000 revolutions per minute for 30 seconds [1].

    - Talent placing the sample in the spin-coater.  TXT: Clean residual photoresist from the coater using acetone

  - While minimizing contact with the coated surface, transfer the silicon wafer to a hot plate set to 70 degrees Celsius [1].  Incubate the silicon wafer on the hot plate, increasing the temperature by 10 degrees Celsius every 3 to 5 minutes until the temperature reaches 115 degrees Celsius [2].

    - Talent using tweezers to gently place the wafer onto the pre-heated hot plate.

    - Talent increasing the temperature setting of the hot plate.

  - Then, turn off the hot plate and allow the silicon wafer to cool until its temperature is below 65 degrees Celsius [1].

    - Talent turning off the hot plate.

  - Using forceps, transfer the cooled wafer to the mask aligner [1]. Load both the silicon wafer and the appropriate photomask into the aligner according to the manufacturer's or site-specific protocols [2].

    - Talent using forceps to move the wafer into the mask aligner.

    - Talent loading photomask and aligning it with the wafer.

  - Now, expose the wafer to ultraviolet radiation with energy of approximately 400 millijoules per square centimeter [1]. Calculate the required exposure time using the formula [2-TXT].

    - Talent placing the sample in a UV chamber.

    - Talent setting the exposure time of the UV chamber.

TXT: Exposure time s= Desired Energy (mJcm2)Lamp Power (mWcm2)

- Wafer Development, Silanization and PDMS Deposition

  - After rehydration and heat-treatment, submerge the wafer in the appropriate developer [1]. Then, gently rinse both sides of the wafer with de-ionized water for 30 seconds [2].

    - Shot of the wafer in the developer.

    - Talent holding the wafer under a DI water stream, rinsing both surfaces.

  - After drying the developed wafer using nitrogen gas [1], transfer it into a desiccator [2].

    - Talent using a nitrogen gas nozzle to dry the wafer.

    - Talent placing the wafer inside a desiccator.

  - Place a small aluminum container in the desiccator [1] and add 1 drop of silane into the aluminum container [2-TXT].

    - Talent placing a small aluminum container inside the desiccator.

    - Talent pipetting a single drop of silane into the aluminum container. TXT: Trichloro(1H, 1H, 2H, 2H-perfluorooctyl) silane

  - After desiccation, pour the mixed and degassed polydimethylsiloxane onto the master mold inside a Petri dish [1-TXT].  Incubate the dish at 65 degrees Celsius overnight to allow PDMS to fully cure [2].

    - Talent pouring PDMS mixture gently into a Petri dish containing the master. TXT: PDMS: Polydimethylsiloxane

    - Talent turning on the incubator and adjusting the settings.

- Polydimethylsiloxane (PDMS) Device Assembly

  - Around the device features, use a scalpel or razor blade to cut out rectangular pieces of PDMS from the master layer [1]. Ensure each piece includes adequate flanking space to allow proper bonding contact and fits a 22 by 22-millimeter glass coverslip [2].

    - Talent cutting along the boundary around device features with a scalpel.

    - Close-up of a rectangular PDMS piece with correct size.

  - Place the PDMS on a spare sacrificial PDMS layer, avoiding hard surfaces [1]. Then, using a clean 1.5-millimeter hole punch, make inlet and outlet holes in each PDMS piece [2].

    - Talent aligning PDMS on another sacrificial PDMS layer..

    - Shot of hole punch pressing into PDMS to create holes.

  - Now, retrieve a 22 by 22-millimeter glass coverslip and clean it using a wipe wetted with isopropyl alcohol [1]. Then, plasma clean the glass coverslip under vacuum for 5 minutes using clean dry air plasma [2].

    - Talent picking up a coverslip and wiping it with an IPA-wetted wipe.

    - Talent placing the cleaned coverslip into the plasma cleaner and starting the cleaning cycle.

  - Wipe both the glass coverslip and the feature side of the PDMS with isopropyl alcohol-wetted wipes [1] before placing both into the plasma cleaner and simultaneously plasma clean them for 30 seconds under vacuum using clean dry air plasma [2].

    - Talent wiping both surfaces with IPA-wetted wipes.

    - Talent placing PDMS and coverslip into the plasma cleaner and starting the cycle.

  - After cleaning, invert the PDMS so its feature side faces downward [1]. Place the PDMS onto the glass coverslip [2] and press lightly to encourage bonding [3].

    - Talent aligning and inverting the PDMS piece.

    - Shot of placing the PDMS over the coverslip.

    - Talent gently pressing the PDMS onto the coverslip.

# Results

- Results

  - Stabilized microtubule extensions were bent by flowing buffer solution perpendicular to their growth direction, demonstrating the capacity to apply directional force within the device [1].

    - LAB MEDIA: Figure 5. Video editor: Mark the bent lines labeled “Stabilized extension” near the “Direction of flow” arrow.

  - Near-surface flow velocity experienced by microtubules was calculated as 92 micrometers per second using simulation and analytical modeling based on the Navier-Stokes equation [1].

    - LAB MEDIA: Figure 6.

  - Computational simulations demonstrated the establishment of stable gradients across the device [1], confirmed experimentally by a fluorescent dye showing predictable concentration patterns [2].

    - LAB MEDIA: Figure 7 Video editor: Highlight left image.

    - LAB MEDIA: Figure 7 Video editor: Highlight right image.

  - Dual-labeled microtubule extensions confirmed gradient-based partitioning, with different fluorescent proteins dominating at distinct spatial zones along the device [1].

    - LAB MEDIA: Figure 8. Video editor: Sequentially Highlight B C D

# Pronunciation Guide:

# 1. Microtubule

# Pronunciation link:
https://www.merriam-webster.com/dictionary/microtubule
IPA: /ˈmaɪ.krəˌtuː.bjuːl/
Phonetic Spelling: mai-kroh-too-byool

# 2. Photolithography

# Pronunciation link:
https://www.merriam-webster.com/dictionary/photolithography
IPA: /ˌfoʊ.t̬oʊ.lɪˈθɑː.grə.fi/
Phonetic Spelling: foh-toh-li-thaa-gruh-fee

# 3. Polydimethylsiloxane (PDMS)

# Pronunciation link:
https://www.howtopronounce.com/polydimethylsiloxane
IPA: /ˌpɒ.liˌdaɪˌmɛ.θəlˈsɪ.ləˌkseɪn/
Phonetic Spelling: pah-lee-dai-meth-uhl-sih-luh-ksayn

# 4. Isopropyl

# Pronunciation link:
https://www.merriam-webster.com/dictionary/isopropyl
IPA: /ˌaɪ.səˈproʊ.pəl/
Phonetic Spelling: eye-suh-proh-puhl

# 5. Navier-Stokes

# Pronunciation link:
https://www.howtopronounce.com/navier-stokes
IPA: /ˈnæv.i.eɪ stoʊks/
Phonetic Spelling: nav-ee-ay stohks

# 6. Desiccator

# Pronunciation link:
https://www.merriam-webster.com/dictionary/desiccator
IPA: /ˈdɛs.ɪˌkeɪ.tɚ/
Phonetic Spelling: deh-sih-kay-ter

# 7. Trichloro(1H, 1H, 2H, 2H-perfluorooctyl) silane

# Pronunciation link:
https://www.howtopronounce.com/trichloro-1h-1h-2h-2h-perfluorooctyl-silane
IPA: /traɪˈklɔː.roʊ pɜːrˈflʊə.roʊˌɑːk.təl ˈsɪ.leɪn/
Phonetic Spelling: try-klor-oh per-floo-roh-ok-til si-layn

# 8. Coverslip

# Pronunciation link:
https://www.merriam-webster.com/dictionary/coverslip
IPA: /ˈkʌv.ɚ.slɪp/
Phonetic Spelling: kuh-ver-slip

# 9. Fluorescent

# Pronunciation link:
https://www.merriam-webster.com/dictionary/fluorescent
IPA: /flʊˈrɛs.ənt/ or /ˌflɔːˈrɛs.ənt/
Phonetic Spelling: floor-ess-uhnt

# 10. Plasma Cleaner

# Pronunciation link:
https://www.howtopronounce.com/plasma-cleaner
IPA: /ˈplæz.mə ˈkliː.nɚ/
Phonetic Spelling: plaz-muh klee-ner

# 11. Degassed

# Pronunciation link:
https://www.howtopronounce.com/degassed
IPA: /diːˈɡæst/
Phonetic Spelling: dee-gast

# 12. Spin Coater

# Pronunciation link:
https://www.howtopronounce.com/spin-coater
IPA: /spɪn ˈkoʊ.tɚ/
Phonetic Spelling: spin koh-ter