# Submission ID #: 68230

# Scriptwriter Name: Sulakshana Karkala

# Project Page Link: https://review.jove.com/account/file-uploader?src=20810198

# Title: Optimized Fabrication Procedure for High-Quality Graphene-Based Moiré Superlattice Devices

# Authors and Affiliations:

# Shuwen Sun, Pablo Jarillo-Herrero

# Department of Physics, Massachusetts Institute of Technology, Cambridge

# Corresponding Authors:

Pablo Jarillo-Herrero	(pjarillo@mit.edu)

# Email Addresses for All Authors:

Shuwen Sun		(shuwen@mit.edu)

Pablo Jarillo-Herrero	(pjarillo@mit.edu)

## Author Questionnaire

1. Microscopy: Does your protocol require the use of a dissecting or stereomicroscope for performing a complex dissection, microinjection technique, or something similar? No

2. Software: Does the part of your protocol being filmed include step-by-step descriptions of software usage?  Yes, all done

3. Filming location: Will the filming need to take place in multiple locations?   No

Current Protocol Length

Number of Steps:  32

Number of Shots:  60

# Introduction

  - Pablo Jarillo-Herrero: Our research is focused on the quantum electronic properties of two-dimensional materials and their heterostructures, aiming to discover and investigate new quantum phenomena and develop novel electronic devices.

    - INTERVIEW: Named Talent says the statement above in an interview-style shot, looking slightly off-camera.

What significant findings have you established in your field?

  - Pablo Jarillo-Herrero: We pioneered the field of “twistronics”, where the properties of 2D materials heterostructures change as a function of the angle between the layers. The most impactful discovery was superconductivity in magic-angle graphene.

    - INTERVIEW: Named Talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B.roll: 2.8

What are the current experimental challenges?

  - Shuwen Sun: Achieving a precise twist angle remains challenging due to heterostrain, disorder, and lattice relaxation introduced during the nanofabrication process, which often lead to device inhomogeneity and limit reproducibility across samples.

    - INTERVIEW: Named Talent says the statement above in an interview-style shot, looking slightly off-camera.

How will your findings advance research in your field?

  - Shuwen Sun: This protocol reflects our experience optimizing each fabrication step to improve uniformity and yield, enabling more researchers to reliably build high-quality graphene moiré devices and accelerate progress in this field.

    - INTERVIEW: Named Talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B.roll:3.4

# Videographer: Obtain headshots for all authors available at the filming location.

# Protocol

- Laser Patterning and Pickup of Top Hexagonal Boron Nitride Layer

Demonstrator: Shuwen Sun

  - To begin, place a graphene wafer on the sample stage of the transfer setup integrated with a supercontinuum laser [1]. Use Peek Through to make the Inkscape window semi-transparent while floating above the camera window [2]. Use the Draw Bezier curves and straight lines function in Inkscape to outline the graphene boundary and the planned laser-cutting lines [3].

    - WIDE: Talent places the graphene wafer on the sample stage.

Added Shot: SCREEN: 68230_2.1-2.3_3.x.mp4	00:11-00:18

    - SCREEN: 68230_2.1-2.3_3.x.mp4	01:54-02:21 .

  - Now power on the laser and increase the intensity until the beam spot is visible [1]. Adjust the sample stage to align the beam spot with the start of a planned laser-cutting line [2-TXT].

    - Talent switching on the laser and gradually increasing intensity.
AND
SCREEN: 68230_2.1-2.3_3.x.mp4	02:58-03:08 
Video Editor: Please play both shots side by side

    - Talent adjusting the stage so the laser spot aligns with the beginning of a cutting line. TXT: Adjust laser intensity to suitable level
AND
SCREEN: 68230_2.1-2.3_3.x.mp4	03:26-03:29 
Video Editor: Please play both shots side by side

  - Next, move the sample stage to guide the beam spot along the planned laser-cutting line [1]. After zeroing the laser intensity, inspect the laser-cutting line [2-TXT].

    - Talent guiding the stage to trace along the laser-cutting path.
AUTHOR’S NOTE: Taken as 2 shots

    - SCREEN: 68230_2.1-2.3_3.x.mp4	03:37-03:51 TXT: Repeat steps until all planned lines are laser cut

  - To pickup the top hexagonal boron nitride flake, adjust the orientation of the flake until the straight edge is vertical and positioned on the right side [1-TXT].

    - SCREEN : 68230_2.4-2.10.mp4	00:00-00:19. TXT: Outline flake boundary in Inkscape

  - Gently clamp the glass slide with the PC/PDMS (P-C-and-P-D-M-S) stamp inside the socket at a downward tilt angle of 2 to 3 degrees [1]. Slide the socket to the left using the sliding tray until the glass slide is positioned above the sample wafer then manually lock it in place [2].

    - Talent clamping the glass slide into the socket at a tilt. TXT: PC/PDMS: polycarbonate/Polydimethylsiloxane

    - Shot of the socket being slide to the left and locked.

  - After setting the sample stage temperature to 50 degrees Celsius, engage the glass slide downward using the Z direction actuator [1-TXT]. Focus the microscope on the polycarbonate film and inspect the surface cleanness [2].

    - Talent engaging the actuator to lower the stamp. TXT: Speed: 1 mm/s until stamp is 2 mm above wafer

    - SCREEN: 68230_2.4-2.10.mp4	01:27-01:31

  - Move the hexagonal boron nitride flake to the selected clean region and engage the slide further downward [1-TXT]. When the polycarbonate film and wafer are nearly in the same focal plane, reduce the speed to 5 micrometers per second [2].

    - SCREEN: 68230_2.4-2.10.mp4		02:06-02:30 TXT: Slide speed: 0.1 mm/s. Reduce to 5 µm/s when the polycarbonate film and wafer are nearly in the same focal plane

    - SCOPE/SCREEN: Talent adjusting the speed and continuing to engage slowly.
NOTE: Shot deleted by authors

  - Now engage the stamp onto the wafer with a speed of 5 micrometers per second until it completely covers the hexagonal boron nitride flake [1]. Then set the sample stage temperature to 80 degrees Celsius [2].

    - SCREEN: 68230_2.4-2.10.mp4		03:15-03:32.

    - Talent adjusting the stage temperature to 80 degrees Celsius.

  - After the sample stage temperature reaches 80 degrees Celsius, disengage the stamp with 5 micrometers per second until the wavefront is close to the hexagonal boron nitride straight edge then pick up the flake with a reduced speed of 2 micrometers per second [1].

    - Shot of the sample stage temperature reaching 80 degrees Celsius
AND
SCREEN: 68230_2.4-2.10.mp4		04:02-05:00. 
Video Editor: Please play both shots side by side

  - Once picked up, increase the speed to 5 micrometers per second to detach the polycarbonate film from the wafer [1]. Switch off the stage heater and open the water-cooling system [2].

    - SCREEN: 68230_2.4-2.10.mp4		05:10-05:20.

    - Talent turning off the heater and turning on the water cooling system.

  - When the temperature drops below 45 degrees Celsius, close the water-cooling system [1]. Disengage the glass slide all the way up at 1 millimeter per second [2].

    - Talent closing the water-cooling system.

    - Shot of the glass slide being disengaged.

- Picking up the Graphene Moiré Superlattice

  - Place the wafer with the freshly laser-cut graphene on the sample stage and locate the graphene using the 10X objective [1]. Adjust the flake orientation so the laser cutting lines are parallel to the hexagonal boron nitride straight edge [2].

    - SCOPE/SCREEN: 68230_2.1-2.3_3.x.mp4	06:28-06:47.

    - SCOPE/SCREEN: 68230_2.1-2.3_3.x.mp4	06:47-07:01.

  - Outline the graphene boundary in Inkscape, including the laser-cutting lines [1]. Use Peek Through to make the drawing semi-transparent while floating above the camera window [2].

    - SCREEN: 68230_2.1-2.3_3.x.mp4	07:05 
Video Editor: Please freeze frame here .

    - SCREEN: Peek Through is being used to make the drawing semi-transparent.
NOTE: Shot deleted by Authors

  - Now, move the glass slide with the top hexagonal boron nitride flake to the pre-engage position with the PC/PDMS stamp 2 millimeters above the graphene wafer [1]. Align the flake’s straight edge with the center of the laser-cut line to match the hexagonal boron nitride with the graphene drawing [2]. Tune the microscope to focus on the graphene and align it to its Inkscape drawing [3].

    - Shot of the glass slide being moved to the pre-engage position with the top flake above the wafer.

    - SCREEN: 68230_2.1-2.3_3.x.mp4	08:22-08:35	.

    - SCREEN: 68230_2.1-2.3_3.x.mp4	08:45-08:54.

  - Then, focus on the top flake and move the glass slide in XY (X-Y) direction to align it to its drawing [1]. After refocusing on a focal plane slightly higher than the pre-cut graphene, engage the glass slide downward at 0.1 millimeter per second until the top flake comes into focus [2].

    - SCREEN: 68230_2.1-2.3_3.x.mp4	09:07-09:19.

    - SCREEN: 68230_2.1-2.3_3.x.mp4	09:38-09:55

  - Refocus on the graphene and set the speed to 5 micrometers per second [1]. Engage the stamp slowly until the flake becomes roughly visible while ensuring no contact with the wafer [2-TXT]. Continue to engage the stamp downward until it contacts the wafer [3].

    - SCOPE/SCREEN: 68230_2.1-2.3_3.x.mp4	10:13-10:25

    - SCOPE/SCREEN: 68230_2.1-2.3_3.x.mp4	10:30-10:54. TXT: Realign both the graphene and hBN to their drawings

    - SCOPE/SCREEN: 68230_2.1-2.3_3.x.mp4	11:21-11:38.

  - Engage the stamp at 0.5 micrometers per second until the wavefront is close to the left edge of the flake [1]. Reduce the speed to 0.02 micrometers per second and continue engagement to contact the first graphene piece [2].

    - SCOPE/SCREEN: 68230_2.1-2.3_3.x.mp4	11:47-12:09.

    - SCOPE/SCREEN: 68230_2.1-2.3_3.x.mp4	12:09-12:20,15:58-16:14 .

  - Once the flake fully covers the first graphene piece and is pinned at the straight edge, stop the engagement [1]. Clear hysteresis by moving the stage upward at 5 micrometers per second until the wavefront starts retracting [2].

    - SCOPE/SCREEN: 68230_2.1-2.3_3.x.mp4	20:40-21:03

    - SCOPE/SCREEN: 68230_2.1-2.3_3.x.mp4	21:03-21:16

  - Set a disengaging speed of 0.02 micrometers per second to pick up the graphene gently [1]. When the wavefront moved away from the flake, increase the speed to 5 micrometers per second to fully detach the stamp from the wafer [2].

    - SCOPE/SCREEN: 68230_2.1-2.3_3.x.mp4	21:22-21:45 .

    - SCOPE/SCREEN: 68230_2.1-2.3_3.x.mp4	41:07-41:32

  - Now copy the entire graphene drawing in Inkscape and rotate it by the desired twist angle [1].

    - SCREEN: 68230_2.1-2.3_3.x.mp4	41:53-42:15
Video Editor: Please speed up the video .

  - Align the second graphene piece in the copied drawing with the first piece in the original drawing to maximize overlap [1-TXT]. Align the remaining graphene on the wafer to the copied drawing [2].

    - SCREEN: 68230_2.1-2.3_3.x.mp4	42:25-42:38 TXT: Rotate sample by desired twist angle .

    - SCOPE/SCREEN: 68230_2.1-2.3_3.x.mp4	43:12-43:22.

  - Focus on the top hexagonal boron nitride flake on the glass slide and align it to the drawing [1-TXT].

    - SCOPE/SCREEN: 68230_2.1-2.3_3.x.mp4	43:28-43:50	. TXT: Examine quality of top stack under microscope then repeat steps with remaining graphene

  - After aligning the flakes to the drawings, repeat the demonstrated steps to pick up the remaining graphene [1]. Once picked up, examine the quality of top stack under microscope [2].
NOTE: Step is a repetition of demonstrated procedure. It has been converted to on-screen text

    - SCOPE/SCREEN: 68230_2.1-2.3_3.x.mp4	44:42-1:12:03.

    - SCOPE/SCREEN68230_2.1-2.3_3.x.mp4	.

- Encapsulation of the Graphene Moiré Superlattice

  - Place the wafer with the pre-cleaned bubble-free bottom gate on the sample stage [1]. Outline the boundary of the bottom gate using Inkscape [2]. Align the drawing of the top stack to that of the bottom gate to place the twisted bilayer graphene on the graphite finger [3].

    - Talent positioning the wafer with bottom gate on the stage.

    - SCREEN: 68230_4.x.mp4	00:18-00:40, 01:12-01:17 
Video Editor: Please speed up the video .

Added shot SCREEN: 68230_4.x.mp4		01:32-01:50

  - Set the sample stage temperature to 160 degrees Celsius to tear off the polycarbonate film after encapsulation [1]. Then load the glass slide with the top stack and move it to the pre-engage position [2]. Roughly align both the bottom gate and the top stack to the drawings [3].

    - Talent setting the stage heater to 160 degrees Celsius.

    - Talent loading the glass slide with the top stack and moving it to the pre-engage position.

    - SCREEN: 68230_4.x.mp4		03:41-03:56, 04:02-04:12 .

  - Focus on the bottom gate, then slightly raise the focal plane [1-TXT].

    - SCREEN: 68230_4.x.mp4	04:26-04:43		  TXT: Engage slide downward at 0.1 mm/s until top stack becomes visible

  - Identify another middle focal plane between the bottom gate and top stack [1]. Then set the speed to 5 micrometers per second and engage the stamp until the top stack is visible [2]. Align both to the drawings accurately [3-TXT].

    - SCREEN: 68230_4.x.mp4	05:03-05:08	.

    - SCREEN: 68230_4.x.mp4	05:09-05:49	
Video Editor: Please speed up the video .

SCREEN: 68230_4.x.mp4	05:50-06:08 . TXT: Repeat until bottom gate and top stack are almost in the same focal plane, and the sample stage temperature > 150 °C

  - When the sample stage is above 150 degrees Celsius, engage the stamp at 5 micrometers per second until the wave front is close to the bottom gate, then reduce the speed to 0.5 micrometers per second [1].

    - SCREEN: 68230_4.x.mp4	08:09-08:21.

  - Slowly engage the top stack onto the bottom gate [1]. Once the wavefront passes the top stack, increase the speed back to 5 micrometers per second to fully engage the stamp onto the wafer [2-TXT]. Then disengage the stamp at 5 micrometers per second [3-TXT].

    - SCREEN: 68230_4.x.mp4	08:43-08:55.

    - SCREEN: 68230_4.x.mp4	09:07-09:40 TXT: Wait for 1 min to soften PC film

    - SCREEN: 68230_4.x.mp4	10:53-11:09. TXT: The retracting wavefront denotes the detachment between the PC film and PDMS stamp

  - After fully separating the stamp from the wafer, lift the stamp upward for 3 seconds at 5 micrometers per second [1]. Begin moving it in the X-Y directions to tear off the polycarbonate film [2].

    - SCREEN: 68230_4.x.mp4	11:11-11:16

    - SCREEN: 68230_4.x.mp4	11:23-11:48.

  - Fully disengage the glass slide at 1 millimeter per second and remove it from the socket [1]. Switch off the stage heater and activate the water-cooling system [2].

    - Talent lifting and removing glass slide.

    - Talent switching off heater and activating cooling.

  - Once the temperature drops to room temperature, remove the wafer and inspect under an optical microscope [1].

    - Talent transferring the wafer to a microscope.

# Results

- Results

  - Four-fold degenerate Landau fans emerged from both the charge neutrality point and superlattice gaps in the high-quality magic-angle twisted bilayer graphene device [1], breaking down into two-fold or one-fold degeneracies at higher magnetic fields [2].

    - LAB MEDIA: Figure 8A. Video editor: Highlight the symmetrical red-and-blue striped patterns radiating between 0 to 3

    - LAB MEDIA: Figure 8A. Video editor: please highlight the area of the graph at 3 and 4

  - Symmetry-broken two-fold degenerate Landau fans were identified at half-filling states indicating correlated insulating behavior [1]. The superconducting dome was located underneath the Landau fan around the half-filling state [2].

    - LAB MEDIA: Figure 8A. Video editor: please highlight the area at ±2

    - LAB MEDIA: Figure 8A. Video editor: please highlight the low-field area at -2

  - Temperature-dependent resistance measurements revealed two superconducting domes at both sides of the half-filling state with the maximum critical temperature reaching approximately 1.7 Kelvin [1].

    - LAB MEDIA: Figure 8B. Video editor: please highlight the dotted area

  - Among 14 measured devices, the optimal critical temperature peaked at a twist angle near 1.08 degrees, consistent with theoretical predictions [1].

    - LAB MEDIA: Figure 8C. Video editor: Focus on the tallest data point in the plot

  - Disordered devices near the magic angle exhibited significantly reduced critical temperatures compared to high-quality devices [1], as seen in their resistance versus temperature profiles [2].

    - LAB MEDIA: Figure 8C. Video editor: Please highlight the two green data points

    - LAB MEDIA: Figure 8D. Video editor: Please highlight the orange and pink curves

- Pronunciation Guide:
Moiré

  - Pronunciation link: https://www.merriam-webster.com/dictionary/moire

  - IPA: /mwɑːˈreɪ/

  - Phonetic Spelling: mwah-ray

- Superlattice

  - Pronunciation link: https://www.howtopronounce.com/superlattice

  - IPA: /ˌsuː.pɚˈlæt.ɪs/

  - Phonetic Spelling: soo-per-lat-iss

- Graphene

  - Pronunciation link: https://www.merriam-webster.com/dictionary/graphene

  - IPA: /ˈɡræˌfiːn/

  - Phonetic Spelling: gra-feen

- Heterostructure

  - Pronunciation link: https://www.howtopronounce.com/heterostructure

  - IPA: /ˈhɛt̬.ə.roʊˌstrʌk.tʃɚ/

  - Phonetic Spelling: heh-tuh-roh-struhk-chur

- Twistronics

  - Pronunciation link: https://www.howtopronounce.com/twistronics

  - IPA: /twɪsˈtrɑː.nɪks/

  - Phonetic Spelling: twis-trah-niks

- Hexagonal Boron Nitride

  - Pronunciation links:

    - Hexagonal: https://www.merriam-webster.com/dictionary/hexagonal

    - Boron: https://www.merriam-webster.com/dictionary/boron

    - Nitride: https://www.merriam-webster.com/dictionary/nitride

  - IPA: /hɛkˈsæɡənl ˈbɔːrɑːn ˈnaɪˌtraɪd/

  - Phonetic Spelling: hek-sag-uh-nuhl bore-on nye-tride

- Polydimethylsiloxane (PDMS)

  - Pronunciation link: https://www.howtopronounce.com/polydimethylsiloxane

  - IPA: /ˌpɑː.li.daɪˌmɛ.θəlˈsɪ.lɑːk.seɪn/

  - Phonetic Spelling: pah-lee-dye-meth-uhl-sih-lock-sayn

- Polycarbonate

  - Pronunciation link: https://www.merriam-webster.com/dictionary/polycarbonate

  - IPA: /ˌpɑː.liˈkɑːr.bə.neɪt/

  - Phonetic Spelling: pah-lee-kar-buh-nayt

- Landau

  - Pronunciation link: https://www.howtopronounce.com/landau

  - IPA: /ˈlæn.daʊ/

  - Phonetic Spelling: lan-dow

- Inkscape

  - Pronunciation link: https://www.howtopronounce.com/inkscape

  - IPA: /ˈɪŋk.skeɪp/

  - Phonetic Spelling: ing-skayp

- Degenerate

  - Pronunciation link: https://www.merriam-webster.com/dictionary/degenerate

  - IPA: /dɪˈdʒenərət/

  - Phonetic Spelling: dih-jen-uh-ruht

- Heterostrain

  - Pronunciation link: No confirmed link found

  - IPA: /ˈhɛt̬.ə.roʊ.streɪn/

  - Phonetic Spelling: heh-tuh-roh-strayn

- Nanofabrication

  - Pronunciation link: https://www.howtopronounce.com/nanofabrication

  - IPA: /ˌnæn.oʊˌfæb.rɪˈkeɪ.ʃən/

  - Phonetic Spelling: nan-oh-fab-ri-kay-shun

- Cryogenic

  - Pronunciation link: https://www.merriam-webster.com/dictionary/cryogenic

  - IPA: /ˌkraɪ.oʊˈdʒɛn.ɪk/

  - Phonetic Spelling: kry-oh-jen-ik

- Superconductivity

  - Pronunciation link: https://www.merriam-webster.com/dictionary/superconductivity

  - IPA: /ˌsuː.pɚ.kənˌdʌkˈtɪ.və.ti/

  - Phonetic Spelling: soo-per-kuhn-duhk-tiv-uh-tee