# Submission ID #: 68230

# Scriptwriter Name: Sulakshana Karkala

# Project Page Link: https://review.jove.com/account/file-uploader?src=20810198

# Title: Optimized Fabrication Procedure for High-Quality Graphene-Based Moiré Superlattice Devices

# Authors and Affiliations:

# Shuwen Sun, Pablo Jarillo-Herrero

# Department of Physics, Massachusetts Institute of Technology, Cambridge

☐   All author names and affiliations are correct (city/state/country information not included in video title page).

# Corresponding Authors:

Pablo Jarillo-Herrero	(pjarillo@mit.edu)

# Email Addresses for All Authors:

Shuwen Sun		(shuwen@mit.edu)

Pablo Jarillo-Herrero	(pjarillo@mit.edu)

## Author Questionnaire

1. Microscopy: Does your protocol require the use of a dissecting or stereomicroscope for performing a complex dissection, microinjection technique, or something similar?  Enter Yes or No.

If Yes, can you record movies/images using your own microscope camera?

Enter Yes or No.

If your protocol involves microscopy but you are not able to record movies/images with your microscope camera, JoVE will need to use our SCOPE kit.

If your microscope does not have a camera port, the SCOPE kit will be attached to one of the eyepieces and you will have to perform the procedure using one eye.

Enter make and model of microscope.

If a dissection or stereo microscope is required for your protocol, please list all shots from the script that will be visualized using the microscope (shots are indicated with the 3-digit numbers, like 2.1.1, 2.1.2, etc.).

Click here to list microSCOPE/SCREEN shots, using the shot numbers from the protocol section of the video script.

2. Software: Does the part of your protocol being filmed include step-by-step descriptions of software usage?  Enter Yes or No.

If Yes, we will need you to record using screen recording software.

We recommend using the screen capture program OBS. JoVE’s tutorial for using OBS Studio is provided at this link: https://review.jove.com/v/5848/screen-capture-instructions-for-authors?status=a7854k

As these files are necessary for finalizing your script, please upload all screen-captured video files to your project page as soon as possible.

3. Filming location: Will the filming need to take place in multiple locations?   Enter Yes or No.

If Yes, how far apart are the locations? Click to enter distance between locations.

To ensure that your script can be filmed in one day, the protocol sections are cumulatively restricted to 55 shots (shots are the 3-digit numbers like 2.1.1, 2.1.2…etc)

Current Protocol Length

Number of Steps:  32

Number of Shots:  60

# Introduction

Videographer: Obtain headshots for all authors available at the filming location.

Answers to these questions will become interview statements that you will deliver on camera.

- Answer the 1st REQUIRED question and at least 2 other questions (1.2 – 1.10) below. Up to 5 interview statements will be included in the video.

- Enter the full name of the author who will deliver the statement.

- If possible, each author should deliver no more than two statements.

- Answer in full sentences, in a style suitable for being spoken aloud.

- Limit the length of each statement to 30 words or fewer.

- Answers will be edited for length, clarity, and consistency with journal style guidelines.

REQUIRED: What is the SCOPE of your research? What questions are you trying to answer?

  - Enter author name.: Click here to answer question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

What are the most recent developments in your field of research?

  - Enter author name: Click here to answer question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

What technologies are currently used to advance research in your field?

  - Enter author name: Click here to answer question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

What are the current experimental challenges?

  - Enter author name: Click here to answer question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

What significant findings have you established in your field?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

What research gap are you addressing with your protocol?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

What advantage does your protocol offer compared to other techniques?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

How will your findings advance research in your field?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

What new scientific questions have your results paved the way for?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

What research questions will your laboratory focus on in the future?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

Videographer: Obtain headshots for all authors available at the filming location.

# Testimonial Questions (OPTIONAL):

Answers to these questions will not appear in the video but may be featured in our journal's promotional materials.

- Enter the full name of the author who will deliver the statement.

- Answer in full sentences, in a style suitable for being spoken aloud.

- Answers will be mildly edited for clarity.

- Limit the length of each statement to 50 words or fewer.

How do you think publishing with JoVE will enhance the visibility and impact of your research?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 50 or fewer words.

Can you share a specific success story or benefit you’ve experienced—or expect to experience—after using or publishing with JoVE? (This could include increased collaborations, citations, funding opportunities, streamlined lab procedures, reduced training time, cost savings in the lab, or improved lab productivity.)

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 50 or fewer words.

# Protocol

Please review this section to make sure that it accurately describes your protocol. Use Track Changes when making edits or revisions.

- The two-digit steps (e.g., 2.1., 2.2.) are the narration.  JoVE is responsible for the narration of the protocol and results.

- Red italics are pronunciation guides indicating how the word will be spoken.

- Filming should take no more than 10 minutes per step. If a step takes more than 10 minutes, prepare the product for that step in advance.

- The three-digit shots (e.g., 2.1.1., 2.2.2.) are the actions that the videographer will capture.

- Laser Patterning and Pickup of Top Hexagonal Boron Nitride Layer

Demonstrator: Click here to enter name of demonstrator(s)

If the same person is the demonstrator throughout, mention them once here and remove the "Demonstrator" field from the other sections; if the demonstrator changes, retain the field in the respective sections.

AUTHORS: Please specify which shots will require the use of a microscope by placing “SCOPE” in front of the shot. Similarly identify the SCREEN capture shots with “SCREEN”

  - To begin, place a glass slide with a graphene wafer on the sample stage of an integrated laser instrument [1]. Use the Draw Bezier curves and straight lines function in Inkscape to outline the graphene boundary and the planned laser-cutting lines [2].
Authors: Please create screen capture videos of the shots labeled as SCREEN, create a screenshot summary, and upload the files to your project page as soon as possible: https://review.jove.com/account/file-uploader?src=20810198

    - WIDE: Talent places the graphene wafer on the sample stage.

    - SCREEN: The Draw Bezier curves and straight lines function is being used to outline the graphene boundary and planned laser cutting lines.

  - Now power on the laser and increase the intensity until the beam spot is visible [1]. Adjust the sample stage to align the beam spot with the start of a planned laser-cutting line [2-TXT].

    - Talent switching on the laser and gradually increasing intensity.

    - Talent adjusting the stage so the laser spot aligns with the beginning of a cutting line. TXT: Adjust laser intensity to suitable level

  - Next, move the sample stage to guide the beam spot along the planned laser-cutting line [1]. After zeroing the laser intensity, inspect the laser-cutting line [2].

    - Talent guiding the stage to trace along the laser-cutting path.

    - Shot of the flake showing the cut line.

  - To pickup the top hexagonal boron nitride flake, adjust the orientation of the flake until the straight edge is vertical and positioned on the right side [1-TXT].

    - SCREEN: The flake orientation is being adjusted until the straight edge is vertical and positioned on the right side. TXT: Outline flake boundary in Inkscape

  - Gently clamp the glass slide with the PC/PDMS (P-C-or-P-D-M-S) stamp inside the socket at a downward tilt angle of 2 to 3 degrees [1]. Slide the socket to the left using the sliding tray until the glass slide is positioned above the sample wafer then manually lock it in place [2].

    - Talent clamping the glass slide into the socket at a tilt. TXT: PC/PDMS: polycarbonate/Polydimethylsiloxane

    - Shot of the socket being slide to the left and locked.

  - After setting the sample stage temperature to 50 degrees Celsius, engage the glass slide downward using the Z direction actuator [1-TXT]. Focus the microscope on the polycarbonate film and inspect the surface cleanness [2].

    - Talent engaging the actuator to lower the stamp. TXT: Speed: 1 mm/s until stamp is 2 mm above wafer

    - SCOPE/SCREEN: View of the polycarbonate surface.

  - Move the hexagonal boron nitride flake to the selected clean region and engage the slide further downward [1-TXT]. When the polycarbonate film and wafer are nearly in the same focal plane, reduce the speed to 5 micrometers per second [2].

    - SCOPE/SCREEN: The flake is being positioned over the clean surface region. TXT: Slide speed: 0.1 mm/s

    - Talent adjusting the speed and continuing to engage slowly.

  - Now engage the stamp onto the wafer with a speed of 5 micrometers per second until it completely covers the hexagonal boron nitride flake [1]. Then set the sample stage temperature to 80 degrees Celsius [2].

    - SCOPE/SCREEN: The stamp is being engaged until contact.

    - Talent adjusting the stage temperature to 80 degrees Celsius.

  - After the temperature is reached, disengage the stamp with 5 micrometers per second until the wavefront is close to the hexagonal boron nitride straight edge then pick up the flake [1-TXT].

    - Talent slowly disengaging the stamp near the hBN straight edge. TXT: Reduce speed to 2 µm/s to pick up the hBN flake

  - Once picked up, increase the speed to 5 micrometers per second to detach the polycarbonate film from the wafer [1]. Switch off the stage heater and open the water-cooling system [2].

    - SCOPE/SCREEN: Shot of the polycarbonate film detaching from wafer.

    - Talent turning off the heater and turning on the water cooling system.

  - When the temperature drops below 45 degrees Celsius, close the water-cooling system [1].  Disengage the glass slide all the way up at 1 millimeter per second [2].

    - Talent closing the water-cooling system.

    - SCREEN: The glass slide is being disengaged.

- Picking up the Graphene Moiré Superlattice

Demonstrator: Click here to enter name of demonstrator(s)

  - Place the wafer with the freshly laser-cut graphene on the sample stage and locate the graphene using the 10X objective [1]. Adjust the flake orientation so the laser cutting lines are parallel to the hexagonal boron nitride straight edge [2].

    - SCOPE/SCREEN: View through 10x objective showing graphene flake.

    - SCOPE/SCREEN: The flake is being rotated until laser lines are parallel to the hBN edge.

  - Outline the graphene boundary in Inkscape, including the laser-cutting lines [1]. Use Peek Through to make the drawing semi-transparent while floating above the camera window [2].

    - SCREEN: Inkscape window showing boundary being traced with Bezier tool.

    - SCREEN: Peek Through is being used to make the drawing semi-transparent.

  - Now, move the glass slide with the top hexagonal boron nitride flake to the pre-engage position with the PC/PDMS stamp 2 millimeters above the graphene wafer [1]. Place the flake straight edge in the middle of the laser-cutting line that separates the central graphene pieces to align it with the graphene drawings [2]. Tune the microscope to focus on the graphene and align it to its Inkscape drawing [3].

    - SCOPE/SCREEN: The glass slide is being moved to the pre-engage position with the top flake above the wafer.

    - SCOPE/SCREEN: Overlay alignment in Inkscape with hBN edge centered on laser-cut line.

    - SCOPE/SCREEN: View aligning real graphene with drawing.

  - Then, focus on the top flake and move the glass slide in XY (X-Y) direction to align it to its drawing [1]. After refocusing on the pre-cut graphene, engage the glass slide downward at 0.1 millimeter per second until the top flake comes into focus [2].

    - SCOPE/SCREEN: The top flake is being focused and the glass slide is being moved in the XY direction.

    - SCOPE/SCREEN: The slide is being engaged downward until hBN comes into focus.

  - Refocus on the graphene and set the speed to 5 micrometers per second [1]. Engage the stamp slowly until the flake becomes roughly visible while ensuring no contact with the wafer [2-TXT]. Continue to engage the stamp downward until it contacts the wafer [3].

    - SCOPE/SCREEN: The focus is being adjusted on the graphene and the speed is being adjuted.

    - SCOPE/SCREEN: The stamp is being lowered until the flake is roughly visible. TXT: Realign both the graphene and hBN to their drawings

    - SCOPE/SCREEN: The stamp is being lowered until it contacts the wafer.

  - To use a mechanical method without hysteresis, engage the stamp at 5 micrometers per second until the wavefront is close to the left edge of the flake [1]. Reduce the speed to 0.02 micrometers per second and continue engagement to contact the first graphene piece [2].

    - SCOPE/SCREEN: The stamp is being lowered until the wavefront is close to the left edge of the flake.

    - SCOPE/SCREEN: The stamp is lowered until it contacts the first graphene piece.

  - Once the flake fully covers the first graphene piece and is pinned at the straight edge, stop the engagement [1]. Clear hysteresis by moving the stage upward at 5 micrometers per second until the wavefront starts retracting [2].

    - SCOPE/SCREEN: View showing hBN flake covering graphene.

    - SCOPE/SCREEN: The stage is being moved upward until the wavefront starts retracting.

  - Set a disengaging speed of 0.02 micrometers per second to pick up the graphene gently [1]. When the wavefront moved away from the flake, increase the speed to 5 micrometers per second to fully detach the stamp from the wafer [2].

    - Talent starting disengagement at low speed.

    - SCOPE/SCREEN: Shot of the stamp fully detaching from the wafer.

  - Now copy the entire graphene drawing in Inkscape and rotate it by the desired twist angle [1].

    - SCREEN: Graphene drawing being copied into Inkscape and rotated.

  - Align the second graphene piece in the copied drawing with the first piece in the original drawing to maximize overlap [1-TXT]. Align the remaining graphene on the wafer to the copied drawing [2].

    - SCREEN: Drawings are being overlaid to show graphene overlap. TXT: Rotate sample stage by desired twist angle

    - SCOPE/SCREEN: Graphene on wafer is being aligned to rotated drawing.

  - Focus on the top hexagonal boron nitride flake on the glass slide and align it to the drawing [1-TXT].

    - SCOPE/SCREEN: The flake is being focused and aligned with the drawing. TXT: Examine quality of top stack under microscope

- Encapsulation of the Graphene Moiré Superlattice

Demonstrator: Click here to enter name of demonstrator(s)

  - Place the wafer with the pre-cleaned bubble-free bottom gate on the sample stage [1]. Outline the boundary of the bottom gate using Inkscape [2].

    - Talent positioning the wafer with bottom gate on the stage.

    - SCREEN: Inkscape window showing boundary traced with Bezier tool.

  - Set the sample stage temperature to 160 degrees Celsius to tear off the polycarbonate film after encapsulation [1]. Then load the glass slide with the top stack and move it to the pre-engage position [2]. Roughly align both the bottom gate and the top stack to the drawings [3].

    - Talent setting the stage heater to 160 degrees Celsius.

    - Talent loading the glass slide with the top stack and moving it to the pre-engage position.

    - SCREEN: Overlay alignment of top stack and bottom gate.

  - Focus on the bottom gate, then slightly raise the focal plane [1-TXT].

    - SCREEN: The bottom gate is being focused and the focal plane is being slightly raised.  TXT: Engage slide downward at 0.1 mm/s until top stack becomes visible

  - Identify another middle focal plane between the bottom gate and top stack [1]. Then set the speed to 5 micrometers per second and engage the stamp until the top stack is visible [2-TXT]. Align both to the drawings accurately [3].

    - SCREEN: Another middle focal plane between the bottom gate and top stack is being located.

    - SCREEN: Stamp is being engaged until stack appears. TXT: Keep aligning until bottom gate and top stack are in the same focal plane

    - SCREEN: Bottom gate and top stack are being aligned to the drawings.

  - Now engage the stamp at 5 micrometers per second until it contacts the wafer then reduce the speed to 0.5 micrometers per second [1].

    - SCREEN: The stamp is being lowered until it contacts the wafer then its speed is being reduced.

  - Slowly engage the top stack onto the bottom gate [1]. Once the wavefront passes the top stack, increase the speed back to 5 micrometers per second to fully engage the stamp onto the wafer [2-TXT]. Then disengage the stamp at 5 micrometers per second [3].

    - SCREEN: The top stack is being engaged onto the bottom gate.

    - SCREEN: The entire stamp is being engaged onto the wafer at 5 µm/s. TXT: Wait for 1 min to soften PC film

    - SCREEN: The stamp is being retracted at 5 µm/s

  - Lift the stamp upward for 3 seconds at 5 micrometers per second [1]. Begin moving it to tear off the polycarbonate film [2].

    - SCREEN: The stamp is being lifted.

    - SCREEN: The stamp is being used to detach PC film.

  - Fully disengage the glass slide at 1 millimeter per second and remove it from the socket [1]. Switch off the stage heater and activate the water-cooling system [2].

    - Talent lifting and removing glass slide.

    - Talent switching off heater and activating cooling.

  - Once the temperature drops to room temperature, remove the wafer and inspect under an optical microscope [1].

    - Talent transferring the wafer to a microscope.

# Results

Please review this section to make sure that it accurately reflects your findings.

- This section will not be recorded by the videographer. It only includes the figures/tables from your manuscript (called LAB MEDIA).

- Use Track Changes when making edits or revisions. Ensure the voiceover length is below 200 words. Current word count: 139

- Please note that the video cannot include voiceover without an accompanying visual.

# AUTHORS:  Please confirm that the results have been accurately summarized

- Results

  - Four-fold degenerate Landau fans emerged from both the charge neutrality point and superlattice gaps in the high-quality magic-angle twisted bilayer graphene device [1], breaking down into two-fold or one-fold degeneracies at higher magnetic fields [2].

    - LAB MEDIA: Figure 8A. Video editor: Highlight the symmetrical red-and-blue striped patterns radiating between 0 to 3

    - LAB MEDIA: Figure 8A. Video editor: please highlight the area of the graph at 3 and 4

  - Symmetry-broken two-fold degenerate Landau fans were identified at half-filling states indicating correlated insulating behavior [1]. The superconducting dome was located underneath the Landau fan around the half-filling state [2].

    - LAB MEDIA: Figure 8A. Video editor: please highlight the area at +2

    - LAB MEDIA: Figure 8A. Video editor: please highlight the area at -2

  - Temperature-dependent resistance measurements revealed two superconducting domes at both sides of the half-filling state with the maximum critical temperature reaching approximately 1.7 kelvin [1].

    - LAB MEDIA: Figure 8B. Video editor: please highlight the dotted area

  - Among 14 measured devices, the optimal critical temperature peaked at a twist angle near 1.08 degrees, consistent with theoretical predictions [1].

    - LAB MEDIA: Figure 8C. Video editor: Focus on the tallest data point in the plot

  - Disordered devices near the magic angle exhibited significantly reduced critical temperatures compared to high-quality devices [1], as seen in their resistance versus temperature profiles [2].

    - LAB MEDIA: Figure 8C. Video editor: Please highlight the two green data points

    - LAB MEDIA: Figure 8D. Video editor: Please highlight the orange and pink curves