# Submission ID #: 68230

# Scriptwriter Name: Sulakshana Karkala

# Project Page Link: https://review.jove.com/account/file-uploader?src=20810198

# Title: Optimized Fabrication Procedure for High-Quality Graphene-Based Moiré Superlattice Devices

# Authors and Affiliations:

# Shuwen Sun, Pablo Jarillo-Herrero

# Department of Physics, Massachusetts Institute of Technology, Cambridge

# Corresponding Authors:

Pablo Jarillo-Herrero	(pjarillo@mit.edu)

# Email Addresses for All Authors:

Shuwen Sun		(shuwen@mit.edu)

Pablo Jarillo-Herrero	(pjarillo@mit.edu)

## Author Questionnaire

1. Microscopy: Does your protocol require the use of a dissecting or stereomicroscope for performing a complex dissection, microinjection technique, or something similar? Yes

Authors: Please create scope videos of the shots labeled as SCOPE and upload the files to your project page as soon as possible: https://review.jove.com/account/file-uploader?src=20810198

All scope videos regardless of the type of microscope used (BF, Electron, dissecting, stereo, etc) are recognized as SCOPE shots. Please provide the SCOPE footage where applicable

2. Software: Does the part of your protocol being filmed include step-by-step descriptions of software usage?  Yes

We recommend using the screen capture program OBS. JoVE’s tutorial for using OBS Studio is provided at this link: https://review.jove.com/v/5848/screen-capture-instructions-for-authors?status=a7854k

As these files are necessary for finalizing your script, please upload all screen-captured video files to your project page as soon as possible: https://review.jove.com/account/file-uploader?src=20810198

SCREEN: 1.1.2,1.4.1,1.6.2,1.7.1,1.7.2,1.8.1,1.10.1,2.1.1-2.1.2,2.2.1-2.2.2,2.3.2-2.3.3,2.4.1-2.4.2,2.5.1-2.5.3,2.6.1-2.6.2,2.7.1-2.7.2,2.8.2,2.9.1,2.10.1-2.10.2,2.11.1,2.12.1-2.12.2,3.1.2,3.2.3,3.3.1,3.4.1-3.4.3,3.5.1,3.6.1-3.6.3,3.7.1-3.7.2

3. Filming location: Will the filming need to take place in multiple locations?   No

Current Protocol Length

Number of Steps:  32

Number of Shots:  60

# Introduction

# NOTE: Introductory statements were not provided

# Protocol

- Laser Patterning and Pickup of Top Hexagonal Boron Nitride Layer

Demonstrator: Shuwen Sun

AUTHORS: Please specify which shots will require the use of a microscope by placing “SCOPE” in front of the shot. Similarly identify the SCREEN capture shots with “SCREEN”

  - To begin, place a graphene wafer on the sample stage of the transfer setup integrated with a supercontinuum laser [1]. Use the Draw Bezier curves and straight lines function in Inkscape to outline the graphene boundary and the planned laser-cutting lines [2].
Authors: Please create screen capture videos of the shots labeled as SCREEN, create a screenshot summary, and upload the files to your project page as soon as possible: https://review.jove.com/account/file-uploader?src=20810198

    - WIDE: Talent places the graphene wafer on the sample stage.

    - SCREEN: The Draw Bezier curves and straight lines function is being used to outline the graphene boundary and planned laser cutting lines.

  - Now power on the laser and increase the intensity until the beam spot is visible [1]. Adjust the sample stage to align the beam spot with the start of a planned laser-cutting line [2-TXT].

    - Talent switching on the laser and gradually increasing intensity.

    - Talent adjusting the stage so the laser spot aligns with the beginning of a cutting line. TXT: Adjust laser intensity to suitable level

  - Next, move the sample stage to guide the beam spot along the planned laser-cutting line [1]. After zeroing the laser intensity, inspect the laser-cutting line [2-TXT].

    - Talent guiding the stage to trace along the laser-cutting path.

    - Shot of the flake showing the cut line. TXT: Repeat steps until all planned lines are laser cut

  - To pickup the top hexagonal boron nitride flake, adjust the orientation of the flake until the straight edge is vertical and positioned on the right side [1-TXT].

    - SCREEN: The flake orientation is being adjusted until the straight edge is vertical and positioned on the right side. TXT: Outline flake boundary in Inkscape

  - Gently clamp the glass slide with the PC/PDMS (P-C-and-P-D-M-S) stamp inside the socket at a downward tilt angle of 2 to 3 degrees [1]. Slide the socket to the left using the sliding tray until the glass slide is positioned above the sample wafer then manually lock it in place [2].

    - Talent clamping the glass slide into the socket at a tilt. TXT: PC/PDMS: polycarbonate/Polydimethylsiloxane

    - Shot of the socket being slide to the left and locked.

  - After setting the sample stage temperature to 50 degrees Celsius, engage the glass slide downward using the Z direction actuator [1-TXT]. Focus the microscope on the polycarbonate film and inspect the surface cleanness [2].

    - Talent engaging the actuator to lower the stamp. TXT: Speed: 1 mm/s until stamp is 2 mm above wafer

    - SCOPE/SCREEN: View of the polycarbonate surface.

  - Move the hexagonal boron nitride flake to the selected clean region and engage the slide further downward [1-TXT]. When the polycarbonate film and wafer are nearly in the same focal plane, reduce the speed to 5 micrometers per second [2].

    - SCOPE/SCREEN: The flake is being positioned over the clean surface region. TXT: Slide speed: 0.1 mm/s

    - SCOPE/SCREEN: Talent adjusting the speed and continuing to engage slowly.

  - Now engage the stamp onto the wafer with a speed of 5 micrometers per second until it completely covers the hexagonal boron nitride flake [1]. Then set the sample stage temperature to 80 degrees Celsius [2].

    - SCOPE/SCREEN: The stamp is being engaged until contact.

    - Talent adjusting the stage temperature to 80 degrees Celsius.

  - After the temperature is reached, disengage the stamp with 5 micrometers per second until the wavefront is close to the hexagonal boron nitride straight edge then pick up the flake [1-TXT].

    - Talent slowly disengaging the stamp near the hBN straight edge. TXT: Reduce speed to 2 µm/s to pick up the hBN flake

  - Once picked up, increase the speed to 5 micrometers per second to detach the polycarbonate film from the wafer [1]. Switch off the stage heater and open the water-cooling system [2].

    - SCOPE/SCREEN: Shot of the polycarbonate film detaching from wafer.

    - Talent turning off the heater and turning on the water cooling system.

  - When the temperature drops below 45 degrees Celsius, close the water-cooling system [1]. Disengage the glass slide all the way up at 1 millimeter per second [2].

    - Talent closing the water-cooling system.

    - Shot of the glass slide being disengaged.

- Picking up the Graphene Moiré Superlattice

  - Place the wafer with the freshly laser-cut graphene on the sample stage and locate the graphene using the 10X objective [1]. Adjust the flake orientation so the laser cutting lines are parallel to the hexagonal boron nitride straight edge [2].

    - SCOPE/SCREEN: View through 10x objective showing graphene flake.

    - SCOPE/SCREEN: The flake is being rotated until laser lines are parallel to the hBN edge.

  - Outline the graphene boundary in Inkscape, including the laser-cutting lines [1]. Use Peek Through to make the drawing semi-transparent while floating above the camera window [2].

    - SCREEN: Inkscape window showing boundary being traced with Bezier tool.

    - SCREEN: Peek Through is being used to make the drawing semi-transparent.

  - Now, move the glass slide with the top hexagonal boron nitride flake to the pre-engage position with the PC/PDMS stamp 2 millimeters above the graphene wafer [1]. Place the flake straight edge in the middle of the laser-cutting line that separates the central graphene pieces to align the hexagonal boron nitride drawing with the graphene drawing [2]. Tune the microscope to focus on the graphene and align it to its Inkscape drawing [3].

    - Shot of the glass slide being moved to the pre-engage position with the top flake above the wafer.

    - SCOPE/SCREEN: Overlay alignment in Inkscape with hBN edge centered on laser-cut line.

    - SCOPE/SCREEN: View aligning real graphene with drawing.

  - Then, focus on the top flake and move the glass slide in XY (X-Y) direction to align it to its drawing [1]. After refocusing on a focal plane slightly higher than the pre-cut graphene, engage the glass slide downward at 0.1 millimeter per second until the top flake comes into focus [2].

    - SCOPE/SCREEN: The top flake is being focused and the glass slide is being moved in the XY direction.

    - SCOPE/SCREEN: The slide is being engaged downward until hBN comes into focus.

  - Refocus on the graphene and set the speed to 5 micrometers per second [1]. Engage the stamp slowly until the flake becomes roughly visible while ensuring no contact with the wafer [2-TXT]. Continue to engage the stamp downward until it contacts the wafer [3].

    - SCOPE/SCREEN: The focus is being adjusted on the graphene and the speed is being adjusted.

    - SCOPE/SCREEN: The stamp is being lowered until the flake is roughly visible. TXT: Realign both the graphene and hBN to their drawings

    - SCOPE/SCREEN: The stamp is being lowered until it contacts the wafer.

  - Engage the stamp at 5 micrometers per second until the wavefront is close to the left edge of the flake [1]. Reduce the speed to 0.02 micrometers per second and continue engagement to contact the first graphene piece [2].

    - SCOPE/SCREEN: The stamp is being lowered until the wavefront is close to the left edge of the flake.

    - SCOPE/SCREEN: The stamp is lowered until it contacts the first graphene piece.

  - Once the flake fully covers the first graphene piece and is pinned at the straight edge, stop the engagement [1]. Clear hysteresis by moving the stage upward at 5 micrometers per second until the wavefront starts retracting [2].

    - SCOPE/SCREEN: View showing hBN flake covering graphene.

    - SCOPE/SCREEN: The stage is being moved upward until the wavefront starts retracting.

  - Set a disengaging speed of 0.02 micrometers per second to pick up the graphene gently [1]. When the wavefront moved away from the flake, increase the speed to 5 micrometers per second to fully detach the stamp from the wafer [2].

    - Talent starting disengagement at low speed.

    - SCOPE/SCREEN: Shot of the stamp fully detaching from the wafer.

  - Now copy the entire graphene drawing in Inkscape and rotate it by the desired twist angle [1].

    - SCREEN: Graphene drawing being copied in Inkscape and rotated.

  - Align the second graphene piece in the copied drawing with the first piece in the original drawing to maximize overlap [1-TXT]. Align the remaining graphene on the wafer to the copied drawing [2].

    - SCREEN: Drawings are being overlaid to show graphene overlap. TXT: Rotate sample stage by desired twist angle

    - SCOPE/SCREEN: Graphene on wafer is being aligned to rotated drawing.

  - Focus on the top hexagonal boron nitride flake on the glass slide and align it to the drawing [1-TXT].

    - SCOPE/SCREEN: The flake is being focused and aligned with the drawing. TXT: Examine quality of top stack under microscope

  - After aligning the flakes to the drawings, repeat the demonstrated steps to pick up the remaining graphene [1]. Once picked up, examine the quality of top stack under microscope [2].

    - SCOPE/SCREEN: Pick up the remaining graphene flake following the same procedures as above.

    - SCOPE/SCREEN: Examine quality of top stack under microscope.

- Encapsulation of the Graphene Moiré Superlattice

  - Place the wafer with the pre-cleaned bubble-free bottom gate on the sample stage [1]. Outline the boundary of the bottom gate using Inkscape [2].

    - Talent positioning the wafer with bottom gate on the stage.

    - SCREEN: Inkscape window showing boundary traced with Bezier tool.

  - Set the sample stage temperature to 160 degrees Celsius to tear off the polycarbonate film after encapsulation [1]. Then load the glass slide with the top stack and move it to the pre-engage position [2]. Roughly align both the bottom gate and the top stack to the drawings [3].

    - Talent setting the stage heater to 160 degrees Celsius.

    - Talent loading the glass slide with the top stack and moving it to the pre-engage position.

    - SCREEN: Overlay alignment of top stack and bottom gate.

  - Focus on the bottom gate, then slightly raise the focal plane [1-TXT].

    - SCREEN: The bottom gate is being focused and the focal plane is being slightly raised.  TXT: Engage slide downward at 0.1 mm/s until top stack becomes visible

  - Identify another middle focal plane between the bottom gate and top stack [1]. Then set the speed to 5 micrometers per second and engage the stamp until the top stack is visible [2]. Align both to the drawings accurately [3-TXT].

    - SCREEN: Another middle focal plane between the bottom gate and top stack is being located.

    - SCREEN: Stamp is being engaged until stack appears.

    - SCREEN: Bottom gate and top stack are being aligned to the drawings. TXT: Repeat until bottom gate and top stack are almost in the same focal plane, and the sample stage temperature > 150 °C

  - Now engage the stamp at 5 micrometers per second until the wavefront is close to the bottom gate, then reduce the speed to 0.5 micrometers per second [1].

    - SCREEN: The stamp is being lowered until the wavefront is close to the bottom gate, then its speed is being reduced.

  - Slowly engage the top stack onto the bottom gate [1]. Once the wavefront passes the top stack, increase the speed back to 5 micrometers per second to fully engage the stamp onto the wafer [2-TXT]. Then disengage the stamp at 5 micrometers per second [3].

    - SCREEN: The top stack is being engaged onto the bottom gate.

    - SCREEN: The entire stamp is being engaged onto the wafer at 5 µm/s. TXT: Wait for 1 min to soften PC film

    - SCREEN: The stamp is being retracted at 5 µm/s

  - Lift the stamp upward for 3 seconds at 5 micrometers per second [1]. Begin moving it in the X-Y directions to tear off the polycarbonate film [2].

    - SCREEN: The stamp is being lifted.

    - SCREEN: The stamp is being used to detach PC film.

  - Fully disengage the glass slide at 1 millimeter per second and remove it from the socket [1]. Switch off the stage heater and activate the water-cooling system [2].

    - Talent lifting and removing glass slide.

    - Talent switching off heater and activating cooling.

  - Once the temperature drops to room temperature, remove the wafer and inspect under an optical microscope [1].

    - Talent transferring the wafer to a microscope.

# Results

# AUTHORS:  Please confirm that the results have been accurately summarized

- Results

  - Four-fold degenerate Landau fans emerged from both the charge neutrality point and superlattice gaps in the high-quality magic-angle twisted bilayer graphene device [1], breaking down into two-fold or one-fold degeneracies at higher magnetic fields [2].

    - LAB MEDIA: Figure 8A. Video editor: Highlight the symmetrical red-and-blue striped patterns radiating between 0 to 3

    - LAB MEDIA: Figure 8A. Video editor: please highlight the area of the graph at 3 and 4

  - Symmetry-broken two-fold degenerate Landau fans were identified at half-filling states indicating correlated insulating behavior [1]. The superconducting dome was located underneath the Landau fan around the half-filling state [2].

    - LAB MEDIA: Figure 8A. Video editor: please highlight the area at ±2

    - LAB MEDIA: Figure 8A. Video editor: please highlight the low-field area at -2

  - Temperature-dependent resistance measurements revealed two superconducting domes at both sides of the half-filling state with the maximum critical temperature reaching approximately 1.7 Kelvin [1].

    - LAB MEDIA: Figure 8B. Video editor: please highlight the dotted area

  - Among 14 measured devices, the optimal critical temperature peaked at a twist angle near 1.08 degrees, consistent with theoretical predictions [1].

    - LAB MEDIA: Figure 8C. Video editor: Focus on the tallest data point in the plot

  - Disordered devices near the magic angle exhibited significantly reduced critical temperatures compared to high-quality devices [1], as seen in their resistance versus temperature profiles [2].

    - LAB MEDIA: Figure 8C. Video editor: Please highlight the two green data points

    - LAB MEDIA: Figure 8D. Video editor: Please highlight the orange and pink curves