# Submission ID #: 68246

# Scriptwriter Name: Poornima G

# Project Page Link: https://review.jove.com/account/file-uploader?src=20815078

# Title: Assessing Disaster Resilience of Concrete with Titanium Dioxide Nanoparticles

# Authors and Affiliations:

# Matheus Wesley Rodrigues1,2, Priscila Custódio de Matos1,2, Leonardo Pereira Franchi3, Tiago Alves Jorge de Souza4,5

# 1São Paulo State University | UNESP, Department of Environmental Sciences, SP, Brazil

# 2Brazilian National Center for Monitoring and Alert Natural Disasters (Cemaden)

# 3Department of Biochemistry and Molecular Biology at the Federal University of Goiás, GO, Brazil

# 4Municipal Faculty Professor Franco Montoro| FMPFM, Mogi Guaçu, SP, Brazil

# 5Adventist University Center of São Paulo| UNASP-EC, Engenheiro Coelho

# Corresponding Authors:

# Tiago Alves Jorge de Souza 		tiagoajs@hotmail.com

# Email Addresses for All Authors:

Matheus Wesley Rodrigues 		matheus.w.rodrigues@unesp.br

Priscila Custódio de Matos 		priscila.custodio-matos@unesp.br

# Leonardo Pereira Franchi 		leonardofranchi@ufg.br

# Tiago Alves Jorge de Souza 		tiagoajs@hotmail.com

## Author Questionnaire

1. Microscopy: Does your protocol require the use of a dissecting or stereomicroscope for performing a complex dissection, microinjection technique, or something similar?  No

2. Software: Does the part of your protocol being filmed include step-by-step descriptions of software usage?  No

3. Filming location: Will the filming need to take place in multiple locations?   Enter Yes or No.

Current Protocol Length

Number of Steps: 18

Number of Shots: 33

Authors, as you have not returned the script with interview answers, I have deleted the interview part from the video script. However, your protocol remains unchanged and please proceed with the shoot as described below.

- Videographer: Please obtain headshots for the authors who are present at the shoot location

# Protocol

- Specimen Preparation and Curing

  - To begin, prepare four groups of specimens using a concrete mix of Portland CPII (C-P-eye-eye) cement, crushed stone, medium-washed river sand, and water, maintaining a water to cement ratio of 0.5 [1-TXT]. For each 3.63-kilogram specimen, weigh appropriate amounts of cement, sand, gravel [2-TXT], and add water [3-TXT].

    - WIDE: Talent organizing four labeled trays for specimens. TXT: Cement:Sand:Gravel = 1:2:3 Video editor: This is a ratio

    - Close up of adding cement, sand and crushed stone to the container. TXT: Cement: 558.46 g; Sand: 1,116.92 g; Gravel: 1,675.38 g; Water: 279.23 g

    - Close up of adding water in a graduated container. TXT: Add any additive to the dry ingredients first

  - Homogenize all components thoroughly to obtain the most uniform mass possible [1]. Cast the mixed concrete into the molds [2] and inspect the mixture for signs of aggregate segregation, free-water accumulation, or staining from unmixed material to ensure a uniform consistency for representative results [3].

    - Talent mixing the concrete until the mass appears uniform.

    - Talent pouring the mixed concrete from the mixing container toward prepared molds.

    - Close-up of the mix surface showing no aggregate segregation, free water, or unmixed streaks.

  - Now, mold the test specimens in cylindrical metal forms 10 centimeters in diameter and 20 centimeters in height [1]. Fill each mold so the concrete reaches the designated level with uniform distribution [2-TXT].

    - Talent positioning cylindrical metal molds labeled with diameter and height specifications.

    - Talent distributing the concrete evenly into the mold until it reaches the marked level without overfilling. TXT: Avoid voids

  - Produce Sample A and designate it as the negative control without any additives to serve as the baseline for comparison with the other specimens [1].

    - Talent preparing and labeling Sample A while referencing the listed standards.

  - Produce Sample B by incorporating 1 percent Nano titanium dioxide, approximately 36.3 grams, into the concrete mix [1]. Distribute the nanoparticles evenly across the mass to prevent agglomeration [2]. Similarly prepare samples C and D, ensuring homogeneity among the sample sets [3-TXT].

    - Talent weighing 36.3 grams of Nano titanium dioxide.

    - Talent nano titanium dioxide to the container and thoroughly mixing to disperse nanoparticles uniformly.

    - Talent placing sample C and D beside samples A and B. TXT: Sample C: 2% NanoTiO₂ ; Sample D: 3% NanoTiO₂

  - Now, prepare Sample E by incorporating a 3 percent copper-based plasticizer additive, approximately 108.9 grams, into the concrete mix [1] and designate this sample as the positive control to compare the effect of the plasticizer relative to the other samples [2].

    - Talent weighing 108.9 grams of the copper-based plasticizer and combining it with the mix as per the dilution step.

    - Talent labeling Sample E as “Positive control – plasticizer.”

  - Store all samples in an area with controlled conditions, protected from environmental influences, to await the curing time [1].

    - Talent transferring labeled molds to a controlled-condition storage area and closing the chamber.

  - Cure the specimens in a humidity-controlled area maintained at a temperature of around 23 degrees Celsius and a relative humidity of at least 95 percent for 24 hours [1]. After this initial period, submerge the specimens in lime-saturated water maintained at the same temperature of 23 degrees Celsius, for continued curing over the designated period [2].

    - Talent placing freshly molded specimens into a humidity-controlled chamber set to 23 degrees Celsius and 95 percent relative humidity.

    - Talent transferring cured specimens after 24 hours from the chamber into a tank filled with lime-saturated water.

  - After curing, remove the specimens [1] and measure the weight of each specimen to confirm that each has an average mass of 3.63 kilograms [2].

    - Talent removing specimens from the curing tank and gently drying the surface with a cloth.

    - Talent placing a specimen on a precision balance.

  - Condition the specimens at room temperature of around 23 degrees Celsius, according to the following schedule [1].

    - TEXT ON PLAIN BACKGROUND:

7 days: Samples A1, B1, C1, D1 and E1

14 days: Samples A2, B2, C2, D2 and E2

28 days: Samples A3, B3, C3, D3 and E3

- Compressive Strength Testing

  - Subject each specimen to an axial compression test using a universal tensile and compression testing machine [1].

    - Talent pointing to the universal testing machine in the laboratory and switching it on.

  - Ensure that the load cell capacity of the testing machine is compatible with the specimen dimensions [1], and verify that a digital control system is enabled for real-time monitoring and recording of the applied load [2].

    - Talent examining the load cell capacity on the machine’s display.

    - Show the digital control interface displaying load readings and the active recording system.

  - Continue applying the compressive load until the specimen fails [1], and record the maximum supported load at the moment of rupture [2].

    - Talent monitoring the machine as the specimen compresses and begins to crack.

    - Talent noting in the notebook.

  - Compute the compressive strength of each specimen using the formula [1].

    - TEXT ON PLAIN BACKGROUND:

fc​ = Fmax​​ / A

where:

fc​ = compressive strength (N/mm2),

Fmax​ = maximum recorded load (N)

A = test specimen cross-sectional area (mm²). 1 N/mm2 = 1 MPa

  - Then, conduct the compressive-strength test by positioning each cylindrical specimen measuring 100 millimeters in diameter and 200 millimeters in height vertically at the center of the hydraulic press [1]. Ensure proper contact between the specimen and the loading plates [2-TXT].

    - Talent centering a cylindrical specimen on the press base and lowering the upper loading plate to touch the specimen.

    - Close-up of the contact surfaces to confirm proper seating and alignment according to standard. TXT: Align according to ABNT NBR 5739:2018

  - Apply the axial load continuously and without impact at a rate of around 0.45 megapascals per second [1]. Repeat this procedure for all three specimen sets: control, titanium dioxide-doped, and copper-based additive samples [2].

    - Show the test rate setting adjusted to 0.45 megapascals per second.

    - Talent removing the previous sample and placing the next one.

  - Record all values systematically for later comparison among the different sample sets [1].

    - Display a digital spreadsheet or data logger with organized results for all samples.

  - Finally, compare the recorded compressive strength values to assess the mechanical behavior and performance differences between the control, titanium dioxide-doped, and copper-based additive specimens [1].

    - Show plotted comparison charts on a computer screen showing variations and talent pointing to the data and analysing.

# Results

- Results

  - Compression tests showed that concrete specimens containing 1% titanium dioxide by mass had higher compressive strength [1] than both the control concrete [2] and those with 3% copper-based plasticizer [3].

    - LAB MEDIA: Figure 3. Video editor: Highlight all the bars for B.

    - LAB MEDIA: Figure 3. Video editor: Highlight the bars labeled A.

    - LAB MEDIA: Figure 3. Video editor: Highlight the bars labeled E.

  - Among samples subjected to 28 days of curing during compressive strength testing, specimens B3, C3, and D3 appeared visibly lighter in color [1] than specimens labeled A3 and E3 [2].

    - LAB MEDIA: Figure 2. Video editor: Highlight the specimens labeled B3, C3, and D3, showing their lighter coloration.

    - LAB MEDIA: Figure 2. Video editor: Highlight the specimens labeled A3 and E3, which are darker in color.

  - The specimen labeled B had the highest compressive strength after 28 days of curing at 17,379 megapascals [1].

    - LAB MEDIA: Table 2. Video editor: Highlight the cell in the row labeled “B” and column labeled “28 Days” with the value 17,379.

  - Specimens labeled A and E showed lower compressive strength values after 28 days of curing, with values of 13,018 and 9,725 megapascals, respectively [1].

    - LAB MEDIA: Table 2. Video editor: Highlight the cell in the row labeled “A” and column labeled “28 Days” with the value 13,018.

    - LAB MEDIA: Table 2. Video editor: Highlight the cell in the row labeled “E” and column labeled “28 Days” with the value 9,725.

  Portland cement
Pronunciation link: https://www.collinsdictionary.com/dictionary/english/portland-cement collinsdictionary.com+2oxfordlearnersdictionaries.com+2
IPA: /ˈpɔrt-lənd ˈsɪmɛnt/
Phonetic Spelling: port-lund si-ment

  homogenize
Pronunciation link: https://www.merriam-webster.com/dictionary/homogenize Merriam-Webster+2collinsdictionary.com+2
IPA: /həˈmɑː.dʒə.naɪz/
Phonetic Spelling: huh-mahr-juh-nyz

  agglomeration
Pronunciation link: https://dictionary.cambridge.org/pronunciation/english/agglomeration Cambridge Dictionary+1
IPA: /əˌɡlɑː.məˈreɪ.ʃən/
Phonetic Spelling: uh-glah-muh-RAY-shuhn

  segregation
Pronunciation link: https://dictionary.cambridge.org/pronunciation/english/segregation Cambridge Dictionary+1
IPA: /ˌsɛɡ.rəˈɡeɪ.ʃən/
Phonetic Spelling: seg-ruh-GAY-shuhn

  saturation
Pronunciation link: https://dictionary.cambridge.org/us/pronunciation/english/saturation Cambridge Dictionary
IPA: /ˌsætʃ.əˈreɪ.ʃən/
Phonetic Spelling: satch-uh-RAY-shuhn