# Submission ID #: 68313

# Scriptwriter Name: Poornima G

# Project Page Link: https://review.jove.com/account/file-uploader?src=20835513

# Title: Scalable Syntheses of Graphene Oxide and Reduced Graphene Oxide Using Cascade Design Oxidation and Highly Basic Reduction Reactions

# Authors and Affiliations:

# Hon Nhien Le1,2, Thi Bich Duyen Luu1,2, Lam Nhu Pham1,2, Thi Bang Tam Dao1,2, Trung Do Nguyen1,2, Chi Nhan Ha Thuc1,2, Van Hieu Le1–3

# 1Faculty of Materials Science and Technology, VNUHCM University of Science

# 2Vietnam National University, Ho Chi Minh City (VNUHCM)

# 3Multifunctional Materials Laboratory, VNUHCM University of Science

# Corresponding Authors:

# Hon Nhien Le				lhnhien@hcmus.edu.vn

# Email Addresses for All Authors:

Thi Bich Duyen Luu			21250057@student.hcmus.edu.vn

Lam Nhu Pham			21250090@student.hcmus.edu.vn

Thi Bang Tam Dao			dtbtam@hcmus.edu.vn

Trung Do Nguyen			ntdo@hcmus.edu.vn

Chi Nhan Ha Thuc			htcnhan@hcmus.edu.vn

# Van Hieu Le				lvhieu@hcmus.edu.vn

# Hon Nhien Le				lhnhien@hcmus.edu.vn

## Author Questionnaire

1. We have marked your project as author-provided footage, meaning you film the video yourself and provide JoVE with the footage to edit. JoVE will not send the videographer. Please confirm that this is correct.

√ Correct

2. Microscopy: Does your protocol require the use of a dissecting or stereomicroscope for performing a complex dissection, microinjection technique, or something similar?  No

3. Software: Does the part of your protocol being filmed include step-by-step descriptions of software usage?  No

4. Proposed filming date: To help JoVE process and publish your video in a timely manner, please indicate the proposed date that your group will film here: 06/20/2025

When you are ready to submit your video files, please contact our Content Manager, Utkarsh Khare.

Current Protocol Length

Number of Steps:  13

Number of Shots:  30

# Introduction

  - Chi Nhan Ha Thuc: Our research scope is oxidation–reduction technologies for producing graphene oxide and reduced graphene oxide nanomaterials. We develop protocols for chemical oxidation–reduction reactions with optimized safety and efficiency.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B-roll: 2.1.2

What technologies are currently used to advance research in your field?

  - Thi Bang Tam Dao: I think new technologies that improve safety and efficiency in Hummers oxidation reactions and alkaline reduction reactions are important to the production of graphene oxide and reduced graphene oxide.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B-roll: 2.3.1

What are the current experimental challenges?

  - Trung Do Nguyen: Scale-up of graphite oxidation reaction requires a safe and efficient protocol. Besides, cost effectiveness, eco-friendliness and graphene restacking are challenges in chemical reduction reactions.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B-roll: 2.5.1

What significant findings have you established in your field?

  - Hon Nhien Le: We presented cascade-design oxidation reaction harnessing exothermic energies for self-heating reactions, saving chemicals, energy and time. Reduction reaction using basic ammonia is simple and effective for non-stacked reduced graphene oxide.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B-roll: 4.1.1

What research questions will your laboratory focus on in the future?

  - Van Hieu Le: Our laboratories will develop the protocols of oxidation – reduction reactions for scale-up productions and practical applications of graphene-based materials. Especially, as-synthesized graphene is useful for water purification, photocatalysts, energy storage and conversion.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B-roll: 4.2.1

# Protocol

- Scalable Production of Graphite Oxide Using Cascade Design Oxidation Reaction

Demonstrator: Hon Nhien Le, Thi Bich Duyen Luu, Lam Nhu Pham

NOTE: Author revised timestamps included by the scriptwriter. Use relevant part from author provided timestamps

  - To begin, add 5 grams of graphite powder to a 50-milliliter glass beaker and add 50 milliliters of 97 percent sulfuric acid to the beaker [1]. Stir the three suspensions of graphite and sulfuric acid magnetically at ambient conditions for at least 1 hour [2].

    - 1.1.1 Prepare 50 mL graphite H2SO4.MOV Timestamps: 00:30 – 00:45.

    - 1.1.2 Stir three graphite H2SO4 suspensions.MOV Timestamps: 01:30 – 01:45.

  - In a 250-milliliter glass Erlenmeyer flask, add 100 milliliters of 97 percent sulfuric acid [1]. Slowly add 10 grams of potassium permanganate to the sulfuric acid solution under magnetic stirring to dissolve and prepare about 100 milliliters of manganese and sulfuric acid solution [2].

    - 1.2.1. Add 50 mL H2SO4.MOV Timestamps: 00:05 – 00:20 .

    - 1.2.1. Add 10 g KMnO4.MOV Timestamps: 00:00 – 00:20 and 1.2.1. Stir three Mn VII solutions.MOV Timestamps: 00:40 – 00:55.

  - Slowly pour one previously prepared graphite and sulfuric acid suspension into the manganese and sulfuric acid solution under magnetic stirring in the 250 milliliter glass Erlenmeyer flask [1]. After 9 minutes in a water bath, continue stirring the reaction mixture at room temperature. Allow the reaction temperature to peak between 48 and 52 degrees Celsius and gradually return to room temperature [2]. Stir all three mixtures of graphite, manganese, and sulfuric acid magnetically at room temperature [3].

    - 1.3.2. Conduct the first cascade step.MOV Timestamps: 00:00 – 00:45.

    - 1.3.3. A reaction unit in ambient.MOV Timestamps: 00:27 – 00:42.

    - 1.3.5 Stir three reaction units.MOV Timestamps: 00:30 – 00:45.

  - Next, carefully pour the first Erlenmeyer flask of graphite, manganese, and sulfuric acid mixture into a 2 liter beaker of water under agitation [1]. Use an infrared thermometer to measure the reaction temperature, which rises to approximately 59 degrees Celsius [2].

    - 1.4.2. 1.4.3. 1.4.4. Conduct the second cascade.MOV Timestamps: 00:04 – 01:04.

  - Then, slowly add the second Erlenmeyer flask of graphite, manganese, and sulfuric acid mixture to raise the temperature to about 80 degrees Celsius [1]. Add the third Erlenmeyer flask of mixture to increase the temperature to approximately 94 degrees Celsius [2]. Gradually pour 450 milliliters of 5 percent hydrogen peroxide solution into the beaker, observing a slight temperature rise from the exothermic reaction [3].

    - File name: 1.4.2. 1.4.3. 1.4.4. Conduct the second cascade.MOV Timestamps: 01:57 – 02:47, 03:08 – 03:18.

    - File name: 1.4.2. 1.4.3. 1.4.4. Conduct the second cascade.MOV Timestamps: 03:40 – 04:15, 05:05 – 05:15.

File name: 1.4.5. Agitate the reaction.MOV Timestamps: 00:04 – 00:19

    - 1.5.2. Add 450 mL H2O2 solution.MOV Timestamps: 00:05 – 00:20, 01:23 – 01:33.

  - Now, pour the entire reaction mixture into 50 milliliter centrifuge tubes [1]. Centrifuge at 1500 g for 5 minutes at ambient temperature [2]. Collect the sedimented solids to mix them with 1 liter of 5 percent hydrochloric acid solution [3]. After agitating the acidic suspension for at least 1 hour, centrifuge at 1500 g for 10 minutes, and use a vacuum filtration system with pure water to wash the sedimented graphite oxide solid [4].

    - 1.6.1. Centrifuge the suspension.MOV Timestamps: 00:26 – 00:36.

1.6.1. Centrifuge the suspension.MOV Timestamps: 00:55 – 01:05.

1.6.1. Centrifuge and collect the solid.MOV Timestamps: 01:25 – 01:30.

    - 1.6.4. Washing GrO in vacuum filtration.MOV Timestamps: 00:25 – 00:35.

  - Next, dry the washed graphite oxide slurry in a drying oven set to 80 degrees Celsius [1]. Then, using a stainless steel or ceramic mortar and pestle, grind the dried material to produce a graphite oxide powder [2].

    - 1.7.1. Dry GrO at 80 C.MOV Timestamps: 00:20 – 00:40.

    - 1.7.1. Grind GrO material.MOV Timestamps: 00:34 – 00:45, 01:03 – 01:12.

And 
1.7.1. Collect GrO powder.MOV Timestamps: 00:12 – 00:22

  - Use scanning electron microscopy and energy-dispersive X-ray spectroscopy to characterize the obtained graphite oxide and graphene oxide [1].

    - 1.8.2. SEM EDS characterization of GrO.MOV Timestamps: 00:20 – 00:40.

- Reduction of Graphene Oxide Dispersion using Highly Basic Ammonia Solution

  - Drop 25 to 28 percent ammonia solution gradually into the aqueous dispersion of graphite oxide until the pH reaches 10 [1]. Sonicate the dispersion using an ultrasonic probe set to 100 watts power, with a continuous cycle and amplitude of 80 percent [2].

    - 2.1.1. Prepare GrO dispersion pH 10.MOV Timestamps: 00:15 – 00:25, 01:25 – 01:35.

    - 2.1.2. Sonicate GrO dispersion.MOV Timestamps: 00:15 – 00:30.

  - Pour the 1 liter dispersion of graphene oxide into a 1-liter round glass reactor [1]. Add 111 milliliters of 25 to 28 percent ammonia solution to raise the pH above 11 and make the mixture highly basic [2]. Heat the reaction mixture to 90 degrees Celsius without stirring [3].

    - 2.2.1. Add GO and NH3 solution.MOV Timestamps: 00:10 – 00:30, 01:30 – 01:40

    - File name: 2.2.2. Heat the reaction to 90 C (1).MOV Timestamps: 00:10 – 00:30.

    - File name: 2.2.2. Heat the reaction to 90 C (2).MOV Timestamps: 00:10 – 00:30.

  - Then, filter the reduced graphene oxide mixture using filter fabrics or cellulose filter paper [1] and collect the hydrogel in a plastic box for storage [2].

    - 2.3.1. Filter RGO suspension (1).MOV Timestamps: 00:15 – 00:45.

    - File name: 2.3.1. Filter RGO suspension (2).MOV Timestamps: 00:10 – 00:25, 00:40 – 00:50

    - 2.3.2. Collect RGO hydrogel for storage.MOV Timestamps: 00:10 – 00:25.

  - Use scanning electron microscopy and energy-dispersive X-ray spectroscopy to characterize the reduced graphene oxide hydrogel [1].

    - 2.4.2. SEM imaging of RGO structure.MOV Timestamps: 00:10 – 00:30, 00:44 – 00:54.

  - Finally, disperse 0.1 gram of reduced graphene oxide hydrogel in 300 milliliters of water [1]. Use agitation followed by sonication to ensure a homogeneous dispersion of RGO nanosheets, indicating good aqueous dispersibility [2].

    - File name: 2.4.3. Sonicate RGO dispersion (1).MOV Timestamps: 00:25 – 00:40

    - File name: 2.4.3. RGO dispersion after sonication (2).MOV Timestamps: 00:25 – 00:35

# Results

- Results

  - The X-ray diffraction pattern of graphite oxide powder revealed a peak at 10.8 degrees, corresponding to an intersheet distance of 8.19 angstroms [1], and a peak at 42.2 degrees [2].

    - LAB MEDIA: Figure 2A. Video editor: Highlight the sharp peak labeled 10.8° on the left side of the XRD graph.

    - LAB MEDIA: Figure 2A. Video editor: Highlight the smaller peak labeled 42.2° on the right side of the XRD graph.

  - SEM images confirmed the multilayer structure of graphite oxide particles [1], and elemental mapping displayed uniform distributions of carbon and oxygen atoms [2].

    - LAB MEDIA: Figure 3B,C.

    - LAB MEDIA: Figure 3D E F.

  - EDS spectrum and elemental analysis of graphene oxide indicated 64.02% carbon atoms [1] and 35.98% oxygen atoms, giving a C/O atomic ratio of 1.78 [2].

    - LAB MEDIA: Figure 4B. Video editor: Highlight the atom percentage values 64.02 in the right-hand column.

    - LAB MEDIA: Figure 4B. Video editor: Highlight the atom percentage values 35.98 in the right-hand column.

  - SEM images of GO nanosheets exfoliated from graphite oxide at 1000 parts per million concentration revealed successful separation into thin sheets [1].

    - LAB MEDIA: Figure 4C,D. Video editor: Highlight the dispersed thin flake structures across both SEM images.

  - XRD patterns of reduced graphene oxide hydrogel and powder revealed a broad peak at 27.7 degrees for hydrogel [1], while powder exhibited sharper peaks at 10.1, 26.6, and 42.6 degrees [2].

    - LAB MEDIA: Figure 5A. Video editor: Highlight the blue broad peak at 27.7° labeled as "RGO hydrogel".

    - LAB MEDIA: Figure 5A. Video editor: Highlight the sharp black peaks at 10.1°, 26.6°, and 42.6° labeled as "RGO powder".

  - SEM images of dehydrated RGO hydrogel revealed non-stacked nanosheets [1], and porous morphology of assembled RGO structures [2].

    - LAB MEDIA: Figure 6B.

    - LAB MEDIA: Figure 6C.

  - Elemental mapping of the RGO hydrogel structure demonstrated uniform distributions of carbon and oxygen atoms throughout the matrix, with a C/O (C-Oh) atomic ratio of 4.16 [1].

    - LAB MEDIA: Figure 6 D E F

  - SEM images of dehydrated RGO nanosheets revealed a wrinkled morphology and thin sheet structure [1].

    - LAB MEDIA: Figure 7C,D.

Pronunciation Guide:

- Graphene

- Pronunciation link: https://www.merriam-webster.com/dictionary/graphene

- IPA: /ˈɡræˌfiːn/

- Phonetic Spelling: gra-feen

- Cascade

- Pronunciation link: https://www.merriam-webster.com/dictionary/cascade

- IPA: /kæˈskeɪd/

- Phonetic Spelling: kas-kayd

- Graphite

- Pronunciation link: https://www.merriam-webster.com/dictionary/graphite

- IPA: /ˈɡræˌfaɪt/

- Phonetic Spelling: gra-fite

- Potassium Permanganate

- Pronunciation link: https://www.merriam-webster.com/dictionary/potassium%20permanganate

- IPA: /pəˈtæsiəm pərˈmæŋɡəˌneɪt/

- Phonetic Spelling: puh-ta-see-um per-man-guh-nayt

- Hydrogen Peroxide

- Pronunciation link: https://www.merriam-webster.com/dictionary/hydrogen%20peroxide

- IPA: /ˈhaɪdrədʒən pəˈrɑːksaɪd/

- Phonetic Spelling: hy-droh-jen puh-rok-side

- Hydrochloric Acid

- Pronunciation link: https://www.merriam-webster.com/dictionary/hydrochloric%20acid

- IPA: /ˌhaɪdrəˈklɔːrɪk ˈæsɪd/

- Phonetic Spelling: hy-droh-klor-ik a-sid

- Oxide

- Pronunciation link: https://www.merriam-webster.com/dictionary/oxide

- IPA: /ˈɑːksaɪd/

- Phonetic Spelling: ok-side

- Oxidation

- Pronunciation link: https://www.merriam-webster.com/dictionary/oxidation

- IPA: /ˌɑːksɪˈdeɪʃən/

- Phonetic Spelling: ok-si-day-shun

- Reduction

- Pronunciation link: https://www.merriam-webster.com/dictionary/reduction

- IPA: /rɪˈdʌkʃən/

- Phonetic Spelling: ri-duk-shun