# Submission ID #: 68394

# Scriptwriter Name: Poornima G

# Project Page Link: https://review.jove.com/account/file-uploader?src=20860218

# Title: In Situ Photo-Rheology Monitors Viscoelastic Changes in Photo-Responsive Polymer Networks

# Authors and Affiliations:

# Eleanor L. Quirk1, Michael C. Burroughs1, Danielle J. Mai1,2

# 1Department of Chemical Engineering, Stanford University

# 2Department of Materials Science and Engineering, Stanford University

# Corresponding Authors:

# Danielle J. Mai			djmai@stanford.edu

# Email Addresses for All Authors:

Eleanor L. Quirk		eleanorq@stanford.edu

# Michael C. Burroughs		mcburrou@stanford.edu

# Danielle J. Mai			djmai@stanford.edu

## Author Questionnaire

1. Microscopy: Does your protocol require the use of a dissecting or stereomicroscope for performing a complex dissection, microinjection technique, or something similar?  No

2. Software: Does the part of your protocol being filmed include step-by-step descriptions of software usage?  Yes, all done

3. Filming location: Will the filming need to take place in multiple locations?   No

If Yes, how far apart are the locations? N/A

Current Protocol Length

Number of Steps:  21

Number of Shots:  39 (14 SC)

# Introduction

Videographer: Obtain headshots for all authors available at the filming location.

  - Danielle Mai: We engineer polymers to advance materials for human health and planetary health. We investigate how molecular design impacts material properties, including mechanical strength, stimuli-responsive behavior, and recyclability [1].

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B-roll: 2.3.1

What technologies are currently used to advance research in your field?

  - Michael Burroughs: In polymer engineering, mechanical tests are used to understand material strength and durability. Integrating mechanical tests with chemical or optical measurements allows us to study molecular features underlying these properties [1].

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B-roll: 3.1.2

What research gap are you addressing with your protocol?

  - Eleanor Quirk: We hope to reduce the barrier to entry for researchers who want to use photo-rheology. We describe how we designed our instrument and how others can design their own system [1].

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B-roll: 5.1.1

What advantage does your protocol offer compared to other techniques?

  - Michael Burroughs: In situ photo-rheology measures a material’s mechanical response during photo-stimulation. This approach allows us to track materials as they are formed or as they change in response to light [1].

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B-roll: 4.2.1

What new scientific questions have your results paved the way for?

  - Eleanor Quirk: Our studies shed light on the design of photo-responsive polymer networks, which invite new questions about tuning their mechanical properties. For example, how might we formulate recyclable networks [1]?

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B-roll:5.3.1

Videographer: Obtain headshots for all authors available at the filming location.

# Protocol

- Setting up the Rheometer

Demonstrator: Eleanor Quirk

  - To begin, install the upper Peltier plate and geometry on the rheometer [1]. Next, install the lower optics plate to enable uniform irradiation of samples during photo-rheology measurements [2]. Use an optics plate that is transparent to the wavelengths of interest to allow light transmission through the plate [3].

    - WIDE: Talent showing the rheometer installed with peltier plate.

    - Talent placing the lower optics plate onto the setup area.

    - Close-up of the transparent lower plate installed.

  - Wipe the lower optics plate clean and dry [1]. Then, center the light source under the transparent plate [2], and secure it using posts, holders, or other appropriate supports [3].

    - Talent wiping the optics plate with a lint-free cloth.

    - Talent aligning the light source beneath the plate. Note: 2.2.2 and 2.2.3 are shot together as 2.2.2

    - Talent securing the light source using support structures.

  - Now, place a photodiode power sensor connected to an optical power meter on top of the transparent plate, with the sensor facing downward toward the light source [1]. If necessary, take measures to prevent exposure to light [2]. Then, turn on the light [3] and measure the light intensity using the power meter [4-TXT].

    - Talent positioning the photodiode sensor on the plate.

    - Talent placing UV-blocking sheets to block the light. Note: Mislabeled as 2.3.1. Please match the shot action.

    - Talent activating the light source.

    - Shot of the optical power meter showing the readings. TXT: Repeat the intensity measurement periodically as the light source ages

  - If required, adjust the light intensity using a light source driver [1]. Mark the positions of the light source supports to allow reproducible placement for future experiments [2-TXT].

    - Talent rotating a knob or adjusting settings on the light source driver.

    - Talent marking the positions of light source support structures with a marker or tape.

- Loading the Sample onto the Rheometer

  - Estimate the required sample volume using the formula for the volume of a cylinder and dispense slightly more to avoid under-filling [1-TXT]. For a low-viscosity liquid sample such as 100 milligrams per milliliter of PEG (peg)-anthracene in water, pipette 75 microliters onto the center of the optics plate [2].

    - Talent calculating and writing in a notebook. TXT: Determine a suitable gap height that allows uniform UV irradiation

    - Talent pipetting the liquid sample onto the center of the transparent optics plate.

  - Next, lower the rheometer head until the geometry contacts the sample, then pause to avoid forming bubbles [1].

    - Talent lowering the geometry slowly as it makes contact with the liquid.

  - View the sample through the optics plate to check for bubble formation [1]. If bubbles are visible, raise the geometry to break the connection between the plates [2], then gently rotate and lower the geometry again to reestablish contact [3].

    - Shot of the view through the optics plate.

    - Talent raising the geometry slightly. Note: 3.3.2 and 3.3.3 are shot together

    - Talent gently rotating the geometry and re-lowering it to contact the sample. NOTE: Added extra optional shot: 3.3.2-A and 3.3.3-A (with break in liquid)

  - Then, gradually lower the geometry until reaching the final experimental gap height [1-TXT].

    - Talent lowering the head in small steps while monitoring the sample. TXT: Continue observing for bubble formation throughout the process

  - Now, gently rotate the geometry to homogenize the liquid sample [1].

    - Talent manually rotating the top geometry part of the rheometer.

  - To prevent evaporation over short timescales, soak lint-free wipes in water [1-TXT] and place them near the sample to create a high-humidity environment around the sample [2-TXT].

    - Talent soaking a lint-free wipe in water. TXT: Minimize evaporation during the experiment Note: 3.6.1 and 3.6.2 are shot together

    - Talent positioning the moist lint-free wipe close to the sample on the stage. TXT: Ensure the wipes do not touch the sample or the geometry

  - For longer measurements, seal the sample with an immiscible layer such as mineral oil to isolate it from the ambient environment [1-TXT].

    - Talent carefully pipetting mineral oil around the perimeter of the aqueous sample. TXT: Mineral oil prevents evaporation during longer experiments

  - Close the upper Peltier plate jacket to protect the sample from ambient light and temperature changes [1]. Then, add additional shielding like UV-blocking sheets as needed to protect from harmful stray irradiation [2].

    - Talent closing the jacket around the rheometer's upper plate.

    - Talent placing UV-blocking panels around the instrument.

  - To determine an appropriate strain for dynamic experiments, perform preliminary strain amplitude sweeps on the sample to identify the linear viscoelastic region [1]. Sweep the strain from 1 percent to 1000 percent at a constant frequency of 10 radians per second before and after UVA-induced network formation [2]. Use a 10 percent strain for this sample to ensure linear viscoelasticity both before and after network formation [3].

    - SCREEN: 68394_3.10.1.-3.10.2._t1_precrosslink.mp4 00:18-00:22.

    - SCREEN: 68394_3.10.1.-3.10.2._t3_precrosslink.mp4 03:35-03:55. Video editor: Highlight the sample title “pre-crosslink”

    - SCREEN: 68394_3.10.1.-3.10.3._t1_postcrosslink.mp403:10-03:32. Video editor: Highlight the sample title “post-crosslink”

- Conducting a Photo-Rheology Experiment

  - Set the sample temperature to 22 degrees Celsius [1]. Pre-shear the sample for 10 seconds, then allow it to equilibrate for another 60 seconds [2].

    - SCREEN: 68394_4.1.1._4.1.2._4.2.1._4.3.1._4.6.1._t1.mp4 00:05-00:10 Video editor: Highlight the temperature value of 22 degrees Celsius

    - SCREEN: 68394_4.1.1._4.1.2._4.2.1._4.3.1._4.6.1._t1.mp4 00:05-00:10 Video editor: Highlight the “equilibration box” covering the duration 60 seconds

  - Perform a frequency sweep before irradiation, ranging from 100 radians per second to 0.1 radians per second [1]. Use the sweep results to confirm the initial physical state of the sample [2].

    - SCREEN: 68394_4.1.1._4.1.2._4.2.1._4.3.1._4.6.1._t1.mp4 00:15-00:20 Video editor: Highlight the “angular frequency” line showing 100 to 0.1 rad/s.

    - SCREEN: 68394_4.1.1-4.6.2._t1.mp4 03:53-04:03.

  - Set an oscillation time sweep to span the irradiation process, including buffer periods before and after light exposure [1].

    - SCREEN: 68394_4.1.1._4.1.2._4.2.1._4.3.1._4.6.1._t1.mp4 00:25-00:40

  - Take measurements for 60 seconds prior to UVA irradiation, continue for 1 hour during irradiation, and measure for 10 seconds after irradiation [1]. Use 10 radians per second frequency and 10 percent strain amplitude throughout the sweep [2].

    - SCREEN: 68394_4.1.1-4.6.2._t1.mp4  00:10:45-00:11:05 Video editor: Highlight the 60 seconds tick mark on the x-axis (step time)

    - SCREEN: 68394_4.1.1-4.6.2._t1.mp4   Video editor: Highlight the “angular frequency” line showing 10 rad/s on the right panel.

  - Confirm that the sample temperature is stable during irradiation despite the energy input [1].

    - SCREEN: 68394_4.1.1-4.6.2._t1.mp4 00:47:38-00:47:47. Video editor: Highlight the rows “temperature showing 22 degrees” and “set temperature showing 22 degrees celsius” on the right panel

  - Finally, perform a second frequency sweep after irradiation, using the same frequency range as before [1], to compare post-irradiation viscoelastic properties with the initial measurements [2].

    - SCREEN: 68394_4.1.1-4.6.2._t1.mp4  01:11:00-01:11:10.

    - SCREEN: 68394_4.1.1-4.6.2._t1.mp4  01:11:10-01:11:20 (Video Editor: Keep this continuous with 4.6.1)

# Results

- Results

  - Before irradiation, the amplitude sweep revealed a strain-independent region across the full range of 1% to 1000%, indicating a broad linear viscoelastic region [1]. After 1 hour of irradiation, the linear viscoelastic region extended only to 100% strain, beyond which a yielding event occurred [2].

    - LAB MEDIA: Figure 6. Video editor: Focus on the left graph labeled "Before crosslinking"

    - LAB MEDIA: Figure 6. Video editor: Focus on the right graph labeled "After crosslinking"

  - Before irradiation, the frequency sweep showed a slight frequency dependence, consistent with a viscoelastic liquid [1]. After 1 hour of irradiation, the moduli showed minimal dependence on frequency with elastic moduli exceeding viscous moduli, confirming the material's solid-like behavior [2].

    - LAB MEDIA: Figure 5. Video editor: Highlight the left graph labeled "Before crosslinking"

    - LAB MEDIA: Figure 5. Video editor: Highlight the left graph labeled "After crosslinking"

  - Increasing the polymer concentration from 20 to 100 milligrams per milliliter led to faster cross-linking, as indicated by an earlier crossover between the elastic and viscous moduli [1]. This change also resulted in stiffer networks, reflected by higher plateau values of the elastic modulus [2].

    - LAB MEDIA: Figure 7. Video editor: Sequentially show red, green and blue line curves .

    - LAB MEDIA: Figure 7. Video editor: Highlight the blue curve.

# Pronunciation guide:

# 1. Rheometer

# Link: https://www.merriam-webster.com/dictionary/rheometer oed.com+13definitions.net+13howtopronounce.com+13
IPA: /ˈriːəˌmɛtər/
Phonetic: REE-ə-meh-tər

# 2. Peltier

# Link: https://www.merriam-webster.com/dictionary/Peltier%20effect 
IPA: /ˈpɛltiər/
Phonetic: PEL-tee-er

# 3. Photodiode

# Link: https://www.merriam-webster.com/dictionary/photodiode 
IPA: /ˌfoʊˈtoʊˌdaɪ.oʊd/
Phonetic: foh-TOH-die-ohd

# 4. Photometer (related term)

# Link: https://www.merriam-webster.com/dictionary/photometer 
IPA: /fəˈtɒmətər/
Phonetic: foh-TAW-muh-tər

# 5. Photorheology

# Link: No confirmed link found
IPA: /ˌfoʊtoʊˌriːˈɒlədʒi/
Phonetic: foh-toh-ree-AW-luh-jee

# 6. Geometry (rheometer geometry)

# Link: https://www.merriam-webster.com/dictionary/geometry 
IPA: /dʒiˈɑmətɹi/
Phonetic: jee-AW-muh-tree

# 7. Equilibrate

# Link: https://www.merriam-webster.com/dictionary/equilibrate 
IPA: /ɪˈkwɪlɪbreɪt/
Phonetic: ih-KWIL-ih-brayt