# Submission ID #: 68405

# Scriptwriter Name: Sulakshana Karkala

# Project Page Link: https://review.jove.com/account/file-uploader?src=20863573

# Title: Reproducible Manufacturing of SPOT as a High-Throughput Scaffold-Based Culture Platform

# Authors and Affiliations:

# Ruonan Cao1*, Nancy T. Li2*, Chantelle B. Shing1, Zoe Kutulakos3, Cassidy M. Tan2, Alison P. McGuigan1,2

# 1Institute of Biomedical Engineering, University of Toronto

# 2Department of Chemical Engineering and Applied Chemistry, University of Toronto

# 3Department of Engineering Science, University of Toronto

# *These authors contributed equally to this work

# Corresponding Authors:

Alison P. McGuigan	(alison.mcguigan@utoronto.ca)

# Email Addresses for All Authors:

Ruonan Cao		(ruonan.cao@mail.utoronto.ca)

Nancy T. Li		(n2li@oicr.on.ca)

Chantelle Shing            (chantelle.shing@mail.utoronto.ca)

Zoe Kutulakos		(zoe.kutulakos@mail.utoronto.ca)

Cassidy M. Tan	(cassidy.tan@mail.utoronto.ca)

Alison P. McGuigan	(alison.mcguigan@utoronto.ca)

## Author Questionnaire

1. Microscopy: Does your protocol require the use of a dissecting or stereomicroscope for performing a complex dissection, microinjection technique, or something similar? No

2. Software: Does the part of your protocol being filmed include step-by-step descriptions of software usage? No

3. Filming location: Will the filming need to take place in multiple locations? No

Current Protocol Length

Number of Steps:  16

Number of Shots:  44

# Introduction

Videographer: Obtain headshots for all authors available at the filming location.

  - Ruonan Cao: Our research focuses on developing high-throughput scaffold-supported platforms for robust, reproducible patient-derived organoid cultures to improve drug screening assay workflow and help advance disease modelling.

    - INTERVIEW: Named Talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B.roll: 3.3

What technologies are currently used to advance research in your field?

  - Chantelle Shing: Automated liquid handlers, scaffold-supported hydrogel platforms, organ-on-a-chip technologies, and single-cell assays like flow cytometry and CyTOF are some of the currently available technologies.

    - INTERVIEW: Named Talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B.roll:3.1

What are the current experimental challenges?

  - Ruonan Cao: Current challenges include preserving hydrogel integrity, overcoming gel meniscus for real-time imaging, and ensuring uniform cell distribution in long-term organoid-based assays.

    - INTERVIEW: Named Talent says the statement above in an interview-style shot, looking slightly off-camera.

What advantage does your protocol offer compared to other techniques?

  - Chantelle Shing: Our protocol enables consistent scaffold-supported hydrogel loading, minimizes meniscus issues, supports long-term organoid culture, and integrates smoothly with automated liquid handlers and high-content imaging systems.

    - INTERVIEW: Named Talent says the statement above in an interview-style shot, looking slightly off-camera.

What research questions will your laboratory focus on in the future?

  - Alison McGuigan: We are most excited about using our disease modelling platforms to explore disease progression mechanisms in disease such as cancer and the development of obesity.

    - INTERVIEW: Named Talent says the statement above in an interview-style shot, looking slightly off-camera.

Videographer: Obtain headshots for all authors available at the filming location.

Ethics Title Card
This research has been approved by the Ethics Board at the University of Toronto

# Protocol

- Fabrication and Assembly of 96- and 384-SPOT Platforms for Organoid Cultures

Demonstrator: Ruonan Cao

  - To begin, take a PMMA (P-M-M-A)-patterned scaffold for either 96- or 384-SPOT (Spot) [1-TXT]. Trim the excess paper around the blue region of the scaffold, leaving a 5-millimeter white margin around the perimeter [2]. Ensure the resulting sheet measures approximately 760 millimeters by 1300 millimeters [3].

    - WIDE: Talent holding a PMMA patterned scaffold for SPOT.
TXT: PMMA: Polymethyl Methacrylate; 
SPOT: Scaffold-supported Platform for Organoid-based Tissues

    - Shot of excess paper being cut off from a blue-centered scaffold while leaving a white margin. 
Videographer’s Note: 2.1.2 is combined with 2.1.3

    - Shot of the final sheet.

  - To prepare a 96-SPOT scaffold for assembly, lay a piece of polyethylene film over a rigid acrylic support [1]. Place this film-covered support onto the work surface [2] and lay the scaffold on top of the polyethylene film [3].

    - Talent spreading polyethylene film over a large acrylic board.
Videographer’s Note: 2.2.1 is combined with 2.2.2

    - Shot of the film covered support being placed on the work surface.

    - Talent positioning the scaffold centrally on top of the polyethylene film.

  - Align the edge of a ruler between the first two rows of the scaffold to avoid tracing into the wells [1]. Place the tracing wheel at the bottom of the scaffold [2] and roll it upward to the top, guided by the ruler [3-TXT].

    - Talent carefully positioning a ruler between scaffold rows.
Videographer’s Note: 2.3.1 is combined with 2.3.2-3

    - Shot of the tracing wheel being placed at the bottom of the scaffold.

    - Talent rolling a tracing wheel along the scaffold’s inter-row space using the ruler as a guide. TXT: Repeat for all 7 inter-row and inter-column spaces

  - For a 384-SPOT scaffold, do not perform perforation [1].

    - Shot of the unperforated 384 SPOT scaffold.

  - Next, lay the scaffold with the rough side facing up on a PDMS (P-D-M-S) slab, ensuring rows run horizontally [1-TXT]. Use the priming line to determine which side is rough [2].

    - Talent orienting the scaffold correctly and placing it onto the polydimethylsiloxane slab. TXT: PDMS: Polydimethylsiloxane
Videographer’s Note: 2.5.1 is combined with 2.5.2

    - Talent pointing to the priming line.

  - Then smoothen the scaffold onto the slab to remove wrinkles or bubbles [1]. Remove the protective layer from the non-engraved side of the double-sided tape [2]. Slightly buckle the tape in the middle [3] and align the middle two columns of the tape with the scaffold [4].

    - Talent smoothing the scaffold flat.

    - Talent peeling off the tape’s protective layer.

    - Shot of the tape being buckled in the middle. 
Videographer’s Note: 2.6.3 is combined with 2.6.4

    - Talent aligning the tape to the centre of the scaffold.

  - Now, press the middle of the tape onto the scaffold to secure alignment [1]. Smooth the tape outward from the centre to affix it evenly [2].

    - Talent pressing down on the centre of the tape to make first contact.

    - Talent pressing along the tape from the centre outwards to secure it.
Videographer’s Note: 2.7.1 is combined with 2.7.2

  - Using tweezers, gently lift the scaffold from the PDMS slab [1].  Store the slab for future use [2].

    - Talent using tweezers to lift the scaffold.

    - Talent placing the slab into storage.

  - To attach the scaffold to the second well tape, flip the scaffold so the smooth, non-taped side faces up on the workbench [1]. Remove the middle protective layer from the engraved side of the second tape to expose two central columns [2-TXT].

    - Talent rotating the scaffold carefully to expose the smooth side.

    - Talent peeling back the centre section of the engraved tape. TXT: If using a non-engraved design, remove the full protective layer from one side

  - Slightly buckle the middle of the second tape and align it to the middle columns of the scaffold [1]. Then press the tape’s centre to fix it in place [2]. If engraved tape is used, remove the remaining protective layers adjacent to the exposed centre [3]. Smoothen the tape starting from the middle and moving outward [4].

    - Talent gently bending the tape and aligning it over the scaffold.

    - Talent pressing down the tape’s centre section.
Videographer’s Note: 2.10.1 is combined with 2.10.2

    - Talent peeling off adjacent protective layers.
Videographer’s Note: 2.10.3 is combined with 2.10.4

    - Talent smoothing out the tape with a firm gloved hand.

  - To attach the scaffold to the bottomless plate, remove the protective layer [1].

    - Talent removing the middle section for engraved version.

  - Align the scaffold under the bottomless plate with a lid [1]. Once aligned, press down its middle onto the plate [1]. If using engraved tape, remove adjacent layers and smooth the scaffold onto the plate outward from the centre [3].

    - Talent aligning scaffold to the underside of the bottomless plate. 
Videographer’s Note: 2.12.1 is combined with 2.12.2

    - Talent pressing the scaffold onto the plate underside.

    - Talent peeling additional tape layers and smoothing scaffold.

  - To attach the scaffold to the polycarbonate film, use tweezers to carefully loosen the protective layer from one side of the polycarbonate film [1]. Then slowly peel off the protective layer, without causing any indentations in the film [2]. Repeat the process for the second side [3]. Then set the film aside on the workbench [4].

    - Shot of the protective layer being loosened from one side of the polycarbonate film, with tweezers. 
Videographer’s Note: 2.13.1 is combined with 2.13.2-4

    - Talent peeling off the protective film layer.

    - Talent peeling off second side.

    - Talent laying the film aside on the workbench.

  - Peel the protective tape layer from the plate bottom and press the polycarbonate film onto the scaffold from the center outwards [1]. Then firmly press the polycarbonate film onto the scaffold to ensure each well has a defined border [2]. Using a precision knife , carefully cut off any excess material from the bottom of the plate [3].

    - Talent removing tape and pressing the polycarbonate film into position.
Videographer’s Note: 2.14.1 is combined with 2.14.2

    - Talent using hands to seal the film over the plate.

    - Talent trimming edges neatly using a knife .

  - After full assembly, place the 96-SPOT plate into a clear resealable plastic bag [1] and take it outside the biosafety cabinet [2].

    - Talent placing the plate in a resealable bag.

    - Talent moving it outside the biosafety cabinet.

  - Place a rigid acrylic support underneath the plate [1] and clamp both at opposite corners [2-TXT]. Store the plate in a clean, dry space until further use [3].

    - Talent positioning the acrylic support .
Videographer’s Note: 2.16.1 is combined with 2.16.2

    - Talent clamping the corners. TXT: Keep clamped for at least 30 min on each corner before use

    - Talent placing the assembled plate on a clean shelf or storage drawer.
Videographer’s Note: shot involves unclamping before storing, and then showing 384 spot variation

# Results

- Results

  - No media leakage or exchange was observed when alternating wells in the 384-SPOT plate were filled with fluorescein and PBS during a 30-day test period, confirming the efficacy of the PMMA barrier in maintaining well-to-well isolation [1].

    - LAB MEDIA: Figure 7A and B. Video Editor: Please show A first and then B

  - GFP-expressing pancreatic tumor organoids seeded into 96-SPOT plates remained viable and expanded progressively from day 0 through day 12 of culture [1].

    - LAB MEDIA: Figure 7C. Video editor: Highlight the top row images corresponding to “OT2” from day 0 to Day 12

  - On day 12, SPOT-grown organoids displayed strong cytokeratin 19 [1] and zonula occludens-1 expression, along with the presence of internal lumen structures [2].

    - LAB MEDIA: Figure 7D. Video editor: Please highlight the top row corresponding to “CK19”

    - LAB MEDIA: Figure 7D. Video editor: Please highlight the bottom row corresponding to “ZO-1”. Also emphasise the area pointed at by the white arrows in the left most image in the row

  - Suboptimal and optimal tissue seeding outcomes in 384-SPOT plates were visually distinguishable by edge definition and cell distribution uniformity [1].

    - LAB MEDIA: Figure 8A. Video editor: Highlight the image labelled “Not optimal”

  - Consistently uniform seeding was achieved across the entire 96-SPOT and 384-SPOT plates using the automated liquid handler [1].

    - LAB MEDIA: Figure 8B and C.

# Pronunciation Guide:

# Plymethyl Methacrylate (PMMA)

# Pronunciation link: https://www.howtopronounce.com/pmma justpronounce.com+10How To Pronounce+10How To Pronounce+10

# IPA: /ˌpɑliˌmɛθəl mɛθəˈkrɪleɪt/

# Phonetic spelling: PAH-lee-meth-uhl meth-uh-KRIL-ayt

# Polydimethylsiloxane (PDMS)

# Pronunciation link: https://www.howtopronounce.com/polydimethylsiloxane Forvo.com+8How To Pronounce+8YouTube+8

# IPA: /ˌpɑliˌdaɪˌmɛθəlˌsɪlɒkˌseɪn/

# Phonetic spelling: PAH-lee-dye-MEH-thul-sil-OX-ayn

# Hydrogel

# Pronunciation link: https://www.merriam-webster.com/dictionary/hydrogel YouGlish+14YouGlish+14YouTube+14Merriam-Webster+13Merriam-Webster+13WordReference+13

# IPA: /ˈhaɪdroʊˌdʒɛl/

# Phonetic spelling: HY-droh-jel

# Organoid

# Pronunciation link: https://www.merriam-webster.com/medical/organoid Definitions+15Merriam-Webster+15Merriam-Webster+15

# IPA: /ˈɔrɡəˌnɔɪd/

# Phonetic spelling: OR-guh-noid

# Meniscus

# Pronunciation link: https://www.merriam-webster.com/dictionary/meniscus Merriam-Webster+12How To Pronounce+12YouTube+12Merriam-Webster+15Merriam-Webster+15OpenMD+15

# IPA: /məˈnɪskəs/

# Phonetic spelling: muh-NIS-kuhs

# Fluorescein

# Pronunciation link: https://www.merriam-webster.com/dictionary/fluorescein Pronounce Kiwi+2How To Pronounce+2Cambridge Dictionary+2Merriam-Webster+5Merriam-Webster+5Merriam-Webster+5

# IPA: /flu̇ˈɒr-əˌsin/ or /flu̇ˈrɛs-in/

# Phonetic spelling: floo-OR-uh-seen or floo-ress-een

# Cytokeratin

# Pronunciation link: https://www.merriam-webster.com/medical/cytokeratin Merriam-Webster+1Merriam-Webster+1Merriam-Webster+13Merriam-Webster+13Oxford English Dictionary+13

# IPA: /ˌsaɪtoʊˈkɛrətɪn/

# Phonetic spelling: SIGH-toh-KEHR-uh-tin

# Epithelium

# Pronunciation link: https://www.merriam-webster.com/dictionary/epithelium Merriam-Webster

# IPA: /ˌɛpəˈθiliəm/

# Phonetic spelling: EH-puh-THEE-lee-um

# Fluorescence

# Pronunciation link: https://www.merriam-webster.com/dictionary/fluorescence How To Pronounce+15YouTube+15Merriam-Webster+15Merriam-Webster+6Merriam-Webster+6Merriam-Webster+6

# IPA: /ˌfluːəˈrɛsəns/

# Phonetic spelling: floo-uh-RESS-ens

# CyTOF (time-of-flight cytometry)

# Pronunciation link: No confirmed link found

# IPA: /ˈsaɪtoʊf/

# Phonetic spelling: SIGH-tohf