# Submission ID #: 68499

# Scriptwriter Name: Poornima G

# Project Page Link: https://review.jove.com/account/file-uploader?src=20892243

# Title: Scalable Step-by-Step Approach of Sustainable Bioplastic Production from Food Waste

# Authors and Affiliations:

# Xueyao Zhang1, Mingxi Wang1, Yebo Li2, Stephanie Lansing3, Zhi-Wu Wang1

# 1Department of Biological Systems Engineering, Virginia Polytechnic Institute and State University

# 2Quasar Energy Group

# 3Department of Environmental Science and Technology, University of Maryland

# Corresponding Authors:

# Zhi-Wu Wang		wzw@vt.edu

# Email Addresses for All Authors:

Xueyao Zhang		xueyao@vt.edu

Mingxi Wang		mingxiwang@vt.edu

Yebo Li			yli@quasareg.com

Stephanie Lansing	slansing@umd.edu

# Zhi-Wu Wang		wzw@vt.edu

## Author Questionnaire

1. Microscopy: Does your protocol require the use of a dissecting or stereomicroscope for performing a complex dissection, microinjection technique, or something similar?  No

2. Software: Does the part of your protocol being filmed include step-by-step descriptions of software usage?  Yes

Videographer: Please record the computer screen for the shots labeled as SCREEN

3. Filming location: Will the filming need to take place in multiple locations?   No

Current Protocol Length

Number of Steps:  23

Number of Shots:  46 (5 SC)

# Introduction

Videographer: Obtain headshots for all authors available at the filming location.

  - Xueyao Zhang: We developed a scalable process to convert food waste into biodegradable plastic using halophilic microbes, which addresses both plastic pollution and organic waste challenges.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B-roll: 2.3.1

What are the current experimental challenges in your field of research?

  - Mingxi Wang: Key challenges include managing feedstock variability, scaling up without contamination, and achieving high-purity bioplastics while avoiding expensive or hazardous chemical processes.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B-roll: 2.5.1

What significant findings have you established in your field?

  - Xueyao Zhang: We achieved 93% recovery of biodegradable plastic from food waste using only water, offering a chemical-free solution for downstream processing.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B-roll: 3.3.2

How will your findings advance research in your field?

  - Mingxi Wang: Our work demonstrates a viable path from lab to pilot scale for converting food waste into high-quality bioplastics, paving the way for industrial implementation and broader circular economy practices.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B-roll: 4.3.1

Videographer: Obtain headshots for all authors available at the filming location.

# Protocol

- Volatile Fatty Acid (VFA) Production Through Arrested Anaerobic Digestion (aAD)

Demonstrator: Mingxi Wang

  - To begin, add 10 kilograms of food waste into a 5-gallon bucket [1]. Pour 2.5 liters of water into the bucket containing the food waste [2]. Connect the blender to a power source [3]. Submerge the blade into the food waste and water mixture [4], then press the Start button to begin blending [5]. Continue blending for at least 30 minutes until the mixture is fully homogenized [6].

    - WIDE: Talent placing 10 kilograms pre-weighed food waste into a 5-gallon bucket. NOTE: The action was modified

    - Talent pouring 2.5 liters of water into the bucket.

    - Talent plugging the blender into a power source.

    - Talent lowering the blender blade into the mixture.

    - Talent pressing the Start button on the blender.

    - Close-up of the mixture being blended to a smooth consistency.

  - Prior to feeding, temporarily increase the digester stirring speed from 150 revolutions per minute to 200 revolutions per minute and maintain this speed for 20 minutes [1].

    - Shot of the stirring speed setting being changed.

  - Then, open the discharge valve at the bottom of the pilot anaerobic acidogenic digester and release approximately 26.7 liters of digestate [1]. Collect the discharged digestate into labeled buckets [2] and store them at 4 degrees Celsius for volatile fatty acid analysis and subsequent solid-liquid separation [4-TXT].

    - Talent opening the discharge valve and releasing digestate into buckets.

    - Talent positioning labeled buckets under the valve to collect the digestate.

    - Talent placing collected buckets in a refrigerator at 4 °C. TXT: Organic loading rate (OLR): 2.5 g VS/L-day; VS of the food waste slurry:  ~14.5%

  - Now, add water to a separate bucket containing 4.1 kilograms of the wet food waste slurry until the total volume reaches 26.7 liters [1]. Using a peristaltic pump, feed the 26.7 liters of food waste slurry into the anaerobic acidogenic digester [2].

    - Talent adding water to the slurry to bring total volume to 26.7 liters.

    - Talent operating a peristaltic pump to transfer the slurry into the digester.

  - Turn off the peristaltic pump and unplug it from the power source [1]. Reset the stirring speed of the pilot digester and continue stirring for 30 minutes [2]. Add sodium hydroxide pellets proportionally to the digestate volume to adjust the pH to 5.5 [3].

    - Talent switching off the pump and unplugging it.

    - Talent resetting the stirring speed. NOTE: The action was modified

    - Talent adding measured sodium hydroxide pellets to the digester.

  - Check the pilot digester to ensure all valves are fully closed [1].

    - Talent inspecting the digester.

- Recovering VFA for Polyhydroxyalkanoate (PHA) Fermentation

  - Turn on the main power switch of the disc centrifuge [1] and wait until the word STANDSTILL (stand still) appears on the Human-Machine Interface system screen [2]. Check that the lubricant oil level is above the minimum threshold [3].

    - Talent switching on the main power of the disc centrifuge.

    - SCREEN: Show STANDSTILL status text appearing on the HMI screen. Videographer: Please record the computer screen for the shots labeled as SCREEN

    - Talent inspecting the oil level indicator on the centrifuge.

  - Open the valve of the water utility line and adjust the pressure to 45 pounds per square inch [1] and then open the valve of the air utility line. Adjust the pressure to 90 pounds per square inch [2].

    - Talent opening the water utility line valve and setting the pressure gauge to 45 psi.

    - Talent opening the air utility valve and setting the gauge to 90 psi.

  - Now, press the Green button on the HMI screen to start the production process of the disc centrifuge [1]. Wait for the centrifuge to complete its automated checks [2].

    - SCREEN: Show the Green button being pressed on the HMI screen.

    - SCREEN: Display the system performing pre-checks with progress or status bars visible.

  - Monitor the system until it reaches the full set speed, indicated by the word STANDBY (stand by) on the HMI system screen [1].

    - SCREEN: Show the word STANDBY appearing on the HMI system as the centrifuge stabilizes at full speed.

  - Ensure the inlet hose is fully submerged in the container holding discharged digestate [1] and connect the supernatant outlet pipe to an empty 5-gallon bucket for supernatant collection [2]. Then, attach the solid outlet pipe to a separate empty bucket to collect the residual solids [3].

    - Talent placing the inlet hose into the digestate container.

    - Talent attaching the supernatant outlet to a labeled 5-gallon bucket.

    - Talent attaching the solid outlet to another labeled empty bucket.

  - Using a peristaltic pump, begin feeding the digestate to the inlet of the disc centrifuge [1]. Simultaneously, press the PROD (production) button on the HMI screen [2].

    - Talent operating the peristaltic pump to deliver digestate to the centrifuge.

    - SCREEN: Show the PROD button being clicked on the HMI screen.

  - After 30 minutes of operation, press the Discharge button on the HMI system screen to release both solids and supernatant into their respective buckets [1].

    - Show the Discharge button being pressed and the output flowing into labeled buckets.

- Pilot-Scale PHA Fermentation and PHA Downstream Recovery

Demonstrators: Xueyao Zhang, Mingxi Wang

  - Turn on the water bath heating switch and set the temperature to 37 degrees Celsius [1]. Then, turn adjust the speed of the stirrer to 150 revolutions per minute [2].

    - Talent flipping the switch on the water bath and adjusting the temperature to 37 degrees Celsius.

    - Talent setting the stirrer to 150 revolutions per minute.

  - Turn on the air pump of the pilot fermenter [1] to aerate 40-liters of food waste digestate supernatant, prepared using the optimal dilution factor with supplementation and inoculation, in the 50-liter glass fermenter [2].

    - Talent switching on the air pump.

    - Shoot of the liquid level of 40 liters.

  - Collect a fermentation sample daily [1] and measure the optical density at 600 nanometers [2].

    - Talent using a syringe to collect a sample and adding it into a 96-well plate.

    - Talent placing the sample in the 96-well plate in the spectrophotometer to measure OD.

  - For downstream recovery, feed the Haloferax mediterranei fermentation broth to the disc centrifuge to separate the salty supernatant and the cells [1]. Collect the harvested cells from the solid outlet for subsequent cell lysis [2].

    - Talent pumping in fermentation broth into the inlet of the disc centrifuge.

    - Talent collecting the solids from the outlet into a labeled container for cell lysis.

  - Resuspend the harvested cells in water at a ratio of 100 milliliters per gram of wet cells [1] and mix the suspension at 150 revolutions per minute for 2 hours at room temperature to induce cell lysis by osmotic pressure shock [2].

    - Talent adding measured water to harvested cells in.

    - Talent placing the beaker on a magnetic stirrer and setting it to 150 revolutions per minute.

  - Centrifuge the lysed cell suspension at 10,000 g for 30 minutes [1] and collect the PHA or PHA granules into a fresh container [2].

    - Talent loading the lysed suspension in centrifuge tubes into a centrifuge.

    - Talent collecting the PHA or PHA granules into a separate container using a spatula. NOTE: The action was modified

  - Freeze-dry the PHA granules at minus 50 degrees Celsius for approximately 48 hours until a constant weight is achieved to obtain crude PHA powder [1].

    - Talent placing PHA granules in the freeze dryer.

  - Next, add ethanol to the crude PHA powder at a ratio of 10 milliliters per gram to eliminate residual impurities [1]. Centrifuge the mixture at 10,000 g for 30 minutes to collect purified PHA granules [2-TXT].

    - Talent adding ethanol to the crude powder in a conical tube using a pipette.

    - Talent placing the sample tube in a centrifuge. TXT: Dispose of the supernatant

  - Finally, freeze-dry the purified PHA pellets at minus 50 degrees Celsius [1] for approximately 48 hours to obtain final purified PHA powder [2]. NOTE: VO modified to accommodate the extra shot

    - Talent placing the sample in the freeze dryer.

Added shot: Talent presenting the purified PHA powder and showcasing a final product sample.

# Results

- Results

  - After bench-scale PHA fermentation, Haloferax mediterranei showed the highest optical density at 600 nanometers and intracellular PHA content when cultured in food waste digestate supernatant diluted two times [1], while no growth or PHA production occurred in the undiluted medium, confirming the presence of inhibitory compounds [2].

    - LAB MEDIA: Figure 7. Video editor: Highlight the line labeled "2-time dilution" in A and bar “2” in B.

    - LAB MEDIA: Figure 7. Video editor: Highlight the line labeled "1-time dilution" in A and bar labeled "1" in B.

  - During pilot-scale fermentation, optical density at 600 nanometers peaked at 192 hours [1], and intracellular PHA content peaked at 120 hours [2].

    - LAB MEDIA: Figure 8A. Video editor: Highlight the peak of the curve around 192 hours.

    - LAB MEDIA: Figure 8B. Video editor: Highlight the bar at “120” hours, which reaches the tallest height.

  - The PHA powder recovered through the 2 hour water treatment exhibited a purity of around 84% with the colour indicating the presence of impurities, such as carotenoids [1, 2].

    - LAB MEDIA: Figure 6A. Video editor: Highlight the reddish-pink colored powder at the center of the image. Show 5.3.1 and 5.3.2 side by side

    - LAB MEDIA: Table 5. Video editor: Highlight the box showing 84.

  - Ethanol purification after water-based extraction improved PHA purity to around 96%, resulting in a white powder free of pigment impurities [1, 2].

    - LAB MEDIA: Figure 6B. Video editor: Highlight the white powder in the center of the image. Show 5.4.1 and 5.4.2 side by side

    - LAB MEDIA: Table 5. Video editor: Highlight the box showing 96.

Pronunciation guide:

### 1. Anaerobic

- Pronunciation link: https://www.merriam-webster.com/dictionary/anaerobic

- IPA: /ˌæn.əˈroʊ.bɪk/

- Phonetic Spelling: an-uh-ROH-bikmerriam-webster.com+4merriam-webster.com+4merriam-webster.com+4

### 2. Acidogenic

- Pronunciation link: https://www.merriam-webster.com/medical/acidogenic

- IPA: /ˌæs.ɪ.dəˈdʒɛn.ɪk/

- Phonetic Spelling: as-ih-doh-JEN-ikmerriam-webster.com+1merriam-webster.com+1

### 3. Peristaltic

- Pronunciation link: https://www.merriam-webster.com/dictionary/peristaltic

- IPA: /ˌpɛr.əˈstɔːl.tɪk/

- Phonetic Spelling: per-uh-STAWL-tikmerriam-webster.com+1merriam-webster.com+1

### 4. Digester

- Pronunciation link: https://www.merriam-webster.com/dictionary/digester

- IPA: /daɪˈdʒɛs.tər/

- Phonetic Spelling: dy-JESS-termerriam-webster.commerriam-webster.com

### 5. Optical

- Pronunciation link: https://www.merriam-webster.com/dictionary/optical

- IPA: /ˈɑːp.tɪ.kəl/

- Phonetic Spelling: OP-tih-kuhlmerriam-webster.com+1merriam-webster.com+1

### 6. Polyhydroxyalkanoate

- Pronunciation link: No confirmed link found

- IPA: /ˌpɒl.i.haɪˌdrɒk.siˌæl.kəˈnoʊ.eɪt/

- Phonetic Spelling: pol-ee-hy-DROK-see-al-kuh-NOH-atemerriam-webster.com

### 7. Haloferax mediterranei

- Pronunciation link: No confirmed link found

- IPA: /ˌheɪ.loʊˈfɛr.æks ˌmɛd.ɪ.təˈreɪ.ni.aɪ/

- Phonetic Spelling: HAY-loh-FER-aks MED-ih-tuh-RAY-nee-eye

### 8. Peristalsis

- Pronunciation link: https://www.merriam-webster.com/dictionary/peristalsis

- IPA: /ˌpɛr.əˈstɔːl.sɪs/

- Phonetic Spelling: per-uh-STAWL-sismerriam-webster.com

### 9. Densitometer

- Pronunciation link: https://www.merriam-webster.com/dictionary/densitometer

- IPA: /ˌdɛn.sɪˈtɒm.ɪ.tər/

- Phonetic Spelling: den-sih-TOM-ih-termerriam-webster.com

### 10. Acetogen

- Pronunciation link: https://www.merriam-webster.com/dictionary/acetogen

- IPA: /əˈsiː.tə.dʒən/

- Phonetic Spelling: uh-SEE-tuh-jenmerriam-webster.com