# Submission ID #: 68540

# Scriptwriter Name: Poornima G

# Project Page Link: https://review.jove.com/account/file-uploader?src=20904748

# Title: Residue-Free Fabrication of van der Waals Heterostructures of Two-Dimensional Materials

# Authors and Affiliations:

# Minyoung Lee*, Changho Kim*, Jae Hun Seol1

# 1School of Mechanical and Robotics Engineering, Gwangju Institute of Science and Technology

*These authors contributed equally

# Corresponding Authors:

# Jae Hun Seol		jhseol@gist.ac.kr

# Email Addresses for All Authors:

# Minyoung Lee		minyounglee@gm.gist.ac.kr

# Changho Kim		umtoss530@gist.ac.kr

# Jae Hun Seol		jhseol@gist.ac.kr

## Author Questionnaire

1. Microscopy: Does your protocol require the use of a dissecting or stereomicroscope for performing a complex dissection, microinjection technique, or something similar?  No

2. Software: Does the part of your protocol being filmed include step-by-step descriptions of software usage?  No

3. Filming location: Will the filming need to take place in multiple locations?   No

Current Protocol Length

Number of Steps:  13

Number of Shots:  18

# Introduction

Videographer: Obtain headshots for all authors available at the filming location.

  - Changho Kim: We aim to develop a residue-free fabrication method for 2D heterostructures that avoids exposure to any residues and temperature changes, while ensuring the devices remain clean and high quality.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B-roll: 2.3.1

What are the current experimental challenges?

  - Minyoung Lee: Transferring individual 2D flakes for multi-stacked heterostructures is technically challenging, and polymers or solvents often leave residues at the interface, disrupting clean stacking between layers.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B-roll: 3.1.1

What significant findings have you established in your field?

  - Changho Kim: We established a novel method that enables precise 2D heterostructure assembly using only van der Waals forces through bottom-up, top-down, and modular stacking techniques.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B-roll: 4.2.1

What research questions will your laboratory focus on in the future?

  - Jae Hun Seol: We plan to apply this method to various applications, such as optical or gas sensors, that require complex heterostructures with clean and high-quality interfaces.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B-roll: 2.2.1

Videographer: Obtain headshots for all authors available at the filming location.

# Protocol

- Acquiring the Residue-Free Region

Demonstrator: Minyoung Lee

Videographer: Please film the steps 2.1 to 2.5

  - To begin, prepare a piece of bulk crystal using a cotton swab and a razor blade [1].

    - WIDE: Talent using a razor blade and cotton swab to extract a section of bulk crystal.

  - Attach the prepared crystal onto the adhesive surface of a pre-exfoliation stamp [1] and place another pre-exfoliation stamp on top of the crystal to form a sandwich configuration [2].

    - Talent placing the crystal onto the sticky surface of the first stamp.

    - Talent aligning and pressing a second stamp over the crystal to make a sandwich.

  - Gently exfoliate the sandwiched crystal [1] and repeat this process 3 to 5 times to obtain a clean and uniform sub-micron-thick crystal [2].

    - Talent lifting and pressing the stamps repeatedly to exfoliate the crystal.

    - Shot of a clean and uniform sub-micron-thick crystal.

  - Now, place the pre-exfoliated crystal onto the sample stage [1] and secure the tape stamp with a tilt angle of at least 5 degrees onto the magnetic plate of the stamp manipulator using a magnet [2].

    - Talent positioning the exfoliated crystal on the flat sample stage.

    - Talent attaching the tilted tape stamp to the magnetic holder using a small magnet.

  - Align the tape stamp above the pre-exfoliated crystal by adjusting the sample stage [1].

    - Talent slowly turning knobs or sliding controls to center the tape stamp over the crystal.
AUTHOR’S NOTE: Please use the shot showing adjustment of the sample stage’s x-axis. Although we also recorded a version adjusting the stamp manipulator’s x-axis, this should not be used

  - Attach the tape stamp to the top surface of the crystal by adjusting the stamp manipulator in the negative Z direction and gently exfoliate the thin residue-free region by adjusting the stamp manipulator in the positive Z direction [1].

    - SCOPE: Video 1.avi 00:00 – 00:11

  - Adhere the residue-free region firmly to the substrate by adjusting the stamp manipulator in the negative Z direction [1].

    - SCOPE: Video 2.avi 00:00 – 00:02 and FILE: Video 3.avi 00:04 – 00:04

  - Then, exfoliate the single flake by adjusting the stamp manipulator in the positive Z direction [1].

    - SCOPE: Video 2.avi 00:04 – 00:08 and FILE: Video 3.avi 00:06 – 00:12

- Fabrication of Residue-Free van der Waals Heterostructure Assemblies Through Bottom-Up Stacking Process

  - Pick up the molybdenum disulfide flake with the MoS2 (M-O-S-2) residue-free stamp [1-TXT] and release it onto the h-BN (H-B-N) flake, to assemble the structure [2-TXT].

    - SCOPE: Video 4.avi 00:00 – 00:05. TXT: MoS2: Molybdenum Disulfide

    - SCOPE: Video 4.avi 00:08 – 00:14 TXT: h-BN: Hexagonal Boron Nitride

  - Pick up another h-BN flake and release it on the MoS2 and h-BN structure [1].

    - SCOPE: Video 4.avi 00:16 – 00:31

  - Next, pick up the h-BN flake using the MoS2 residue-free stamp [1].

    - SCOPE: Video 5.avi 00:04 – 00:07

  - Use the picked-up HBN flake to cover the MoS2 flake, and then pick up the MoS2 flake with the already picked-up h-BN flake, forming a h-BN and MoS2 structure [1].

    - SCOPE: Video 5.avi 00:08 – 00:12

  - Finally, release the combined structure onto another h-BN flake [1] and then release the Hetero B onto the Hetero A [2].

    - SCOPE: Video 5.avi 00:13 – 00:20

    - SCOPE: Video 6.avi 00:04 – 00:11

# Results

- Results

  - The symmetrical hexagonal atomic structure of residue-free MoS2 was confirmed using high-resolution transmission electron microscopy and selected area electron diffraction pattern analysis [1].

    - LAB MEDIA: Figure 7.

  - Energy-dispersive X-ray spectroscopy mapping revealed strong molybdenum and sulfur signals [1] and minimal carbon and oxygen, confirming the absence of polymer residue and oxidation on the molybdenum disulfide flakes [2].

    - LAB MEDIA: Figure 7A. Video editor: Highlight the EDS maps showing MO and S images.

    - LAB MEDIA: Figure 7A. Video editor: Highlight the EDS maps showing C and O images.

  - Atomic force microscopy analysis showed that the thicknesses of transferred h-BN and MoS2 flakes were 18.34 nanometers and 5.27 nanometers, respectively [1].

    - LAB MEDIA: Figure 8. Video editor: Highlight the values 18.34 nm and 5.27 nm in B and E.

  - The root-mean-square roughness values of 0.143 nanometers for h-BN and 0.153 nanometers for MoS2 confirmed excellent flatness with minimal surface irregularities [1].

    - LAB MEDIA: Figure 8. Video editor: Highlight the blue boxes displaying the Rq values 0.143 nm and 0.153 nm in B and E.

  - Raman spectroscopy analysis revealed peak positions at approximately 1365 and 383 inverse centimeters for h-BN and MoS2, respectively, indicating strain-free transfer [1].

    - LAB MEDIA: Figure 8. Video editor: Highlight the peaks E2g in C and E12g in F.

  - Distinct manipulation methods allowed successful assembly of the heterostructures via both bottom-up and top-down stacking [1].

    - LAB MEDIA: Figure 9. Video editor: Highlight the labeled regions “Hetero A” and “Hetero B” in panels A and B.

  - The assembled heterostructures exhibited randomly distributed gas-filled blisters at the heterointerface without any applied force [1].

    - LAB MEDIA: Figure 10B. Video editor: Highlight the optical image of “as assembled” showing “gas blisters”.

  - Application of increasing forces from 30 to 1000 nano-newtons progressively reduced blister size and count [1].

    - LAB MEDIA: Figure 10B. Video editor: Sequentially highlight the images and the corresponding graphs from “30” to “1000 nN".

Pronunciation Guide:

1. van der Waals

Pronunciation link (Merriam-Webster):
https://www.merriam-webster.com/dictionary/van%20der%20Waals
IPA: /væn dər ˈvɑlz/
Phonetic Spelling: van-der-VAHLZ

2. heterostructure

Pronunciation link (Merriam-Webster — hetero-):
https://www.merriam-webster.com/dictionary/hetero
(and structure)
IPA: /ˌhɛtərəʊˈstrʌktʃər/ → American /ˌhɛtərəˈstrʌktʃɚ/
Phonetic Spelling: HET-uh-roh-STRUK-cher

3. molybdenum disulfide (MoS₂)

Pronunciation link (Merriam-Webster — molybdenum):
https://www.merriam-webster.com/dictionary/molybdenum
IPA: /məˈlɪbdəˌnəm daɪˈsʌlfaɪd/
Phonetic Spelling: muh-LIB-duh-num die-SUL-fide

4. hexagonal boron nitride (h-BN)

Pronunciation link (Merriam-Webster — hexagonal):
https://www.merriam-webster.com/dictionary/hexagonal
IPA: /hɛkˈsæɡənəl ˈbɔrɒn naɪˌtraɪd/
Phonetic Spelling: hek-SAG-uh-nul BOR-on NY-tride

5. exfoliate

Pronunciation link (Merriam-Webster):
https://www.merriam-webster.com/dictionary/exfoliate
IPA: /ɪkˈsfoʊliˌeɪt/
Phonetic Spelling: ik-SFOH-lee-ayt

6. nanometer

Pronunciation link (Merriam-Webster):
https://www.merriam-webster.com/dictionary/nanometer
IPA: /ˈnænəˌmiːtər/
Phonetic Spelling: NAN-uh-mee-ter

7. atomic force microscopy

Pronunciation link (Merriam-Webster — atomic):
https://www.merriam-webster.com/dictionary/atomic
Pronunciation link (Merriam-Webster — microscopy):
https://www.merriam-webster.com/dictionary/microscopy
IPA: /əˈtɑmɪk fɔrs maɪˈkrɑskəpi/
Phonetic Spelling: uh-TOM-ik force my-KROS-kuh-pee

8. Raman spectroscopy

Pronunciation link (Merriam-Webster — Raman):
https://www.merriam-webster.com/dictionary/raman
Pronunciation link (Merriam-Webster — spectroscopy):
https://www.merriam-webster.com/dictionary/spectroscopy
IPA: /ˈrɑːmɑn spɛkˈtrɑskəpi/
Phonetic Spelling: RAH-man spek-TRAW-skuh-pee

9. energy-dispersive X-ray spectroscopy (EDS/XPS)

Pronunciation link (Merriam-Webster — dispersive):
https://www.merriam-webster.com/dictionary/dispersive
IPA: /ˈɛnərdʒi dɪˈspɜrsɪv ɛks reɪ spɛkˈtrɑskəpi/
Phonetic Spelling: EN-er-jee dis-PUR-siv ex RAY spek-TRAW-skuh-pee

10. nanonewton

Pronunciation link (Merriam-Webster — newton):
https://www.merriam-webster.com/dictionary/newton
IPA: /ˈnænəˈnuˌtɑn/
Phonetic Spelling: NAN-uh-NEW-ton