# Submission ID #: 68714

# Scriptwriter Name: Sulakshana Karkala

# Project Page Link: https://review.jove.com/account/file-uploader?src=20957818

# Title: Optimizing and Evaluating Hand-Drawing and Wet-Spinning for Recombinant Spider Silk Fiber Production

# Authors and Affiliations:

# Anupama Ghimire1*, Hina Batool1*, Sara Evans2*, Suad Rashid1*, Donovan L. Rainey1, Andrew A.Y. Chen1, Xiang-Qin Liu1, Jan K. Rainey1-3

# 1Department of Biochemistry & Molecular Biology, Dalhousie University

# 2Department of Chemistry, Dalhousie University

# 3School of Biomedical Engineering, Dalhousie University

# *These authors contributed equally

# Corresponding Authors:

# Jan K. Rainey					jan.rainey@dal.ca

# Email Addresses for All Authors:

Anupama Ghimire				an696021@dal.ca

Hina Batool					hn701981@dal.ca

Sara Evans					sara.evans@dal.ca

Suad Rashid					suad.rashid@dal.ca

Donovan L. Rainey				donovanlrainey@gmail.com

Andrew A.Y. Chen				an259012@dal.ca

Xiang-Qin Liu					paul.liu@dal.ca

Jan K. Rainey					jan.rainey@dal.ca

## Author Questionnaire

1. Microscopy: Does your protocol require the use of a dissecting or stereomicroscope for performing a complex dissection, microinjection technique, or something similar?  Yes

If Yes, can you record movies/images using your own microscope camera?

Yes

4.4.2., 4.5.1., 4.6.2.

Authors: Please create scope videos of the shots labeled as SCOPE and upload the files to your project page as soon as possible: https://review.jove.com/account/file-uploader?src=20957818

2. Software: Does the part of your protocol being filmed include step-by-step descriptions of software usage?  Yes

Videographer: Please film the computer screen for all shots labeled SCREEN

3. Filming location: Will the filming need to take place in multiple locations?   Yes

11 floors (same building)

Current Protocol Length

Number of Steps:  20

Number of Shots:  55

# Introduction

Videographer: Obtain headshots for all authors available at the filming location.

REQUIRED: What is the scope of your research? What questions are you trying to answer?

  - Jan Rainey: We investigate understudied spider silk proteins to understand their biophysical properties before and after self-assembly, enabling rational engineering of advanced silk-based biomaterials.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera

What are the current experimental challenges?

  - Suad Rashid: Current experimental challenges include purifying high-molecular-weight spidroins, solubilizing silk proteins for fiber formation, and controlling humidity and temperature during production.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera

What research gap are you addressing with your protocol?

  - Hina Batool: Our protocol overcomes the challenge of obtaining pure, consistent spider silk fibers by enabling individual silk production for accurate property characterization.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera

What advantage does your protocol offer compared to other techniques?

  - Sara Evans: Our protocol allows us greater flexibility when choosing a protein. We can spin recombinant proteins that combine multiple silk types or fuse a silk protein to a biologically relevant peptide.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera

Videographer: Obtain headshots for all authors available at the filming location.

# Testimonial Questions (OPTIONAL):

# Videographer: Please capture all testimonial shots in a wide-angle format with sufficient headspace, as the final videos will be rendered in a 1:1 aspect ratio. Testimonial statements will be presented live by the authors, sharing their spontaneous perspectives.

What problem in your field of research does your JoVE article address?

  - Jan Rainey, Professor, Dalhousie University: (authors will present their testimonial statements live)

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera

How does the video format of your article help you to share your work with the broader scientific community?

  - Jan Rainey, Professor, Dalhousie University: (authors will present their testimonial statements live)

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera

# Protocol

- Hand-Pulling and Mounting of Spider Silk Fibers for Characterization

Demonstrator: Suad Rashid

  - To begin, prepare a C-shaped paper frame with a 1 by 0.5-centimeter window [1]. Place it on a glass slide [2]. Then, secure the upper portion of the frame to the slide using adhesive tape [3].

    - WIDE: Talent cutting a C-shaped paper holder from 3 x 2 cm rectangular piece of paper.

    - Shot of the C-shaped holder being taped on a microscope slide.

    - Talent placing double-sided tape on either side of the 1 cm gap.

  - Affix transparent tape to one arm of the frame to create a hydrophobic surface for dope solution deposition [1]. Then attach double-sided tape to the opposite arm to secure the fiber [2].  NOTE: Not filmed

    - Shot of transparent tape being fixed to one arm of the frame.

    - Shot of double sided tape being placed on the opposite arm of the frame.

  - Next, deposit ten to twenty microliters of spider silk protein spinning dope solution onto the transparent tape at room temperature [1]. Submerge a 200-microliter plastic pipette tip into the dope droplet [2] and draw it vertically out at a constant speed of approximately 6 millimeters per second to pull fibers [3].

    - Talent pipetting 10 to 20 µL dope solution onto transparent tape

    - Shot of the pipette tip being submerged into droplet.

    - Shot of tip pulling fiber from solution.

  - Now, guide the hand-pulled fiber across the frame window [1], attach it to the double-sided tape, and allow it to dry at room temperature [2-TXT]. Secure both ends of the dried fiber with additional tape [3]. Focus on the portion of the fiber that spans the paper frame for subsequent characterization [4].

    - Talent guiding the hand-pulled fibre across the frame window.

    - Shot of the fibre being attached onto the window with double-sided tape.

    - Talent securing both ends of fiber with tape

    - Talent pointing to fibre spanning the paper frame.  NOTE: Shots 2.3.3, 2.4.1 and 2.4.2 were combined as one shot.

- Wet-Spinning and Post-Spin Processing of Synthetic Spider Silk Fibers

Demonstrators: Hina Batool

  - For wet spinning, centrifuge the spider silk dope solution at 7830 rpm for thirty minutes at room temperature [1] and collect the supernatant for fiber spinning [2].

    - Talent placing a labelled tube with dope solution in a centrifuge.

    - Shot of the supernatant being pipetted out of the centrifuged tube.

  - Load 50 to 80 microliters of spinning dope solution into a syringe that serves as a spinneret [1]. Secure the syringe in a syringe pump [2] and set the extrusion rate to 0.600 milliliters per hour using the pump controls [3].

    - Talent drawing the dope solution into a syringe.

    - Shot of the syringe being placed in a syringe pump.

    - The pump extrusion rate is being set to six hundred microliters per hour.

  - Now prepare a coagulation bath comprising ninety-five percent ethanol and five percent deionized water [1]. Position the syringe pump so that the syringe needle is immersed in the coagulation bath [2]. Then attach the rollers to the spinning apparatus [3], adjust the roller speed using the motor control software [4], and turn on the necessary motors [5].

    - Talent mixing ethanol and deionized water in a beaker.

    - Shot of the syringe needle being submerged in the coagulation bath.

    - Talent attaching rollers to the spinning apparatus.

    - SCREEN: The roller speed being input into the instrument.  Videographer: Please film the computer screen for this shot

    - Talent switching on the motors.

  - After starting the syringe pump, use tweezers to guide the fiber forming in the coagulation bath [1]. To collect spun fibers, guide the forming fiber onto the first roller, ensuring the rotation matches the extrusion rate [2]. To perform post-spin stretching in the air, set roller 2 to rotate faster than roller 1 [3], guide the fiber from coagulation over roller 1 and collect it on roller 2 [4].

    - Shot of tweezers being used to guide fibre formation.

    - Shot of the fibre being guided onto the 1st roller.

    - The roller 2 is being set to rotate faster than roller 1.

    - Shot of the fiber being guided from roller 1 to roller 2.

  - To perform post-spin stretching after immersion in solvent, fill a solvent bath [1]. Guide the fiber from coagulation around roller 1 [2], then roller 3 in the solvent bath [3], and collect it on roller 2 in air, rotating faster than the other two rollers [4].

    - Talent filling a solvent bath with desired solvent.

    - Shot of fibre being guided around roller 1.

    - Shot of fiber being guided around roller 3 in the solvent bath.

    - Shot of fiber being guided around roller 2, rotating in air.

NOTE: Shots 3.6.2, 3.6.3, and 3.6.4 were combined as one shot.

- Optical Evaluation and Tensile Testing of Individual Fibers

Demonstrator: Hina Batool

  - Remove a fiber from the roller it was collected on [1] and cut an approximately 2-centimeter-long segment [2].

    - Shot of a fibre being removed from the roller it was collected on.

    - Shot of the fibre being cut into a 2 cm long segment. NOTE: Shots 4.1.1 and 4.1.2 were combined as one shot.

  - Place the cut segment on the double-sided tape, aligning its long axis parallel to the holder’s bottom edge [1], then secure it with masking tape on top of the double-sided tape, on both sides [2]. Firmly secure the bottom of the paper holder to the slide to prevent fiber movement during use, using additional tape [3]. Then, store the mounted fiber slides in a slide storage box until imaging or tensile testing [4].

    - Talent placing the cut segment on the double-sided tape.

    - Shot of the segment being taped with masking tape, on both sides.

    - Shot of the paper holder bottom being fixed to the slide with more masking transparent tape.

    - Talent placing slide in storage box.

  - To determine the diameter and evaluate any defects, examine the mounted fibers under an optical microscope [1]. Screen the entire fiber length for imperfections such as necking, twisting, bulging, or double fibers [2-TXT].

    - Talent placing the slide with fibre under an optical microscope.

    - SCOPE: Revised_SCOPE_4.3.2.mp4: 00:05:20

  - For fibers without defects, capture three micrographs at 10X (Ten-X) along the fiber’s long axis, at the middle, and at each end [1].

    - SCOPE: Revised_SCOPE_4.4.1.mp4: 00:04:00:25

  - Use polarized light microscopy to assess molecular alignment. Examine the fiber with an inverted microscope featuring a rotatable stage and a ninety-degree polarizer. [1-TXT]. Capture an image of the fiber to evaluate its birefringence [2].

    - Talent placing the fiber slide under an inverted microscope.

    - SCOPE: Revised_SCOPE_4.5.2.mp4 00:12-00:20

  - For tensile testing with a home-built apparatus, detach the C-shaped paper frame holding the fiber from the slide [1] and secure it to a clamp attached to a weight [2].

    - Talent detaching the C-shaped paper frame from the slide.

    - Talent attaching it to a clamp with a weight.

  - Transfer the weighted clamp onto an empty analytical balance [1], then attach the top of the paper frame to a clamp connected to the syringe pump [2].  Cut one side of the paper holder to allow free fiber movement [3].

    - Talent placing the weighted clamp onto a empty analytical balance.

    - Talent attaching the top of the paper frame to a clamp connect to the syringe pump.

    - Shot of the one side of the paper holder being cut.

  - Now, tare the balance to zero out the mass of the weight and clamp [1]. Click OK in the balance control software [2], then press the Run button on the syringe pump [3].

    - Talent pressing Tare on the analytical balance.

    - SCREEN: OK is being clicked.  Videographer: Please film the computer screen for this shot  NOTE: 4.8.3 is moved here as per authors’s request

    - Talent pressing the Run button on the syringe pump.

  - When the fiber breaks, press Stop on the syringe pump [1] and click Yes in the balance software to log weight versus time [2]. Perform FTIR spectroscopy to evaluate fiber-state secondary structure [3].

    - Talent pressing Stop button.  NOTE: 4.9.1 and 4.9.2 are filmed in a single shot

    - SCREEN: The Yes option is being clicked.  Videographer: Please film the computer screen for this shot

    - Talent in front of the computer looking at the FTIR spectra.

# Results

- Results

  - An ideal dope solution appeared completely clear and viscous without any visible precipitates, indicating full protein dissolution [1], whereas incomplete dissolution resulted in either a cloudy mixture [2] or visible particulate matter [3].

    - LAB MEDIA: Figure 7A.

    - LAB MEDIA: Figure 7C

    - LAB MEDIA: Figure 7B

  - Fibers produced without post-spin drawing showed a consistent diameter under optical microscopy [1], but those subjected to 4 times stretching in 40% ethanol exhibited a visibly thinner and more uniform morphology [2].

    - LAB MEDIA: Figure 8A. Video editor: Highlight the top-left panel labelled AS,

    - LAB MEDIA: Figure 8A. Video editor: Highlight the bottom-left panel labelled 4x-EtOH

  - Higher birefringence in fibers subjected to 4 times ethanol stretching compared to the as-spun condition, indicating increased molecular alignment [1]. Defective fiber segments, such as kinks and irregular bends, were visible in some samples, rendering them unsuitable for analysis [2].

    - LAB MEDIA: Figure 8B.	Video editor: Highlight the bottom-right panel labelled 4x-EtOH

    - LAB MEDIA: Figure 9. Video editor: Please sequentially highlight A and then B

  - Fibers drawn 4 times in ethanol demonstrated the highest tensile strength [1], while fibers spun in air 4 times exhibited brittle behavior with low extensibility [2].

    - LAB MEDIA: Figure 10. Video editor: Highlight the dark blue curve labelled 4x-EtOH

    - LAB MEDIA: Figure 10. Video editor: Highlight the purple curve labelled 4x-air,

  - FTIR spectra of silk fibers showed characteristic protein bands, including amide I peaks, consistent across conditions [1]. Second derivative analysis is useful for identifying key components of the amide I peak [2].

    - LAB MEDIA: Figure 11C and D.

    - LAB MEDIA: Figure 11 E and F	Video Editor: Please highlight the red curves in both graphs

  - Deconvolution of the amide I region revealed a higher proportion of β (beta) -sheet content in the 4 times ethanol condition [1] compared to the as-spun state, regardless of analysis method used [2].

    - LAB MEDIA: Figure 11G and H Video editor: please highlight the red curve corresponding to b-sheet in both graphs

    - LAB MEDIA: Figure 11I and J . Video editor: please highlight the red curve corresponding to b-sheet in both graphs

- Electroporation
Pronunciation link: https://www.merriam-webster.com/dictionary/electroporation
IPA: /ɪˌlek.troʊ.pəˈreɪ.ʃən/
Phonetic Spelling: ih·lek·troh·puh·ray·shuhn

- EBY100
Pronunciation link: No confirmed link found
IPA: No verified IPA available
Phonetic Spelling: ee·bee·why·one·zero·zero

- Glycerol
Pronunciation link: https://www.merriam-webster.com/dictionary/glycerol
IPA: /ˈɡlɪs.əˌrɔːl/
Phonetic Spelling: glis·uh·rawl

- Erlenmeyer
Pronunciation link: https://www.merriam-webster.com/dictionary/Erlenmeyer%20flask
IPA: /ˈɝː.lənˌmaɪ.ɚ/
Phonetic Spelling: er·len·my·er

- Micropipette
Pronunciation link: https://www.merriam-webster.com/dictionary/micropipette
IPA: /ˌmaɪ.kroʊ.paɪˈpet/
Phonetic Spelling: my·kroh·pie·pet

- Spectrophotometer
Pronunciation link: https://www.merriam-webster.com/dictionary/spectrophotometer
IPA: /ˌspek.troʊ.fəˈtɑː.mə.tɚ/
Phonetic Spelling: spek·troh·fuh·tom·uh·ter

- Optical density
Pronunciation link: https://www.merriam-webster.com/dictionary/optical
IPA: /ˈɑːp.tɪ.kəl ˈden.sə.ti/
Phonetic Spelling: op·tih·kuhl den·suh·tee

- Microcuvette
Pronunciation link: No confirmed link found
IPA: No verified IPA available
Phonetic Spelling: my·kroh·kyoo·vet

- Conditioning buffer
Pronunciation link: https://www.merriam-webster.com/dictionary/conditioning
IPA: /kənˈdɪʃ.ə.nɪŋ ˈbʌf.ɚ/
Phonetic Spelling: kuhn·dish·uh·ning buf·er

- Sorbitol
Pronunciation link: https://www.merriam-webster.com/dictionary/sorbitol
IPA: /ˈsɔːr.bəˌtɔːl/
Phonetic Spelling: sor·bih·tol

- Electrocompetent
Pronunciation link: No confirmed link found
IPA: No verified IPA available
Phonetic Spelling: ih·lek·troh·kom·puh·tuhnt

- Resuspend
Pronunciation link: https://www.merriam-webster.com/dictionary/resuspend
IPA: /ˌriː.səˈspend/
Phonetic Spelling: ree·suh·spend

- Centrifugation
Pronunciation link: https://www.merriam-webster.com/dictionary/centrifugation
IPA: /ˌsen.trə.fjuːˈɡeɪ.ʃən/
Phonetic Spelling: sen·truh·fyoo·gay·shuhn

- Plasmid
Pronunciation link: https://www.merriam-webster.com/dictionary/plasmid
IPA: /ˈplæz.mɪd/
Phonetic Spelling: plaz·mid

- Linearized
Pronunciation link: https://www.merriam-webster.com/dictionary/linearize
IPA: /ˈlɪn.i.əˌraɪzd/
Phonetic Spelling: lin·ee·uh·ryzd

- Cuvette
Pronunciation link: https://www.merriam-webster.com/dictionary/cuvette
IPA: /kjuːˈvet/
Phonetic Spelling: kyoo·vet

- TRP1
Pronunciation link: No confirmed link found
IPA: No verified IPA available
Phonetic Spelling: tee·ar·pee·one

- Fluorescence-activated cell sorting
Pronunciation link: https://www.merriam-webster.com/dictionary/fluorescence
IPA: /flɔːˈres.əns ˈæk.təˌveɪ.t̬ɪd sel ˈsɔːr.tɪŋ/
Phonetic Spelling: floor·ess·uhns ak·tuh·vay·tid sel sor·ting

- Hemagglutinin
Pronunciation link: https://www.merriam-webster.com/dictionary/hemagglutinin
IPA: /ˌhiː.məˈɡluː.t̬ən.ɪn/
Phonetic Spelling: hee·muh·gloo·tuh·nin

- Fluorescein isothiocyanate
Pronunciation link: https://www.merriam-webster.com/dictionary/fluorescein
IPA: /ˌflʊr.əˈsiː.ɪn ˌaɪ.soʊˌθaɪ.oʊˈsaɪ.ə.neɪt/
Phonetic Spelling: floor·uh·see·in eye·soh·thy·oh·sy·uh·nayt

- Phycoerythrin
Pronunciation link: https://www.merriam-webster.com/dictionary/phycoerythrin
IPA: /ˌfaɪ.koʊ.əˈrɪθ.rɪn/
Phonetic Spelling: fy·koh·uh·rith·rin