# Submission ID #: 68736

# Scriptwriter Name: Sulakshana Karkala

# Project Page Link: https://review.jove.com/account/file-uploader?src=20964528

# Title: Improved Polydimethylsiloxane (PDMS) Double Casting via Silicone Oil Treatment for Densely Packed Microstructure Replication

# Authors and Affiliations:

# Yoonjae Lee, Taehoon Kim, Jae Hun Seol

# School of Mechanical and Robotics Engineering, Gwangju Institute of Science and Technology

# Corresponding Authors:

Jae Hun Seol 		(jhseol@gist.ac.kr)

# Email Addresses for All Authors:

Yoonjae Lee		(yoonjae10@gm.gist.ac.kr)

Taehoon Kim		(enormerit@gm.gist.ac.kr)

Jae Hun Seol 		(jhseol@gist.ac.kr)

## Author Questionnaire

1. Microscopy: Does your protocol require the use of a dissecting or stereomicroscope for performing a complex dissection, microinjection technique, or something similar?  No

2. Software: Does the part of your protocol being filmed include step-by-step descriptions of software usage?  No

3. Filming location: Will the filming need to take place in multiple locations?   Yes, 50 m apart in the same building

Current Protocol Length

Number of Steps:  14

Number of Shots:  31

# Introduction

Videographer: Obtain headshots for all authors available at the filming location.

REQUIRED: What is the scope of your research? What questions are you trying to answer?

  - Yoonjae Lee: To address demolding challenges in dense and high-aspect-ratio microstructures, we modified the PDMS double casting process by adding a silicone oil treatment step applied with a tensioned thread.

    - INTERVIEW: Named Talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B.roll:2.6

What advantage does your protocol offer compared to other techniques?

  - Yoonjae Lee: Our protocol offers a simple, cost-effective solution that avoids the need for expensive equipment or specialized materials, enabling reliable replication of dense microstructures without damage.

    - INTERVIEW: Named Talent says the statement above in an interview-style shot, looking slightly off-camera.

What research questions will your laboratory focus on in the future?

  - Taehoon Kim: Our laboratory will focus on automating the oil application process and developing custom silicone oils to identify optimal conditions for improved reproducibility and precision.

    - INTERVIEW: Named Talent says the statement above in an interview-style shot, looking slightly off-camera.

Videographer: Obtain headshots for all authors available at the filming location.

# Protocol

- Fabrication of PDMS mold from a Silicon Mold

Demonstrator: Yoonjae Lee

  - To begin, mix a solution of hexane and OTS (O-T-S) in a 40 to 1 volume ratio using a clean glass beaker and a stirring rod [1-TXT]. Cover the beaker with aluminum foil to minimize evaporation [2].

    - WIDE: Talent mixing hexane and OTS in a clean glass beaker using a stirring rod. TXT: OTS: Octadecyltrichlorosilane

    - Talent covering the glass beaker with aluminum foil.

  - Sonicate the sealed glass beaker into a room-temperature ultrasonic bath filled with water [1-TXT]. Then immerse the pre-etched silicon mold with a hole array into the prepared hexane-OTS solution [2].

    - Talent placing the covered glass beaker into an ultrasonic bath. TXT: Sonication: 40 kHz, 135 W, 5 min

    - Talent placing the silicon mold vertically into the solution using tweezers.

  - Now use clean tweezers to gently lift the entire silicon mold vertically out of the solution [1]. Immediately transfer it to a fresh beaker containing neat hexane [2]. Then rinse by gently agitating it back and forth 5 to 10 times [3].

    - Talent lifting the silicon mold from the beaker using tweezers.

    - Talent transferring the mold to a fresh beaker with neat hexane.

    - Talent rinsing the mold in neat hexane by moving it gently back and forth.

  - Gently dry the mold using a nitrogen blower held approximately 3 centimeters away for 6 to 10 seconds until no visible moisture remains [1].

    - Talent drying the mold using a nitrogen blower from a short distance.

  - Next, mix the PDMS (P-D-M-S) base and curing agent in a 10 to 1 weight ratio in a clean plastic Petri dish [1-TXT]. Place the mixture into a chamber and degas at 160 torr [2].

    - Talent mixing the PDMS base and curing agent in a Petri dish. TXT: PDMS: Polydimethylsiloxane

    - Talent placing the Petri dish into a vacuum chamber for degassing.

  - Lightly coat a clean plastic Petri dish with silicone oil of 100 centistokes viscosity using a lint-free wiper pre-soaked with the oil [1]. Then place the OTS-coated silicon mold face-up in the centre of the coated Petri dish [2].

    - Talent wiping the surface of the Petri dish using an oil-soaked lint-free wiper.

    - Talent positioning the coated silicon mold in the Petri dish.

  - Slowly pour the degassed PDMS mixture over the mold until it is fully covered [1]. Degas the filled mold again in the vacuum bubble remover until no visible bubbles remain [2].

    - Talent pouring the polydimethylsiloxane mixture over the mold.

    - Talent placing the Petri dish back into the vacuum chamber.

  - Now, place the Petri dish on a preheated hot plate set to 90 degrees Celsius to cure the PDMS [1]. Once cured, gently peel the PDMS mold from the silicon mold, ensuring the microstructure remains intact [2].

    - Talent placing the Petri dish on the hot plate.

    - Talent carefully peeling the cured polydimethylsiloxane mold from the silicon mold.

- Fabrication of PDMS Product from PDMS Mold

  - Place the fabricated PDMS mold on a hot plate set to 150 degrees Celsius [1]. After 3 days of thermal aging, immerse the mold in silicone oil of 100 centistokes viscosity [2].

    - Talent placing the polydimethylsiloxane mold onto a hot plate.

    - Talent submerging the mold in silicone oil.

  - Degas the oil-immersed mold under vacuum at 160 torr for 10 to 15 minutes [1]. Then, remove the mold using tweezers [2] and gently wipe the surface 3 to 5 times with a clean lint-free wiper to leave a uniform thin film of oil [3].

    - Talent placing the mold in a vacuum chamber for degassing.

    - Talent removing the mold with tweezers.

    - Talent wiping the mold with a lint-free wiper.

  - Next, prepare a PDMS mixture at a 10 to 1 base to curing agent weight ratio, using the same mixing and degassing method as before [1]. Gently pour the degassed mixture onto the treated mold, allowing it to spread and reach at least halfway up the micropillars [2].

    - Talent preparing and degassing the polydimethylsiloxane mixture.

    - Talent pouring the mixture over the mold, showing it rising along the micropillars.

  - Secure a 0.5-micrometre nylon thread under gentle tension [1]. Swipe the thread once or twice across the PDMS surface in one direction to reduce excess oil between micropillars [2]. Then degas the mold with the thin PDMS layer in a vacuum chamber until no air bubbles remain [3].

    - Talent securing the nylon thread under tension.

    - Talent swiping the thread across the mold surface.

    - Talent placing the mold into a vacuum chamber.

  - To fabricate a hole-array pattern PDMS product, lightly coat a clean plastic Petri dish with silicone oil [1]. Place the PDMS mold into the coated Petri dish [2] and pour the degassed PDMS mixture over it until the desired height is reached [3].

    - Talent coating the Petri dish with silicone oil.

    - Talent placing the mold in the dish.

    - Talent pouring the polydimethylsiloxane mixture.

  - Degas the mold assembly once more to eliminate any trapped air bubbles [1]. Then place the Petri dish on a preheated hot plate set to 110 degrees Celsius and cure until fully solidified [2].

    - Talent placing the Petri dish into the vacuum chamber.

    - Talent placing the Petri dish on a hot plate.

# Results

- Results

  - The silicon mold featured a dense array of circular holes measuring 143 micrometres in diameter with 150 micrometre spacing [1], and a depth of 284 micrometres, yielding a 2 to 1 aspect ratio [2].

    - LAB MEDIA: Figure 3A.

    - LAB MEDIA: Figure 3B.

  - The PDMS mold replicated from the silicon template produced micropillars measuring 142 micrometres in diameter [1] and 283 micrometres in height closely matching the original dimensions[2].

    - LAB MEDIA: Figure 4A.

    - LAB MEDIA: Figure 4B.

  - The PDMS replica aged 1 day showed severe tearing and disintegration of wall structures during demolding [1]. After 2 days of aging, distinct pillar outlines became visible, but the walls remained heavily damaged due to insufficient release [2].

    - LAB MEDIA: Figure 5A.

    - LAB MEDIA: Figure 5B.

  - With 3 days of aging and no oil layer, cross-linking between cured and uncured PDMS resulted in recombined structures [1]. Using low-viscosity MR-100 (M-R-One-Hundred) oil after 3 days of aging led to poor coverage and tearing, as the oil drained off vertical sidewalls [2]. High-viscosity oil formed a thick coating, preventing mold filling and causing the final product to appear wavy and malformed [3].

    - LAB MEDIA: Figure 5C.

    - LAB MEDIA: Figure 5D.

    - LAB MEDIA: Figure 5E.

  - Under optimized conditions of 3 days thermal aging and 100 centistokes silicone oil coating, the final replica preserved hole-patterned microstructures with 148 micrometres diameter [1] and 280 micrometres height, showing minor dimensional variation but intact structure [2].

    - LAB MEDIA: Figure 6A.

    - LAB MEDIA: Figure 6B.