# Submission ID #: 68755

# Scriptwriter Name: Pallavi Sharma

# Project Page Link: https://review.jove.com/account/file-uploader?src=20970323

Title: Fabrication of a Solution-gated Indium–Tin–Oxide-based One-piece Transistor Enabling Sensitive Biosensing

# Authors and Affiliations:

Ritsu Katayama Naganuma, Toshiya Sakata*

Department of Materials Engineering, School of Engineering, The University of Tokyo

☐   All author names and affiliations are correct (city/state/country information not included in video title page).

# Corresponding Authors:

Toshiya Sakata 			(sakata@biofet.t.u-tokyo.ac.jp)

# Email Addresses for All Authors:

Ritsu Katayama Naganuma		(katayama@biofet.t.u-tokyo.ac.jp)

Toshiya Sakata 			(sakata@biofet.t.u-tokyo.ac.jp)

## Author Questionnaire

1. Microscopy: Does your protocol require the use of a dissecting or stereomicroscope for performing a complex dissection, microinjection technique, or something similar?  Enter Yes or No.

If Yes, can you record movies/images using your own microscope camera?

Enter Yes or No.

If your protocol involves microscopy but you are not able to record movies/images with your microscope camera, JoVE will need to use our scope kit.

If your microscope does not have a camera port, the scope kit will be attached to one of the eyepieces and you will have to perform the procedure using one eye.

Enter make and model of microscope.

If a dissection or stereo microscope is required for your protocol, please list all shots from the script that will be visualized using the microscope (shots are indicated with the 3-digit numbers, like 2.1.1, 2.1.2, etc.).

Click here to list microscope shots, using the shot numbers from the protocol section of the video script.

2. Software: Does the part of your protocol being filmed include step-by-step descriptions of software usage?  Enter Yes or No.

If Yes, we will need you to record using screen recording software.

We recommend using the screen capture program OBS. JoVE’s tutorial for using OBS Studio is provided at this link: https://review.jove.com/v/5848/screen-capture-instructions-for-authors?status=a7854k

# As these files are necessary for finalizing your script, please upload all screen-captured video files to your project page as soon as possible. https://review.jove.com/account/file-uploader?src=20970323

3. Filming location: Will the filming need to take place in multiple locations?   Enter Yes or No.

If Yes, how far apart are the locations? Click to enter distance between locations.

To ensure that your script can be filmed in one day, the protocol sections are cumulatively restricted to 55 shots (shots are the 3-digit numbers like 2.1.1, 2.1.2…etc)

Current Protocol Length

Number of Steps:  31

Number of Shots:  54

# Introduction

Videographer: Obtain headshots for all authors available at the filming location.

Answers to these questions will become interview statements that you will deliver on camera.

- Answer the 1st REQUIRED question and at least 2 other questions (1.2 – 1.10) below. Up to 5 interview statements will be included in the video.

- Enter the full name of the author who will deliver the statement.

- If possible, each author should deliver no more than two statements.

- Answer in full sentences, in a style suitable for being spoken aloud.

- Limit the length of each statement to 30 words or fewer.

- Answers will be edited for length, clarity, and consistency with journal style guidelines.

REQUIRED: What is the scope of your research? What questions are you trying to answer?

  - Enter author name.: Click here to answer question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

What are the most recent developments in your field of research?

  - Enter author name: Click here to answer question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

What technologies are currently used to advance research in your field?

  - Enter author name: Click here to answer question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

What are the current experimental challenges?

  - Enter author name: Click here to answer question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

What significant findings have you established in your field?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

What research gap are you addressing with your protocol?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

What advantage does your protocol offer compared to other techniques?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

How will your findings advance research in your field?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

What new scientific questions have your results paved the way for?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

What research questions will your laboratory focus on in the future?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

Videographer: Obtain headshots for all authors available at the filming location.

# Testimonial Questions (OPTIONAL):

Answers to these questions will not appear in the video but may be featured in our journal's promotional materials.

- Enter the full name of the author who will deliver the statement.

- Answer in full sentences, in a style suitable for being spoken aloud.

- Answers will be mildly edited for clarity.

- Limit the length of each statement to 50 words or fewer.

How do you think publishing with JoVE will enhance the visibility and impact of your research?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 50 or fewer words.

Can you share a specific success story or benefit you’ve experienced—or expect to experience—after using or publishing with JoVE? (This could include increased collaborations, citations, funding opportunities, streamlined lab procedures, reduced training time, cost savings in the lab, or improved lab productivity.)

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 50 or fewer words.

# Protocol

Please review this section to make sure that it accurately describes your protocol. Use Track Changes when making edits or revisions.

- The two-digit steps (e.g., 2.1., 2.2.) are the narration.  JoVE is responsible for the narration of the protocol and results.

- Red italics are pronunciation guides indicating how the word will be spoken.

- Filming should take no more than 10 minutes per step. If a step takes more than 10 minutes, prepare the product for that step in advance.

- The three-digit shots (e.g., 2.1.1., 2.2.2.) are the actions that the videographer will capture.

- Fabrication of One-Piece ITO-ISFET

Demonstrator: Click here to enter name of demonstrator(s)

If the same person is the demonstrator throughout, mention them once here and remove the "Demonstrator" field from the other sections; if the demonstrator changes, retain the field in the respective sections.

  - To begin, wash the glass substrate by sonicating it in acetone, methanol, and water for 5 minutes each [1]. Using a nitrogen gas blower, dry the substrate thoroughly [2], and bake it on a hot plate at 110 degrees Celsius for more than 5 minutes to ensure it is completely dry [3].

    - WIDE: Talent placing the glass substrate in a sonication bath filled with acetone.

    - Talent drying the substrate using a nitrogen gas blower.

    - Talent placing the dried substrate on a hot plate set to 110 degrees Celsius.

  - Spin-coat the dried glass substrate with an OFPR-800 (O-P-F-R-Eight-Hundred) layer by spinning at 500 rpm for 5 seconds, followed by 3000 rpm for 30 seconds [1-TXT].

    - Talent placing the substrate onto the spin coater and setting it to 500 revolutions per minute for 5 seconds. TXT: Examine the surface for uniformity of coating

  - Prebake the coated substrate on a hot plate at 110 degrees Celsius for 5 minutes [1]. Allow the substrate to cool down to room temperature before proceeding [2].

    - Talent placing the coated substrate on a hot plate set to 110 degrees Celsius.

    - Talent removing the substrate from the hot plate and setting it aside to cool to room temperature.

  - Position the photomask film on the photoresist-coated side of the substrate and use tape to fix it securely in place [1]. Then, expose the substrate to ultraviolet light using a photolithography machine for 40 seconds [2].

    - Talent placing the photomask film on top of the coated substrate and fixing it with tape.

    - Talent placing the prepared substrate into the photolithography machine.

  - Now, take the substrate out of the photolithography machine and carefully remove the photomask from the surface [1].

    - Talent removes the exposed substrate and removes the photomask.

  - To develop the photoresist, immerse the substrate in NMD-3 (N-M-D-Three) developer for 1 minute [1] and verify that a sharp pattern is formed [2]. Then, dip the substrate in water to wash away the developer [3].

    - Talent submerging the substrate in a container filled with NMD-3 developer.

    - Talent inspecting the photoresist pattern for clarity and sharpness.

    - Talent dipping the developed substrate into a water bath for rinsing.

  - After drying the washed substrate by blowing nitrogen gas, bake it on a hot plate at 110 degrees Celsius for 5 minutes [1].

    - Talent placing the dried substrate on a hot plate set to 110 degrees Celsius for post-baking.

  - To begin deposition, fix the substrate onto a substrate holder using tape [1] and introduce it into the vacuum chamber of a sputtering machine [2]. Pump down the sputtering chamber pressure to below 10-3 pascals [3].

    - Talent placing the substrate onto a holder and taping it down securely.

    - Talent inserting the taped holder into the vacuum chamber of the sputtering machine.

    - Show the sputtering machine interface as the vacuum pump is engaged and the chamber pressure drops below 10⁻³ pascals.

  - Then, deposit a 100-nanometer thick layer of indium tin oxide via radio frequency sputtering at 4 nanometers per minute under argon, without substrate heating [1].

    - Show the sputtering parameters on instrument display, including target composition, 4 nanometers per minute deposition rate.

  - To lift off the photoresist, sonicate the substrate in acetone, methanol, and then water for 5 minutes [1-TXT].

    - Talent placing the substrate in an acetone bath and starting sonication. TXT: Ensure no ITO fragments remain on substrates

  - Then, blow the substrate dry using a nitrogen gas blower [1] and bake it on a hot plate at 110 degrees Celsius until fully dry [2].

    - Talent blowing the substrate surface dry with nitrogen gas.

    - Talent placing the substrate on a hot plate set to 110 degrees Celsius for drying.

  - To spin-coat the clean substrate with SU-8 (S-U-Eight) 3005 (Three-Zero-Zero-Five) spin at 500 rpm for 5 seconds, followed by 6000 rpm for 30 seconds [1-TXT]. Prebake the SU-8-coated substrate on a hot plate set to 95 degrees Celsius [2-TXT].

    - Talent placing the substrate onto the spin coater and setting the initial spin to 500 revolutions per minute for 5 seconds. TXT: Check the coated surface for uniformity

    - Talent placing the coated substrate on a hot plate at 95 degrees Celsius. TXT: Cool the substrate to RT

  - Then, place the photomask film on the photoresist-coated substrate and secure it with tape to prevent any movement during exposure [2].

    - Talent aligning the photomask film over the SU-8 coated substrate and taping it onto the substrate.

  - Expose the SU-8 coated substrate to ultraviolet light for 7 seconds using a photolithography machine [1]. Then, remove the substrate from the machine and carefully detach the photomask [2].

    - Talent placing the substrate in the photolithography machine and initiating the 7-second ultraviolet exposure.

    - Talent removing the substrate and peeling off the photomask.

  - Postbake the exposed substrate first at 65 degrees Celsius for 2 minutes, then at 95 degrees Celsius and continue baking for 5 minutes [1].

    - Talent transferring the substrate to a hot plate set to 95 degrees Celsius.

  - Immerse the substrate in SU-8 developer for 3 minutes under strong agitation to develop the photoresist [1]. Rinse the substrate in 2-propanol for 1 minute [2-TXT] and dry the developed substrate using a nitrogen gas blower [3].

    - Talent shaking the SU-8 developer container vigorously while the substrate is immersed for 3 minutes.

    - Talent dipping the developed substrate in 2-propanol for rinsing. TXT: Ensure that the photoresist is fully developed

    - Talent blowing nitrogen gas across the surface of the cleaned and developed substrate.

  - To begin forming the semiconductive indium tin oxide channel, prepare 0.1 molar hydrochloric acid solution [1]. Connect the source and drain electrodes to a semiconductor parameter analyzer [2].

    - WIDE: Talent measuring and preparing 0.1 molar hydrochloric acid in a labeled beaker.

    - Talent attaching source and drain pads on the substrate to the semiconductor parameter analyzer.

  - On the analyzer interface, select the Classic Test tab, then choose the I/V-t Sampling (I-V-T-Sampling) option. Set the sampling interval to 0.5 seconds [1]. Apply a voltage of 1 volt between the source and drain electrodes and record the initial current [2].

    - SCREEN: Show the analyzer interface with the cursor selecting the Classic Test tab and I/V-t Sampling test mode . The sampling interval is input as 0.5 seconds.

Authors: Please create screen capture videos of the shots labeled as SCREEN, create a screenshot summary, and upload the files to your project page as soon as possible: https://review.jove.com/account/file-uploader?src=20970323

    - SCREEN: Show the semiconductor parameter analyzer interface displaying the applied voltage of 1 volt and the initial current reading.

  - Using a micropipette, place a 30-microliter drop of the prepared hydrochloric acid solution directly onto the exposed indium tin oxide channel area [1-TXT].

    - Talent using a micropipette to carefully dispense a 30 microliter drop of hydrochloric acid onto the channel. TXT: Ensure the droplet fully covers the entire channel region

  - Monitor the current between the source and drain electrodes continuously and observe the conductivity change during etching. Continue the process until the current drops to 10 percent of the initial value [1].

    - SCREEN: Show the live current graph on the analyzer as etching progresses. Highlight the decreasing current trend indicating conductivity change.

  - Immediately rinse the etched indium tin oxide channel with deionized water to stop the etching once the current reaches 10% of the initial current [1]. Dry the one-piece transistor by gently blowing nitrogen gas over the rinsed substrate using a nitrogen gas blower [2-TXT].

    - Talent using a pipette to rinse the channel area thoroughly with deionized water.

    - Talent drying the device with gentle nitrogen gas flow focused on the channel area. TXT:  Store the dried devices in a vacuum desiccator until further use

- Electrical Measurements of One-piece ITO-ISFET

  - Using a test fixture, connect the source and drain electrodes of the one-piece transistor to the semiconductor parameter analyzer [1]. Place a silicone O-ring around the surface of the indium tin oxide channel to form a liquid well [2].

    - Talent connecting probe wires from the test fixture to the source and drain terminals on the one-piece transistor.

    - Talent positioning and gently pressing a silicone O-ring onto the substrate to surround the ITO channel.

  - Add 30 microliters of phosphate buffer or another standard pH buffer solution into the silicone O-ring well while making full contact with the indium tin oxide channel surface [1].

    - Talent pipetting 30 microliters of buffer solution into the silicone well.

  - Then, insert a silver or silver chloride reference electrode into a saturated potassium chloride solution, which is connected to the gate electrolyte by a salt bridge [1]. Connect the silver or silver chloride reference electrode to the semiconductor parameter analyzer so that it functions as the gate electrode [2].

    - Talent placing the Ag/AgCl reference electrode into a beaker containing saturated potassium chloride.

    - Talent attaching the wire from the reference electrode to the gate input port of the semiconductor parameter analyzer.

  - Turn on the B1500A (B-Fifteen-Hundred) device and start the EasyEXPART (Easy-Expart) software. Then, open the Workspace interface to begin setup [1].

    - SCREEN: Show the B1500A power switch being turned on and the EasyEXPART software launching. Show the software interface as the user clicks to open the Workspace.

  - On the semiconductor parameter analyzer, select the Classic Test tab, then choose the I/V Sweep mode [1]. Connect the source electrode to ground to establish a reference potential [2].

    - SCREEN: Show the analyzer interface with the user clicking on the Classic Test tab. Selection of the I/V Sweep option on the menu.

    - Talent connecting the source electrode lead to the ground terminal on the test fixture or analyzer.

  - Set the applied drain voltage to a constant value of 1 volt [1]. Set the sweep range of gate voltages, from minus 0.8 volts to plus 0.8 volts, and adjust the sweep rate to approximately 50 millivolts per second [2].

    - SCREEN: Show the voltage setting interface where V D S is input and locked at 1 volt.

    - SCREEN: Show the gate voltage range input set from -0.8 to +0.8 volts and adjust the sweep rate to 50 mV/s.

  - Set the number of iterations to 10 cycles and specify that only the data from the final cycle should be used for analysis [1]. Simultaneously, ensure that the leak current between the source and gate electrodes is recorded and start the measurement [2].

    - SCREEN: Show the iteration count set to 10 and the data selection set to "Last Cycle".

    - SCREEN: Display of the software settings indicating that Igs is being tracked. Measurement is being started.

  - Set the gate voltage, to increase sequentially from 0 volts to 0.8 volts in 0.1 volt intervals [1]. For each gate voltage value, set the drain voltage to sweep from 0 volts to 1 volt in 0.01-volt intervals and start the measurement [2].

    - SCREEN: Show the software input where V G S values are listed incrementally from 0 to 0.8 volts in steps of 0.1 volts.

    - SCREEN: Show the sweep settings where V D S is configured to increment from 0 to 1 volt in steps of 0.01 volts and start the measurement.

  - Remove the silicone O-ring from around the channel surface [1], then rinse the channel area thoroughly with deionized water [2]. Dry the one-piece indium tin oxide device using a nitrogen gas blower [3=TXT].

    - Talent gently peeling off the silicone O-ring from the substrate.

    - Talent rinsing the ITO channel area using a pipette filled with deionized water.

    - Talent drying the cleaned device with a nitrogen gas blower. TXT: Store the fully dried device in a vacuum desiccator

# Results

Please review this section to make sure that it accurately reflects your findings.

- This section will not be recorded by the videographer. It only includes the figures/tables from your manuscript (called LAB MEDIA).

- Use Track Changes when making edits or revisions. Ensure the voiceover length is below 200 words. Current word count: 144.

- Please note that the video cannot include voiceover without an accompanying visual.

- Results

  - The indium tin oxide ion-sensitive field-effect transistor demonstrated a steep subthreshold slope of approximately 81 millivolts per decade, indicating near-ideal switching behavior at 25 degrees Celsius [1].

    - LAB MEDIA: Figure 3A  Video editor: Highlight the text “SS = 81 mV/dec.” on the inset graph.

  - The gate leakage current remained four orders of magnitude lower than the drain current, even when the channel was directly exposed to the electrolyte solution [1]. The drain current increased with the drain voltage and showed saturation behavior at each gate voltage, confirming good field-effect transistor characteristics [2].

    - LAB MEDIA: Figure 3B.

    - LAB MEDIA: Figure 3C. Video editor: Highlight the set of blue curves, especially focusing on the highest curve labelled “VGS = 0.8 V”.

  - The on-off current ratio exceeded 10,000 for channel thicknesses below 20 nanometers [1] but dropped drastically at greater thicknesses [2].

    - LAB MEDIA: Figure 4. Video editor: Highlight the cluster of red dots above 10⁴ on the left side of the vertical dashed line.

    - LAB MEDIA: Figure 4. Video editor: Highlight the group of red dots near 10⁰ to 10¹ on the right side of the dashed line.

  - The one-piece indium tin oxide ion-sensitive field-effect transistor responded linearly to pH changes, exhibiting a voltage shift of approximately 51 millivolts per pH unit [1]. The pH sensitivity increased slightly after 5 days of wet storage, approaching the ideal Nernstian limit [2], and was retained even after 16 days [3].

    - LAB MEDIA: Figure 5A. Video editor: Highlight the dashed trendline labelled “51 mV/pH” in the inset plot.

    - LAB MEDIA: Figure 5B. Video editor: Highlight the second bar (5 days)

    - LAB MEDIA: Figure 5B. Video editor: Highlight the third bar (16 days)