# Submission ID #: 68828

# Scriptwriter Name: Pallavi Sharma

# Project Page Link: https://review.jove.com/account/file-uploader?src=20992588

Title: Synthesis and Performance Evaluations of ZnCoS/ZnCdS with Twin Crystal Structure for Multifunctional Redox Photocatalysis in Energy Applications

# Authors and Affiliations:

Tan Ji Siang1,2*, Peipei Zhang3, Binghui Chen1,2,3, Wee-Jun Ong1,2,3,4,5,6*

1School of Energy and Chemical Engineering, Xiamen University Malaysia

2Center of Excellence for NaNo Energy & Catalysis Technology (CONNECT), Xiamen University Malaysia

3State Key Laboratory of Physical Chemistry of Solid Surfaces, College of Chemistry and Chemical Engineering, Xiamen University

4Gulei Innovation Institute, Xiamen University

5Shenzhen Research Institute of Xiamen University

6 Department of Chemical and Biologicalneering, College of Engineering, Korea University

☐   All author names and affiliations are correct (city/state/country information not included in video title page).

# Corresponding Authors:

Wee-Jun Ong		(weejun.ong@xmu.edu.my)

Tan Ji Siang		(jisiang.tan@xmu.edu.my)

# Email Addresses for All Authors:

Peipei Zhang 		(ppzhang0604@163.com)

Binghui Chen 		(chenbh@xmu.edu.my)

Wee-Jun Ong		(weejun.ong@xmu.edu.my)

Tan Ji Siang		(jisiang.tan@xmu.edu.my)

## Author Questionnaire

1. Microscopy: Does your protocol require the use of a dissecting or stereomicroscope for performing a complex dissection, microinjection technique, or something similar?  Enter Yes or No.

If Yes, can you record movies/images using your own microscope camera?

Enter Yes or No.

If your protocol involves microscopy but you are not able to record movies/images with your microscope camera, JoVE will need to use our scope kit.

If your microscope does not have a camera port, the scope kit will be attached to one of the eyepieces and you will have to perform the procedure using one eye.

Enter make and model of microscope.

If a dissection or stereo microscope is required for your protocol, please list all shots from the script that will be visualized using the microscope (shots are indicated with the 3-digit numbers, like 2.1.1, 2.1.2, etc.).

Click here to list microscope shots, using the shot numbers from the protocol section of the video script.

2. Software: Does the part of your protocol being filmed include step-by-step descriptions of software usage?  Enter Yes or No.

If Yes, we will need you to record using screen recording software.

We recommend using the screen capture program OBS. JoVE’s tutorial for using OBS Studio is provided at this link: https://review.jove.com/v/5848/screen-capture-instructions-for-authors?status=a7854k

As these files are necessary for finalizing your script, please upload all screen-captured video files to your project page as soon as possible.

3. Filming location: Will the filming need to take place in multiple locations?   Enter Yes or No.

If Yes, how far apart are the locations? Click to enter distance between locations.

To ensure that your script can be filmed in one day, the protocol sections are cumulatively restricted to 55 shots (shots are the 3-digit numbers like 2.1.1, 2.1.2…etc)

Current Protocol Length

Number of Steps:  18

Number of Shots:  41

# Introduction

Videographer: Obtain headshots for all authors available at the filming location.

Answers to these questions will become interview statements that you will deliver on camera.

- Answer the 1st REQUIRED question and at least 2 other questions (1.2 – 1.10) below. Up to 5 interview statements will be included in the video.

- Enter the full name of the author who will deliver the statement.

- If possible, each author should deliver no more than two statements.

- Answer in full sentences, in a style suitable for being spoken aloud.

- Limit the length of each statement to 30 words or fewer.

- Answers will be edited for length, clarity, and consistency with journal style guidelines.

REQUIRED: What is the scope of your research? What questions are you trying to answer?

  - Enter author name.: Click here to answer question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

What are the most recent developments in your field of research?

  - Enter author name: Click here to answer question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

What technologies are currently used to advance research in your field?

  - Enter author name: Click here to answer question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

What are the current experimental challenges?

  - Enter author name: Click here to answer question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

What significant findings have you established in your field?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

What research gap are you addressing with your protocol?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

What advantage does your protocol offer compared to other techniques?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

How will your findings advance research in your field?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

What new scientific questions have your results paved the way for?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

What research questions will your laboratory focus on in the future?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

Videographer: Obtain headshots for all authors available at the filming location.

# Testimonial Questions (OPTIONAL):

# Videographer: Please capture all testimonial shots in a wide-angle format with sufficient headspace, as the final videos will be rendered in a 1:1 aspect ratio. Testimonial statements will be presented live by the authors, sharing their spontaneous perspectives.

- Testimonial statements will not appear in the video but may be featured in the journal’s promotional materials.

- Provide the full name and position (e.g., Director of [Institute Name], Senior Researcher [University Name], etc.) of the author delivering the testimonial.

- Please answer the testimonial question live during the shoot, speaking naturally and in your own words in complete sentences.

How do you think publishing with JoVE will enhance the visibility and impact of your research?

  - Enter author name, Enter author title: (authors will present their testimonial statements live)

Can you share a specific success story or benefit you’ve experienced—or expect to experience—after using or publishing with JoVE? (This could include increased collaborations, citations, funding opportunities, streamlined lab procedures, reduced training time, cost savings in the lab, or improved lab productivity.)

  - Enter author name, Enter author title: (authors will present their testimonial statements live)

# Protocol

Please review this section to make sure that it accurately describes your protocol. Use Track Changes when making edits or revisions.

- The two-digit steps (e.g., 2.1., 2.2.) with purple font are the narration.  JoVE is responsible for the narration of the protocol and results.

- Red italics are pronunciation guides indicating how the word will be spoken.

- Filming should take no more than 10 minutes per step. If a step takes more than 10 minutes, prepare the product for that step in advance.

- The three-digit shots (e.g., 2.1.1., 2.2.2.) are the actions that the videographer will capture.

- Preparation of ZnCoS/ZnCdS Photocatalyst

Demonstrator: Click here to enter name of demonstrator(s)

If the same person is the demonstrator throughout, mention them once here and remove the "Demonstrator" field from the other sections; if the demonstrator changes, retain the field in the respective sections.

  - To begin, place a 100-milliliter beaker on the work surface [1] and pour 40 milliliters of ethylene glycol solution into it [2]. Using a spatula, add zinc acetate dihydrate, cobalt acetate tetrahydrate, and thioacetamide into the solution [3-TXT]. Subject the solution to ultrasonic treatment for 30 minutes [4], then stir it continuously for 4 hours at ambient temperature [5].

    - WIDE: Talent placing a 100 milliliter beaker on the work surface.

    - Talent pouring 40 milliliters of ethylene glycol into it.

    - Talent adding zinc acetate dihydrate into the beaker with labelled bottles of cobalt acetate tetrahydrate, and thioacetamide in the background. TXT: Zn(CH3COO)2·2H2O: 0.22g; Co(CH3COO)2·4H2O: 0.5 g, CH3CSNH2: 0.3 g

    - Talent placing the beaker into an ultrasonic cleaner and starts it.

    - Talent placing the solution on a magnetic stirrer.

  - Transfer the resulting mixture into a 100-milliliter synthetic polymer-lined stainless-steel autoclave [1]. Then, transfer the solution into a preheated oven and heat at 180 degrees Celsius for 12 hours [2].

    - Talent pouring the prepared mixture into a stainless-steel autoclave.

    - Talent places the solution in a laboratory oven set to 180 degrees Celsius.

  - Using a centrifuge, collect the dark gray precipitate [1]. Then, wash the precipitate three times, each with deionized water and ethanol [2].

    - Talent shows the precipitate after centrifugation.

    - Talent washing the precipitate with deionized water and ethanol alternately.

  - Dry the washed, dark gray sample in an oven overnight at 60 degrees Celsius to obtain a dark gray zinc-cobalt sulfide powder [1].

    - Talent placing the washed sample into a drying oven set at 60 degrees Celsius.

  - To synthesize zinc cadmium sulfide, pour 40 milliliters of deionized water into a 100-milliliter beaker [1]. Using a spatula, add zinc acetate dihydrate, cadmium acetate dihydrate, sodium sulfide hydrate, and thioacetamide into the solution [2][3]. Subject the solution to ultrasonic treatment for 30 minutes [4], followed by stirring for 3 hours at ambient temperature [5].

    - Talent placing a 100 milliliter beaker and pouring 40 milliliters of deionized water into it.

    - Talent adding zinc acetate dihydrate into the beaker.

    - TEXT ON A PLAIN BACKGROUND

Zn(CH3COO)2·2H2O: 0.22g

Cd(CH3COO)2·2H2O: 0.27g

Na2S·xH2O: 0.16 g

CH3CSNH2: 0.15g

    - Talent places the beaker into an ultrasonic cleaner.

    - Talent placing the mixture on a magnetic stirrer.

  - Next, add 0.2 molar sodium hydroxide aqueous solution drop-wise into the stirred solution to adjust the pH to 7.0 [1]. Transfer the adjusted solution into a 100-milliliter synthetic polymer-lined stainless-steel autoclave [2]. Then, place the solution in an oven and heat it at 180 degrees Celsius for 24 hours [3].

    - Talent using a pipette to add 0.2 molar sodium hydroxide solution drop-wise into the beaker while monitoring the pH.

    - Talent transferring the adjusted solution into a stainless-steel autoclave.

    - Talent placing the solution into an oven preheated to 180 degrees Celsius.

  - Using a centrifuge, collect the yellowish precipitate [1], then wash the precipitate three times, each with deionized water and ethanol [2].

    - Talent shows the pellet formed after centrifugation.

    - Talent washing the resulting yellowish precipitate sequentially with deionized water and ethanol.

  - Transfer the washed yellowish precipitate into an oven and dry it overnight at 60 degrees Celsius to obtain zinc cadmium sulfide solid powder [1].

    - Talent placing the washed yellowish precipitate into a drying oven set at 60 degrees Celsius.

  - To synthesize the photo catalyst, dissolve 4 milligrams of zinc cobalt sulfide and 0.196 grams of zinc cadmium sulfide into 40 milliliters of deionized water [1].  After ultrasonication, collect the yellowish precipitate [2], then wash the sample three times each with deionized water and ethanol [3].

    - Talent adding zinc cobalt sulfide and zinc cadmium sulfide powders into a beaker containing 40 milliliters of deionized water.

    - Talent shows the pellet formed after centrifugation.

    - Talent washing the precipitate alternately with deionized water and ethanol three times.

  - Transfer the washed yellowish precipitate into an oven and dry it overnight at 60 degrees Celsius [1]. The final product is a yellowish zinc cobalt sulfide and zinc cadmium sulfide solid powder [2].

    - Talent placing the yellowish precipitate into an oven set at 60 degrees Celsius.

    - Close-up of the dried yellowish zinc cobalt sulfide/zinc cadmium sulfide powder in a container.

- Photoredox Dual Reaction of Benzyl Alcohol Oxidation and H2 Production Measurement

Demonstrator: Click here to enter name of demonstrator(s)

  - Add 20 milligrams of the synthesized photocatalyst and 60 milliliters of benzyl alcohol aqueous solution into a 100-milliliter beaker [1]. Place the beaker in an ultrasonic cleaner and perform ultrasonication for 30 minutes [2].

    - Talent adding 20 milligrams of photocatalyst and pouring 60 milliliters of benzyl alcohol aqueous solution into a 100 milliliter beaker.

    - Talent operating the ultrasonic cleaner with the beaker inside for 30 minutes.

  - Then, transfer the solution into a three-necked top-irradiation reactor cell [1] and insert a magnetic stirrer bar [2]. Maintain the solution under slow stirring throughout the entire reaction process [3].

    - Talent transferring the ultrasonicated solution into a three-necked top-irradiation reactor.

    - Talent placing a magnetic stir bar inside.

    - Shot of the solution stirring slowly during the reaction.

  - Next, connect a moisture trap to the downstream side of the reactor cell [1]. Then connect the outlet to the gas sampling loop inlet of the gas chromatography system [2]. Further, connect the gas sampling loop outlet to the reactor cell inlet to form a closed gas circulation system [3].

    - Talent attaching a moisture trap to the downstream port of the reactor cell.

    - Talent connecting tubing from the moisture trap to the gas sampling loop inlet of the gas chromatography system.

    - Talent connecting the gas sampling loop outlet back to the reactor cell inlet to complete a closed-loop system.

  - Seal the reactor with a glass window [1]. Then purge nitrogen gas at a flow rate of 50 milliliters per minute through the reactor for 30 minutes to remove all air inside [2].

    - Talent placing a glass window on top of the reactor and securing the seal.

    - Talent turning on the nitrogen supply and adjusting the flow rate to 50 milliliters per minute for purging.

  - Now, turn on the peristaltic pump and set the flow rate to 20 milliliters per minute to circulate the nitrogen gas within the closed gas circulation system [1].

    - Talent switching on the peristaltic pump and setting the digital flow controller to 20 milliliters per minute.

  - Switch on the Xenon lamp at 15 volts and position it so that the light passes through the glass window and reaches the solution inside the reactor [1-TXT].

    - Talent switching on the Xenon lamp and adjusting its position in front of the reactor glass window. TXT: Light intensity: 84.6 mW/cm²; Distance: 15 cm

  - Once the reaction is complete, using a 0.22-micrometer nylon syringe filter, filter 1 milliliter of the suspension [1]. Dilute the filtered suspension with deionized water in a ratio of 1 to 9 [2].

    - Talent drawing 1 milliliter of the reaction suspension into a syringe and attaching a 0.22 micrometer nylon filter.

    - Talent diluting the filtered sample in a tube with deionized water at a 1 to 9 volume ratio.

  - Finally, use a high-performance liquid chromatography system equipped with a photodiode array detector and a high-performance 100 Angstrom column [1-TXT].

    - Show the HPLC setup with a photodiode array detector and Poroshell 120 EC-C18 column installed. TXT: Mobile phase: H₂O/ACN (60:40); Detection: 254 nm

# Results

Please review this section to make sure that it accurately reflects your findings.

- This section will not be recorded by the videographer. It only includes the figures/tables from your manuscript (called LAB MEDIA).

- Use Track Changes when making edits or revisions. Ensure the voiceover length is below 200 words. Current word count: 179.

- Please note that the video cannot include voiceover without an accompanying visual.

- Results

  - The high-resolution transmission electron microscopy images confirmed the coexistence of zinc blende and wurtzite phases in Zinc cadmium sulphide [1], and an interphase boundary clearly distinguished the two crystalline domains [2].

    - LAB MEDIA: Figure 1A and B. Video editor: Highlight the labels and lines showing "ZB ZnCdS (111) 0.32 nm" and "WZ ZnCdS (100) 0.36 nm" on the left and right sides of the image.

    - LAB MEDIA: Figure 1A and B. Video editor: Highlight the region marked as "ZB/WZ interphase" in the center of the image.

  - The interface structure of the Zinc cobalt sulphide and Zinc cadmium sulphide heterojunction was distinctly observed [1], demonstrating the successful incorporation of Zinc cobalt sulphide on the zinc blende and wurtzite interphases of Zinc cadmium sulphide  [2].

    - LAB MEDIA: Figure 1C.

    - LAB MEDIA: Figure 1C. Video editor: Trace or outline the wavy interface separating the ZnCoS and ZnCdS regions.

  - The UV-Visible absorbance spectra showed that Zinc cadmium sulphide had a higher absorbance in the visible region compared to Zinc cobalt sulphide [1], and the Zinc cobalt sulphide and Zinc cadmium sulphide heterojunction exhibited slightly enhanced absorbance over Zinc cadmium sulphide alone [2].

    - LAB MEDIA: Figure 2A. Video editor: Highlight the green dashed line labeled ZnCdS that shows a higher drop across 400–600 nm.

    - LAB MEDIA: Figure 2A. Video editor: Highlight the purple dashed line labeled ZnCoS/ZnCdS that follows above ZnCdS in the visible range.

  - The optical bandgap of Zinc cadmium sulphide was calculated to be approximately 2.49 electron volts based on Tauc plot analysis [1].

    - LAB MEDIA: Figure 2B.

  - Nitrogen adsorption-desorption isotherms revealed that the Zinc cobalt sulphide and Zinc cadmium sulphide samples exhibited mesoporous characteristics, with a sharp increase in adsorption at relative pressure near 1.0 [1].

    - LAB MEDIA: Figure 3A. Video editor: Highlight the steep upward curve on the far right of the graph around P/P₀ = 1.0.

  - The pore size distribution of Zinc cobalt sulphide and Zinc cadmium sulphide was concentrated primarily between 25 and 35 nanometers, confirming the mesoporous nature of the material [1].

    - LAB MEDIA: Figure 3B. Video editor: Highlight the two peak regions within the 25–35 nm range of the x-axis.