# Submission ID #: 68870

# Scriptwriter Name: Pallavi Sharma

# Project Page Link: https://review.jove.com/files_upload.php?src=21005398

Title: Solar-Driven Electrochemical Green Fuel Production from CO₂ and Water Using Ti₃C₂Tₓ MXene-Supported CuZn and NiCo Catalysts

# Authors and Affiliations:

Nusrat Rashid1*, Shurui Yang1, Preetam Kumar Sharma1, Zahra Albu1, Anupma Thakur2, Babak Anasori2,3, Mojtaba Abdi-Jalebi1*

1Institute for Materials Discovery, University College London

2School of Materials Engineering, Purdue University

3School of Mechanical Engineering, Purdue University

☐   All author names and affiliations are correct (city/state/country information not included in video title page).

# Corresponding Authors:

Nusrat Rashida		(nusrat.rashid@ucl.ac.uk)

Mojtaba Abdi-Jalebia		(m.jalebi@ucl.ac.uk)

# Email Addresses for All Authors:

Shurui Yang shurui.yang.22@ucl.ac.uk

Preetam Kumar Sharma preetam.sharma@ucl.ac.uk

Zahra Albua zahra.albu.22@ucl.ac.uk

Anupma Thakur thakur40@purdue.edu

Babak Anasori banasori@purdue.edu

## Author Questionnaire

1. Microscopy: Does your protocol require the use of a dissecting or stereomicroscope for performing a complex dissection, microinjection technique, or something similar?  Enter Yes or No.

If Yes, can you record movies/images using your own microscope camera?

Enter Yes or No.

If your protocol involves microscopy but you are not able to record movies/images with your microscope camera, JoVE will need to use our scope kit.

If your microscope does not have a camera port, the scope kit will be attached to one of the eyepieces and you will have to perform the procedure using one eye.

Enter make and model of microscope.

If a dissection or stereo microscope is required for your protocol, please list all shots from the script that will be visualized using the microscope (shots are indicated with the 3-digit numbers, like 2.1.1, 2.1.2, etc.).

Click here to list microscope shots, using the shot numbers from the protocol section of the video script.

2. Software: Does the part of your protocol being filmed include step-by-step descriptions of software usage?  Enter Yes or No.

If Yes, we will need you to record using screen recording software.

We recommend using the screen capture program OBS. JoVE’s tutorial for using OBS Studio is provided at this link: https://review.jove.com/v/5848/screen-capture-instructions-for-authors?status=a7854k

As these files are necessary for finalizing your script, please upload all screen-captured video files to your project page as soon as possible.

3. Filming location: Will the filming need to take place in multiple locations?   Enter Yes or No.

If Yes, how far apart are the locations? Click to enter distance between locations.

4. Testimonials (optional): Would you be open to filming two short testimonial statements live during your JoVE shoot? These will not appear in your JoVE video but may be used in JoVE’s promotional materials. Enter Yes or No.

If Yes, please provide the full name and position (e.g., Director of [Institute Name], Senior Researcher [University Name], etc.) of the author willing to participate.

Enter full author name, Enter author position

To ensure that your script can be filmed in one day, the protocol sections are cumulatively restricted to 55 shots (shots are the 3-digit numbers like 2.1.1, 2.1.2…etc)

Current Protocol Length

Number of Steps: 27

Number of Shots: 56

# Introduction

Videographer: Obtain headshots for all authors available at the filming location.

Answers to these questions will become interview statements that you will deliver on camera.

- Answer up to 2 introduction and up to 3 conclusion questions. No more than 5 interview statements will be included in the video.

- Enter the full name of the author who will deliver the statement.

- Speak naturally and avoid reading the lines.

- Answer in full sentences, the questions will not be displayed in the video.

- Limit the length of each statement to 20 words or fewer.

- Answers will be edited for length, clarity, and consistency with journal style guidelines.

INTRODUCTION:

What is the scope of your research? What questions are you trying to answer?

  - Enter author name.: Click here to answer question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 20 or fewer words.

What are the most recent developments in your field of research?

  - Enter author name: Click here to answer question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 20 or fewer words.

What technologies are currently used to advance research in your field?

  - Enter author name: Click here to answer question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 20 or fewer words.

What are the current experimental challenges?

  - Enter author name: Click here to answer question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 20 or fewer words.

CONCLUSION:

What significant findings have you established in your field?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 20 or fewer words.

What research gap are you addressing with your protocol?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 20 or fewer words.

What advantage does your protocol offer compared to other techniques?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 20 or fewer words.

How will your findings advance research in your field?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 20 or fewer words.

What new scientific questions have your results paved the way for?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 20 or fewer words.

What questions will future research focus on?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 20 or fewer words.

Videographer: Obtain headshots for all authors available at the filming location.

# Protocol

Please review this section to make sure that it accurately describes your protocol. Use Track Changes when making edits or revisions.

- The two-digit steps (e.g., 2.1., 2.2.) with purple font are the narration.  JoVE is responsible for the narration of the protocol and results.

- Red italics are pronunciation guides indicating how the word will be spoken.

- Filming should take no more than 10 minutes per step. If a step takes more than 10 minutes, prepare the product for that step in advance.

- The three-digit shots (e.g., 2.1.1., 2.2.2.) are the actions that the videographer will capture.

- Fabrication of MXene-Supported Electrodes

Demonstrator: Click here to enter name of demonstrator(s)

If the same person is the demonstrator throughout, mention them once here and remove the "Demonstrator" field from the other sections; if the demonstrator changes, retain the field in the respective sections.

  - To begin, clean the nickel foam using acetone [1]. Then, sonicate the nickel foam in deionized water for 5 minutes [2].

    - WIDE: Talent placing nickel foam into a beaker containing acetone.

    - Talent placing the cleaned nickel foam into a sonicator filled with deionized water.

  - Under the fume hood, soak the carbon fiber paper in 1 molar nitric acid for 20 minutes to activate it while wearing gloves and appropriate personal protective equipment [1].

    - Talent placing a piece of carbon fiber paper into a beaker containing 1 molar nitric acid under a fume hood.

  - Immerse the cleaned nickel foam in MXene (M-Xene) solution for 5 minutes [1]. Then, dry it at room temperature under vacuum [2] and label the resulting sample as MXene-Nickel-Foam [3].

    - Talent immersing the nickel foam into a beaker containing MXene solution.

    - Talent placing the soaked nickel foam inside a vacuum chamber at room temperature.

    - Talent labeling the dried sample as MXene-Ni-Foam.

  - Now, load 50 milliliters of MXene solution into a spray gun [1]. Spray the MXene ink from 5 centimeters onto the activated carbon fiber paper, ensuring the entire surface of the 2 centimeter by 2 centimeter piece is covered [2]. Label the coated sample as MXene-CFP (M-Xene-G-F-P) [3].

    - Talent filling a spray gun reservoir with 50 milliliters of MXene solution.

    - Talent holding the spray gun 5 centimeters above the carbon fiber paper and spraying evenly.

    - Talent labels the sample as MXene-CFP.

  - Next, add copper and zinc precursor solutions into a glass electrochemical cell [1]. Insert a silver or silver chloride reference electrode, a platinum counter electrode, and the MXene-CFP working electrode into the cell [2]. Then, connect each electrode to its respective terminal on the potentiostat [3-TXT].

    - Talent pouring copper and zinc solutions into a glass electrochemical cell.

    - Talent placing Ag/AgCl reference electrode, platinum counter electrode, and MXene-CFP working electrode into the solution.

    - Talent connecting each electrode to its corresponding port on the potentiostat. TXT: Electrolyte bath: 50 mL DI water with 30 mM Cu citrate + 10 mM Zn oxalate

  - Apply the given pulsed current deposition sequence and repeat for 1,000 times to deposit the copper-zinc layer [1]. Label the final electrode as Copper zinc at Ti₃C₂Tₓ-MXene-CFP [2].

    - TEXT ON A PLAIN BACKGROUND

-10 mA/cm² for 1 s

0mA/cm² (null pulse) for 0.5 s

+10 mA/cm² for 0.5 s

    - Talent labeling the completed electrode.

  - In a separate electrochemical cell, add nickel and cobalt precursor solutions [1]. Use the same electrode configuration but replace the working electrode with the MXene-Nickel-Foam [2]. Connect all electrodes to the appropriate inputs on the potentiostat, ensuring the MXene-Ni-Foam is connected as the working electrode [3]. Prepare the electrolyte bath with 50 milliliters of 50 millimolar nickel nitrate and cobalt nitrate dissolved in deionized water [4-TXT].

    - Talent pouring nickel nitrate and cobalt nitrate solutions into a glass electrochemical cell.

    - Talent placing the MXene-Ni-Foam as the working electrode.

    - Talent connecting each electrode to the correct port on the potentiostat.

    - Talent adding electrolyte solution in the cell. TXT: Repeat 1000 sets to obtain NiCo@Ti3C2Tx-MXene-Ni-Foam

  - Then, fill a spray gun with 50 milliliters of platinum on carbon solution [1]. From 5 centimeters, spray-coat the platinum on carbon onto a nickel mesh [2]. Dry the coated mesh in a vacuum oven at 60 degrees Celsius to create the reference cathode for water electrolysis [3].

    - Talent filling the reservoir of a spray gun with 50 milliliters of platinum on carbon solution.

    - Talent spraying platinum on carbon evenly over a piece of nickel mesh.

    - Talent placing the sprayed nickel mesh into a vacuum oven and setting the temperature to 60 degrees Celsius.

- Electrochemical CO2 Reduction

  - To assemble a hydrogen-cell, insert an alkaline exchange membrane to separate the two chambers [1].

    - Talent inserting an alkaline exchange membrane into the slot.

  - Use nickel foam as the anode and a 2-centimeter by 2-centimeter Copper-Zinc at Ti₃C₂Tₓ-MXene-CFP electrode as the cathode [1]. Then, fill both chambers with 1 molar potassium hydroxide solution as the electrolyte [2]. Check the membrane junction thoroughly for any electrolyte leaks and tighten the junction if needed [3].

    - Talent placing nickel foam into the anode compartment and the CuZn-MXene-CFP into the cathode compartment.

    - Talent pouring 1 molar potassium hydroxide into both chambers.

    - Talent inspecting the membrane junction closely.

  - Now, insert a mercury or mercury oxide reference electrode into the cathode chamber [1] and seal the entire system to ensure it is gas-tight [2]. Add one tube for carbon dioxide inlet and another for the gas outlet in the cathodic chamber [3].

    - Talent inserting a mercury/mercury oxide electrode into the cathode side.

    - Talent sealing the system.

    - Talent connecting two flexible tubes to the cathodic chamber—one labeled for CO₂ inlet and one for gas outlet.

  - Then, purge carbon dioxide into the cathodic chamber at a rate of 30 milliliters per minute for 15 minutes to saturate the electrolyte [1].

    - Talent opening the carbon dioxide gas line and setting the flowmeter to 30 milliliters per minute.

  - Illuminate the photovoltaic cell with 1-sun intensity [1] and connect it to the cell [2].

    - Talent illuminating the cell

    - Talent connecting the cell.

  - Now, record cyclic voltammetry from 0 volts to minus 2.5 volts at a scan rate of 50 millivolts per second and EIS at open circuit potential [1].

    - Cyclic voltammetry and EIS are being recorded.

  - Perform a zero-ampere chrono potentiometric measurement for 2 hours [1]. Record the current periodically using a multimeter to calculate the faradaic efficiency of the products [2].

    - Show the potentiostat interface with the current set to 0 ampere.

    - Talent using a multimeter to manually record current readings at regular intervals from the output terminals.

  - Connect the gas outlet of the cathodic chamber to a gas chromatograph for in-line sampling every 10 minutes [1]. Program the gas chromatograph to detect and quantify permanent gases using a packed column such as a molecular sieve [2]. Set the oven temperature to start at 150 degrees Celsius with a 2-minute hold, then ramp to 200 degrees Celsius with a 1-minute hold for effective separation and elution of gases [3].

    - Talent attaching tubing from the cathodic chamber to the inlet of a gas chromatograph.

    - SCREEN: Show the GC software interface displaying the selection of a molecular sieve packed column and settings for gas identification.

Authors: Please create screen capture videos of the shots labeled as SCREEN, create a screenshot summary, and upload the files to your project page as soon as possible: https://review.jove.com/files_upload.php?src=21005398

    - SCREEN: Show the oven temperature programming—initial temperature of 150 degrees Celsius held for 2 minutes, ramped to 200 degrees Celsius with a 1-minute hold.

- Electrochemical Water Electrolysis (OER)

  - Repeat the H-cell assembly using Nickel cobalt at Ti₃C₂Tₓ-MXene-Nickel-Foam as the anode and platinum on carbon-coated nickel mesh as the cathode [1]. Insert a mercury or mercury oxide reference electrode into the anodic chamber along with the working electrode [2].

    - Talent placing NiCo-MXene-Ni-Foam in the anodic chamber and Pt/C-Ni mesh in the cathodic chamber of a new H-cell setup.

    - Talent inserting the Hg/HgO electrode into the anodic chamber and adjusting its position next to the working electrode.

  - Fill both chambers of the H-cell with 1 molar potassium hydroxide solution [1].

    - Talent pouring 1 molar potassium hydroxide solution into both the anodic and cathodic chambers using a beaker.

  - Record cyclic voltammetry from 0 volts to 1.2 volts at a scan rate of 50 millivolts per second [1] and EIS (E-I-S) under open circuit conditions [2]. Use the OCP (O-C-P) determination function on the Autolab potentiostat to record the open circuit potential [3].

    - SCREEN: Show CV scan parameters being set—range from 0 to 1.2 volts at 50 millivolts per second.

    - SCREEN: Show EIS parameters.

    - SCREEN: Show selection of OCP determination function on the Autolab software interface and activation of the recording.

  - Now, illuminate the photovoltaic cell using a solar simulator positioned 5 centimeters away, set to 1-sun light intensity [1].

    - Talent aligning the solar simulator 5 centimeters from the PV cell and switching it on.

  - Connect the terminals of the photovoltaic cell to the electrodes [1] and perform a zero-ampere chrono potentiometric measurement. Monitor and log the current continuously for efficiency calculations [1].

    - Talent connecting the photovoltaic cell leads to the anode and cathode of the H-cell.

    - SCREEN: Show potentiostat display recording a chrono potentiometric curve at 0 ampere while current readings are logged periodically.

  - Now, connect the gas outlet of the cathode chamber to a gas chromatograph [1]. Then, analyze hydrogen gas production every 10 minutes using a thermal conductivity detector and nitrogen as the carrier gas [2].

    - Talent attaching tubing from the cathode outlet to the inlet of a gas chromatograph.

    - Show the thermal conductivity detection panel.

- Zero-Gap Electrolyzer Assembly

  - After washing the components with water, start assembling a zero-gap electrolyzer cell [1]. Prepare clean polyvinyl propylene tubing and attach compatible push and pull valves to create junctions between different parts of the alkaline water electrolysis setup [2].

    - Shot of all the required components placed on a clean bench.

    - Talent attaching push and pull valves at junctions to create secure connectors.

  - Stack the cell components sequentially, starting with the cell anode plate, NiCo at Ti₃C₂Tₓ-MXene-Ni-Foam anode, gasket, alkaline exchange membrane, another gasket, Platinum-carbon cathode, and finally the cathode cell plate [1]. Use alignment rods if available, or firmly position the layers manually on a table to keep them in place [2].

    - Talent laying down the cell anode plate, followed by NiCo-MXene-Ni-Foam anode, the gasket, Pt/C cathode, and the cathode cell plate in sequence.

    - Talent aligning all components on a flat surface while keeping them stationary by applying even pressure.

  - To assemble the zero-gap electrolyzer, align all layers and end plates properly and secure it using screws [1].

    - Talent aligning the cell layers and securing them with screws.

  - Connect the assembled cell to peristaltic pumps circulating 30 percent potassium hydroxide at a flow rate of 30 milliliters per minute [1-TXT].

    - Talent attaching inlet and outlet tubing from the peristaltic pump to the electrolyzer. TXT: Adjust flow rate as needed for gas removal and performance

  - Maintain the electrolyte reservoir at 60 degrees Celsius using an oil bath [1]. Monitor the temperature with a probe and avoid touching the cell or reservoir without thermal gloves [2].

    - Talent placing the reservoir containing potassium hydroxide into an oil bath set at 60 degrees Celsius.

    - Talent inserting a digital temperature probe into the reservoir.

# Results

Please review this section to make sure that it accurately reflects your findings.

- This section will not be recorded by the videographer. It only includes the figures/tables from your manuscript (called LAB MEDIA).

- Use Track Changes when making edits or revisions. Ensure the voiceover length is below 200 words. Current word count: 182.

- Please note that the video cannot include voiceover without an accompanying visual.

- Results

  - The diffraction pattern of Ti₃AlC₂ MAX exhibited characteristic peaks for M₃AlC₂ structure [1], and after selective etching and delamination, the peaks shifted to lower angles, suggesting the synthesis of Ti₃C₂Tₓ MXene [2].

    - LAB MEDIA: Figure 1A. Video editor: Highlight the top panel showing the (002) peak for Ti₃AlC₂ MAX with a diamond symbol.

    - LAB MEDIA: Figure 1A. Video editor: Highlight the bottom panel showing the shifted (002) peak for Ti₃C₂Tₓ MXene with a star symbol.

  - The scanning electron microscope image of the Ti₃AlC₂ MAX phase revealed its layered morphology [1].

    - LAB MEDIA: Figure 1B.

  - After selective etching and delamination, the scanning electron microscope image of Ti₃C₂Tₓ MXene deposited on an alumina anodic template exhibited a flake-like morphology consisting of single to few-layers [1].

    - LAB MEDIA: Figure 1C.

  - X-ray diffraction [1] and scanning electron microscope images confirmed the structures of copper zinc at Ti₃C₂Tₓ MXene at CFP and Nickel cobalt at Ti₃C₂Tₓ MXene at nickel foam [2].

    - LAB MEDIA: Figure 2A.

    - LAB MEDIA: Figure 2B.

  - Cyclic voltammetry measurements in 1 molar potassium hydroxide showed distinct curves for carbon dioxide reduction by Copper zinc at MXene and CFP [1] and for water electrolysis by nickel-cobalt at MXene and Nickel-Foam [2]

    - LAB MEDIA: Figure 4A. Video editor: Highlight the blue CV curve labeled “NiCo@MXene@Ni-Foam” on the upper half of the plot.

    - LAB MEDIA: Figure 4A. Video editor: Highlight the red CV curve labeled “CuZn@MXene@CFP” on the lower half of the plot.

  - EIS revealed different resistance profiles for the cathode copper-zinc at MXene and CFP in carbon dioxide reduction [1] and the anode nickel cobalt at MXene and nickel-Foam in water electrolysis [2].

    - LAB MEDIA: Figure 4B. Video editor: Highlight the red curve labeled “NiCo@MXene@Ni-Foam” with smaller arc.

    - LAB MEDIA: Figure 4B. Video editor: Highlight the blue curve labeled “CuZn@MXene@CFP” with larger arc.

  - The CV profile and chrono amperograms were observed at different applied cell potentials [1].

    - LAB MEDIA: Figure 4C and D.