# Submission ID #: 68871

# Scriptwriter Name: Sulakshana Karkala

# Project Page Link: https://review.jove.com/account/file-uploader?src=21005703

# Title: Production and Use of Customizable Agarose Molds for Scaffold-Free Mouse Ovarian Follicle Culture

# Authors and Affiliations:

# Hannes Campo1*, Prianka H. Hashim1*, Emily J. Zaniker-Gomez1, Samuel Gauthier1, Zihang Yan2, Hao Zhang2, James A. Ankrum3, Francesca E. Duncan1

# 1Department of Obstetrics and Gynecology, Feinberg School of Medicine, Northwestern University

# 2Department of Biomedical Engineering, Northwestern University

# 3Roy J. Carver Department of Biomedical Engineering, Pappajohn Biomedical Institute, University of Iowa

# *These authors contributed equally

☐   All author names and affiliations are correct (city/state/country information not included in video title page).

# Corresponding Authors:

Hannes Campo				hannes.campo@northwestern.edu

Francesca E. Duncan				f-duncan@northwestern.edu

# Email Addresses for All Authors:

Hannes Campo				hannes.campo@northwestern.edu

Prianka H. Hashim				prianka.hashim@northwestern.edu

Emily J. Zaniker				emily.zaniker@northwestern.edu

Samuel Gauthier				samuelj.gauthier@gmail.com

Zihang Yan					zihangyan2028@u.northwestern.edu

Hao Zhang					hfzhang@northwestern.edu

James A. Ankrum				james-ankrum@uiowa.edu

Francesca E. Duncan				f-duncan@northwestern.edu

## Author Questionnaire

1. Microscopy: Does your protocol require the use of a dissecting or stereomicroscope for performing a complex dissection, microinjection technique, or something similar?  Enter Yes or No.

If Yes, can you record movies/images using your own microscope camera?

Enter Yes or No.

If your protocol involves microscopy but you are not able to record movies/images with your microscope camera, JoVE will need to use our scope kit.

If your microscope does not have a camera port, the scope kit will be attached to one of the eyepieces and you will have to perform the procedure using one eye.

Enter make and model of microscope.

If a dissection or stereo microscope is required for your protocol, please list all shots from the script that will be visualized using the microscope (shots are indicated with the 3-digit numbers, like 2.1.1, 2.1.2, etc.).

Click here to list microscope shots, using the shot numbers from the protocol section of the video script.

2. Software: Does the part of your protocol being filmed include step-by-step descriptions of software usage?  Enter Yes or No.

If Yes, we will need you to record using screen recording software.

We recommend using the screen capture program OBS. JoVE’s tutorial for using OBS Studio is provided at this link: https://review.jove.com/v/5848/screen-capture-instructions-for-authors?status=a7854k

As these files are necessary for finalizing your script, please upload all screen-captured video files to your project page as soon as possible.

3. Filming location: Will the filming need to take place in multiple locations?   Enter Yes or No.

If Yes, how far apart are the locations? Click to enter distance between locations.

4. Testimonials (optional): Would you be open to filming two short testimonial statements live during your JoVE shoot? These will not appear in your JoVE video but may be used in JoVE’s promotional materials. Enter Yes or No.

To ensure that your script can be filmed in one day, the protocol sections are cumulatively restricted to 55 shots (shots are the 3-digit numbers like 2.1.1, 2.1.2…etc)

Current Protocol Length

Number of Steps: 27

Number of Shots: 50

# Introduction

Videographer: Obtain headshots for all authors available at the filming location.

Answers to these questions will become interview statements that you will deliver on camera.

- Answer the 1st REQUIRED question and at least 2 other questions (1.2 – 1.10) below. Up to 5 interview statements will be included in the video.

- Enter the full name of the author who will deliver the statement.

- If possible, each author should deliver no more than two statements.

- Answer in full sentences, in a style suitable for being spoken aloud.

- Limit the length of each statement to 30 words or fewer.

- Answers will be edited for length, clarity, and consistency with journal style guidelines.

REQUIRED: What is the scope of your research? What questions are you trying to answer?

  - Enter author name.: Click here to answer question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

What are the most recent developments in your field of research?

  - Enter author name: Click here to answer question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

What technologies are currently used to advance research in your field?

  - Enter author name: Click here to answer question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

What are the current experimental challenges?

  - Enter author name: Click here to answer question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

What significant findings have you established in your field?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

What research gap are you addressing with your protocol?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

What advantage does your protocol offer compared to other techniques?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

How will your findings advance research in your field?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

What new scientific questions have your results paved the way for?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

What research questions will your laboratory focus on in the future?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

Videographer: Obtain headshots for all authors available at the filming location.

Ethics Title Card

This research has been approved by the Institutional Animal Care and Use Committee (IACUC) at Northwestern University

# Protocol

Please review this section to make sure that it accurately describes your protocol. Use Track Changes when making edits or revisions.

- The two-digit steps (e.g., 2.1., 2.2.) with purple font are the narration.  JoVE is responsible for the narration of the protocol and results.

- Red italics are pronunciation guides indicating how the word will be spoken.

- Filming should take no more than 10 minutes per step. If a step takes more than 10 minutes, prepare the product for that step in advance.

- The three-digit shots (e.g., 2.1.1., 2.2.2.) are the actions that the videographer will capture.

- Custom CAD Design of 24-Well Silicone Micromolds for Follicle Culture Systems

Demonstrator: Click here to enter name of demonstrator(s)

If the same person is the demonstrator throughout, mention them once here and remove the "Demonstrator" field from the other sections; if the demonstrator changes, retain the field in the respective sections.

  - To begin, launch the CAD software on a computer system [1]. Open the 24-well master mold base design .step (dot-step) file on the software [2].
Authors: Please create screen capture videos of the shots labeled as SCREEN, create a screenshot summary, and upload the files to your project page as soon as possible: https://review.jove.com/account/file-uploader?src=21005703

    - WIDE: Talent sitting at workstation and opening CAD software.
AUTHORS: Please note that JoVE requires the opening shot to be a wide, non-screen capture. This shot was added specifically to meet that requirement.

    - SCREEN: The 24-well master mold base design .step file is being opened.

  - Select the internal surface area of the object [1], then navigate to the Solid tab in the Design workspace and select Create Sketch to insert the desired micromold design [2].

    - SCREEN: The internal surface area of the mold is being selected.

    - SCREEN: The Solid tab is being navigated to, then Create Sketch is being clicked.

  - Now, introduce the desired x and y dimensions and number of the microwells [1], then select Finish Sketch on the toolbar [2].

    - SCREEN: The dimensions and count of microwells are being entered into the design interface.

    - SCREEN: Finish Sketch is being clicked in the toolbar.

  - Create the 800 micrometer deep microwells using the Extrude function by sequentially selecting Solid , Create and Extrude [1]. Choose the Cut operation to form the microwell cavity [2].

    - SCREEN: Cursor navigating to Solid > Create > Extrude and selecting the sketch.

    - SCREEN: Talent selecting Cut operation and confirming the extrusion.

  - Now, choose a 0.100 millimeter radius fillet for the top of the microwells by clicking on Design, Solid, Modify and Fillet [1]. Export a copy of the new master mold design in .step format by selecting File and pressing Export [2].

    - SCREEN: Cursor clicking on Design>Solid> Modify > Fillet and applying a 0.100 millimeter radius to the microwell top.

    - SCREEN: Cursor navigating to File and clicking Export, selecting the .step format.

  - Open the 24-well silicone cast container 1 .step file [1], then insert the new master mold design as an external component by choosing Solid , Insert and Insert Component [2].

    - SCREEN: The 24-well silicone cast container 1 .step file is being loaded in the CAD software.

    - SCREEN: Cursor selecting Insert Component under the Solid tab.

  - Next, right-click on the inserted component and select Break Link to remove the reference to the master mold design [1].

    - SCREEN: Cursor right-clicking on the component and selecting Break Link from the dropdown menu.

  - Center the new master mold design within the 24-well silicone cast container 1 surface, ensuring it faces inward [1]. Select OK to align the objects [2].

    - SCREEN: Talent dragging the master mold component to align with the container.

    - SCREEN: Cursor clicking OK to finalize alignment.

  - Select the Cut operation, using the container as the target body and the master mold as the tool body to create the silicone molding cavity [1].

    - SCREEN: Cursor choosing the Cut operation and confirming the tool and target bodies.

  - Save and export the new 24-well silicone mold 1 as .stl (dot-S-T-L) and .step files [1].

    - SCREEN: Talent saving and exporting the file formats from the File menu.

- Fabrication and Sterilization of Multi-Layered Silicone Micromolds for Follicle Culture

Demonstrator: Click here to enter name of demonstrator(s)

  - Open the .stl files of the new 24-well silicone mold 1 and 24-well silicone cast container 2 using 3D print preparation software [1]. Orient the print with micropillars facing upwards and use the Drill Hole function to create a 1-millimeter wide opening to the side of the print [2].

    - SCREEN: Talent launching the 3D print software and loading the two .stl files.

    - SCREEN: Cursor rotating the model and selecting the Drill Hole tool to add the opening.

  - Print both container designs at a 25 micrometer layer thickness [1].

    - SCREEN: Talent initiating the 3D print process and selecting 25 micrometer resolution settings.

  - Inspect each print using a stereomicroscope [1-TXT]. Carefully ensure that all micropillars are separated and uniform in size and appearance [2].
Authors: Please create scope videos of the shots labeled as SCOPE and upload the files to your project page as soon as possible: https://review.jove.com/account/file-uploader?src=21005703

    - Talent placing print under stereomicroscope. TXT: Discard any 3D prints with imperfections

    - SCOPE: Clear view of uniformly separated micropillars under the stereomicroscope.

  - Cover the outside of the print with parafilm if the drill channel is not filled and store until further use [1].

    - Talent wrapping parafilm around the print and placing it in storage.

  - Next, place the prepared silicone in a vacuum desiccator for 5 minutes to remove air bubbles [1-TXT]. Pour the silicone mixture with a uniform flow into the 3D-printed mold, ensuring the level matches or is slightly below the mold surface for flatness [2]. Remove trapped air with a P200 pipette tip and degas again if needed [3].

    - Talent placing silicone mixture into vacuum desiccator and running degassing cycle. TXT: Repeat degassing upto 2x

    - Talent pouring silicone into mold with steady stream.

    - Talent using pipette tip to remove bubbles and reinserting into desiccator.

  - Cure the silicone at room temperature for at least 5 hours or preferably overnight [1].

    - Talent placing mold on flat surface and labeling it with curing time.

  - After curing, remove the silicone from the mold [1] and inspect the micromolds under a stereomicroscope [2]. Remove any excess material from the drill channel [3] and discard molds with bridging or damaged wells [4].

    - Talent demolding silicone carefully.

    - SCOPE: Shot of the micromolds being seen under a stereomicroscope.

    - Talent trimming excess material from drill channel.

    - SCOPE: Micromolds with bridging defects being identified and discarded.

  - Next, place the silicone mold into silicone mold container 2 for the second molding step, ensuring the side opening is aligned [1]. Spray the silicone mold lightly with embryo-safe mineral oil [2]. Wipe off the excess from the microwells [3].

    - Talent placing first mold into second container and verifying position.

    - Talent spraying the silicone mold with mineral oil.

    - Talent  blotting the microwells carefully.

  - Repeat the silicone mixing procedure and pour the new mixture into the second container, maintaining the level at or below the mold surface [1-TXT].

    - Talent mixing and pouring silicone into the container holding mold 1. TXT: Cure at RT for 5 h or overnight

  - The next day, separate the silicone from the 3D printed mold and the silicone molds 1 and 2 from each other [1].  After inspecting them microscopically,  discard the molds with bubbles or excess oil in the wells [2].

    - Talent gently separating two silicone molds.

    - Talent separating out defective molds and discarding them.

  - Now, wash the silicone mold with 70 percent ethanol [1].  Let it air dry for 30 minutes inside a laminar flow hood [2].

    - Talent spraying mold with 70% ethanol.

    - Talent placing the sterilized molds on a sterile surface in hood.

  - Once dry, place the mold into a sterilization pouch before autoclaving [1].

    - Talent sealing pouch and placing it in autoclave. TXT: Jacket pressure: 20 psi, Chamber temperature: 250 °F, Sterilizing time: 15 min

- Scaffold-Free Follicle Culture and Timelapse Imaging Using Agarose Micromolds

Demonstrator: Click here to enter name of demonstrator(s)

  - Seed secondary follicles from mice ovaries into pre-equilibrated agarose molds submerged in growth medium [1]. Under a microscope, use a 200-micrometer stripper tip to transfer 10 multilayer secondary follicles per micromold, placing them in adjacent microwells [2].

    - Talent preparing agarose mold setup.

    - SCOPE: Stripper tip transferring follicles into microwells.

  - Bend the stripper tip slightly to enhance precision during follicle transfer [1]. Transfer the follicles quickly to prevent pH or temperature fluctuations [2]. Confirm that all 10 follicles are similarly sized before finalizing the setup [3].

    - Talent bending stripper tip with sterile tweezers.

    - Talent working efficiently under microscope.

    - SCOPE: Final view of evenly spaced and sized follicles.

  - Next, place a light focuser cap on a handheld microscope [1]. Insert the microscope with mount into incubator and connect to laptop with software [2].

    - Talent placing light cap on microscope.

    - Talent positioning microscope and connecting laptop.

  - Position and align the culture well under microscope and adjust height and focus so all follicles are visible [1]. Use Auto White Balance (AWB) (Auto-White-Balance-A-W-B) and LED (L-E-D) Control, turn off Auto Exposure (AE) (Auto-Exposure-A-E), and select optimal exposure time [2-TXT].

    - Talent adjusting microscope focus.

    - SCREEN: AutoExposure is being turned off and the optimal exposure time is being selected. 
TXT: Ensure mold alignment is the same before and after each media change

  - Start timelapse imaging with a duration of 8 days and an interval of 30 min (minutes). Select Photo and turn off LED when not capturing images [1].

    - SCREEN: Software interface showing timelapse setup parameters and capture starting.

# Results

Please review this section to make sure that it accurately reflects your findings.

- This section will not be recorded by the videographer. It only includes the figures/tables from your manuscript (called LAB MEDIA).

- Use Track Changes when making edits or revisions. Ensure the voiceover length is below 200 words. Current word count: 209

- Please note that the video cannot include voiceover without an accompanying visual.

- Results

  - Follicles cultured in agarose micromolds showed continuous growth and antral cavity formation [1].

    - LAB MEDIA: Figure 6A. Video editor: Sequentially show images for D0 to D8

  - After induction of ovulation, follicles cultured in agarose micromolds yielded more ovulated eggs compared to those in alginate [1], though the spindle morphology of MII (M-Two) eggs did not differ significantly between groups [2].

    - LAB MEDIA: Figure 6B. Video editor: Highlight the post-hCG image in the agarose row

    - LAB MEDIA: Figure 6C. Video editor: Show the images side-by-side for both alginate and agarose conditions

  - Alginate-encapsulated follicles did not maintain their position during culture and are incompatible with timelapse imaging [1].

    - LAB MEDIA: Figure 6F 	Video Editor: Please sequentially highlight images labeled 0 h, 8 h, 16 h and 24 h

  - Individual follicle morphology, including Feret’s diameter, circularity, and aspect ratio could be tracked and measured throughout the culture period in agarose micromolds [2].

    - LAB MEDIA: Figure 6G Video Editor: Please sequentially show i to iii

  - Optical coherence tomography enabled 3D visualization of internal follicle structures such as antral cavities and follicle walls within micromolds [1], and also captured dynamic follicle rupture events during ovulation [2].

    - LAB MEDIA: Figure 7A. Video editor: Highlight the two large round follicles imaged by OCT.

    - LAB MEDIA: Figure 7B.

  - Agarose micromolds enabled histological analysis of multiple follicles in the same plane after paraffin embedding and sectioning [1], allowing identification of tissue presence or absence [2] and supporting H&E staining [3].

    - LAB MEDIA: Figure 7C(i-ii).

    - LAB MEDIA: Figure 7C(iii). Video editor: Please show the white arrow when VO says “presence” and green arrow when VO says “absence”.

    - LAB MEDIA: Figure 7C(iv).

  - A custom mold compatible with 96-well plates was designed for high-throughput culture, featuring 10 microwells per unit [1], and was successfully fabricated and visualized using silicone casting [2].

    - LAB MEDIA: Figure 8A(i–iii). Video editor: Sequentially show i to iii

    - LAB MEDIA: Figure 8C.

  - The design was compatible with both 3D printing [1] and downstream live imaging techniques, making it adaptable to a wide range of follicle culture stages [2].

    - LAB MEDIA: Figure 8D.

    - LAB MEDIA: Figure 8E