# Submission ID #: 68896

# Scriptwriter Name: Poornima G

# Project Page Link: https://review.jove.com/account/file-uploader?src=21013328

# Title: NiO Nanoflowers for Non-Enzymatic Amperometric Detection of Glucose

# Authors and Affiliations:

# Piyush Choudhary1, Chhavi Chetiwal1, Vijay K. Singh2, Ambesh Dixit1,3

# 1A-MAD Laboratory, Department of Physics, Indian Institute of Technology, Jodhpur

# 2Department of Physics, Indian Institute of Technology, Ropar

# 3Rishabh Centre for Research and Innovation in Clean Energy, Indian Institute of Technology, Jodhpur

# Corresponding Authors:

Ambesh Dixit 			ambesh@iitj.ac.in

# Email Addresses for All Authors:

Piyush Choudhary 		choudhary.25@iitj.ac.in

Chhavi Chetiwal 		m23ph1004@iitj.ac.in

# Vijay Kumar Singh 		vksingh@iitrpr.ac.in

Ambesh Dixit 			ambesh@iitj.ac.in

## Author Questionnaire

1. We have marked your project as author-provided footage, meaning you film the video yourself and provide JoVE with the footage to edit. JoVE will not send the videographer. Please confirm that this is correct.

√ Correct

2. Microscopy: Does your protocol require the use of a dissecting or stereomicroscope for performing a complex dissection, microinjection technique, or something similar?  No

3. Software: Does the part of your protocol being filmed include step-by-step descriptions of software usage?  Yes, all done

4. Proposed filming date: To help JoVE process and publish your video in a timely manner, please indicate the proposed date that your group will film here:  11/10/2025

When you are ready to submit your video files, please contact our Content Manager, Utkarsh Khare.

Current Protocol Length

Number of Steps:  25

Number of Shots:  55 (14 SC)

# Introduction

INTRODUCTION:

What is the scope of your research? What questions are you trying to answer?

  - Piyush Choudhary: The objective of this research is to demonstrate the effective processes involved in non-enzymatic electrochemical glucose detection.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B-roll: 2.3.1

What are the most recent developments in your field of research?

  - Piyush Choudhary: Transition Metal-Oxide nanoparticles have been an upcoming trend in modern glucose sensors thus giving rise to an era of non-enzymatic glucose sensors.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B-roll: 3.3.1

CONCLUSION:

What advantage does your protocol offer compared to other techniques?

  - Piyush Choudhary: Almost all current glucometers in the market rely on enzymes for the detection of glucose. The NiO nanoflower catalyst is among the best materials for replacing enzymes in glucose sensing.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B-roll: 4.2.1

How will your findings advance research in your field?

  - Piyush Choudhary: This video article paves the way for better understanding of procedures specially for beginners and researchers starting afresh in the field of biosensors.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B-roll: 6.2.1

# Protocol

- NiO Nanostructured Flower Synthesis

Demonstrator: Piyush Choudhary

  - To begin, prepare a 6 millimolar solution of nickel chloride dihydrate in 10 milliliters of ethanol [1].

    - WIDE: Talent adding nickel chloride dihydrate to a clean beaker.

  - In a separate beaker, prepare 10 milliliters of a 3 percent polyvinylpyrrolidone or PVP solution in deionized water [1]. Ultrasonicate the solution for 5 minutes at 40 kilohertz and 50 watts [2], then mechanically stir it for an additional 5 minutes [3-TXT].

    - Talent adding deionized water to a beaker containing PVP.

    - Talent placing the beaker in the ultrasonic bath and setting the frequency to 40 kilohertz and power to 50 watts.

    - Talent mechanically stirring the solution for 5 minutes using a magnetic stirrer. TXT: Repeat the ultrasonication and stirring cycle 2x

  - Once the PVP is completely dissolved, use a pipette to add 10 milliliters of the PVP solution dropwise into 10 milliliters of the nickel precursor solution under vigorous stirring [1]. Continue stirring the mixture for 30 minutes after the PVP addition [2].

    - Talent using a pipette to add the PVP solution dropwise into the nickel precursor solution while stirring continuously.

    - Talent placing the solution on a magnetic stirrer.

  - Next, add 10 milliliters of an 18 millimolar urea solution, prepared in a 1 to 1 mixture of deionized water and ethanol, dropwise to the stirred mixture [1]. Ensure that the total volume of the resulting solution is 30 milliliters [2].

    - Talent pipetting the urea solution dropwise into the beaker containing the nickel–PVP mixture.

    - Close-up shot showing the total solution volume reaching 30 milliliters mark on the beaker.

  - Stir the complete solution for 10 minutes [1]. Then, transfer it into a polytetrafluoroethylene vessel and seal the vessel inside a stainless steel autoclave [2].

    - Talent increasing the speed of the magnetic stirrer.

    - Talent carefully pouring the mixed solution into a polytetrafluoroethylene vessel and sealing it securely within the stainless steel autoclave.

  - Place the sealed autoclave in an electric oven set at 160 degrees Celsius and maintain it for 6 to 8 hours [1]. After completion, allow the autoclave to cool naturally to room temperature [2].

    - Talent placing the sealed autoclave into an electric oven and setting the temperature to 160 degrees Celsius.

    - Shot of turning off the oven.

  - Now, centrifuge the resultant product at 26.88 g to collect the green-colored, gelatinous nickel hydroxide precipitate [1]. Decant the clear supernatant solvent [2] and wash the precipitate with ethanol or deionized water at least three times [3]. Dry the washed precipitate at 70 degrees Celsius for 10 hours in an electric oven [4].

    - Talent loading the centrifuge tubes into the centrifuge.

    - Talent decanting the clear solvent from the centrifuged mixture.

    - Talent adding the green precipitate with ethanol or deionized water.

    - Talent placing the washed precipitate in an electric oven set at 70 degrees Celsius for 10 hours.

  - Then, place the dried powder in a box furnace set at 450 degrees Celsius for 4 hours to anneal [1] and obtain the pure-phase nickel oxide nanoflakes, which appear grey in color [2].

    - Talent placing the dried powder sample into a box furnace.

    - Close-up Shot of the grey nanoflakes.

- Electrode Fabrication

  - Polish the glassy carbon electrode with 0.05 micrometer alumina nanoparticle slurry on a clean electrode polishing pad by moving it repeatedly in the shape of the numeral eight [1]. Rinse the electrode immediately with deionized water [2] and ultrasonicate it using a bath sonicator in isopropyl alcohol and deionized water for 2 minutes each at 40 kilohertz and 50 watts [3].

    - Talent rubbing the glassy carbon electrode with 0.05 micrometer alumina nanoparticle slurry on a polishing pad in a figure-eight motion.

    - Talent adding deionized water to the polished electrode.

    - Talent placing the electrode in a bath sonicator containing isopropyl alcohol and deionized water.

  - Next, add a known mass of nickel oxide nanoflake powder, ranging from 3 to 15 milligrams, to 3 milliliters of deionized water to prepare a nanoparticle suspension [1]. Adjust the amount of powder so that the nanoparticle concentration ranges between 1 and 5 milligrams per milliliter [2].

    - Talent weighing nickel oxide nanoflake powder in a beaker.

    - Talent adding water to the beaker with nanoflake powder.

  - Place the mixture in a bath ultrasonicator for 10 to 20 minutes to achieve a uniform dispersion [1-TXT].

    - Talent placing the beaker containing the nanoparticle suspension into a bath sonicator. TXT: Ensure that no precipitates or settled particles remain

  - Now, cast 10 microliters of the aliquot by drop-casting it onto the cleaned surface of the glassy carbon electrodes [1]. Label the electrodes as NiO (N-I-O) NF 1 to NiO NF 5 and allow the modified electrodes to dry at room temperature overnight for 10 to 12 hours [2].

    - Talent pipetting and drop-casting 10 microliters of nanoparticle suspension onto the surface of the cleaned electrodes.

    - Talent labeling the electrodes sequentially as NiO NF 1 through NiO NF 5. NOTE: Not filmed, VO merged with the next shot

    - Talent placing the coated electrodes on a clean bench surface.

  - Use a diluted binder solution containing 0.5 weight percent in ethanol to compactly bind the nanoparticles onto the surface of the electrodes [1]. Carefully drop-cast 6 microliters of the binder solution onto each modified electrode [2] and let them dry in air at room temperature for 30 minutes [3]. Keep the prepared electrodes in a desiccator until further use [4].

    - Talent mixing the diluted binder solution in ethanol.

    - Talent drop-casting 6 microliters of the binder solution onto each electrode.

    - Talent placing the electrodes on work bench.

    - Talent placing the dried electrodes carefully inside a desiccator and closing the lid securely.

- Electrochemical Detection Process

  - Take 20 milliliters of 0.1 molar sodium hydroxide solution in the electrochemical cell to prepare the electroanalytical solution [1]. Use a three-electrode setup to analyze the glucose concentration [2]. Insert the silver or silver chloride electrode with 3 molar potassium chloride as the reference electrode and the platinum wire as the counter electrode [3].

    - Talent pouring 20 milliliters of 0.1 molar sodium hydroxide solution into the electrochemical cell.

    - Talent assembling the three-electrode system on the electrochemical workstation.

    - Close-up shot showing the silver/silver chloride reference electrode and platinum wire counter electrode properly positioned in the electrochemical cell.

  - Activate the nickel oxide nanoflake-modified glassy carbon electrode by stabilizing it with 15 cycles of cyclic voltammetry [1-TXT]. Set the potential window between 0 and 0.8 volts at a scan rate of 200 millivolts per second [2]. Observe that the nickel(III)/nickel(II) (nickel 3 to 2) reduction peak potential typically appears around 0.4 to 0.6 volts [3].

    - Talent placing the NiO NF@GCE electrode into the electrochemical cell. TXT: NiO NF@GCE: Nickel Oxide Nanoflake-Modified Glassy Carbon Electrode

    - SCREEN: Screen-4.2.2.mp4 00:08-00:20.

    - SCREEN: Screen-4.2.3.mp4

  - After stabilization, run chronoamperometry for real-time glucose detection using the glassy carbon electrode [1]. Firstly, establish the baseline by running chronoamperometry at the nickel reduction potential or glucose oxidation potential for 100 seconds [2]. Once the base current is established, pause the chronoamperometric experiment by selecting the Pause button in the software [3].

    - SCREEN: Screen-4.3.1.mp4

    - SCREEN: Screen-4.3.2.mp4 00:01-00:05 AND-00:20-00:24.

    - SCREEN: Screen-4.3.3.mp4 00:08-00:15.

  - Next, prepare a 2 molar glucose stock solution for analysis [1].

    - Talent mixing the glucose stock solution by inverting the tube.

  - Lift the electrode stand and add 10 microliters of the glucose stock solution to the electroanalytical solution to achieve a final glucose concentration of 1 millimolar [1-TXT]. Stir the solution for 30 seconds to achieve uniform mixing [2].

    - Talent lifting the electrode stand and pipetting 10 microliters of glucose stock into the electrochemical cell. TXT: Ensure negligible total volume change

    - Talent stirring the cell solution gently.

  - Place the electrodes back into their previous positions and resume the chronoamperometric measurement after 5 seconds by pressing the Resume button in the software [1]. Choose a 30-second analysis window for the chronoamperometric detection of different glucose concentrations [2].

    - SCREEN: Screen-4.6.1.mp4 .

    - SCREEN: Screen-4.6.2.mp4 Video editor: Please speed up.

  - Repeat the process of glucose addition and measurement to gradually increase the glucose concentration up to 15 millimolar and record the corresponding chronoamperometric responses [1].

    - Talent adding glucose aliquots to the cell.

- Optimization of Electrochemical Process Parameters

  - Using a low loading concentration of the nanomaterial, optimize the potential window where the Faradaic reaction occurs [1-TXT]. Perform an initial broad scan from negative 1 volt to positive 1 volt using cyclic voltammetry [2].

    - SCREEN: Screen-5.1.1.mp4. TXT: Use ~1mg/mL nanomaterial

    - SCREEN: Screen-5.1.2.mp4.

  - Identify a smaller potential range where the Faradaic reaction occurs by locating the reduction and oxidation peaks in the cyclic voltammogram [1-TXT].  Collect the cyclic voltammograms for the electrochemical process within the selected potential range [2].

    - SCREEN: Screen-5.2.1.mp4. TXT: Use 0.1 - 0.8 V window for NiO NF@GCE based electrodes in 0.1 M NaOH

    - SCREEN: Screen-5.2.2.mp4.

  - Now, add a small amount of glucose, typically 1 millimolar, to the electrochemical solution to generate distinct redox peaks [1]. Observe that the glucose addition enhances the peak corresponding to glucose oxidation, helping to resolve multiple peaks in the voltammogram [2].

    - Talent pipetting 10 microliters of glucose solution into the electrochemical cell.

    - SCREEN: Screen-5.3.2.mp4.

  - Identify the anodic peak potential corresponding to glucose oxidation, which changes with glucose concentration [1]. Measure chronoamperometric responses slightly above this potential for accurate detection [2].

    - SCREEN: Screen-4.2.3.mp4. 00:07-00:09 NOTE: Authors asked to reuse this clip

    - SCREEN: Screen-5.4.2.mp4.

  - Finally, once the potential window and glucose oxidation potential are determined, optimize the loading concentration by varying the nanomaterial suspension concentration drop-cast onto the electrode [1].

    - Talent drop-casting nanomaterial onto the electrode.

# Results

- Results

  - The X-ray diffraction pattern of the nickel oxide nanoflowers showed distinct peaks corresponding to the 111, 200, 220, 311, and 222 planes of nickel oxide, confirming phase-pure formation [1].

    - LAB MEDIA: Figure 1A. Video editor: Highlight the 5 peaks.

  - The Raman spectrum of nickel oxide nanoflowers displayed characteristic peaks at 512, 692, 1073, and 1460 inverse centimeters, confirming the nickel oxide phase [1].

    - LAB MEDIA: Figure 1B. Video editor: Highlight the four labelled peaks at 512, 692, 1073, and 1460 on the Raman spectrum.

  - The low-magnification micrograph showed uniformly distributed flower-shaped nickel oxide particles [1] and the high-magnification micrograph revealed marigold flower-like spherical particles with an average diameter of approximately 0.91 micrometer [1].

    - LAB MEDIA: Figure 1C.

    - LAB MEDIA: Figure 1D.

  - The cyclic voltammograms for different loading concentrations of nickel oxide nanoflowers showed increasing peak currents up to 4 milligrams per milliliter, after which they saturated [1].

    - LAB MEDIA: Figure 2A. Video editor: Highlight the curve labelled 5 mg/mL and the curve labelled 4 mg/mL.

  - Chronoamperometric responses obtained for different nanomaterial loadings demonstrated that electrodes with 4 milligrams per milliliter loading showed the highest current response to glucose [1].

    - LAB MEDIA: Figure 2B. Video editor: Emphasize the purple trace graph corresponding to 4 mg/mL .

  - The current response plotted against glucose concentration confirmed a higher slope for the 4 milligram per milliliter nickel oxide nanoflower electrode, indicating greater sensitivity [1].

    - LAB MEDIA: Figure 2C. Video editor: Highlight the line corresponding to 4 mg/mL NiO NF

  - The cyclic voltammogram of nickel oxide nanoflower-coated electrodes recorded with and without 2 millimolar glucose revealed an enhancement of the nickel redox peak upon glucose addition [1].

    - LAB MEDIA: Figure 2D. Video editor: Highlight the line corresponding to “nafion NiO NF4 @GCE+ 2mM glucose .

  - The chronoamperometric selectivity response indicated excellent discrimination against ascorbic acid, sucrose, fructose, and sodium chloride at 0.1 millimolar concentration [1].

    - LAB MEDIA: Figure 4A. Video editor: Sequentially highlight each labelled spike corresponding to AA, sucrose, fructose, and NaCl.

  - The chronoamperometric curves recorded across multiple cycles showed reproducible current responses, confirming electrode repeatability [1].

    - LAB MEDIA: Figure 4C. Video editor: Display the overlapping traces for cycle 1, cycle 5, cycle 10, and cycle 20 to show consistent current steps.

- Millimolar
Pronunciation link: https://www.merriam-webster.com/dictionary/millimolar
IPA: /ˌmɪləˈmoʊlər/
Phonetic Spelling: mil·uh·moh·ler

- Nickel chloride dihydrate
Pronunciation link: https://www.merriam-webster.com/dictionary/nickel
IPA: /ˈnɪkəl/
Phonetic Spelling: nik·uhl
(compound term; element pronunciation used as reference)

- Polyvinylpyrrolidone
Pronunciation link: https://www.merriam-webster.com/dictionary/polyvinylpyrrolidone
IPA: /ˌpɑːliˌvaɪnəlpɪˈroʊlɪˌdoʊn/
Phonetic Spelling: pol·ee·vy·nuhl·pih·roh·luh·dohn

- Ultrasonicate
Pronunciation link: https://www.merriam-webster.com/dictionary/ultrasonicate
IPA: /ˌʌltrəˈsɑːnɪˌkeɪt/
Phonetic Spelling: uhl·truh·saa·nih·kayt

- Kilohertz
Pronunciation link: https://www.merriam-webster.com/dictionary/kilohertz
IPA: /ˈkɪləˌhɝːts/
Phonetic Spelling: kil·uh·hurts

- Centrifuge
Pronunciation link: https://www.merriam-webster.com/dictionary/centrifuge
IPA: /ˈsɛntrəˌfjuːdʒ/
Phonetic Spelling: sen·truh·fyooj

- Polytetrafluoroethylene
Pronunciation link: https://www.merriam-webster.com/dictionary/polytetrafluoroethylene
IPA: /ˌpɑːliˌtɛtrəˌflʊroʊˈɛθɪˌliːn/
Phonetic Spelling: pol·ee·teh·truh·floor·oh·eth·uh·leen

- Autoclave
Pronunciation link: https://www.merriam-webster.com/dictionary/autoclave
IPA: /ˈɔːtəˌkleɪv/
Phonetic Spelling: aw·tuh·klayv

- Anneal
Pronunciation link: https://www.merriam-webster.com/dictionary/anneal
IPA: /əˈniːl/
Phonetic Spelling: uh·neel

- Nanoflakes
Pronunciation link: https://www.merriam-webster.com/dictionary/nano-
IPA: /ˈnænoʊˌfleɪks/
Phonetic Spelling: nan·oh·flayks

- Nanoflowers
Pronunciation link: https://www.merriam-webster.com/dictionary/nano-
IPA: /ˈnænoʊˌflaʊərz/
Phonetic Spelling: nan·oh·flow·erz

- Glassy carbon electrode
Pronunciation link: https://www.merriam-webster.com/dictionary/electrode
IPA: /ɪˈlɛkˌtroʊd/
Phonetic Spelling: ih·lek·trohd

- Chronoamperometry
Pronunciation link: https://www.merriam-webster.com/dictionary/chronoamperometry
IPA: /ˌkrɑːnoʊˌæmpəˈrɑːmətri/
Phonetic Spelling: kron·oh·am·puh·rah·muh·tree

- Cyclic voltammetry
Pronunciation link: https://www.merriam-webster.com/dictionary/voltammetry
IPA: /ˌvoʊlˈtæmɪtri/
Phonetic Spelling: vohlt·am·uh·tree

- Faradaic
Pronunciation link: https://www.merriam-webster.com/dictionary/faradaic
IPA: /fəˈreɪdɪk/
Phonetic Spelling: fuh·ray·dik

- Anodic
Pronunciation link: https://www.merriam-webster.com/dictionary/anodic
IPA: /əˈnɑːdɪk/
Phonetic Spelling: uh·nod·ik

- Raman
Pronunciation link: https://www.merriam-webster.com/dictionary/Raman
IPA: /ˈrɑːmən/
Phonetic Spelling: rah·muhn

- Diffraction
Pronunciation link: https://www.merriam-webster.com/dictionary/diffraction
IPA: /dɪˈfrækʃən/
Phonetic Spelling: dih·frak·shuhn

- Alumina
Pronunciation link: https://www.merriam-webster.com/dictionary/alumina
IPA: /əˈluːmɪnə/
Phonetic Spelling: uh·loo·mih·nuh

- Nafion
Pronunciation link: https://www.merriam-webster.com/dictionary/Nafion
IPA: /ˈnæfiˌɑːn/
Phonetic Spelling: naf·ee·on