# Submission ID #: 68982

# Scriptwriter Name: Pallavi Sharma

# Project Page Link: https://review.jove.com/files_upload.php?src=21039558

Title: Preparation of Carbon Fiber and Bamboo Fiber Reinforced Poly (Butylene Adipate-Co-Terephthalate) Foams by Supercritical Carbon Dioxide Foaming

# Authors and Affiliations:

Guanxian Qiu1,2, Ce Sun1,3,4, Haoran Yang1, Xiaojian Zhou2, Haiyan Tan1, Guoming Xu4, Yanhua Zhang1

1Northeast Forestry University Engineering Consulting and Design Research Institute Co., Ltd

2Guangxi Eco-engineering Vocational and Technical College, Liuzhou, China

3Key Laboratory of National Forestry and Grassland Administration on Highly-Efficient Utilization of Forestry Biomass Resources in Southwest China, Southwest Forestry University

4Hangzhou Longju Synthetic Material Co., Ltd

# Corresponding Authors:

Ce Sun 			(sunce@nefu.edu.cn)

Guoming Xu 		(nihaoa147852@126.com)

Yanhua Zhang 		(zhangyanhua@nefu.edu.cn)

# Email Addresses for All Authors:

Guanxian Qiu 		(2022011226@nefu.edu.cn)

Haoran Yang 		(WHITEPOPLARDZCL@nefu.edu.cn)

Xiaojian Zhou 		(xiaojianzhou@swfu.edu.cn)

Haiyan Tan 		(tanhaiyan@nefu.edu.cn)

Ce Sun 			(sunce@nefu.edu.cn)

Guoming Xu 		(nihaoa147852@126.com)

Yanhua Zhang 		(zhangyanhua@nefu.edu.cn)

## Author Questionnaire

1. We have marked your project as author-provided footage, meaning you film the video yourself and provide JoVE with the footage to edit. JoVE will not send the videographer. Please confirm that this is correct.

√ Correct

2. Microscopy: Does your protocol require the use of a dissecting or stereomicroscope for performing a complex dissection, microinjection technique, or something similar? No

3. Software: Does the part of your protocol being filmed include step-by-step descriptions of software usage? No

4. Proposed filming date: To help JoVE process and publish your video in a timely manner, please indicate the proposed date that your group will film here:28/09/2025

When you are ready to submit your video files, please contact our China Location Producer, Yuan Yue.

Current Protocol Length

Number of Steps: 24

Number of Shots: 45

# Introduction

  - Yanhua Zhang: This research focuses on developing PBAT/CF/BF composite foams using scCO₂ foaming technology to elucidate how fiber synergy enhances anti-shrinkage properties, reduces density, and improves compression resilience of the foams.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

What significant findings have you established in your field?

  - Guanxian Qiu: The PBAT/CF/BF composite foam studied provides an effective solution for the manufacture of degradable, shrink-resistant, lightweight and high-strength polyester foam, which has application prospects in packaging, thermal insulation, and other fields.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

NOTE: Due to quality issues, omit 1.3 and 1.4

What advantage does your protocol offer compared to other techniques?

  - Ce Sun: Our protocol uses a synergistic fiber blend (CF/BF) with scCO₂ foaming. This combination significantly reduces foam shrinkage while enhancing strength. It provides a green, efficient manufacturing solution for high-performance biodegradable foams.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera. Suggested B-roll: 4.2

How will your findings advance research in your field?

  - Ce Sun: Our findings offer a novel fiber synergy strategy to suppress foam shrinkage. This enables high-expansion biodegradable foams for sustainable applications.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

What questions will future research focus on?

  - Guanxian Qiu: Future research may focus on exploring the long-term degradation behavior of composite foam in different environments and assessing the economic feasibility and environmental impact of composite foam production.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

# Protocol

- Weighing, Pre-Mixing, and Melt-Extrusion of PBAT/CF

Demonstrator: Guanxian Qiu

  - To begin, place the PBAT (P-Bat), CF (C-F), and BF (B-F) in an oven set at 80 degrees Celsius and incubate for 8 hours [1]. Using an electronic balance, weigh PBAT and CF proportionally to make a total of 200 grams [2].

    - WIDE: Talent placing PBAT, CF, and BF samples loaded in a tray into the oven.

    - Talent weighing PBAT and carbon fiber.

  - Pour the weighed PBAT and carbon fiber into a polyethylene bag [1]. Mix the contents thoroughly by shaking and kneading the bag for 5 minutes to achieve a uniform preliminary dispersion [2].

    - Talent pouring the weighed PBAT and carbon fiber into a polyethylene bag.

    - Talent kneading and shaking the bag continuously on the bench for 5 minutes.

  - Then, turn on the power switch of the twin-screw extruder [1]. Set the temperature of each heating zone on the extruder to 135, 145, 155, 165, and 160 degrees Celsius, respectively [2].

    - Talent flipping the main power switch on the twin-screw extruder machine.

    - Show the extruder control panel as the operator adjusts zone temperatures.

  - Set the host screw rotation speed to 5 revolutions per minute and the feeder rotation speed to 3 revolutions per minute [1].

    - Show the host speed setting being adjusted to 5 revolutions per minute on the control panel.

  - Next, add pure PBAT pellets into the feed hopper of the extruder and operate the machine for 10 minutes to clean the screw [1]. Switch the feedstock to the PBAT and 20CF premixed material and extrude continuously [2].

    - Talent pouring pure PBAT pellets into the extruder feed hopper and starting the machine.

    - Talent pouring the PBAT and carbon fiber premix into the extruder hopper.

  - Then, collect the extruded material from the outlet [1] and crush it into granules using a powder granulator [2].

    - Talent collecting the extruded strand.

    - Talent feeding the extrudate into the powder granulator and operating the machine to produce granules.

- Compression Molding of Crushed PBAT/CF Premix

Demonstrator: Ce Sun

  - Turn on the power switch of the flat vulcanizing machine [1]. Then, set the temperature of both the upper and lower plates to 165 degrees Celsius [2].

    - Talent switching on the flat vulcanizing machine at the control panel.

    - Display the temperature control screen while setting the upper and lower plates to 165 degrees Celsius.

  - Measure 60 grams of the prepared granules according to the mold dimensions [1-TXT]. Lay a polytetrafluoroethylene film over a flat gasket [2] and immediately position the mold on top [3].

    - Talent weighing out exactly 60 grams of crushed granules on an electronic balance. TXT: Dimensions: 100 mm × 100 mm × 4 mm

    - Talent laying a polytetrafluoroethylene film neatly over the surface of the flat gasket.

    - Talent placing the mold directly on top of the film-covered gasket.

  - Evenly distribute the weighed granules into the mold cavity [1]. Cover the mold with another polytetrafluoroethylene film [2] and place a second flat gasket on top [3].

    - Talent spreading the 60 grams of material evenly within the mold using a spatula or gloved hands.

    - Talent placing a second polytetrafluoroethylene film over the filled mold.

    - Talent placing a flat gasket carefully over the film-covered mold.

  - Then, place the assembled mold setup at the center of the heating plate of the flat vulcanizing machine [1].

    - Talent positioning the mold assembly at the center of the heated plate.

  - Initiate the mold closing process on the flat vulcanizing machine, apply a pressure of 1 megapascal [1], and maintain the pressure for 3 minutes to expel trapped air and prevent bubble formation [2].

    - Display the pressure setting being adjusted to 1 megapascal.

    - Shot of the machine while the mold closing process is running.

  - Continue the mold closing operation, increase the pressure to 10 megapascals [1], and maintain this pressure for 10 minutes to ensure the material melts and fills the mold uniformly [2].

    - Display the pressure adjustment to 10 megapascals.

    - Talent monitoring the system.

  - Then, turn off the heating system [1], activate the cooling mechanism on the vulcanizing machine [2], and wait until the temperature drops below 40 degrees Celsius before depressurizing and removing the mold [3].

    - Talent turning off the heating controls on the machine.

    - Show the cooling system being activated on the control interface.

    - Talent checking the temperature display, then carefully opening the mold and removing it.

- ScCO2 Foaming Process

Demonstrator: Guanxian Qiu

  - Using a blade, cut the molded sheet into pieces [1-TXT].

    - Talent cut the flat molded sheet into pieces. TXT: Dimensions: 10 mm × 10 mm × 4 mm

  - Place the cut sample panels into the reaction vessel [1]. Using a wrench, tighten the bolts of the reactor lid and close the reactor securely [2]. Then, close the exhaust valve of the reaction kettle to seal the system [3].

    - Talent gently places multiple cut panels into the open chamber of the reactor.

    - Talent uses a wrench tool to fasten each bolt around the reactor lid and seal the chamber completely.

    - Talent turns the exhaust valve knob on the reaction kettle to the closed position.

  - Now, open the valve of the carbon dioxide cylinder [1]. After that, open the intake valve of the booster pump [2].

    - Talent rotating the main valve on the carbon dioxide cylinder.

    - Talent adjusting the intake valve on the booster pump.

  - Then, open the inlet valve of the reactor to inject carbon dioxide gas into the chamber [1]. After that, close the inlet valve of the reactor and allow the chamber to stabilize for 3 minutes [2].

    - Talent opens the reactor’s inlet valve.

    - Talent closing the reactor inlet valve and monitoring the pressure gauge.

  - To discharge air from inside the chamber open the exhaust valve of the reactor [1].

    - Talent opening the reactor exhaust valve.

  - Then, turn on the power switches of both oil baths [1] and set their temperatures to 165 degrees Celsius and 100 degrees Celsius, respectively [2].

    - Talent switching on the two oil baths at their respective control panels.

    - Show the temperature settings being adjusted to 165 degrees Celsius on one oil bath and 100 degrees Celsius on the other.

  - Place the reaction vessel containing the sample into the oil bath set at 165 degrees Celsius and incubate for 10 minutes [1].

    - Talent lowering the sealed reaction vessel into the 165 degrees Celsius oil bath.

  - Open the inlet valve of the reactor to pressurize it with carbon dioxide, set the pressure to 10 megapascals, and maintain the temperature for 10 minutes [1].

    - Talent opening the inlet valve and adjusting the pressure regulator to 10 megapascals.

  - Close the ventilation valve of the carbon dioxide cylinder [1], the intake valve of the booster pump [2], and the inlet valve of the reaction kettle [3].

    - Talent rotating the ventilation valve on the carbon dioxide cylinder to the closed position.

    - Talent turning the intake valve on the booster pump to the off position.

    - Talent securing the inlet valve on the reaction kettle to the closed position.

  - Then, transfer the reaction vessel to the second oil bath set at 100 degrees Celsius and maintain both temperature and pressure for 60 minutes [1].

    - Talent carefully lifting the reaction vessel from the 165 degrees Celsius bath and placing it into the 100 degrees Celsius oil bath.

  - Open the exhaust valve of the reactor and rapidly release the internal pressure within 3 seconds to obtain the foamed material [1].

    - Talent opens the exhaust valve of the reactor and releases the internal pressure.

# Results

- Results

  - Visual inspection confirmed clear differences in foam appearance and expansion with varying fiber content [1].

    - LAB MEDIA: Figure 2A. Video editor: Slowly pan across the labeled foam samples from left to right to show the color and thickness changes.

  - The density of pure PBAT foam was found to be 0.19 grams per cubic centimeter [1], with a foaming ratio of 6.23 [2] and a stabilized shrinkage rate of 55.63% [3].

    - LAB MEDIA: Figure 2B. Video editor: Highlight the orange bar labeled "PBAT/10CF/10BF"

    - LAB MEDIA: Figure 2C. Video editor: Highlight the orange bar labeled "PBAT/10CF/10BF"

  - Scanning electron microscopy revealed that the PBAT and 20CF foam had the largest cell size [1], followed by PBAT and 20BF [2], while foams with combined CF and BF showed intermediate sizes [3].

    - LAB MEDIA: Figure 3B. Video editor: Zoom in on the large circular cell structures labeled “CF nucleation sites.”

    - LAB MEDIA: Figure 3F. Video editor: Highlight the visibly large pores surrounded by “BF nucleation sites.”

    - LAB MEDIA: Figure 3C–E Video editor: Cycle through these three panels, briefly highlighting the moderate-sized cells in each.

  - The PBAT, CF, and BF foams exhibited the most uniform cell size distribution compared to CF-only or BF-only formulations [1].

    - LAB MEDIA: Figure 4. Video editor: Show the bell-shaped red curve  in 4C, E and F

  - The PBAT, 5CF, and 15BF foam achieved the highest cell density at 3.63 million cells per cubic centimeter [1].

    - LAB MEDIA: Figure 5. Video editor: Highlight the tall cyan-colored bar labeled "PBAT/5CF/15BF", which reaches the highest point on the y-axis.

  - The compressive strength was highest in PBAT,15CF, and 5BF foam, reaching 0.26 megapascals [1]. All composite foam samples exhibited consistent compressive resilience across the 0-50% strain range [2].

    - LAB MEDIA: Figure 6A. Video editor: Highlight the tall blue bar labeled "PBAT/15CF/5BF"

    - LAB MEDIA: Figure 6B–F. Video editor: Sequentially show each of the line graphs, emphasizing the upward curves extending to 50 percent strain.

- Polyethylene
Pronunciation link: https://www.merriam-webster.com/dictionary/polyethylene
IPA: /ˌpɑːliˈɛθəˌliːn/
Phonetic Spelling: paa·lee·eth·uh·leen

- Carbon fiber
Pronunciation link: https://www.merriam-webster.com/dictionary/carbon%20fiber
IPA: /ˈkɑːrbən ˌfaɪbər/
Phonetic Spelling: kar·buhn fy·ber

- Polytetrafluoroethylene
Pronunciation link: https://www.merriam-webster.com/dictionary/polytetrafluoroethylene
IPA: /ˌpɑːliˌtɛtrəˌflʊəroʊˈɛθəˌliːn/
Phonetic Spelling: paa·lee·teh·truh·floor·oh·eth·uh·leen

- Extruder
Pronunciation link: https://www.merriam-webster.com/dictionary/extruder
IPA: /ɪkˈstruːdər/
Phonetic Spelling: ik·stroo·der

- Vulcanizing
Pronunciation link: https://www.merriam-webster.com/dictionary/vulcanizing
IPA: /ˈvʌlkəˌnaɪzɪŋ/
Phonetic Spelling: vul·kuh·nyz·ing

- Megapascal
Pronunciation link: https://www.merriam-webster.com/dictionary/megapascal
IPA: /ˌmɛɡəˈpæskəl/
Phonetic Spelling: meg·uh·pas·kuhl

- Granulator
Pronunciation link: https://www.merriam-webster.com/dictionary/granulator
IPA: /ˈɡræn.jəˌleɪ.tər/
Phonetic Spelling: gran·yuh·lay·ter

- Compression molding
Pronunciation link: https://www.merriam-webster.com/dictionary/compression%20molding
IPA: /kəmˈprɛʃən ˈmoʊldɪŋ/
Phonetic Spelling: kuhm·presh·uhn mohld·ing

- Carbon dioxide
Pronunciation link: https://www.merriam-webster.com/dictionary/carbon%20dioxide
IPA: /ˈkɑːrbən daɪˈɑːksaɪd/
Phonetic Spelling: kar·buhn dy·ok·syd

- Scanning electron microscopy
Pronunciation link: https://www.merriam-webster.com/dictionary/scanning%20electron%20microscopy
IPA: /ˈskænɪŋ ɪˈlɛktrɑn maɪˈkrɑskəpi/
Phonetic Spelling: skan·ing ih·lek·tron my·krah·skuh·pee

- Incubate
Pronunciation link: https://www.merriam-webster.com/dictionary/incubate
IPA: /ˈɪŋkjəˌbeɪt/
Phonetic Spelling: ing·kyuh·bayt

- Reaction vessel
Pronunciation link: https://www.merriam-webster.com/dictionary/reaction%20vessel
IPA: /riˈækʃən ˈvɛsəl/
Phonetic Spelling: ree·ak·shuhn ves·uhl