# Submission ID #: 68982

# Scriptwriter Name: Pallavi Sharma

# Project Page Link: https://review.jove.com/files_upload.php?src=21039558

Title: Preparation of Carbon Fiber and Bamboo Fiber Reinforced Poly (butylene adipate-co-terephthalate) Foams by Supercritical Carbon Dioxide Foaming

# Authors and Affiliations:

Guanxian Qiu1,2, Ce Sun1,3,4*, Haoran Yang1, Xiaojian Zhou2, Haiyan Tan1, Guoming Xu4*, Yanhua Zhang1*

1Northeast Forestry University Engineering Consulting and Design Research Institute Co., Ltd

2Guangxi Eco-engineering Vocational and Technical College, Liuzhou, China

3Key Laboratory of National Forestry and Grassland Administration on Highly-Efficient Utilization of Forestry Biomass Resources in Southwest China, Southwest Forestry University

4Hangzhou Longju Synthetic Material Co., Ltd

☐   All author names and affiliations are correct (city/state/country information not included in video title page).

# Corresponding Authors:

Ce Sun 			(sunce@nefu.edu.cn)

Guoming Xu 		(nihaoa147852@126.com)

Yanhua Zhang 		(zhangyanhua@nefu.edu.cn)

# Email Addresses for All Authors:

Guanxian Qiu 		(2022011226@nefu.edu.cn)

Haoran Yang 		(WHITEPOPLARDZCL@nefu.edu.cn)

Xiaojian Zhou 		(xiaojianzhou@swfu.edu.cn)

Haiyan Tan 		(tanhaiyan@nefu.edu.cn)

Ce Sun 			(sunce@nefu.edu.cn)

Guoming Xu 		(nihaoa147852@126.com)

Yanhua Zhang 		(zhangyanhua@nefu.edu.cn)

## Author Questionnaire

1. We have marked your project as author-provided footage, meaning you film the video yourself and provide JoVE with the footage to edit. JoVE will not send the videographer. Please confirm that this is correct.

☐ Correct

☐ Incorrect

2. Microscopy: Does your protocol require the use of a dissecting or stereomicroscope for performing a complex dissection, microinjection technique, or something similar?  Enter Yes or No.

If a dissection or stereo microscope is required for your protocol, please list all shots from the script that will be visualized using the microscope (shots are indicated with the 3-digit numbers, like 2.1.1, 2.1.2, etc.).

Click here to list microscope shots, using the shot numbers from the protocol section of the video script.

3. Software: Does the part of your protocol being filmed include step-by-step descriptions of software usage?  Enter Yes or No.

If Yes, we will need you to record using screen recording software.

We recommend using the screen capture program OBS. JoVE’s tutorial for using OBS Studio is provided at this link: https://review.jove.com/v/5848/screen-capture-instructions-for-authors?status=a7854k

As these files are necessary for finalizing your script, please upload all screen captured video files to your project page as soon as possible.

4. Proposed filming date: To help JoVE process and publish your video in a timely manner, please indicate the proposed date that your group will film here: MM/DD/YYYY

DO NOT use this draft script for filming. Please wait until your script is finalized to begin the filming process.

When you are ready to submit your video files, please contact our China Location Producer, Yuan Yue.

To ensure that your script can be filmed in one day, the protocol sections are cumulatively restricted to 55 shots (shots are the 3-digit numbers like 2.1.1, 2.1.2…etc)

Current Protocol Length

Number of Steps: 24

Number of Shots: 45

# Introduction

Videographer: Obtain headshots for all authors available at the filming location.

Answers to these questions will become interview statements that you will deliver on camera.

- Answer the 1st REQUIRED question and at least 2 other questions (1.2 – 1.10) below. Up to 5 interview statements will be included in the video.

- Enter the full name of the author who will deliver the statement.

- If possible, each author should deliver no more than two statements.

- Answer in full sentences, in a style suitable for being spoken aloud.

- Limit the length of each statement to 30 words or fewer.

- Answers will be edited for length, clarity, and consistency with journal style guidelines.

REQUIRED: What is the scope of your research? What questions are you trying to answer?

  - Enter author name.: Click here to answer question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

What are the most recent developments in your field of research?

  - Enter author name: Click here to answer question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

What technologies are currently used to advance research in your field?

  - Enter author name: Click here to answer question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

What are the current experimental challenges?

  - Enter author name: Click here to answer question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

What significant findings have you established in your field?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

What research gap are you addressing with your protocol?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

What advantage does your protocol offer compared to other techniques?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

How will your findings advance research in your field?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

What new scientific questions have your results paved the way for?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

What questions will future research focus on?

  - Enter author name: Click here if you choose this question. Please write in a style that you will be comfortable memorizing and speaking aloud. Limit length to 30 or fewer words.

Videographer: Obtain headshots for all authors available at the filming location.

# Protocol

Please review this section to make sure that it accurately describes your protocol. Use Track Changes when making edits or revisions.

- The two-digit steps (e.g., 2.1., 2.2.) with purple font are the narration.  JoVE is responsible for the narration of the protocol and results.

- Red italics are pronunciation guides indicating how the word will be spoken.

- Filming should take no more than 10 minutes per step. If a step takes more than 10 minutes, prepare the product for that step in advance.

- The three-digit shots (e.g., 2.1.1., 2.2.2.) are the actions that the videographer will capture.

- Weighing, Pre-mixing, and Melt-extrusion of PBAT/CF

Demonstrator: Click here to enter name of demonstrator(s)

If the same person is the demonstrator throughout, mention them once here and remove the "Demonstrator" field from the other sections; if the demonstrator changes, retain the field in the respective sections.

  - To begin, place the PBAT (P-Bat), CF (C-F), and BF (B-F) in an oven set at 80 degrees Celsius and incubate for 8 hours [1]. Using an electronic balance, weigh PBAT and CF proportionally to make a total of 200 grams [2].

    - WIDE: Talent placing PBAT, CF, and BF samples loaded in a tray into the oven.

    - Talent weighing PBAT and carbon fiber.

  - Pour the weighed PBAT and carbon fiber into a polyethylene bag [1]. Mix the contents thoroughly by shaking and kneading the bag for 5 minutes to achieve a uniform preliminary dispersion [2].

    - Talent pouring the weighed PBAT and carbon fiber into a polyethylene bag.

    - Talent kneading and shaking the bag continuously on the bench for 5 minutes.

  - Then, turn on the power switch of the twin-screw extruder [1]. Set the temperature of each heating zone on the extruder to 135, 145, 155, 165, and 160 degrees Celsius, respectively [2].

    - Talent flipping the main power switch on the twin-screw extruder machine.

    - Show the extruder control panel as the operator adjusts zone temperatures.

  - Set the host screw rotation speed to 5 revolutions per minute and the feeder rotation speed to 3 revolutions per minute [1].

    - Show the host speed setting being adjusted to 5 revolutions per minute on the control panel.

  - Next, add pure PBAT pellets into the feed hopper of the extruder and operate the machine for 10 minutes to clean the screw [1]. Switch the feedstock to the PBAT and 20CF premixed material and extrude continuously [2].

    - Talent pouring pure PBAT pellets into the extruder feed hopper and starting the machine.

    - Talent pouring the PBAT and carbon fiber premix into the extruder hopper.

  - Then, collect the extruded material from the outlet [1] and crush it into granules using a powder granulator [2].

    - Talent collecting the extruded strand.

    - Talent feeding the extrudate into the powder granulator and operating the machine to produce granules.

- Compression Molding of Crushed PBAT/CF Premix

Demonstrator: Click here to enter name of demonstrator(s)

  - Turn on the power switch of the flat vulcanizing machine [1]. Then, set the temperature of both the upper and lower plates to 165 degrees Celsius [2].

    - Talent switching on the flat vulcanizing machine at the control panel.

    - Display the temperature control screen while setting the upper and lower plates to 165 degrees Celsius.

  - Measure 60 grams of the prepared granules according to the mold dimensions [1-TXT]. Lay a polytetrafluoroethylene film over a flat gasket [2] and immediately position the mold on top [3].

    - Talent weighing out exactly 60 grams of crushed granules on an electronic balance. TXT: Dimensions: 100 mm × 100 mm × 4 mm

    - Talent laying a polytetrafluoroethylene film neatly over the surface of the flat gasket.

    - Talent placing the mold directly on top of the film-covered gasket.

  - Evenly distribute the weighed granules into the mold cavity [1]. Cover the mold with another polytetrafluoroethylene film [2] and place a second flat gasket on top [3].

    - Talent spreading the 60 grams of material evenly within the mold using a spatula or gloved hands.

    - Talent placing a second polytetrafluoroethylene film over the filled mold.

    - Talent placing a flat gasket carefully over the film-covered mold.

  - Then, place the assembled mold setup at the center of the heating plate of the flat vulcanizing machine [1].

    - Talent positioning the mold assembly at the center of the heated plate.

  - Initiate the mold closing process on the flat vulcanizing machine, apply a pressure of 1 megapascal [1], and maintain the pressure for 3 minutes to expel trapped air and prevent bubble formation [2].

    - Display the pressure setting being adjusted to 1 megapascal.

    - Shot of the machine while the mold closing process is running.

  - Continue the mold closing operation, increase the pressure to 10 megapascals [1], and maintain this pressure for 10 minutes to ensure the material melts and fills the mold uniformly [2].

    - Display the pressure adjustment to 10 megapascals.

    - Talent monitoring the system.

  - Then, turn off the heating system [1], activate the cooling mechanism on the vulcanizing machine [2], and wait until the temperature drops below 40 degrees Celsius before depressurizing and removing the mold [3].

    - Talent turning off the heating controls on the machine.

    - Show the cooling system being activated on the control interface.

    - Talent checking the temperature display, then carefully opening the mold and removing it.

- ScCO2 Foaming Process

Demonstrator: Click here to enter name of demonstrator(s)

  - Using a blade, cut the molded sheet into pieces [1-TXT].

    - Talent cut the flat molded sheet into pieces. TXT: Dimensions: 10 mm × 10 mm × 4 mm

  - Place the cut sample panels into the reaction vessel [1]. Using a wrench, tighten the bolts of the reactor lid and close the reactor securely [2]. Then, close the exhaust valve of the reaction kettle to seal the system [3].

    - Talent gently places multiple cut panels into the open chamber of the reactor.

    - Talent uses a wrench tool to fasten each bolt around the reactor lid and seal the chamber completely.

    - Talent turns the exhaust valve knob on the reaction kettle to the closed position.

  - Now, open the valve of the carbon dioxide cylinder [1]. After that, open the intake valve of the booster pump [2].

    - Talent rotating the main valve on the carbon dioxide cylinder.

    - Talent adjusting the intake valve on the booster pump.

  - Then, open the inlet valve of the reactor to inject carbon dioxide gas into the chamber [1]. After that, close the inlet valve of the reactor and allow the chamber to stabilize for 3 minutes [2].

    - Talent opens the reactor’s inlet valve, observing gas flowing into the chamber through the transparent pipeline.

    - Talent closing the reactor inlet valve and monitoring the pressure gauge.

  - Open the exhaust valve of the reactor to discharge air from inside the chamber [1].

    - Talent opening the reactor exhaust valve, with a visible release of internal pressure.

  - Then, turn on the power switches of both oil baths [1] and set their temperatures to 165 degrees Celsius and 100 degrees Celsius, respectively [2].

    - Talent switching on the two oil baths at their respective control panels.

    - Show the temperature settings being adjusted to 165 degrees Celsius on one oil bath and 100 degrees Celsius on the other.

  - Place the reaction vessel containing the sample into the oil bath set at 165 degrees Celsius and incubate for 10 minutes [1].

    - Talent lowering the sealed reaction vessel into the 165 degrees Celsius oil bath.

  - Open the inlet valve of the reactor to pressurize it with carbon dioxide, set the pressure to 10 megapascals, and maintain the temperature for 10 minutes [1].

    - Talent opening the inlet valve and adjusting the pressure regulator to 10 megapascals.

  - Close the ventilation valve of the carbon dioxide cylinder [1], the intake valve of the booster pump [2], and the inlet valve of the reaction kettle [3].

    - Talent rotating the ventilation valve on the carbon dioxide cylinder to the closed position.

    - Talent turning the intake valve on the booster pump to the off position.

    - Talent securing the inlet valve on the reaction kettle to the closed position.

  - Then, transfer the reaction vessel to the second oil bath set at 100 degrees Celsius and maintain both temperature and pressure for 60 minutes [1].

    - Talent carefully lifting the reaction vessel from the 165 degrees Celsius bath and placing it into the 100 degrees Celsius oil bath.

  - Open the exhaust valve of the reactor and rapidly release the internal pressure within 3 seconds to obtain the foamed material [1].

    - Talent opens the exhaust valve of the reactor and releases the internal pressure.

# Results

Please review this section to make sure that it accurately reflects your findings.

- This section will not be recorded by the videographer. It only includes the figures/tables from your manuscript (called LAB MEDIA).

- Use Track Changes when making edits or revisions. Ensure the voiceover length is below 200 words. Current word count: 137.

- Please note that the video cannot include voiceover without an accompanying visual.

- Results

  - Visual inspection confirmed clear differences in foam appearance and expansion with varying fiber content [1].

    - LAB MEDIA: Figure 2A. Video editor: Slowly pan across the labeled foam samples from left to right to show the color and thickness changes.

  - The density of pure PBAT foam was found to be 0.19 grams per cubic centimeter [1], with a foaming ratio of 6.23 [2] and a stabilized shrinkage rate of 55.63% [3].

    - LAB MEDIA: Figure 2B. Video editor: Highlight the orange bar labeled "PBAT/10CF/10BF"

    - LAB MEDIA: Figure 2C. Video editor: Highlight the orange bar labeled "PBAT/10CF/10BF"

  - Scanning electron microscopy revealed that the PBAT and 20CF foam had the largest cell size [1], followed by PBAT and 20BF [2], while foams with combined CF and BF showed intermediate sizes [3].

    - LAB MEDIA: Figure 3B. Video editor: Zoom in on the large circular cell structures labeled “CF nucleation sites.”

    - LAB MEDIA: Figure 3F. Video editor: Highlight the visibly large pores surrounded by “BF nucleation sites.”

    - LAB MEDIA: Figure 3C–E Video editor: Cycle through these three panels, briefly highlighting the moderate-sized cells in each.

  - The PBAT,CF, and BF foams exhibited the most uniform cell size distribution compared to CF-only or BF-only formulations [1].

    - LAB MEDIA: Figure 4. Video editor: Show the bell-shaped red curve  in 4C, E and F

  - The PBAT, 5CF, and 15BF foam achieved the highest cell density at 3.63 million cells per cubic centimeter [1].

    - LAB MEDIA: Figure 5. Video editor: Highlight the tall cyan-colored bar labeled "PBAT/5CF/15BF", which reaches the highest point on the y-axis.

  - The compressive strength was highest in PBAT,15CF, and 5BF foam, reaching 0.26 megapascals [1]. All composite foam samples exhibited consistent compressive resilience across the 0-50% strain range [2].

    - LAB MEDIA: Figure 6A. Video editor: Highlight the tall blue bar labeled "PBAT/15CF/5BF"

    - LAB MEDIA: Figure 6B–F. Video editor: Sequentially show each of the line graphs, emphasizing the upward curves extending to 50 percent strain.