# Submission ID #: 69078

# Scriptwriter Name: Sulakshana Karkala

# Project Page Link: https://review.jove.com/account/file-uploader?src=21068838

# Title: MgO@α-Fe2O3 Based Hydroelectric Cell for Efficient Green Energy Generation

# Authors and Affiliations:

# Priyambada Sahoo1*, Soumya Ranjan Ghadai1*, Ambesh Dixit1,2

# 1Advanced Material and Device Lab, Department of Physics, Indian Institute of Technology-Jodhpur

# 2Rishabh Centre for Research and Innovation in Clean Energy, Indian Institute of Technology, Jodhpur

# *These authors contributed equally

# Corresponding Authors:

# Ambesh Dixit			(ambesh@iitj.ac.in)

# Email Addresses for All Authors:

Priyambada Sahoo		(priyambada.1@iitj.ac.in)

Soumya Ranjan Ghadai	(m23pm2006@iitj.ac.in)

Ambesh Dixit			(ambesh@iitj.ac.in)

## Author Questionnaire

1. We have marked your project as author-provided footage, meaning you film the video yourself and provide JoVE with the footage to edit. JoVE will not send the videographer. Please confirm that this is correct.

√ Correct

2. Microscopy: Does your protocol require the use of a dissecting or stereomicroscope for performing a complex dissection, microinjection technique, or something similar?  No

3. Software: Does the part of your protocol being filmed include step-by-step descriptions of software usage?  No

4. Proposed filming date: To help JoVE process and publish your video in a timely manner, please indicate the proposed date that your group will film here: 02/1/2026

When you are ready to submit your video files, please contact our Content Manager, Utkarsh Khare.

Current Protocol Length

Number of Steps:  17

Number of Shots:  43

# Introduction

Authors: Please note that the questions will not appear on screen. Please answer in stand-alone full sentence with sufficient context.

INTRODUCTION:

NOTE: Use the timestamps given below for intro and conclusion

REQUIRED: What is the scope of your research? What questions are you trying to answer?

  - Priyambada Sahoo: The scope of our research is developing MgO@α-Fe₂O₃ hydroelectric cells and understanding nanocomposite-enhanced water adsorption and charge transport mechanisms.

    - Use V_1.1-1.2_Introduction_R2 :00:00-00:10

What are the most recent developments in your field of research?

  - Priyambada Sahoo: Recent research explores defect associated ferrites and metal oxide and metal organic framework materials beyond simple oxides to enhance water-driven energy generation.

    - V_1.1-1.2_Introduction_R2 00:47-01:05.

CONCLUSION:

What significant findings have you established in your field?

  - Priyambada Sahoo: We established a high-performance MgO@α-Fe₂O₃ hydroelectric cell where optimized ferrite incorporation enhances defects, hydrophilicity, active sites, and doubles power output.

    - V_1.3-1.4-1.5_Conclusion_R2 00:00-00:20.

What research gap are you addressing with your protocol?

  - Priyambada Sahoo: Our protocol addresses the lack of a simple, scalable, and reproducible fabrication method for high-performance hydroelectric cells with controlled defect chemistry.

    - V_1.3-1.4-1.5_Conclusion_R2 00:20-00:44.

What advantage does your protocol offer compared to other techniques?

  - Priyambada Sahoo: Our protocol offers a low-cost, scalable solid-state fabrication approach enabling precise defect tuning and reproducible hydroelectric performance without external bias, light, or complex equipment.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

# Protocol

- Synthesis of Nanostructured Porous Magnesium Oxide–Iron(III) Oxide (MgO@α-Fe₂O₃) Composites via Ball Milling and Calcination

Demonstrator: Priyambada Sahoo

  - To begin, collect magnesium oxide powder and alpha iron(III) (three) oxide powder along with a ball miller, zirconia milling balls, and a milling bowl [1]. Weigh 5 grams of magnesium oxide [2] and add 2 percent, 5 percent, or 10 percent alpha iron(III) oxide, by weight, into a 50-milliliter milling bowl [3]. Add zirconia milling balls maintaining a ball-to-powder ratio of 4 to 1 [4].

    - WIDE: Talent arranging magnesium oxide, alpha iron(III) oxide, milling bowl, and zirconia balls on the workbench.

    - Talent weighing 5 g magnesium oxide.

    - Talent adding alpha iron(III) oxide powders to MgO and transferring them into the milling bowl.

    - Talent adding zirconia balls into the milling bowl.

  - Now, place the loaded bowl into the ball miller [1]. Set the ball rotation speed to 300 revolutions per minute and the bowl rotation speed to 600 revolutions per minute [2]. Ball mill the precursor powders continuously for 24 hours to ensure homogeneous mixing [3].

    - Talent placing the milling bowl into the ball miller.

    - Shot of  the ball miller control panel showing the rotation speeds being set.

    - Shot of  the milling process.

  - Collect the ball-milled powder from the bowl after milling [1] and transfer the powder into a crucible [2]. Place the crucible inside a box furnace and calcine at 600 degrees Celsius for 4 hours to obtain nanostructured porous material [3].

    - Talent collecting the ball-milled powder into a container.

    - Talent transferring the powder into a furnace-compatible crucible.

    - Talent placing the crucible inside the box furnace and closing the furnace door.

  - Observe the color change of the calcined powder from white to dark red with increasing alpha iron(III) oxide weight percentage [1]. Label the prepared nanocomposites as MF0 (M-F-Zero), MF2 (M-F-Two), MF5 (M-F-Five), and MF10 (M-F-Ten) according to their alpha iron(III) oxide content [2].

    - Shot of differently colored powders after calcination.

    - Talent labeling sample containers as MF0, MF2, MF5, and MF10.

- Fabrication and Assembly of MgO@α-Fe₂O₃ Hydroelectric Cell Devices

  - To fabricate the hydroelectric cell device, transfer 1.8 grams of each calcined nanocomposite powder into a mortar [1]. Add 4 drops of 2% polyvinyl alcohol solution [2]. With a pestle, grind the mixture until a dry and homogeneous powder is obtained [3].

    - Talent weighing the calcined powder into a mortar.

    - Talent adding drops of polyvinyl alcohol solution to the powder.

    - Talent grinding the mixture using a pestle.

  - Transfer the prepared powder into a square-shaped mold [1]. Using a hydraulic press, compress the powder into a 2.2 by 2.2 centimeter square pellet [2]. Then remove the pellet carefully from the mold [3].

    - Talent filling the pellet mold with powder.

    - Talent operating the hydraulic press to form the pellet.

    - Talent removing the formed pellet from the mold.

  - Sinter the pellets at 650 degrees Celsius for 4 hours in a box furnace to remove polyvinyl alcohol and obtain compact pellets [1]. Remove the pellets and allow them to cool to room temperature [2].

    - Talent transferring the pellets into the box furnace

    - Talent removing the sintered pellets from the furnace.

  - Next, apply Araldite epoxy onto a zinc sheet to serve as the anode [1]. Attach the sintered pellet firmly onto the zinc sheet [2] and place the assembled structure on a hot plate set to 70 degrees Celsius to improve adhesion [3].

    - Talent applying epoxy onto the zinc sheet.

    - Talent positioning the pellet onto the zinc sheet.

    - Talent placing the device on a hot plate.

  - Using silver paint, apply a comb-pattern electrode on the top surface of the pellet to form the cathode for maximum current collection [1]. Characterize the structural, surface, and chemical properties of the nanocomposites to understand their composition and behavior [2].

    - Talent painting a comb-pattern electrode using silver paste.

Added shot: Reuse

# Results

- Results

  - X-ray diffraction analysis of pristine and nanocomposites confirmed the phase purity of the nanocomposites, with diffraction peaks [1] corresponding exclusively to cubic magnesium oxide [2] and trigonal alpha iron(III) oxide phases, and no impurity peaks detected [3].

    - LAB MEDIA: Figure 3A

    - LAB MEDIA: Figure 3A. Video editor: Please highlight all the peaks labeled “MgO” denoted by a black heart symbol

    - LAB MEDIA: Figure 3A. Video editor: Please highlight all the peaks labeled “αFe2O3” denoted by a red clover symbol

  - The average crystallite size decreased from 24.05 nanometers in MF0 to 19.18 nanometers in MF10 [1], while lattice strain increased with increasing alpha iron(III) oxide content [2].

    - LAB MEDIA: Figure 3B. Video editor: Please highlight the downward trend in the black curve

    - LAB MEDIA: Figure 3B. Video editor: Please highlight the upward trend in the blue curve

  - Fourier transform infrared spectroscopy revealed that with an increase in the content of alpha iron(III) oxide in magnesium oxide, the height of the absorption bands of the surface-adsorbed hydroxyl group between 1400 to 1800 inverse centimeters increased prominently, substantiating the suitability of the nanocomposite for hydroelectric cell applications [1].

    - LAB MEDIA: Figure 4A. Video editor: Highlight the curves from bottomto top sequentially NOTE: Use updated figure 4A from the website

    - LAB MEDIA: Figure 4A. Video editor: Highlight the area between 1400 to 2000 mark on the X axis  in all curves from bottom to top sequentially

  - Raman spectroscopy of the samples confirmed the presence of all 5 Raman vibrational modes of alpha iron(III) oxide in MF2, MF5, and MF10 samples [1] and the MF10 sample showed relatively more prominent peaks [2].

    - LAB MEDIA: Figure 4B. Video editor: Highlight the area between 200-600 mark on X-axis for curves MF2 MF5 MF10

    - LAB MEDIA: Figure 4B. Video editor: Please sequentially highlight A1g, Eg, Eg, A1g, and Eg PEAKS in curve MF10

  - Field Emission Scanning Electron Microscopy analysis showed highly agglomerated spherical-shaped nanoparticles in all samples along with nanoporous structures [1]. The presence of Magnesium, Oxygen, and iron with their atomic and weight percentages was determined using Energy Dispersive X-ray Analysis in MF0 and MF10 samples [2]. Brunauer–Emmett–Teller analysis showed reduced average pore radius and volume from MF0 to MF10 [3].

    - LAB MEDIA: Figure 5 ABCD

    - LAB MEDIA: Figure 5 E and F Video Editor: Please highlight E and F sequentially when Vo says MF0 and MF10

    - LAB MEDIA: Table 2 Video Editor: Please highlight the column “Average Pore Radius (mm)” and “Average pore volume” sequentially from MF0 to MF10 rows

  - X-ray photoelectron spectroscopy confirmed the presence and chemical states of magnesium, oxygen, and iron in the nanocomposites [1] through Mg 1s (Magnesium-1-S), Mg 2p (Magnesium-2-P) [2], O 1s (Oxygen-1-S) [3] and Fe 2p (Iron-2-P) core-level spectra [4].

    - LAB MEDIA: Figure 7A–I.

    - LAB MEDIA: Figure 7A–I. Video editor: Please sequentially highlight A-B

    - LAB MEDIA: Figure 7A–I. Video editor: Please sequentially highlight C to F

    - LAB MEDIA: Figure 7A–I. Video editor: Please sequentially highlight G to I

1. Nanostructured

Pronunciation link: No confirmed link found

IPA: /ˌnænoʊˈstrʌktʃərd/

Phonetic Spelling: nan·oh·struk·cherd

2. Magnesium

Pronunciation link: [https://www.merriam-webster.com/dictionary/magnesium](https://www.merriam-webster.com/dictionary/magnesium)

IPA: /mæɡˈniːziəm, -ʒəm/

Phonetic Spelling: mag·nee·zee·uhm, mag·nee·zhuhm

3. Oxide

Pronunciation link: [https://www.merriam-webster.com/dictionary/oxide](https://www.merriam-webster.com/dictionary/oxide)

IPA: /ˈɑkˌsaɪd/

Phonetic Spelling: ok·side

4. Zirconia

Pronunciation link: [https://www.merriam-webster.com/dictionary/zirconia](https://www.merriam-webster.com/dictionary/zirconia)

IPA: /ˌzɝˈkoʊniə/

Phonetic Spelling: zur·koh·nee·uh

5. Calcination

Pronunciation link: [https://www.merriam-webster.com/dictionary/calcination](https://www.merriam-webster.com/dictionary/calcination)

IPA: /ˌkælsəˈneɪʃən/

Phonetic Spelling: kal·suh·nay·shuhn

6. Hydroelectric

Pronunciation link: [https://www.merriam-webster.com/dictionary/hydroelectric](https://www.merriam-webster.com/dictionary/hydroelectric)

IPA: /ˌhaɪdroʊɪˈlɛktrɪk/

Phonetic Spelling: hy·droh·ih·lek·trik

7. Polyvinyl alcohol

Pronunciation link: [https://www.merriam-webster.com/dictionary/polyvinylalcohol](https://www.merriam-webster.com/dictionary/polyvinylalcohol)

IPA: /ˌpɑliˌvaɪnəl ˈælkəˌhɔl/

Phonetic Spelling: pol·ee·vy·nuhl al·kuh·hawl

8. Anode

Pronunciation link: [https://www.merriam-webster.com/dictionary/anode](https://www.merriam-webster.com/dictionary/anode)

IPA: /ˈæˌnoʊd/

Phonetic Spelling: an·ohd

9. Cathode

Pronunciation link: [https://www.merriam-webster.com/dictionary/cathode](https://www.merriam-webster.com/dictionary/cathode)

IPA: /ˈkæθˌoʊd/

Phonetic Spelling: kath·ohd

10. Diffraction

Pronunciation link: [https://www.merriam-webster.com/dictionary/diffraction](https://www.merriam-webster.com/dictionary/diffraction)

IPA: /dɪˈfrækʃən/

Phonetic Spelling: dih·frak·shuhn

11. Crystallite

Pronunciation link: [https://www.merriam-webster.com/dictionary/crystallite](https://www.merriam-webster.com/dictionary/crystallite)

IPA: /ˈkrɪstəˌlaɪt/

Phonetic Spelling: kris·tuh·lyte

12. Hydroxyl

Pronunciation link: [https://www.merriam-webster.com/dictionary/hydroxyl](https://www.merriam-webster.com/dictionary/hydroxyl)

IPA: /haɪˈdrɑksəl/

Phonetic Spelling: hy·drok·suhl

13. Spectroscopy

Pronunciation link: [https://www.merriam-webster.com/dictionary/spectroscopy](https://www.merriam-webster.com/dictionary/spectroscopy)

IPA: /spɛkˈtrɑskəpi/

Phonetic Spelling: spek·tros·kuh·pee

14. Photoelectron

Pronunciation link: [https://www.merriam-webster.com/dictionary/photoelectron](https://www.merriam-webster.com/dictionary/photoelectron)

IPA: /ˌfoʊtoʊɪˈlɛkˌtrɑn/

Phonetic Spelling: foh·toh·ih·lek·tron

15. Epoxy

Pronunciation link: [https://www.merriam-webster.com/dictionary/epoxy](https://www.merriam-webster.com/dictionary/epoxy)

IPA: /ɪˈpɑksi/

Phonetic Spelling: ih·pok·see

16. Sinter

Pronunciation link: [https://www.merriam-webster.com/dictionary/sinter](https://www.merriam-webster.com/dictionary/sinter)

IPA: /ˈsɪntər/

Phonetic Spelling: sin·ter