# Submission ID #: 69078

# Scriptwriter Name: Sulakshana Karkala

# Project Page Link: https://review.jove.com/account/file-uploader?src=21068838

# Title: MgO@α-Fe2O3 Based Hydroelectric Cell for Efficient Green Energy Generation

# Authors and Affiliations:

# Priyambada Sahoo1*, Soumya Ranjan Ghadai1*, Ambesh Dixit1,2

# 1Advanced Material and Device Lab, Department of Physics, Indian Institute of Technology-Jodhpur, Rajasthan

# 2Rishabh Centre for Research and Innovation in Clean Energy, Indian Institute of Technology, Jodhpur

# *These authors contributed equally

# Corresponding Authors:

# Ambesh Dixit			(ambesh@iitj.ac.in)

# Email Addresses for All Authors:

Priyambada Sahoo		(priyambada.1@iitj.ac.in)

Soumya Ranjan Ghadai	(m23pm2006@iitj.ac.in)

Ambesh Dixit			(ambesh@iitj.ac.in)

## Author Questionnaire

1. We have marked your project as author-provided footage, meaning you film the video yourself and provide JoVE with the footage to edit. JoVE will not send the videographer. Please confirm that this is correct.

√ Correct

2. Microscopy: Does your protocol require the use of a dissecting or stereomicroscope for performing a complex dissection, microinjection technique, or something similar?  No

3. Software: Does the part of your protocol being filmed include step-by-step descriptions of software usage?  No

4. Proposed filming date: To help JoVE process and publish your video in a timely manner, please indicate the proposed date that your group will film here: 02/1/2026

When you are ready to submit your video files, please contact our Content Manager, Utkarsh Khare.

Current Protocol Length

Number of Steps:  17

Number of Shots:  43

# Introduction

Authors: Please note that the questions will not appear on screen. Please answer in stand-alone full sentence with sufficient context.

INTRODUCTION:

REQUIRED: What is the scope of your research? What questions are you trying to answer?

  - Priyambada Sahoo: The scope of our research is developing MgO@α-Fe₂O₃ hydroelectric cells and understanding nanocomposite-enhanced water adsorption and charge transport mechanisms.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

What are the most recent developments in your field of research?

  - Priyambada Sahoo: Recent research explores defect associated ferrites and metal oxide and metal organic framework materials beyond simple oxides to enhance water-driven energy generation.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

CONCLUSION:

What significant findings have you established in your field?

  - Priyambada Sahoo: We established a high-performance MgO@α-Fe₂O₃ hydroelectric cell where optimized ferrite incorporation enhances defects, hydrophilicity, active sites, and doubles power output.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

What research gap are you addressing with your protocol?

  - Priyambada Sahoo: Our protocol addresses the lack of a simple, scalable, and reproducible fabrication method for high-performance hydroelectric cells with controlled defect chemistry.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

What advantage does your protocol offer compared to other techniques?

  - Priyambada Sahoo: Our protocol offers a low-cost, scalable solid-state fabrication approach enabling precise defect tuning and reproducible hydroelectric performance without external bias, light, or complex equipment.

    - INTERVIEW: Named talent says the statement above in an interview-style shot, looking slightly off-camera.

# Protocol

- Synthesis of Nanostructured Porous Magnesium Oxide–Iron(III) Oxide Composites via Ball Milling and Calcination

Demonstrator: Priyambada Sahoo

  - To begin, collect magnesium oxide powder and alpha iron(III) (three) oxide powder along with a ball miller, zirconia milling balls, and a milling bowl [1]. Weigh 5 grams of magnesium oxide [2] and add 2 percent, 5 percent, or 10 percent alpha iron(III) oxide,by weight, into a 50-milliliter milling bowl [3]. Add zirconia milling balls maintaining a ball-to-powder ratio of 4 to 1 [4].

    - WIDE: Talent arranging magnesium oxide, alpha iron(III) oxide, milling bowl, and zirconia balls on the workbench.

    - Talent weighing 5 g magnesium oxide.

    - Talent adding alpha iron(III) oxide powders to MgO and transferring them into the milling bowl.

    - Talent adding zirconia balls into the milling bowl.

  - Place the loaded bowl into the ball miller [1]. Set the ball rotation speed to 300 revolutions per minute and the bowl rotation speed to 600 revolutions per minute [2]. Ball mill the precursor powders continuously for 24 hours to ensure homogeneous mixing [3].

    - Talent placing the milling bowl into the ball miller.

    - Shot of  the ball miller control panel showing the rotation speeds being set.

    - Shot of  the milling process.

  - Collect the ball-milled powder from the bowl after milling [1]. Then transfer the powder into a crucible [2]. Place the crucible inside a box furnace and calcine at 600 degrees Celsius for 4 hours to obtain nanostructured porous material [3].

    - Talent collecting the ball-milled powder into a container.

    - Talent transferring the powder into a furnace-compatible crucible.

    - Talent placing the crucible inside the box furnace and closing the furnace door.

  - Observe the color change of the calcined powder from white to dark red with increasing alpha iron(III) oxide concentration [1]. Label the prepared nanocomposites as MF0 (M-F-Zero), MF2 (M-F-Two), MF5 (M-F-Five), and MF10 (M-F-Ten) according to their alpha iron(III) oxide content [2].

    - Shot of differently colored powders after calcination.

    - Talent labeling sample containers as MF0, MF2, MF5, and MF10.

- Fabrication, and Assembly of MgO@α-Fe₂O₃ Hydroelectric Cell Devices

  - To fabricate the hydroelectric cell device, transfer 1.8 grams of each calcined nanocomposite powder into a mortar [1]. Add 4 drops of 2% polyvinyl alcohol solution [2]. With a pestle, grind the mixture until a dry and homogeneous powder is obtained [3].

    - Talent weighing the calcined powder into a mortar.

    - Talent adding drops of polyvinyl alcohol solution to the powder.

    - Talent grinding the mixture using a pestle.

  - Transfer the prepared powder into a square-shaped mold [1]. Using a hydraulic press, compress the powder into a 2.2 by 2.2 centimeter square pellet [2]. Then remove the pellet carefully from the mold [3].

    - Talent filling the pellet mold with powder.

    - Talent operating the hydraulic press to form the pellet.

    - Talent removing the formed pellet from the mold.

  - Sinter the pellets at 650 degrees Celsius for 4 hours in a box furnace to remove polyvinyl alcohol and obtain compact pellets [2]. Remove the pellets and allow them to cool to room temperature [3].

    - Talent transferring the pellets into the box furnace

    - Talent removing the sintered pellets from the furnace.

  - Next, apply Araldite epoxy onto a zinc sheet to serve as the anode [1]. Attach the sintered pellet firmly onto the zinc sheet [2]. Then place the assembled structure on a hot plate set to 70 degrees Celsius to improve adhesion [3].

    - Talent applying epoxy onto the zinc sheet.

    - Talent positioning the pellet onto the zinc sheet.

    - Talent placing the device on a hot plate.

  - Using silver paint, apply a comb-pattern electrode on the top surface of the pellet to form the cathode for maximum current collection [1].

    - Talent painting a comb-pattern electrode using silver paste.

# Results

- Results

  - X-ray diffraction analysis confirmed the phase purity of magnesium oxide and MgO@α-iron(III) oxide (M-G-O-And-Iron-Oxide) nanocomposites, with diffraction peaks corresponding exclusively to cubic magnesium oxide and trigonal alpha iron(III) oxide phases, and no impurity peaks detected [1].

    - LAB MEDIA: Figure 3A. Video editor: Please sequentially highlight the curves from MF0 to MF10

  - The average crystallite size decreased from 24.05 nanometers in MF0 to 19.18 nanometers in MF10 [1], while lattice strain increased with increasing alpha iron(III) oxide content [2].

    - LAB MEDIA: Figure 3B. Video editor: Please highlight the downward trend in the black curve

    - LAB MEDIA: Figure 3B. Video editor: Please highlight the upward trend in the blue curve

  - Fourier transform infrared spectroscopy revealed enhanced surface hydroxyl group absorption with increasing alpha iron(III) oxide content, indicating improved water adsorption capability [1].

    - LAB MEDIA: Figure 4A. Video editor: Highlight the Fe-OH and H-O-H curves

  - Raman spectroscopy confirmed the formation of MgO@α-iron(III) oxide nanocomposites, with distinct Raman-active vibrational modes appearing in MF2, MF5, and MF10 samples [1].

    - LAB MEDIA: Figure 4B. Video editor: Please sequentially highlight the curves from MF0 to MF10

  - FESEM (F-E-Sem) analysis showed highly agglomerated spherical-shaped nanoparticles in all samples along with nanoporous structures [1]. BET analysis showed reduced pore size from MF0 to MF10 [2].

    - LAB MEDIA: Figure 5 A- D

    - LAB MEDIA: Table 2 Video Editor: Please highlight the column “Average Pore Radius (mm) “

  - X-ray photoelectron spectroscopy confirmed the presence and chemical states of magnesium, oxygen, and iron in MgO@alpha iron(III) oxide nanocomposites through Mg 1s (Magnesium-1-S) , Mg 2p (Magnesium-2-P), O 1s (Oxygen-1-S), and Fe 2p (Iron-2-P) core-level spectra [1].

    - LAB MEDIA: Figure 7A–I. Video editor: Please sequentially highlight A-C, then D to F, G to I